A Comparative Study on Arc- and Vacuum Induction-Melting for High Entropy Shape Memory Alloy Production

- Supplementary Information -

Table S1: Phases, lattice parameters and area fraction (by SEM) of the binary pre-alloys compared by the production technique. The 2σ refinement uncertainty (in ‰) is shown in brackets.

| Sample/ treatment | Phases (spacegroup) | a, Å | b, Å | c, Å | γ, ° | area, norm. %* |
| --- | --- | --- | --- | --- | --- | --- |
| NiTi/ AM | NiTi (Pm-3m) NiTi (P21/m) NiTi2(Fd-3m) | 2.954(1) 3.173(2) 11.321(2) | 2.954(1) 5.011(2) 11.321(2) | 2.954(1) 4.600(1) 11.321(2) | 106.54(5) | 94.9 |
|  |  |  |  |  |  | 5.1 |
| NiTi/ VIM | NiTi (Pm-3m) NiTi (P21/m) NiTi2(Fd-3m) | 3.159(1) 3.030(1) 11.345(2) | 3.159(1) 4.925(2) 11.345(2) | 3.159(1) 4.605(1) 11.345(2) | 104.88(4) | 98.9 |
|  |  |  |  |  |  | 1.1 |
| CoZr/ AM | CoZr (Pm-3m) CoZr2 (I4/mcm) CoZr3 (Cmcm) | 3.193(1) 6.384(1) 3.266(1) | 3.193(1) 6.384(1) 10.833(1) | 3.193(1) 5.503(1) 8.955(1) |  | 26.2 66.7 7.1 |
| CoZr/ VIM | CoZr (Pm-3m) CoZr2 (I4/mcm) CoZr3 (Cmcm) | 3.200(1) 6.380(1) 3.230(1) | 3.200(1) 6.380(1) 10.536(1) | 3.200(1) 5.320(1) 8.974(1) |  | 14.3 85.7 - |
| CuHf/ AM | CuHf2 (I4/mmm) Cu10Hf7 (Aba2) Cu8Hf3 (Pnma) | 3.196(1) 9.293(1) 7.71(1) | 3.196(1) 9.234(1) 8.31(2) | 11.90(1) 12.579(1) 9.965(1) |  | 19.4 79.0 1.6 |
| CuHf/ VIM | CuHf2 (I4/mmm) Cu10Hf7 (Aba2) Cu8Hf3 (Pnma) | 3.204(2) 9.278(1) 7.682(2) | 3.204(2) 9.233(1) 8.300(1) | 11.860(4) 12.584(1) 9.995(2) |  | 17.8 81.3 0.9 |

*all area uncertainties are in the order of 0.2 %

Table S2: Overall chemical composition of the senary alloys produced by AM and VIM in as-cast and heat-treated states determined by EDX in norm.-at.-%

| Sample/ treatment | Ti | Zr | Hf | Co | Ni | Cu |
| --- | --- | --- | --- | --- | --- | --- |
| Nominal | 16.66 | 16.66 | 16.66 | 10 | 20 | 20 |
| AM-AC | 18,76 | 17,33 | 15,74 | 10,13 | 19,22 | 18,82 |
| AM-HT | 18,54 | 16,16 | 16,42 | 11,05 | 19,75 | 18,09 |
| VIM-AC | 22,85 | 18,84 | 14,16 | 8,84 | 16,56 | 18,76 |
| VIM-HT | 20,00 | 18,69 | 14,94 | 9,73 | 18,41 | 18,23 |

Support Figure S1: Refined XRD plots of NiTi after AM casting with difference between observed and calculated data and indexed phase ticks

Support Figure S2: Refined XRD plots of NiTi after VIM casting with difference between observed and calculated data and indexed phase ticks

Support Figure S3: Refined XRD plots of CoZr after AM casting with difference between observed and calculated data and indexed phase ticks

Support Figure S4: Refined XRD plots of CoZr after VIM casting with difference between observed and calculated data and indexed phase ticks

Support Figure S5: Refined XRD plots of CuHf after AM casting with difference between observed and calculated data and indexed phase ticks

Support Figure S6: Refined XRD plots of CuHf after VIM casting with difference between observed and calculated data and indexed phase ticks

Support Figure S7: Refined XRD plots of Ti16.6Zr16.6Hf16.6Co10Ni20Cu20 after AM casting in as-cast state with difference between observed and calculated data and indexed phase ticks

Support Figure S8: Refined XRD plots of Ti16.6Zr16.6Hf16.6Co10Ni20Cu20 after AM casting in heat-treated state with difference between observed and calculated data and indexed phase ticks; (*) signal from embedding

Support Figure S9: Refined XRD plots of Ti16.6Zr16.6Hf16.6Co10Ni20Cu20 after VIM casting in as-cast state with difference between observed and calculated data and indexed phase ticks

Support Figure S10: Refined XRD plots of Ti16.6Zr16.6Hf16.6Co10Ni20Cu20 after VIM casting in heat-treated state with difference between observed and calculated data and indexed phase ticks