Euphorbia neriifolia Extracts as Green Corrosion Inhibitors for Aluminium in Hydrochloric and Nitric Acid Media

Omprakash Meena 1, Sandeep Kaushal 1,*, Sanjeev Kumar 1,*, Jasvir Dalal 3,

1 Regional Institute of Education, NCERT, Ajmer, Rajasthan, India

2 Department of Physics, Chandigarh University, Gharuan, Mohali, 140413, India

3 Department of Physics, Rajdhani College, University of Delhi, Delhi – 110015, India.

Table S1 : Weight loss, percentage inhibition efficiency, surface coverage and corrosion rate for aluminum in 1N HNO3 and 1N HCl for different concentrations of inhibitors.

Temperature : 300±0.10C           Time of Exposure: (0.75 hrs)   	 Area of Specimen :13cm2

| Concentration (%) | Weight Loss (∆w) in g | Inhibition Efficiency (I.E.) (%) | Surface Coverage (Ɵ) | Corrosion Rate in (mm/yr) | logθ1-θ |
| --- | --- | --- | --- | --- | --- |
| 1N HNO3 |  |  |  |  |  |
| Stem |  |  |  |  |  |
| Uninhibited | 0.5191 |  |  | 0.036 |  |
| 0.1 | 0.0746 | 85.62 | 0.8562 | 0.0005 | 0.7748 |
| 0.3 | 0.0671 | 87.07 | 0.8707 | 0.0004 | 0.8282 |
| 0.5 | 0.0501 | 90.34 | 0.9034 | 0.0003 | 0.9708 |
| 0.7 | 0.0383 | 92.62 | 0.9262 | 0.0002 | 1.0986 |
| Leaves |  |  |  |  |  |
| 0.1 | 0.0830 | 84.01 | 0.8401 | 0.0006 | 0.7208 |
| 0.3 | 0.0759 | 85.37 | 0.8537 | 0.0005 | 0.7660 |
| 0.5 | 0.0634 | 87.78 | 0.8778 | 0.0004 | 0.8563 |
| 0.7 | 0.0469 | 90.96 | 0.9096 | 0.0003 | 1.0026 |
| Flower |  |  |  |  |  |
| 0.1 | 0.1001 | 80.71 | 0.8071 | 0.0007 | 0.6215 |
| 0.3 | 0.0905 | 82.56 | 0.8256 | 0.0006 | 0.6752 |
| 0.5 | 0.0697 | 86.57 | 0.8657 | 0.0004 | 0.8092 |
| 0.7 | 0.0499 | 90.38 | 0.9038 | 0.0003 | 0.9728 |
| 1N HCl |  |  |  |  |  |
| Stems |  |  |  |  |  |
| Uninhibited | 0.1950 |  |  | 0.6488 |  |
| 0.1 | 0.0341 | 85.51 | 0.8251 | 0.1134 | 0.6736 |
| 0.3 | 0.0226 | 88.41 | 0.8841 | 0.0750 | 0.8824 |
| 0.5 | 0.0131 | 93.08 | 0.9308 | 0.0435 | 1.1423 |
| 0.7 | 0.0099 | 94.92 | 0.9492 | 0.0329 | 1.2714 |
| Leaves |  |  |  |  |  |
| 0.1 | 0.0509 | 73.89 | 0.7389 | 0.1693 | 0.4517 |
| 0.3 | 0.0432 | 77.84 | 0.7784 | 0.1437 | 0.5156 |
| 0.5 | 0.0301 | 84.56 | 0.8456 | 0.1001 | 0.7385 |
| 0.7 | 0.0251 | 87.12 | 0.8712 | 0.0835 | 0.8301 |
| Flowers |  |  |  |  |  |
| 0.1 | 0.0650 | 66.66 | 0.6666 | 0.2162 | 0.2673 |
| 0.3 | 0.0560 | 71.28 | 0.7128 | 0.1863 | 0.3552 |
| 0.5 | 0.0466 | 76.10 | 0.7610 | 0.1550 | 0.5029 |
| 0.7 | 0.0385 | 80.25 | 0.8025 | 0.1281 | 0.6088 |

Table S2: Weight loss, percentage inhibition efficiency, surface coverage and corrosion rate for aluminum in 2N HNO3 and 2N HCl for different concentration of inhibitors.

Temperature: 300±0.10C    Time of Exposure: (0.25 hrs)            Area of Specimen: 13cm2

| Concentration (%) | Weight Loss (∆w) in g | Inhibition Efficiency (I.E.) (%) | Surface Coverage (𝛉) | Corrosion Rate in (mm/yr) | logθ1-θ |
| --- | --- | --- | --- | --- | --- |
| 2N HNO3 |  |  |  |  |  |
| Stem |  |  |  |  |  |
| Uninhibited | 0.5211 |  |  | 0.0050 |  |
| 0.1 | 0.1252 | 75.97 | 0.7597 | 0.0012 | 0.4998 |
| 0.3 | 0.1129 | 78.33 | 0.7833 | 0.0010 | 0.5580 |
| 0.5 | 0.1003 | 80.75 | 0.8075 | 0.0009 | 0.6227 |
| 0.7 | 0.0866 | 83.38 | 0.8338 | 0.008 | 0.7004 |
| Leaves |  |  |  |  |  |
| 0.1 | 0.1475 | 71.69 | 0.7169 | 0.0014 | 0.4035 |
| 0.3 | 0.1303 | 74.99 | 0.7499 | 0.0012 | 0.4768 |
| 0.5 | 0.1166 | 77.62 | 0.7762 | 0.0011 | 0.5401 |
| 0.7 | 0.1025 | 80.33 | 0.8033 | 0.0009 | 0.6110 |
| Flower |  |  |  |  |  |
| 0.1 | 0.1513 | 70.96 | 0.7096 | 0.0014 | 0.3880 |
| 0.3 | 0.1405 | 73.03 | 0.7303 | 0.0013 | 0.4326 |
| 0.5 | 0.1265 | 75.72 | 0.7572 | 0.0012 | 0.4939 |
| 0.7 | 0.1152 | 77.89 | 0.7789 | 0.0011 | 0.5468 |
| 2N HCl |  |  |  |  |  |
| Stems |  |  |  |  |  |
| Uninhibited | 0.3909 |  |  | 3.9022 |  |
| 0.1 | 0.1041 | 73.36 | 0.7336 | 1.0392 | 0.4399 |
| 0.3 | 0.0896 | 77.07 | 0.7707 | 0.8944 | 0.5264 |
| 0.5 | 0.0721 | 81.55 | 0.8155 | 0.7197 | 0.6454 |
| 0.7 | 0.0516 | 86.79 | 0.8679 | 0.5151 | 0.8175 |
| Leaves |  |  |  |  |  |
| 0.1 | 0.1196 | 69.40 | 0.6940 | 1.1936 | 0.3556 |
| 0.3 | 0.1056 | 72.98 | 0.7298 | 1.0541 | 0.4315 |
| 0.5 | 0.0881 | 77.46 | 0.7746 | 0.8794 | 0.5361 |
| 0.7 | 0.0684 | 82.50 | 0.8250 | 0.6828 | 0.6734 |
| Flowers |  |  |  |  |  |
| 0.1 | 0.1331 | 65.95 | 0.6595 | 1.3287 | 0.2870 |
| 0.3 | 0.1191 | 69.81 | 0.6981 | 1.1779 | 0.3582 |
| 0.5 | 0.1016 | 74.00 | 0.7400 | 1.0142 | 0.4542 |
| 0.7 | 0.0819 | 79.04 | 0.7904 | 0.8176 | 0.5764 |

Table S3 : Weight loss, percentage inhibition efficiency, surface coverage and corrosion rate for aluminium in 3N HNO3 and 3N HCl for different concentration of inhibitors.

Temperature : 300±0.10C     Time of Exposure: (0.133 hrs)      Area of Specimen :13cm2

| Concentration (%) | Weight Loss (∆w) in g | Inhibition Efficiency (I.E.) (%) | Surface Coverage (𝛉) | Corrosion Rate in (mm/yr) | logθ1-θ |
| --- | --- | --- | --- | --- | --- |
| 3N HNO3 |  |  |  |  |  |
| Stem |  |  |  |  |  |
| Uninhibited | 0.5272 |  |  | 0.0079 |  |
| 0.1 | 0.1818 | 65.51 | 0.6551 | 0.0027 | 0.2860 |
| 0.3 | 0.1733 | 67.71 | 0.6771 | 0.0026 | 0.3215 |
| 0.5 | 0.1566 | 70.29 | 0.7029 | 0.0023 | 0.3738 |
| 0.7 | 0.1492 | 71.69 | 0.7169 | 0.0022 | 0.4035 |
| Leaves |  |  |  |  |  |
| 0.1 | 0.1938 | 63.23 | 0.6323 | 0.0029 | 0.2354 |
| 0.3 | 0.1829 | 65.30 | 0.6530 | 0.0027 | 0.2745 |
| 0.5 | 0.1740 | 66.99 | 0.6699 | 0.0026 | 0.3073 |
| 0.7 | 0.1501 | 71.52 | 0.7152 | 0.0022 | 0.3998 |
| Flower |  |  |  |  |  |
| 0.1 | 0.2038 | 61.34 | 0.6134 | 0.0030 | 0.2004 |
| 0.3 | 0.1908 | 63.80 | 0.6380 | 0.0028 | 0.2461 |
| 0.5 | 0.1792 | 66.00 | 0.6600 | 0.0027 | 0.2880 |
| 0.7 | 0.1700 | 67.75 | 0.6775 | 0.0025 | 0.3223 |
| 3N HCl |  |  |  |  |  |
| Uninhibited | 0.5146 |  |  | 9.6563 |  |
| 0.1 | 0.1431 | 72.26 | 0.7226 | 2.6852 | 0.4244 |
| 0.3 | 0.1244 | 75.82 | 0.7582 | 2.3343 | 0.5281 |
| 0.5 | 0.1051 | 79.57 | 0.7957 | 1.9721 | 0.6454 |
| 0.7 | 0.0866 | 83.17 | 0.8317 | 1.625 | 0.8175 |
| Leaves |  |  |  |  |  |
| 0.1 | 0.1606 | 68.79 | 0.6879 | 3.0136 | 0.3432 |
| 0.3 | 0.1419 | 72.52 | 0.7252 | 2.6627 | 0.4214 |
| 0.5 | 0.1226 | 76.17 | 0.7617 | 2.3005 | 0.5046 |
| 0.7 | 0.1041 | 79.67 | 0.7967 | 1.9534 | 0.5931 |
| Flowers |  |  |  |  |  |
| 0.1 | 0.1751 | 65.97 | 0.6597 | 3.2857 | 0.2874 |
| 0.3 | 0.1564 | 69.60 | 0.6960 | 2.9348 | 0.3597 |
| 0.5 | 0.1371 | 73.35 | 0.7335 | 2.5726 | 0.4396 |
| 0.7 | 0.1185 | 76.35 | 0.7635 | 2.2236 | 0.5089 |

Table S4: Reaction number (R) and inhibition efficiency (%) for aluminium in (1N, 2N and 3N) HNO3 and HCl in the absence and presence of inhibitors

Temperature: 300K  0.1K 				       Area of specimen: 13 cm2

| Concentration of Inhibitor (%) Uninhibited (.060) |  | 1N HNO3 |  |  | 2N HNO3 |  | 3N HNO3 |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Reaction number | Inhibition efficiency (ƞ%) | Reaction number |  | Inhibition efficiency (ƞ %) | Reaction number | Inhibition efficiency (ƞ%) |
| Uninhibited |  | 0.3552 |  | 0.6355 |  |  | 0.9270 |  |
| Stem | 0.1 | 0.1602 | 54.93 | 0.3197 |  | 49.69 | 0.5057 | 45.44 |
|  | 0.3. | 0.1501 | 57.74 | 0.3028 |  | 52.35 | 0.4893 | 47.21 |
|  | 0.5 | 0.1384 | 61.03 | 0.2857 |  | 55.04 | 0.4769 | 48.55 |
|  | 0.7 | 0.1262 | 64.27 | 0.2560 |  | 59.71 | 0.4371 | 52.84 |
| Uninhibited |  | 0.3552 |  | 0.6355 |  |  | 0.9270 |  |
| Leaves | 0.1 | 0.1720 | 51.57 | 0.3455 |  | 45.63 | 0.5417 | 34.26 |
|  | 0.3. | 0.1630 | 54.11 | 0.3332 |  | 47.71 | 0.5270 | 43.14 |
|  | 0.5 | 0.1499 | 57.79 | 0.3152 |  | 54.72 | 0.5052 | 45.50 |
|  | 0.7 | 0.1382 | 61.09 | 0.2876 |  | 59.71 | 0.4777 | 48.46 |
| Uninhibited |  | 0.3552 |  | 0.6355 |  |  | 0.9270 |  |
| Flower | 0.1 | 0.1865 | 47.49 | 0.3633 |  | 42.65 | 0.5905 | 36.29 |
|  | 0.3. | 0.1703 | 52.05 | 0.3432 |  | 45.82 | 0.506 | 39.52 |
|  | 0.5 | 0.1620 | 54.39 | 0.3380 |  | 46.64 | 0.5345 | 42.34 |
|  | 0.7 | 0.1517 | 57.29 | 0.3147 |  | 50.32 | 0.5051 | 45.51 |
| Concentration of Inhibitor (%) Uninhibited (.060) |  | 1N HCl |  |  | 2N HCl |  | 3N HCl |  |
|  |  | Reaction number | Inhibition efficiency (ƞ%) | Reaction number |  | Inhibition efficiency (ƞ %) | Reaction number | Inhibition efficiency (ƞ%) |
| Uninhibited |  | 10.66 |  | 68.00 |  |  | 157.89 |  |
| Stem | 0.1 | 0.9333 | 82.51 | 7.200 |  | 73.36 | 21.0526 | 72.26 |
|  | 0.3. | 0.8000 | 88.41 | 6.800 |  | 77.07 | 20.3007 | 75.82 |
|  | 0.5 | 0.6666 | 93.28 | 6.400 |  | 81.55 | 19.5488 | 79.57 |
|  | 0.7 | 0.5333 | 94.92 | 6.000 |  | 86.79 | 18.7969 | 83.17 |
| Uninhibited |  | 10.6666 |  | 68.00 |  |  | 157.8947 |  |
| Leaves | 0.1 | 1.8666 | 73.89 | 9.600 |  | 69.40 | 22.8045 | 68.79 |
|  | 0.3. | 1.7333 | 77.84 | 9.200 |  | 72.98 | 21.0826 | 72.52 |
|  | 0.5 | 1.6000 | 84.56 | 8.800 |  | 77.46 | 20.1007 | 76.17 |
|  | 0.7 | 1.4666 | 87.12 | 8.400 |  | 82.50 | 19.2488 | 79.67 |
| Uninhibited |  | 10.6666 |  | 68.00 |  |  | 157.8947 |  |
| Flower | 0.1 | 2.4000 | 66.66 | 11.600 |  | 65.95 | 25.812 | 65.97 |
|  | 0.3. | 2.2666 | 71.28 | 11.200 |  | 69.81 | 24.0604 | 69.60 |
|  | 0.5 | 2.1333 | 76.10 | 10.800 |  | 74.00 | 23.3082 | 73.35 |
|  | 0.7 | 2.0000 | 80.25 | 10.400 |  | 79.04 | 22.5563 | 76.35 |

Corresponding Authors Email: jasvirdalal2012@gmail.com (J. Dalal), kaushalsandeep33@gmail.com (S. Kaushal), and kumarsanju25@gmail.com (S. Kumar)