Mechanically Synthesized S@rGO Nanocomposites for Dye Photodegradation

Karishma Jain1, Deepika Maan1, Ashish Kumar1, Sushil Kumar Jain1*, Balram Tripathi2

1Department of Physics, Manipal University Jaipur, Jaipur -303007,  India

2Department of Physics, S. S. Jain Subodh PG (Auto.) College Jaipur-302004, India

E-mail: *sushilkumar.jain@jaipur.manipal.edu

Supplementary Material

Figures and Tables

# XRD Studies

Table S1 Estimated values of 2θ and interlayer spacing of reduced graphene sheet

| Sample name | 2θ(°) (hkl) | Interlayer spacing, d (nm) |
| --- | --- | --- |
| pristine rGO | 26.62 (002) | 0.335 |
|  | 54.68 (004) | 0.168 |
| S@rGO-1 | 26.54 (002) | 0.336 |
|  | 54.66 (004) | 0.168 |
| S@rGO-2 | 26.46 (002) | 0.337 |
|  | 54.56 (004) | 0.168 |
| S@rGO-3 | 26.51 (002) | 0.336 |
|  | 54.62 (004) | 0.168 |
| S@rGO-4 | 26.51 (002) | 0.336 |
|  | 54.62 (004) | 0.168 |

Fig. S1 W-H Plot corresponds to the nanomaterials (a) rGO , (b) S@rGO-1, (c) S@rGO-2 , (d) S@rGO-3 , (e) S@rGO-4.

Fig. S2 Column chart depicting crystallinity (in %) of nanocomposites – rGO, S@rGO-1, S@rGO-2 , S@rGO-3 and S@rGO-4

Table S2 Estimated lattice parameter values of nanocomposites

| Sample Name | a (Å) | c(Å) | c/a | Volume(Å3) |
| --- | --- | --- | --- | --- |
| rGO | 2.354 | 6.689 | 2.842 | 32.100 |
| S@rGO-1 | 2.353 | 6.712 | 2.853 | 32.183 |
| S@rGO-2 | 2.352 | 6.729 | 2.861 | 32.237 |
| S@rGO-3 | 2.352 | 6.719 | 2.857 | 32.189 |
| S@rGO-4 | 2.352 | 6.719 | 2.857 | 32.189 |

# Raman Studies

Fig. S3 Detailed Raman spectra.

Table S3 Raman spectra analysis

| Sample name | ID/ IG | I2D/ IG |
| --- | --- | --- |
| rGO | 0.336 | 1.875 |
| S@rGO-1 | 0.039 | 1.478 |
| S@rGO-2 | 0.321 | 0.909 |
| S@rGO-3 | 0.045 | 1.603 |
| S@rGO-4 | 0.076 | 1.632 |

# FT-IR Studies

Table S4 Proposed characteristics of the vibrations as well as corresponding wave numbers related to transmittance peaks of (a) pristine sulfur (b) S@rGO-4, (c) S@rGO-3, (d) S@rGO-2, (e) S@rGO-1 and (f) pristine rGO

| Sr. No. | Position of Bands (in cm-1) | Assignment of Bands |
| --- | --- | --- |
| 1. | 568 | C-C=S vibrations [1] |
| 2. | 595 | to C-H [2]. |
| 3. | 687 | Stretching of C-S bond [3] |
| 4. | 905 | Ring vibrations due to C-S bond [3] |
| 5. | 1016, 1017 | C-O-C Stretching (epoxy group) [4]. |
| 6. | 1024 | C-O Stretching vibration [5]. |
| 7. | 1030 | sp3 C-O Stretching[3] |
| 8. | 1114 | Stretching of C-S bond [3] |
| 9. | 1409 | C-H bending bands [6,7] |
| 10. | 1527 | overlapping of triazenes and azo compounds [8] |
| 11. | 1530, 1550, 1533 | aromatic C=C group [9] |
| 12. | 1642, 1639, 1643,1648 | C=C Stretching vibration [10] |
| 13. | 1696 | Stretching vibration at C=O [11] |
| 14. | 2370 | CO2 bands [7]. |
| 15. | 2935, 2925 | C-H Stretching vibration [10]. |
| 16. | 3442 | O-H bond (hydroxyl group) of alcohols [4] |
| 17. | 3741, 3744 | O-H Stretching of water molecules[12] |

# EDX Studies

Fig. S4 EDX spectra for (a) rGO, (b) S@rGO-1, (c) S@rGO-2, (d) S@rGO-3 and (e) S@rGO-4.

Table S5 EDX analysis of (a) S@rGO-1, (b) S@rGO-2, (c) S@rGO-3 and (d) S@rGO-4

| Element | Weight% | Atomic% | Error% | O: S fraction | O/ S (mole) | C/ O (mole) | C/ (O+S) (mole) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| (a) S@rGO-1 |  |  |  | 10.25 | 20.5 | 31.05 | 29.611 |
| C | 93.6 | 95.5 | 3.3 |  |  |  |  |
| O | 5.4 | 4.1 | 18.3 |  |  |  |  |
| S | 1 | 0.4 | 7 |  |  |  |  |
| (b) S@rGO-2 |  |  |  | 5.81 | 11.625 | 12.774 | 11.762 |
| C | 84.2 | 89.1 | 7.4 |  |  |  |  |
| O | 11.7 | 9.3 | 22.4 |  |  |  |  |
| S | 4.1 | 1.6 | 9.2 |  |  |  |  |
| (c) S@rGO-3 |  |  |  | 0.9 | 3.77 | 76.392 | 60.4031 |
| C | 95.4 | 97.4 | 4.5 |  |  |  |  |
| O | 2.2 | 1.7 | 30.4 |  |  |  |  |
| S | 2.3 | 0.9 | 4 |  |  |  |  |
| (d) S@rGO-4 |  |  |  | 0.66 | 1.33 | 130 | 74.285 |
| C | 94.9 | 97.5 | 5.8 |  |  |  |  |
| O | 1.3 | 1 | 49.3 |  |  |  |  |
| S | 3.8 | 1.5 | 3.7 |  |  |  |  |

# UV-Vis Studies

Fig. S5 Tauc Plot: (αhν)2 vs hν curves for (a) rGO, (b) S@rGO-1, (c) S@rGO-2, (d) S@rGO-3 and (e) S@rGO-4

# Photocatalytic Studies

## MB Dye

Fig. S6 Absorption spectra for (a) Blank MB (b) rGO (c) S@rGO-1 (d) S@rGO-2 (e) S@rGO-3 (f) S@rGO-4. Inset graph illustrates zoomed out view of absorption spectra in the wavelength range - 200 nm to 800 nm.

Fig. S7 (a)Concentration vs. Irradiation time (min) plot (b) ln(Co/ C) vs. Irradiation time (min) plot (c) (1/C) vs. Irradiation time (min) plot

Table S6 The values of the pseudo-zero, pseudo - first and pseudo -second-order rate constants, half-lives and the corresponding correlation coefficients for the photocatalytic degradation of MB.

| Sr. No. | Sample Name | Rate constant (k0) (M min-1) | R2 | Half | Rate constant (k1) (min-1) | R2 | Half | Rate constant (k2) (M-1 min-1) | R2 | Half |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | Life (Co/2k0) |  |  | Life |  |  | Life |
|  |  |  |  | (min) |  |  | (0.693/k1) (min) |  |  | (1/k2Co) (min) |
|  |  | Zero Order |  |  | First Order |  |  | Second Order |  |  |
| 1. | Blank MB | -0.00178 | 0.96968 | 145.17 | 0.00418 | 0.97713 | 165.55 | 0.00989 | 0.98068 | 195.65 |
| 2. | rGO | -0.00362 | 0.98887 | 138.78 | 0.0044 | 0.99337 | 157.5 | 0.00541 | 0.99134 | 183.95 |
| 3. | S@rGO-1 | -0.00564 | 0.98458 | 108.80 | 0.00614 | 0.99001 | 112.87 | 0.00684 | 0.98069 | 119.12 |
| 4. | S@rGO-2 | -0.00566 | 0.98537 | 108.94 | 0.00637 | 0.99106 | 108.79 | 0.00736 | 0.97628 | 110.17 |
| 5. | S@rGO-3 | -0.00722 | 0.99728 | 91.41 | 0.00778 | 0.98562 | 89.07 | 0.00868 | 0.95566 | 87.28 |
| 6. | S@rGO-4 | -0.00829 | 0.99101 | 82.71 | 0.00921 | 0.95119 | 75.24 | 0.01084 | 0.87697 | 67.27 |

## Study of Methylene blue Degradation using FTIR

Fig. S8 (a) FT-IR spectra of methylene blue solution before and after photodegradation using rGO catalyst at 0 min, 40 min and 90 min. (b) FT-IR spectra of methylene blue solution before and after photodegradation using S@rGO-2 catalyst at 0 min and 50 min.

In Figure S8 (a), the transmittance peak observed at 3338 cm-1 assigned to –OH hydroxyl groups [13]. The peak at 2923 cm-1 in Figure S8(a) and S8(b) are associated to vibration obtained from CH groups [14]. In Figure 8(a), peak at 1537 cm-1 and in Figure S8(b), peak at 1533 cm-1 is associated to C=C and C=N vibrations of methylene blue [15]. In Figure S8(a), the slight broadness of peak 3338 cm-1 suggests that OH vibrations or water molecules have ameliorated, which substantiates that slight degradation has occurred and water ions have generated.

## MO Dye

Fig. S9 Absorption spectra for (a) Blank MO (b) rGO (c) S@rGO-1 (d) S@rGO-2 (e) S@rGO-3 (f) S@rGO-4.

Fig. S10 (a) Concentration vs. Irradiation time (min) plot (b) ln(Co/ C) vs. Irradiation time (min) plot (c) (1/C) vs. Irradiation time (min) plot

Fig. S11 FT-IR spectra of methyl orange solution before and after photodegradation using S@rGO-2 catalyst at 0 min, 50 min and 80 min.

Methyl orange solution catalyzed using S@rGO-2 catalyst depicts minimal changes in FT-IR spectra, unveiling that degradation is very less (Fig. S11, Supplementary file).

Table S7 The values of the pseudo-zero, pseudo - first and pseudo -second-order rate constants, half-lives and the corresponding correlation coefficients for the photocatalytic degradation of MO.

| Sr. No. | Sample Name | Rate constant (k0) (M min-1) | R2 | Half | Rate constant (k1) (min-1) | R2 | Half | Rate constant (K2) (M-1 min-1) | R2 | Half |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | Life (Co/2k0) |  |  | Life |  |  | Life |
|  |  |  |  | (min) |  |  | (0.693/k1) ( min) |  |  | (1/k2Co) (min) |
|  |  | Zero Order |  |  | First Order |  |  | Second Order |  |  |
| 1. | Blank MO | -0.000139273 | 0.99434 | 1846.01 | 0.00027489 | 0.99473 | 2521.01 | 0.000542577 | 0.99508 | 3584.32 |
| 2. | rGO | -0.000389636 | 0.96037 | 587.73 | 0.00089831 | 0.96515 | 771.45 | 0.00207 | 0.96945 | 1054.79 |
| 3. | S@rGO-1 | -0.000581818 | 0.98314 | 335.16 | 0.00163 | 0.98411 | 425.15 | 0.0046 | 0.98326 | 557.41 |
| 4. | S@rGO-2 | -0.000793545 | 0.99184 | 266.53 | 0.00207 | 0.98959 | 334.78 | 0.00543 | 0.98605 | 435.37 |
| 5. | S@rGO-3 | -0.00106 | 0.99345 | 215.85 | 0.00265 | 0.98916 | 261.51 | 0.00665 | 0.98206 | 328.62 |
| 6. | S@rGO-4 | -0.000730909 | 0.98562 | 219.11 | 0.00262 | 0.97960 | 264.50 | 0.00942 | 0.96958 | 331.43 |

# References

1. Karikalan N, Karthik R, Chen SM, Karuppiah C, Elangovan A. Sonochemical Synthesis of Sulfur Doped Reduced Graphene Oxide Supported CuS Nanoparticles for the Non-Enzymatic Glucose Sensor Applications. Sci Rep. 2017;7(1):2494. https://doi.org/10.1038/s41598-017-02479-5

2. Korucu H, Şimşek B, Kocakerim MM, Karakaş IH. Effective reduction of graphene oxide using sulfur dioxide-containing chemical compounds. Int J Environ Sci Technol. 2019;16(12):8329–42. https://doi.org/10.1007/s13762-019-02419-y

3. Wadekar PH, Ghosh A, Khose R V., Pethsangave DA, Mitra S, Some S. A novel chemical reduction/co-precipitation method to prepare sulfur functionalized reduced graphene oxide for lithium-sulfur batteries. Electrochim Acta. 2020;344:136147. https://doi.org/10.1016/j.electacta.2020.136147

4. Hidayah NMS, Liu WW, Lai CW, Noriman NZ, Khe CS, Hashim U, et al. Comparison on graphite, graphene oxide and reduced graphene oxide: Synthesis and characterization. AIP Conf Proc. American Institute of Physics Inc.; 2017. p. 150002. https://doi.org/10.1063/1.5005764

5. Witjaksono G, Junaid M, Khir MH, Ullah Z, Tansu N, Saheed MSBM, et al. Effect of nitrogen doping on the optical bandgap and electrical conductivity of nitrogen-doped reduced graphene oxide. Molecules. 2021;26(21):6424. https://doi.org/10.3390/molecules26216424

6. Iskandar F, Setiawan B, Mayangsari TR, Maharsi R, Purwanto A, Aimon AH. Electrochemical impedance analysis of polyvinylpyrrolidone-coated sulfur/reduced graphene oxide (S/rGO) electrode. Mater Res Express. 2019;6(2):025514. https://doi.org/10.1088/2053-1591/aaee41

7. Tarimo DJ, Oyedotun KO, Mirghni AA, Manyala N. Sulphur-reduced graphene oxide composite with improved electrochemical performance for supercapacitor applications. Int J Hydrogen Energy. 2020;45(24):13189–201. https://doi.org/10.1016/j.ijhydene.2020.03.059

8. Gunavathi P, Janaki D, Geethanjali S, Balasubramaniam P, Alagesan A. Characterization and identification of elemental sulphur, iron pyrite, mineral gypsum, Phospho gypsum and marine gypsum by using ATR-FTIR. ~ 80 ~ Pharma Innov J. 2021;10(5):80–6.

9. Chen W, Yan L, Bangal PR. Chemical reduction of graphene oxide to graphene by sulfur-containing compounds. J Phys Chem C. 2010;114(47):19885–90. https://doi.org/10.1021/jp107131v

10. Tian Z, Li J, Zhu G, Lu J, Wang Y, Shi Z, et al. Facile synthesis of highly conductive sulfur-doped reduced graphene oxide sheets. Phys Chem Chem Phys. 2015;18(2):1125–30. https://doi.org/10.1039/c5cp05475c

11. Gunaratna TANR, Prajapati PK, de Silva KMN, de Silva WRM. Comparision of traditional and laboratory methods of sulphur processing. J Ayurveda Integr Med. 2023;14(4):100751. https://doi.org/10.1016/j.jaim.2023.100751

12. Manoratne CH, Rosa SRD, Kottegoda IRM. XRD-HTA, UV Visible, FTIR and SEM Interpretation of Reduced Graphene Oxide Synthesized from High Purity Vein Graphite. Mater Sci Res India. 2017;14(1):19–30. https://doi.org/10.13005/msri/140104

13. Ngullie RC, Bhuvaneswari K, Shanmugam P, Boonyuen S, Smith SM, Sathishkumar M. Magnetically Recoverable Biomass-Derived Carbon-Aerogel Supported ZnO (ZnO/MNC) Composites for the Photodegradation of Methylene Blue. Catalysts. 2022;12(9):1073. https://doi.org/10.3390/catal12091073

14. Djellali S, Touati A, Semmeq A, Kebaili M, Badawi M, Bonilla-Petriciolet A. Unravelling the Methylene Blue Adsorption Mechanism on Doped and Nondoped Polyaniline: A Combined Molecular Modeling and Experimental Investigation. Ponnusamy SK, editor. Int J Chem Eng. 2022;2022:1–18. https://doi.org/10.1155/2022/3181963

15. Bartošová A, Blinová L, Sirotiak M, Michalíková A. Usage of FTIR-ATR as Non-Destructive Analysis of Selected Toxic Dyes. Res Pap Fac Mater Sci Technol Slovak Univ Technol. 2017;25(40):103–11. https://doi.org/10.1515/rput-2017-0012