Supplementary Table 1. Comparison of various key outcomes of green synthesized CeO2 NPs reported in the literatures with our study results.

|  | Our study results | Literatures reported |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Plant’s biological name | Cinnamomum verum | # Calotropis procera | # Portulaca oleracea | # Artabotrys hexapetalus | # Abelmoschus esculentus | # Gloriosa superba | Echinochloa frumentaceae | Centella asiatica | Cucurbita pepo | Tribulus terrestris |
| Precursor used | Cerium nitrate hexahydrate | Cerium chloride | Cerium nitrate hexahydrate | Cerium nitrate hexahydrate | Cerium nitrate hexahydrate | Cerium chloride | Cerium nitrate hexahydrate | Cerium nitrate hexahydrate | Cerium nitrate hexahydrate | - |
| Particle size (nm) | 19.53 | 21 | 4-9 | 14 | 36 | 5 | 31 | 35 | 30 | 100-150 |
| Zeta potential (mV) | -18.7 | - | - | - | - | - | - | - | - | - |
| Structure/ shape | Flake-like structure | Spherical | Quasi-spherical | Spherical | Homogenous | Spherical | Cubic fluorite crystal | Spherical | Face-centered cubic | Irregularly shaped |
| Anti-bacterial activity | Bacillus subtilis | Escherichia coli | - | Staphylococcus aureus | Staphylococcus aureus | Staphylococcus aureus | - | - | - | Pseudomonas aeruginosa |
| Anti-inflammatory activity (% Inhibition) | 70.41% | - | - | - | - | - | - | - | - | 65.2% |
| Anti-oxidant activity (% inhibition or IC50 concentration) | 48.32% | - | - | 70.55 mg/L | 15.47 µg/mL | - | - | 6.95 ± 1.16 μg/mL | - | 82.54% |
| Cell line | NIH3T3 | - | - | - | HT-29 | - | MCF-7 | H-SY5Y | CT26 | - |
| References | - | [1] | [2] | [3] | [4] | [5] | [6] | [7] | [8] | [9] |

Note: It is highly imperative to compare our study results with the existing literature reported on green-synthesized CeO2 NPs, as the source of the plant material, phytoconstituents presence, precursor salt concentration, process parameters, physicochemical properties of the NPs, etc., are different, and therefore, the outcome of the study may differ. However, the authors have tried to compare the results concisely in support of the literature. Please note that the particle size reported in the table may vary, as the literature shown the particle size calculation from different parameters, such as scanning electron microscopy (SEM), transmission electron microscopy (TEM), etc.

References

1. 	Muthuvel A, Jothibas M, Mohana V, Manoharan C. Green synthesis of cerium oxide nanoparticles using Calotropis procera flower extract and their photocatalytic degradation and antibacterial activity. Inorg Chem Commun. 2020;119:108086.

2. 	Hkiri K, Elsayed Ahmed Mohamed H, Ghotekar S, Maaza M. Green synthesis of cerium oxide nanoparticles using Portulaca oleracea Extract: Photocatalytic activities. Inorg Chem Commun. 2024;162:112243.

3. 	Parvathy S, Manjula G, Balachandar R, Subbaiya R. Green synthesis and characterization of cerium oxide nanoparticles from Artabotrys hexapetalus leaf extract and its antibacterial and anticancer properties. Mater Lett. 2022;314:131811.

4. 	Ahmed HE, Iqbal Y, Aziz MH, Atif M, Batool Z, Hanif A, et al. Green synthesis of CeO2 nanoparticles from the Abelmoschus esculentus extract: evaluation of antioxidant, anticancer, antibacterial, and wound-healing activities. Molecules. 2021;26(15):4659.

5. 	Arumugam A, Karthikeyan C, Haja Hameed AS, Gopinath K, Gowri S, Karthika V. Synthesis of cerium oxide nanoparticles using Gloriosa superba L. leaf extract and their structural, optical and antibacterial properties. Materials Science and Engineering: C. 2015;49:408–15.

6. 	Panneerselvam HM, Riyas ZM, Prabhu MR, Sasikumar M, Jeyasingh E. In vitro cytotoxicity assessment of biosynthesized nanoceria against MCF-7 breast cancer cell lines. Applied Surface Science Advances. 2024;21:100603.

7. 	Mamatha MG, Ansari MA, Begum MY, Prasad B. D, Al Fatease A, Hani U, et al. Green Synthesis of Cerium Oxide Nanoparticles, Characterization, and Their Neuroprotective Effect on Hydrogen Peroxide-Induced Oxidative Injury in Human Neuroblastoma (SH-SY5Y) Cell Line. ACS Omega. 2024 Jan 16;9(2):2639–49.

8. 	Mahmoodi P, Motavalizadehkakhky A, Darroudi M, Mehrzad J, Zhiani R. Green synthesis of cerium oxide nanoparticles using zucchini peel extract for cytotoxic and photocatalytic properties. Bioprocess Biosyst Eng. 2023;46(8):1163–73.

9. 	Choudary MRP, Surya M, Saravanan M. Green synthesis of cerium oxide nanoparticles usingTribulus terrestris:  characterization and evaluation of antioxidant, anti-inflammatory and antibacterial efficacy against wound isolates. Biomed Phys Eng Express. 2024 Oct;10(6).