Supporting Information

Moderate Active Fe3+ Doping Enables Improved Cationic and Anionic Redox Reactions for Wide-Voltage-Range Sodium Storage

Congcong Cai,1,2 Xinyuan Li,2 Hao Fan,2 Zhuo Chen,2 Ting Zhu,2 Jiantao Li,4 Ruohan Yu,2 Tianyi Li,5 Ping Hu,1,2,3* and Liang Zhou1,2*

1Hubei Longzhong Laboratory, Wuhan University of Technology (Xiangyang Demonstration Zone), Xiangyang 441000, Hubei, China.

2State Key Laboratory of Advanced Technology for Materials Synthesis and Processing, Wuhan University of Technology, Wuhan 430070, China.

3School of Microelectronics, Hubei University, Wuhan 430062, PR China

4Chemical Sciences and Engineering Division, Argonne National Laboratory, Lemont, IL 60439, USA.

5X-ray Science Division, Argonne National Laboratory, 9700 South Cass Avenue, Lemont, IL 60439, USA.

Corresponding authors: huping316@163.com (Ping Hu); liangzhou@whut.edu.cn (Liang Zhou)

Experimental Section

Materials preparation. The Na0.67Mg0.1FexMn0.9-xO2 (x = 0, 0.1, 0.2) compound was synthesized by a simple organic acid-assisted solid state reaction method. Firstly, oxalic acid (44 mmol) was dissolved in 20 mL deionized water and stirred vigorously for 2 h. Then, NaNO3 (6.7 mmol, 5 wt.% in excess according to stoichiometry), Mg(NO3)2·6H2O (1 mmol), Fe(NO3)3·9H2O (10x mmol), Mn(CH3COO)2·4H2O (9 – 10x mmol) were added stepwise and stirred for 2 h. The suspension was heated to 80 °C overnight to evaporate the water and further dried at 180 °C for 3 h. The as-obtained powder was ground manually and then heated to 500 °C for 2 h. Then the mixture was thoroughly mixed and ground in an agate mortar and pressed into pellets under pressure of 5 MPa. After further heated at in air at 800 °C for 10 h. Then, the sample was naturally cooled down to room temperature, and stored in an Ar-filled glovebox.

Material characterization. X-ray diffraction (XRD) was performed on a Bruker D8 Advance X-ray diffractometer with a Cu Kα X-ray source (λ = 1.5406 Å). Scanning electron microscopy (SEM) were performed on a JEOL-7100F microscope. Transmission electron microscopic (TEM) and high-resolution TEM (HRTEM) images were collected using a JEOL JEM-2100F. High-angle annular dark-field (HAADF)-scanning transmission electron microscopy (STEM) images were conducted on Titans Themis. Raman tests were performed using a Horiba LabRAM HR Evolution with a 532 nm excitation laser. X-ray photoelectron spectroscopy (XPS) was carried out on a Thermo-Fisher Scientific-ESCALAB 250Xi equipped with an Al Kα monochromated X-ray source. X-ray absorption spectroscopy (XAS) measurements were collected at 12-BM-B at the Advanced Photon Source (APS) in Argonne National Laboratory. The radiation was monochromatized by a Si (111) double-crystal monochromator.

Electrochemical Characterization: The electrochemical performances were tested by assembling CR2016 coin cells in the Ar-filled glove box. Sodium foil was used as both the counter and reference electrodes. The working electrodes were prepared by casting the slurry containing 70 wt.% of active materials, 20 wt.% of acetylene black, and 10 wt.% of polyvinylidene fluoride in N-methyl-2-pyrrolidone onto Al foil and dried at 100 °C in a vacuum oven overnight. 1.0 M NaPF6 in propylene carbonate containing 5 % of fluoroethylene carbonate (FEC) was used as the electrolyte and glass fiber was used as the separator. The mass loading of active materials was 1–1.5 mg cm-2. GCD measurements were performed on a NEWARE battery testing system within the potential range of 1.5–4.5 V (vs. Na+/Na). CV tests were conducted on CHI600E electrochemical workstations.

For in-situ XRD test, the electrodes were consisted of 80 wt.% of active materials, 10 wt.% acetylene black and 10 wt.% of polytetrafluoroethylene. For ex-situ measurements, the electrodes were disassembled from the coin cell, washed with electrolyte solution repeatedly, and dried in an Ar-filled glove box.

Fig. S1. XRD patterns of the NMMFs.

Fig. S2. SEM images of the (a) NMM, (b) NMMF-1, and (c) NMMF-2.

Fig. S3. (a) TEM image, (b) SAED, (c) HRTEM, and (d) EDS mapping of NMM.

Fig. S4. (a) TEM image, (b) SAED, (c) HRTEM, and (d) EDS mapping of NMMF-2.

Fig. S5. Fe 2p1/2 and 2p 3/2 XPS peaks of NMM, NMMF-1, and NMMF-2.

Fig. S6. The charge/discharge profiles of NMM and NMMF-2 at 20 mA g-1 in different cycles

Figure S7. The (a) cationic and (b) anionic capacity contributions of NMMFs at the second charge process.

Figure S8. Charge/discharge profiles of (a) NMM, (b) NMMF-1, and (c) NMMF-2 at different current densities.

Figure S9. GITT tests for (a) NMM and (b) NMMF-1, and (c) the calculated Na diffusion coefficient (DNa+).

Table S1. Crystallographic parameters of NMM obtained from XRD Rietveld refinement.

Table S2. Crystallographic parameters of NMMF-1 obtained from XRD Rietveld refinement.