Supporting Information

A Kagome-Derived Mosaic Lattice Family A3V9Te13 (A = Cs, Rb) with Tunable Strong Electronic Correlations

Yusen Xiao1⊥, Zhibin Qiu3,4⊥, Qingchen Duan1, Zhaoyi Li3,4, Xiaotong Xu1, Hengxin Tan2, Shu Guo3,4*, and Ruidan Zhong1,2*

1 Tsung-Dao Lee Institute, Shanghai Jiao Tong University, Shanghai 201210, People’s Republic of China.

2 School of Physics and Astronomy, Shanghai Jiao Tong University, Shanghai 200240, People’s Republic of China.

3 Shenzhen Institute for Quantum Science and Engineering, Southern University of Science and Technology, Shenzhen 518055, China.

4 International Quantum Academy, Shenzhen 518048, China.

KEYWORDS: Kagome-Derived Mosaic Lattice, Geometrical Frustration, Strong Electronic Correlations, Phase Transition

*Correspondence should be addressed to Shu Guo (guos@sustech.edu.cn) and Ruidan Zhong (rzhong@sjtu.edu.cn)

Table of Contents

| Table S1. Crystal Data and Structure Refinements for Cs3V9Te13 (CVT) at 30, 100 and 300 K. | Page S3 |
| --- | --- |
| Table S2. Fractional atomic coordinates and equivalent isotropic displacement parameters (Å2) or CVT at 300 K. | Page S3 |
| Table S3. Crystal Data and Structure Refinements for Rb3V9Te13 (RVT) at 300 K. | Page S4 |
| Table S4. Fractional atomic coordinates and equivalent isotropic displacement parameters (Å2) for RVT at 300 K. | Page S4 |
| Figure S1. Mosaic lattice details for CVT. | Page S5 |
| Figure S2. X-ray diffraction pattern of the CVT single crystal and Rietveld refinement profile of polycrystalline sample. | Page S5 |
| Figure S3. Temperature-dependent single X-ray diffraction patterns of CVT along different crystallographic directions. | Page S6 |
| Figure S4. X-ray Photoelectron Spectroscopy (XPS) spectra for CVT single crystal. | Page S6 |
| Figure S5. Temperature-dependent inverse magnetic susceptibility, (-0)-1, of CVT measured under μ0H = 1 T with the field applied parallel to the ab-plane and the c-axis. | Page S7 |
| Figure S6. Field-dependent magnetization of CVT, measured at various temperatures for the field applied parallel to the ab-plane and the c-axis. | Page S7 |
| Figure S7. a, Temperature-dependent resistivity under zero magnetic field during heating and cooling cycles. b, Temperature-dependent resistivity under different magnetic fields. | Page S8 |
| Figure S8. a, Temperature-dependent specific heat measured during heating and cooling cycles under zero magnetic field. b, Temperature dependence of the entropy change extracted by subtracting a polynomial fit background. | Page S8 |
| Figure S9. X-ray diffraction pattern of the RVT single crystal. The inset shows an optical image of the RVT single crystals. | Page S9 |
| Figure S10. Crystal structure of RVT. a, 3D framework of RVT. b, The V-based 2D Mosaic Lattice. c, Coordination environments for Rb and V atoms, respectively. d, The stacking form of V-based layers. e, Constituent triangular, square, and pentagonal units in a 2D Mosaic Lattice. | Page S9 |
| Figure S11. a, Temperature-dependent magnetization of RVT, measured under different magnetic fields applied parallel to the ab-plane. b, Field-dependent magnetization of RVT at various temperatures for the field applied parallel to the ab-plane and the c-axis. | Page S10 |

Table S1. Crystal Data and Structure Refinements for Cs3V9Te13 (CVT) at 30, 100 and 300 K.

| Empirical formula | Cs3V9Te13 |  |  |
| --- | --- | --- | --- |
| Formula weight | 2516.09 | 2516.09 | 2516.09 |
| Temperature/K | 30 | 100 | 300 |
| Crystal system | Hexagonal | Hexagonal | Hexagonal |
| Space group | P-62m (189) | P-62m (189) | P-62m (189) |
| a/Å | 10.1371(5) | 10.1217(5) | 10.089(3) |
| c/Å | 8.1465(5) | 8.1481(7) | 8.212(3) |
| γ [°] | 120 | 120 | 120 |
| volume/Å3 | 724.98(8) | 722.93(9) | 723.9(5) |
| Z | 1 | 1 | 1 |
| ρcalc /g/cm3 | 5.763 | 5.779 | 5.771 |
| μ/mm-1 | 19.286 | 19.341 | 19.315 |
| F(000) | 1048 | 1048 | 1048 |
| Mo Kα radiation/Å | 0.71073 | 0.71073 | 0.71073 |
| 2θ range for data collection/º | 4.64 to 52.99 | 4.65 to 53.94 | 4.66 to 54.95 |
| Goodness-of-fit | 1.188 | 1.142 | 1.104 |
| Largest diff peak and hole (e/A3) | 2.42 and -1.52 | 1.88 and -0.61 | 1.77 and −1.17 |
| Final R indexes [I ≥ 2σ(I)] | R1 = 0.0309, wR2 = 0.0869 | R1 = 0.0180, wR2 = 0.0420 | R1 = 0.0294, wR2 = 0.0685 |
| Final R indexes [all data] | R1 = 0.0314, wR2 = 0.0872 | R1 = 0.0189, wR2 = 0.0427 | R1 = 0.0304, wR2 = 0.0692 |

Table S2. Fractional atomic coordinates and equivalent isotropic displacement parameters (Å2) or CVT at 300 K.

| Atom | x | y | z | Ueq |
| --- | --- | --- | --- | --- |
| Cs1 | 0.36401(19) | 0.36401(19) | 0 | 0.0336(4) |
| Te1 | 2/3 | 1/3 | 0.25265(16) | 0.0194(3) |
| Te2 | 0 | 0.22819(10) | 0.71992(13) | 0.0168(3) |
| Te3 | 0.41185(15) | 0.41185(15) | 1/2 | 0.0343(5) |
| V1 | 0.1555(4) | 0.1555(4) | 1/2 | 0.0151(8) |
| V2 | 0.8210(3) | 0.2866(3) | 1/2 | 0.0172(6) |

Table S3. Crystal Data and Structure Refinements for Rb3V9Te13 (RVT) at 300 K.

| Empirical formula | Rb3V9Te13 |
| --- | --- |
| Formula weight | 2373.67 |
| Temperature/K | 298(2) |
| Crystal system | Orthorhombic |
| Space group | Cmcm (63) |
| a/Å | 17.5489(13) |
| b/Å | 10.1022(8) |
| c/Å | 15.8691(13) |
| volume/Å3 | 2813.3(4) |
| Z | 4 |
| ρcalc/g/cm3 | 5.604 |
| μ/mm-1 | 21.211 |
| F(000) | 3976.0 |
| Mo Kα radiation/Å | 0.71073 |
| 2θ range for data collection/º | 4.64 to 55.00 |
| Goodness-of-fit on F2 | 1.025 |
| Largest diff peak and hole (e/A3) | 2.148 and -1.519 |
| Final R indexes [I ≥ 2σ(I)] | R1=0.0327, wR2=0.0650 |
| Final R indexes [all data] | R1=0.0439, wR2=0.0701 |

Table S4. Fractional atomic coordinates and equivalent isotropic displacement parameters (Å2) for RVT at 300 K.

| Atom | x | y | z | Ueq | Occupancy |
| --- | --- | --- | --- | --- | --- |
| Te1 | 0.66640(3) | 0.33796(6) | 0.62023(3) | 0.02561(15) | 1 |
| Te2 | 0.38528(3) | 0.72407(5) | 0.63700(3) | 0.01983(14) | 1 |
| Te3 | 0 | 0.56919(7) | 0.86402(5) | 0.01993(18) | 1 |
| Te4 | 0.79518(6) | 0.54361(10) | 0.77289(14) | 0.0463(9) | 0.5 |
| Te5 | 1/2 | 0.42951(14) | 0.77332(16) | 0.0418(9) | 0.5 |
| Rb1 | 1/2 | 1/2 | 1/2 | 0.0516(6) | 1 |
| Rb2 | 0.82328(9) | 1/2 | 1/2 | 0.0465(4) | 1 |
| V1 | 0.92399(11) | 0.41591(17) | 3/4 | 0.0186(4) | 1 |
| V2 | 0.76591(11) | 0.28358(18) | 3/4 | 0.0188(4) | 1 |
| V3 | 0.64462(11) | 0.51489(18) | 3/4 | 0.0184(4) | 1 |
| V4 | 1/2 | 0.6867(2) | 3/4 | 0.0177(6) | 1 |
| V5 | 0.41074(11) | 0.21761(18) | 3/4 | 0.0184(4) | 1 |

Figure S1. Mosaic lattice details for CVT.

Figure S2. X-ray diffraction pattern of the CVT single crystal and Rietveld refinement profile of

polycrystalline sample.

Figure S3. Diffracted reflections in reciprocal lattice planes (0kl), (h0l), and (hk0) determined from experimental data at temperatures of 300 K, 100 K, and 30 K.

Figure S4. X-ray Photoelectron Spectroscopy (XPS) spectra for CVT single crystal.

Figure S5. Temperature-dependent inverse magnetic susceptibility, (-0)-1, of CVT measured under μ0H = 1 T with the field applied parallel to the ab-plane and the c-axis.

Figure S6. Field-dependent magnetization of CVT, measured at various temperatures for the field applied parallel to the ab-plane and the c-axis.

Figure S7. a, Temperature-dependent resistivity under zero magnetic field during heating and cooling cycles. b, Temperature-dependent resistivity under different magnetic fields.

Figure S8. a, Temperature-dependent specific heat measured during heating and cooling cycles under zero magnetic field. b, Temperature dependence of the entropy change extracted by subtracting a polynomial fit background.

Figure S9 X-ray diffraction pattern of the RVT single crystal. The inset shows an optical image of the RVT single crystals.

Figure S10. Crystal structure of RVT. a, 3D framework of RVT. b, The V-based 2D Mosaic Lattice. c, Coordination environments for Rb and V atoms, respectively. d, The stacking form of V-based layers. e, Constituent triangular, square, and pentagonal units in a 2D Mosaic Lattice.

Figure S11. a, Temperature-dependent magnetization of RVT, measured under different magnetic fields applied parallel to the ab-plane. b, Field-dependent magnetization of RVT at various temperatures for the field applied parallel to the ab-plane and the c-axis.