Supporting Information

Facile preparation of NiFe2O4/biochar composite adsorbent for efficient adsorption removal of antibiotics in water

Huagen Liang a, b*, Chenxi Zhu a, b, Anhu Wang a, b, Fu Chen c

a Jiangsu Key Laboratory of Coal-based Greenhouse Gas Control and Utilization, Carbon Neutrality Institute, China University of Mining and Technology, Xuzhou, 221008, China.

b School of Materials Science and Physics, China University of Mining and Technology, Xuzhou, 221008, China.

c School of Public Administration, Hohai University, Nanjing 210098, China.

Fig. S1 TGA and DSC analysis of NFO/BC

Fig. S2 XPS spectra of NFO/BC

Fig. S3 The pore size distribution of NFO/BC before and after TC adsorption

Table S1 Comparison of TC adsorption capacity on different biochars

| Samples | Theoretical maximum adsorption capacity (mg g-1) | Articles |
| --- | --- | --- |
| Fe-N@biochar | 156 | (Mei et al. 2021) |
| Fe/Zn-BC | 145 | (Ma et al. 2021) |
| Fe2O3@sludge | 287 | (Tang et al. 2018) |
| Fe/Mn@BC | 14 | (Zhang et al. 2021) |
| Straw derived MBC | 98 | (Dai et al. 2020) |
| Fe3O4/biochar | 242.67 | (Yang et al. 2021) |
| MgFe2O4/biochar | 120.4 | (Deng et al. 2022) |
| Fe3O4/biochar | 73.4 | (Zhang et al. 2023) |
| γ-Fe2O3/biochar | 34.9 | (Wang et al. 2020) |
| Fe3O4/biochar | 15.3 | (Ryenchindorj et al. 2022) |
| NFO@BC | 420.4 | This work |

Table S2 Parameters of Langmuir and Freundlich models for TC adsorption

| Samples | Freundlich isotherm model |  |  | Langmuir isotherm model |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | n | Kf (mg(n+1) g-1 L-n) | R2 | Qm (mg g-1) | KL (mg L-1) | R2 |
| BC | 1.22 | 1.88 | 0.9984 | 62.14 | 0.006 | 0.9746 |
| NFO | 1.64 | 1.84 | 0.9753 | 60.61 | 0.007 | 0.9923 |
| NFO/BC | 1.79 | 2.71 | 0.9924 | 420.41 | 0.003 | 0.9965 |

Table S3 Kinetic parameters for TC adsorption on different adsorbents

| Samples | Pseudo-first-order |  | Pseudo-second-order |  |  |
| --- | --- | --- | --- | --- | --- |
|  | k1 (×10-1) (min-1) | R2 | k2 (×10-1) (g mg-1 min-1) | qe (mg g-1) | R2 |
| BC | 0.24 | 0.9171 | 0.029 | 12.29 | 0.9652 |
| NFO | 0.32 | 0.9806 | 0.044 | 10.31 | 0.9778 |
| NFO/BC | 0.93 | 0.9596 | 0.066 | 18.85 | 0.9911 |

Table S4 Thermodynamic parameters of TC adsorption on different adsorbents

| Samples | ∆H (kJ mol-1) | ∆S (kJ mol-1 K-1) | ∆G (kJ mol-1) |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  |  | 288.15 K | 298.15 K | 308.15 K |
| BC | 8.7234 | 0.0381 | -2.161 | -2.722 | -2.923 |
| NFO | -17.616 | -0.0527 | -2.536 | -1.717 | -1.482 |
| NFO/BC | 31.384 | 0.1264 | -5.112 | -6.104 | -7.639 |

Table S5 The pore parameters of NFO/BC before and after TC adsorption

| Samples | BET surface area (m2 g-1) | Average pore size (nm) | Pore volume (cm3 g-1) |
| --- | --- | --- | --- |
| Before adsorption | 356.5 | 3.80 | 0.34 |
| After adsorption | 174.6 | 4.39 | 0.19 |

References:

Dai JW, Meng XF, Zhang YH, Huang YJ (2020) Effects of modification and magnetization of rice straw derived biochar on adsorption of tetracycline from water, Bioresour Technol 311:123455. https://doi.org/10.1016/10.1016/j.biortech.2020.123455

Deng Y, Wang M, Yang YP, Li X, Chen WQ, Ao TQ (2022) Enhanced adsorption performance of sulfamethoxazole and tetracycline in aqueous solutions by MgFe2O4-magnetic biochar, Water Sci Technol 86:568-583. https://doi.org/10.1016/10.2166/wst.2022.227

Ma Y, Li M, Li P, Yang L, Wu L, Gao F, Qi X, Zhang Z (2021) Hydrothermal synthesis of magnetic sludge biochar for tetracycline and ciprofloxacin adsorptive removal, Bioresour Technol 319https://doi.org/10.1016/10.1016/j.biortech.2020.124199

Mei YL, Xu J, Zhang Y, Li B, Fan SS, Xu HC (2021) Effect of Fe-N modification on the properties of biochars and their adsorption behavior on tetracycline removal from aqueous solution, Bioresour Technol 325:124732. https://doi.org/10.1016/10.1016/j.biortech.2021.124732

Ryenchindorj U, Zaib Q, Putra AS, Park H-S (2022) Production and characterization of cost-effective magnetic pine bark biochar and its application to remove tetracycline from water, Environ Sci Pollut Res 29:62382-62392. https://doi.org/10.1016/10.1007/s11356-022-19866-9

Tang L, Yu JF, Pang Y, Zeng GM, Deng YC, Wang JJ, Ren XY, Ye SJ, Peng B, Feng HP (2018) Sustainable efficient adsorbent: Alkali-acid modified magnetic biochar derived from sewage sludge for aqueous organic contaminant removal, Chem Eng J 336:160-169. https://doi.org/10.1016/10.1016/j.cej.2017.11.048

Wang JP, Zhang M, Zhou RJ, Li JY, Zhao W, Zhou JH (2020) Adsorption characteristics and mechanism of norfloxacin in water by γ-Fe2O3@BC, Water Sci Technol 82:242-254. https://doi.org/10.1016/10.2166/wst.2020.078

Yang Hc, Yu H, Wang Jh, Ning T, Chen P, Yu J, Di Sy, Zhu Sk (2021) Magnetic porous biochar as a renewable and highly effective adsorbent for the removal of tetracycline hydrochloride in water, Environ Sci Pollut Res 28:61513-61525. https://doi.org/10.1016/10.1007/s11356-021-15124-6

Zhang X, Li YR, Wu MR, Pang Y, Hao ZB, Hu M, Qiu RL, Chen ZH (2021) Enhanced adsorption of tetracycline by an iron and manganese oxides loaded biochar: Kinetics, mechanism and column adsorption, Bioresour Technol 320:124264. https://doi.org/10.1016/10.1016/j.actatropica.2020.124264

Zhang XZ, Zhen DW, Liu FM, Chen R, Peng QR, Wang ZY (2023) An achieved strategy for magnetic biochar for removal of tetracyclines and fluoroquinolones: Adsorption and mechanism studies, Bioresour Technol 369:128440. https://doi.org/10.1016/10.1016/j.biortech.2022.128440

Corresponding authors: lianghg@cumt.edu.cn (Huagen Liang); chenfu@hhu.edu.cn (Fu Chen)