# Supporting Information

Effect of low-carbon coal gangue on the stability and dissolved or-ganic matter characteristics of co-pyrolysis biochar: insights on py-rolysis temperatures and minerals

Table S1 The basic properties and oxide composition of coal gangue.

| Sample | C(%) | H(%) | N(%) | S(%) | SiO2(%) | Al2O3(%) | Fe2O3(%) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Coal gangue | 2.60 | 0.948 | 1.69 | 0.076 | 65.80 | 23.16 | 1.97 |

Table S2 Calculation formula for EEM fluorescence spectral parameters.

| Parameter | Formula |
| --- | --- |
| Fluorescence index (FI) | FI=Fλem=450nmFλem=500nm, λex=370nm |
| Biological index (BIX) | BIX=Fλem=380nmFλem=430nm, λex=310nm |
| Humification index (HIX) | HIX=∑Fλem=435-480nm∑Fλem=300-345nm, λex=255nm |

Table S3 R50 values of straw biochar and coal gangue-straw co-pyrolysis biochar.

| Biochar | R300 | R450 | R600 | W300 | W450 | W600 | C300 | C450 | C600 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| R50 | 0.50 | 0.52 | 0.57 | 0.50 | 0.52 | 0.57 | 0.50 | 0.52 | 0.55 |
| Co-pyrolysis biochar | CR300 | CR450 | CR600 | CW300 | CW450 | CW600 | CC300 | CC450 | CC600 |
| R50 | 0.47 | 0.52 | 0.58 | 0.45 | 0.50 | 0.56 | 0.47 | 0.53 | 0.60 |

Table S4 Basic properties of corn straw biochar and coal gangue-corn straw co-pyrolysis biochar.

| Sample | C300 | C450 | C600 | CC300 | CC450 | CC600 |
| --- | --- | --- | --- | --- | --- | --- |
| C(%) | 51.81 | 54.60 | 51.22 | 43.59 | 41.26 | 41.34 |
| H(%) | 2.89 | 1.64 | 0.75 | 2.33 | 1.30 | 0.65 |
| O(%) | 12.98 | 2.98 | 2.31 | 13.17 | 5.18 | 2.59 |
| Ash(%) | 28.88 | 37.48 | 42.03 | 38.17 | 48.69 | 51.85 |
| H:C | 0.67 | 0.36 | 0.18 | 0.64 | 0.38 | 0.19 |
| O:C | 0.19 | 0.04 | 0.03 | 0.23 | 0.09 | 0.05 |

Table S5 R50 values of corn straw biochar and minerals-corn straw co-pyrolysis biochar.

| Sample | C600 | FeC600 | AlC600 | SiC600 |
| --- | --- | --- | --- | --- |
| R50 | 0.55 | 0.57 | 0.58 | 0.56 |

Table S6 UV-vis and EEM spectra parameters of DOM derived from minerals-corn straw co-pyrolysis biochar.

| Sample |  | SUVA254 (L mg-1 m-1) |  | SUVA260 (L mg-1 m-1) | FI | BIX |  | HIX |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| FeC600 |  | 5.49±0.68 |  | 4.23±0.59 |  | 1.49±0.02 |  | 0.30±0.01 |  | 9.04±0.50 |  |
| AlC600 |  | 9.35±0.98 |  | 7.26±0.80 |  | 1.47±0.02 |  | 0.53±0.01 |  | 11.09±0.26 |  |
| SiC600 |  | 9.71±0.37 |  | 7.78±0.55 |  | 1.42±0.01 |  | 0.60±0.00 |  | 9.99±0.29 |  |

Fig. S1 (a) TGA and DTA curves of  coal gangue and corrected TGA curves of biochar and co-pyrolysis biochar.

Fig. S2 The Raman spectra of corn straw biochar and coal gangue-corn straw co-pyrolysis biochar.

Fig. S3 The DOC content in corn straw biochar and coal gangue-corn straw co-pyrolysis biochar.

Fig. S4 Linear regression analysis of DOC content and R50 values.

Fig. S5 UV-vis patterns of coal gangue and biochar samples.

Fig. S6 Four components and loadings map of DOM.

Fig. S7 Raman spectra of corn straw biochar and minerals-corn straw co-pyrolysis biochar.

Fig. S8 The fluorescence excitation-emission matrix (EEM) spectra of DOM derived from corn straw biochar and minerals-corn straw co-pyrolysis biochar.