Suppl. Fig. 1 Fitting of isotherm data with Temkin models for uptaking 2,4-DCP by UM-CC at pH 8.00 at different temperatures (▀ = 30℃, ▲= 40℃ & ● = 50℃)

Suppl. Table 1. Temkin coefficients for uptaking 2,4-DCP by unmodified coconut coir (UM-CC) at pH 8.00 and at different temperatures

| Temperature (C) | Temkin Coefficients |  |  |
| --- | --- | --- | --- |
|  | AT (L/g) | bT × 10-6 | R2 |
| 30 | 1.00 | 17.89 | 0.545 |
| 40 | 1.00 | 15.17 | 0.634 |
| 50 | 1.00 | 16.26 | 0.573 |