Mechanisms of Microplastics Sorption of Antibiotics and Impacts on Aquatic Ecosystems for Sustainable Development Goals

Obed Nwasen Likpalimora,d*, Shiwen Zhanga, Favour Iwueseter Adagbgab,

Sawyer Fatoyec, King Jones Adegad, Joab Njued

a School of Earth and Environment, Anhui University of Science and Technology, Huainan 232001, PR China.

b School Economics and Management, Anhui University of Science and Technology, Huainan 232001, PR China.

c School of Materials Science and Engineering, Northwestern Polytechnical University, Xi’an 710072, PR China.

d School of Environmental Science and Engineering, Suzhou University of Science and Technology, Suzhou 215009, PR China.

Obed Nwasen Likpalimor a,d (Corresponding Author)*

Email: likpalimor@gmail.com

Table S1. Different types of microplastics and their characteristics.

| MPs | Crystallinity | Polarity Property | Temperature at which glass transitions (Tg, C) | Point of zero charge (PZC) | Density (g/cm3) |
| --- | --- | --- | --- | --- | --- |
| PP | Semicrystalline | Nonpolarity | (-49) - (-20) | 4.26/6.76 | 0.88-1.23 |
| PE | Semicrystalline | Nonpolarity | (-110) - (-125) | 4.30/6.63 | 0.92-0.97 |
| PS | Amorphous | Weak polarity | 90-100 | 3.96/6.69/(3.1-4.3) | 1.04-1.50 |
| PVC | Amorphous | Polarity | 60-100 | 6.65 | 1.15-1.70 |
| MPs | Crystallinity | Polarity Property | Temperature at which glass transitions (Tg, C) | Point of zero charge (PZC) | Density (g/cm3) |
| PET | Amorphous | Polarity | 90 | - | 1.30-1.50 |
| PA | Semicrystalline | Polarity | 73-78 | 6.52 | 1.12-1.14 |

Note: The temperature at which polymer molecules begin to migrate from freezing to moving is known as Tg. The polymer is in a glassy state below this temperature and begins to move and exhibit great elasticity similar to rubber above this temperature. "-" denotes not found in the source material. The order of the crystallinity is as follows: PVC > PP > PA ≈PS > PE (Sources:(1–4).

Table S2. Microplastics and antibiotic interactions

| Microplastic | Antibiotic | Type of interaction | Reference |
| --- | --- | --- | --- |
|  | Levofloxacin | Intermolecular hydrogen bonding, ion exchange, electrostatic interaction, halogen bonds | (5) |
| PE | Tetracycline | surface characteristics, electrostatic interaction, and hydrogen bonding | (6) |
| PE | Oxytetracycline Hydrochloride Tetracycline Chlortetracycline | Hydrogen bonds, electrostatic attraction, and van der Waals forces | (7) |
| HDPE, LDPE, PVC, PP | Enrofloxacin, Norfloxacin, and Ciprofloxacin. | Hydrophobic and electrostatic interaction | (8) |
| Table S2 Cont’d |  |  |  |
| Microplastic | Antibiotic | Type of interaction | Reference |
| PE | Oxytetracycline Hydrochloride Tetracycline Chlortetracycline | Hydrogen bonds, electrostatic attraction, and van der Waals forces | (7) |
| PE, PP | Tylosin | Surface complexations and Hydrophobic interactions | (9) |
| PE | Sulfamethoxazole | electrostatic interactions, Van der Waals and hydrophobic, | (10) |
| PE, PP, PS, PA, PET, PVC | Sulfamethazine | Electrostatic and Van der Waals interactions | (11) |
| PS, PVC | Ciprofloxacin | Electrostatic attraction, π-π, cation exchange, partition, and hydrogen bonding | (12) |
| PE, PS | Cephalosporin, Sulfamethoxazole, and Sulfamethazine | Van der Waals, Hydrophobicity and surface complexation | (11) |
| Nylon | Tetracycline | Van der Waals interactions | (13) |
| PS, PET, POM | Azithromycin Clarithromycin | Hydrophobic interaction | (14) |
| PS | Ciprofloxacin | Hydrophobicity, hydrogen bonding, Electrostatic, and π-π interaction | (15) |

Table S3. Factors influencing antibiotic sorption onto microplastics

| Factor | Type of Interaction | Antibiotic–Microplastic | Effects | Reference |
| --- | --- | --- | --- | --- |
| pH | Electrostatic Interaction | Ciprofloxacin (CPX)–PE | Acidic & Alkaline → Interaction decreased due to electrostatic repulsion | (16) |
|  |  |  | Neutral → Electrostatic interaction dominates |  |
|  |  | Fluoroquinolones (FQ)–PS | Maximum adsorption of FQ over PS between pH ~5–6 | (17) |
|  |  | Oxytetracycline (OTC)–PS | Maximum adsorption at pH 5 due to minimal electrostatic repulsion | (17) |
|  |  | Tylosin (TYL)–PVC, PS, PE, PP | Interaction decreases with increasing pH (3.0–7.2) | (9) |
| pH | Hydrophobic Interaction | Ciprofloxacin (CPX)–PE | Neutral → Hydrophobic interaction dominates | (18) |
|  |  | Tylosin (TYL)–PVC, PS, PE, PP | Hydrophobic interaction dominates at pH >7.2 | (9) |
| pH | van der Waals Interaction | Sulfamethoxazole (SMX)–PE | No significant change upon changing pH | (19) |
| Salinity | Electrostatic Interaction | Fluoroquinolones (FQ)–PS | Increase in salinity reduces adsorption due to NP aggregation & salting-out effect | (17) |
| Salinity | Hydrophobic Interaction | Tetracycline (TC)–PE, PP, PS | Increasing NaCl concentration (0.05–3.5%) had no significant effect | (20) |
| Table S3 Cont’d |  |  |  |  |
| Factor | Type of Interaction | Antibiotic–Microplastic | Effects | Reference |
| Salinity | Hydrophobic Interaction | Tetracycline (TC)–PE, PP, PS | Increasing NaCl concentration (0.05–3.5%) had no significant effect | (19) |
| Salinity | Hydrophobic Interaction | Tylosin (TYL)–PVC, PS, PE, PP | Sorption first increased, then decreased with increasing ionic strength (0–0.1 M) | (9) |
| Salinity | van der Waals Interaction | Sulfamethoxazole (SMX)–PE | No significant change upon changing salinity | (20) |
| Humic Acid | Electrostatic Interaction | Ciprofloxacin (CPX)–PE | Interaction decreases due to higher affinity of CPX for humic acid | (16) |
| Humic Acid | Electrostatic Interaction | Fluoroquinolones (FQ)–PS | Interaction decreases with increasing humic acid concentration | (21) |
| Humic Acid | Electrostatic Interaction | Oxytetracycline (OTC)–PS | Interaction increases due to π-π interaction with humic acid | (22) |
| Other Ions | Electrostatic Interaction | Ciprofloxacin (CPX)–PE | Interaction decreases due to sodium ion disturbance in PE’s electrical double layer | (16) |
| Other Ions | Cationic Bridging Mechanism | Tetracycline (TC)–PE | Interaction decreases with Cu²⁺ but increases with Pb²⁺, Cr³⁺, Cd²⁺, Zn²⁺ due to metal bridging | (5) |
| Other Ions | Cationic Bridging Mechanism | Oxytetracycline (OTC)–PS | Interaction increases with multivalent cations (Ca²⁺) due to ternary complex formation | (22) |

Records identified from*:

Databases (n = 1,500)

Registers (n = 0)

Total records identified (n = 1,500)

Records removed before screening:

Duplicate records removed (n = 350)

Records marked as ineligible by automation tools (n = 0)

Records removed for other reasons (n = 0)

Records screened

(n = 1,200)

Records excluded**

(n = 952)

Reports sought for retrieval

(n = 248)

Reports not retrieved

(n =0)

Reports assessed for eligibility

(n = 248)

Reports excluded: n =76

Reports excluded:

Macroplastic focus (n = 40)

Non-English (n = 20)

Insufficient data (n = 16)

Studies included in review

(n = 172)

Reports of included studies

(n = 172)

Identification of studies via databases and registers

Identification

Screening

Included

Records identified from*:

Databases (n = 1,500)

Registers (n = 0)

Total records identified (n = 1,500)

Records removed before screening:

Duplicate records removed (n = 350)

Records marked as ineligible by automation tools (n = 0)

Records removed for other reasons (n = 0)

Records screened

(n = 1,200)

Records excluded**

(n = 952)

Reports sought for retrieval

(n = 248)

Reports not retrieved

(n =0)

Reports assessed for eligibility

(n = 248)

Reports excluded: n =76

Reports excluded:

Macroplastic focus (n = 40)

Non-English (n = 20)

Insufficient data (n = 16)

Studies included in review

(n = 172)

Reports of included studies

(n = 172)

Identification of studies via databases and registers

Identification

Screening

Included

Figure S1: PRISMA 2020 flow diagram of the literature search and selection process. A total of 1,500 records were identified from six databases. After removing 350 duplicates and screening titles/abstracts, 248 full-text articles were assessed for eligibility. Seventy-six studies were excluded due to macroplastic focus, non-English language, or insufficient data, resulting in 172 studies included in the qualitative synthesis.

References

1. 	Crawford CB, Quinn B. Microplastics, standardisation and spatial distribution. 2017;

2. 	Dong H, Chen Y, Wang J, Zhang Y, Zhang P, Li X, et al. Interactions of microplastics and antibiotic resistance genes and their effects on the aquaculture environments. J Hazard Mater. 2021 Feb 5;403:123961.

3. 	Li X, Chen L, Mei Q, Dong B, Dai X, Ding G, et al. Graphic abstract SC. Water Res [Internet]. 2018; Available from: https://doi.org/10.1016/j.watres.2018.05.034

4. 	Xue X, Hong S, Cheng R, Li H, Qiu L, Fang C. Adsorption characteristics of antibiotics on microplastics: The effect of surface contamination with an anionic surfactant. Chemosphere. 2022 Nov 1;307:136195.

5. 	Yu F, Li Y, Huang G, Yang C, Chen C, Zhou T, et al. Adsorption behavior of the antibiotic levofloxacin on microplastics in the presence of different heavy metals in an aqueous solution. Chemosphere. 2020;260.

6. 	Yu F, Yang C, Huang G, Zhou T, Zhao Y, Ma J. Interfacial interaction between diverse microplastics and tetracycline by adsorption in an aqueous solution. Sci Total Environ [Internet]. 2020;721:137729. Available from: https://doi.org/10.1016/j.scitotenv.2020.137729

7. 	Chen Y, Li J, Wang F, Yang H, Liu L. Adsorption of tetracyclines onto polyethylene microplastics: A combined study of experiment and molecular dynamics simulation. Chemosphere [Internet]. 2021;265:129133. Available from: https://doi.org/10.1016/j.chemosphere.2020.129133

8. 	Puckowski A, Cwie W, Mioduszewska K, Stepnowski P, Bia A. Chemosphere Sorption of pharmaceuticals on the surface of microplastics. 2021;263.

9. 	Guo X, Pang J, Chen S, Jia H. AC SC. 2018;

10. 	Xu S. Decomplexation of Cu(II)/Ni(II)-EDTA by ozone-oxidation process. 2019;(Ii).

11. 	Guo X, Wang J. Sorption of antibiotics onto aged microplastics in freshwater and seawater. Mar Pollut Bull [Internet]. 2019;149(August):110511. Available from: https://doi.org/10.1016/j.marpolbul.2019.110511

12. 	Liu J, Ma Y, Xu T, Shao G. Preparation of zwitterionic hybrid polymer and its application for the removal of heavy metal ions from water. J Hazard Mater [Internet]. 2010;178(1–3):1021–9. Available from: http://dx.doi.org/10.1016/j.jhazmat.2010.02.041

13. 	Lin W, Jiang R, Wu J, Wei S, Yin L, Xiao X, et al. Sorption properties of hydrophobic organic chemicals to micro-sized polystyrene particles. Sci Total Environ [Internet]. 2019;690:565–72. Available from: https://doi.org/10.1016/j.scitotenv.2019.06.537

14. 	González-Pleiter M, Pedrouzo-Rodríguez A, Verdú I, Leganés F, Marco E, Rosal R, et al. Microplastics as vectors of the antibiotics azithromycin and clarithromycin: Effects towards freshwater microalgae. Chemosphere. 2021;268.

15. 	Xiong Y, Zhao J, Li L, Wang Y, Dai X, Yu F, et al. Interfacial Interaction between Micro / Nanoplastics and Typical. Water Res [Internet]. 2020;116100. Available from: https://doi.org/10.1016/j.watres.2020.116100

16. 	Atugoda T, Wijesekara H, Werellagama DRIB, Jinadasa KBSN, Bolan NS, Vithanage M. Adsorptive interaction of antibiotic ciprofloxacin on polyethylene microplastics: Implications for vector transport in water. Environ Technol Innov [Internet]. 2020;19:100971. Available from: https://doi.org/10.1016/j.eti.2020.100971

17. 	Zhang Y, Diehl A, Lewandowski A, Gopalakrishnan K, Baker T. Science of the Total Environment Removal ef fi ciency of micro- and nanoplastics ( 180 nm – 125 μ m ) during drinking water treatment. Sci Total Environ [Internet]. 2020;720:137383. Available from: https://doi.org/10.1016/j.scitotenv.2020.137383

18. 	Atugoda T, Vithanage M, Wijesekara H, Bolan N, Sarmah AK, Bank MS, et al. Interactions between microplastics, pharmaceuticals and personal care products: Implications for vector transport. Environ Int [Internet]. 2021;149:106367. Available from: https://doi.org/10.1016/j.envint.2020.106367

19. 	Xu B, Liu F, Brookes PC, Xu J. The sorption kinetics and isotherms of sulfamethoxazole with polyethylene microplastics. Mar Pollut Bull [Internet]. 2018;131(April):191–6. Available from: https://doi.org/10.1016/j.marpolbul.2018.04.027

20. 	Xu B, Liu F, Brookes PC, Xu J. Microplastics play a minor role in tetracycline sorption in the presence of dissolved organic matter *. Environ Pollut [Internet]. 2018;240:87–94. Available from: https://doi.org/10.1016/j.envpol.2018.04.113

21. 	Zhang C, Wang S, Sun D, Pan Z, Zhou A, Xie S, et al. Microplastic pollution in surface water from east coastal areas of Guangdong, South China and preliminary study on microplastics biomonitoring using two marine fish. Chemosphere [Internet]. 2020;256:127202. Available from: https://doi.org/10.1016/j.chemosphere.2020.127202

22. 	Zhang H, Jiaqing W, Zhou B, Zhou Y, Dai Z, Zhou Q. AC SC. Environ Pollut [Internet]. 2018; Available from: https://doi.org/10.1016/j.envpol.2018.09.122