Mitigating Interfacial Carrier Crowding by An Ultrathin LiF Interlayer Towards Efficient and Stable Perovskite Light-Emitting Diodes

Xiaofei·Zhang1 · Lin Wang1 · Lingmei Kong1 ·Sheng Wang1 · Jun Dai3 ·Guohua Jia4· Xuyong Yang1, 2

1 Key Laboratory of Advanced Display and System Applications of Ministry of Education, Shanghai University,149 Yanchang Road, Shanghai 200072, P. R. China

2 Shanghai University Microelectronic R&D Center, Shanghai University, Shanghai 201900, P. R. China

3 Department of Physics, Jiangsu University of Science and Technology, Zhenjiang 212100, P. R. China

4School of Molecular and Life Sciences, Curtin University, GPO Box U1987, Perth, WA 6845, Australia

* Lin Wang, Xuyong Yang

lin_wang@shu.edu.cn; yangxy@shu.edu.cn

Fig. S1 (a) UPS spectra of high binding energy secondary-electron cutoff (left) and valence band edge regions of perovskite film (right). (b) Perovskite film upon the incident photon energy (hv).

The energy levels of the perovskite layer were calculated from the UV/Vis absorption and Ultraviolet photoelectron spectroscopy (UPS) spectra (Figure S1). UPS spectra are conducted to explore the influence of the perovskite film with LiF interlayer. From the secondary electron cutoff (Ecutoff) region in following figures, the work functions (WF = 21.2 eV - Ecutoff) of the perovskite film with LiF interlayer are 4.64 eV. The corresponding valence band maxima (VBM) is 5.38 eV (VBM = - (Ecutoff + Eonset)). And the conduction band minimum (CBM) is 3.01 eV (CBM = - (VBM - Eg)).

Fig. S2 Photoluminescence quantum yields (PLQYs) of the films without or with LiF interlayer.

Table S1 Performance parameters of PeLEDs based on LiF interlayer of different thicknesses

| Sample | Wavelength (nm) | Max. Luminance (cd m-2) | Max. EQE (%) |
| --- | --- | --- | --- |
| control | 514 | 23984 | 20.68 |
| 1.0 nm | 514 | 26779 | 22.12 |
| 2.0 nm | 514 | 29443 | 23.61 |
| 3.0 nm | 514 | 20663 | 20.68 |

Table S2 Performance parameters of PeLEDs based on LiF interlayer of different location

| Sample | Wavelength (nm) | Max. Luminance (cd m-2) | Max. EQE (%) |
| --- | --- | --- | --- |
| device Ⅰ | 514 | 30845 | 24.03 |
| device Ⅱ | 514 | 26962 | 22.34 |
| device Ⅲ | 514 | 21075 | 20.75 |

Table S3 PL lifetime summary with or without LiF interlayer

| devices | τ1 (ns) | A1 (%) | τ2 (ns) | A2 (%) | τ3 (ns) | A3 (%) | τavg (ns) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| w/o LiF | 10 | 10 | 44 | 42 | 214 | 48 | 122.20 |
| w/LiF | 8 | 12 | 57 | 37 | 278 | 55 | 174.95 |

τavg is calculated by the fitted data of the PL decay curves as follows

τavg=A1τ1+A2τ2+A3τ3

in which A1, A2, and A3 are the amplitudes of each component while τ1, τ2, and τ3 are the corresponding lifetime constants.