Supplementary Information

Defect-engineered Liquid-gated MoS2 field-effect transistor for pH sensing

Chao Wu1,2#, Yunong Xie3#, Quankun Luo4#, Taotao Li2, Yunfei Gao1, Hui Li5, Jianping Shi5, Maguang Zhu2*, Mengmeng Xiao1*

1Key Laboratory for the Physics and Chemistry of Nanodevices, Department of Electronics, Peking University, Beijing 100871, China

2School of Integrated Circuits, Nanjing University, Jiangsu 210023, China

3College of Metrology Measurement and Instrument, China Jiliang University, Hangzhou, Zhejiang 310018, China

4Hunan Institute of Advanced Sensing and Information Technology, Xiangtan University, Hunan 411105, China

5The Institute for Advanced Studies, Wuhan University, Wuhan 430072, China

*Address correspondences: mgzhu@nju.edu.cn, mmxiao@pku.edu.cn,

# These authors contribute equally.

Fig. S1 a and b Optical microscopy images of the as-grown continuous MoS2 films.

Fig. S2 a and b Raman mapping characteristics of E2g and A1g peaks centered at 384 and 403cm-1, respectively.

Fig. S3 XPS spectra of a Mo 3d and b S 2p regions for defective MoS2. Deconvoluted peaks correspond to Mo4+ (3d5/2 at 231.2 eV and 3d3/2 at 234.3 eV), S2- (2p3/2 at 164.0 eV and 2p1/2 at 165.2 eV).

Fig. S4 Transfer characteristics curves of liquid-gated MoS2 FET in PBS (0.1×) solution (pH~7.4) measured with respect to time at Vds = 0.1 V.

Fig. S5 Transfer characteristics curves of liquid-gated MoS2 (low-defect CVD growth without H2) FET in the PBS solutions with different pH values at Vds = 0.1 V.

Table S1 Sensing Performance of Low-material FET pH Sensors:

| Channel Material | Structure | SS (mV/dec) | Current Sensitivity (%/pH-1) | Voltage Sensitivity (mV/pH) | pH Range | Reference |
| --- | --- | --- | --- | --- | --- | --- |
| Graphene | FET | ~1000 | ~30 | 24.6 | 6.0-8.0 | [31] |
| ReS2 | FET | 116 | 126 | 54.8 | 3.21-8.11 | [20] |
| WSe2 | FET | 120 | 100 | 30 | 4.0-7.2 | [22] |
| In2O3 | FET | 81.3 | ~100 | 59±0.6 | 4.0-8.0 | [14] |
| MoS2 | FET | 250 | 142 | ~59.6 | 3.0-8.5 | [24] |
| MoS2 | FET | 78 | 713 | 59 | 3.0-5.0 | [23] |
| MoS2 | FET | 70 | 534.8 | 44 | 4.6-9.5 | This work |