| Nigerian Federal Ministry of Works criteria for subbase requirements applied soil samples aggregates | 1American Association of State Highway and Transportation Officials (AASHTO) criteria for subbase requirements applied to samples. | 2Samples and US Army engineering Corp subgrade and subbase criteria. |
| --- | --- | --- |
| Criteria | Criteria | Criteria |
| Percentage passing sieve no 200; not more than 35% | P 0.075 /P0.425 <2/3 | Percentage passing sieve no 10 =100% |
| Liquid limit not to exceed 30% | Liquid Limit < 25% | Percentage passing sieve no 200; not more than 15% |
| Plasticity Index, not more than 12 | Plasticity Index < 6 | Liquid Limit; not more than 25% |
| 24Hour soaked California Bearing Ratio; 30%Minimum | 24 Hours-soaked California Bearing Ratio; 30%Minimum | Plasticity Index; not more than 5% |
|  |  | Maximum Design CBR of 30% |

Supplement to Table 4.   Subbase requirements by NFMW, AASHTO, US Army Engineering Corp.

1. American Association of State Highways and Transportation Officials (1996) Standard specifications for highway materials: part 1. AASHTO, Washington DC

2. United States Army Field Manual FM No 5-430-00-1 (1994) Airforce joint pamphlet army manual (AFJPAM 32-8013), Vol I. Subgrades and base courses Chapter 5. pp 5–7. Department of the Army, Department of the Air Force Washington, DC.