	Nigerian Federal Ministry of Works criteria for subbase requirements applied soil samples aggregates            
	1American Association of State Highway and Transportation Officials (AASHTO) criteria for    subbase requirements applied to samples.
	2Samples and US Army engineering Corp subgrade and subbase criteria.

	Criteria
	Criteria
	 Criteria

	Percentage passing sieve no 200; not more than 35%
	P 0.075 /P0.425       <2/3
	Percentage passing sieve    no 10 =100%

	Liquid limit not to exceed 30%
	Liquid Limit < 25%
	Percentage passing sieve     no 200; not more than 15%

	Plasticity Index, not more than 12
	Plasticity Index < 6
	Liquid Limit; not more than 25%

	24Hour soaked California Bearing Ratio; 30%Minimum
	24 Hours-soaked California Bearing Ratio; 30%Minimum
	Plasticity Index; not more than 5%

	
	
	Maximum Design CBR of 30%



Supplement to Table 4.   Subbase requirements by NFMW, AASHTO, US Army Engineering Corp.


1. American Association of State Highways and Transportation Officials (1996) Standard specifications for highway materials: part 1. AASHTO, Washington DC
2. United States Army Field Manual FM No 5-430-00-1 (1994) Airforce joint pamphlet army manual (AFJPAM 32-8013), Vol I. Subgrades and base courses Chapter 5. pp 5–7. Department of the Army, Department of the Air Force Washington, DC.











