Supplementary Materials

- Data Processing

To evaluate the multicollinearity of variables to identify if there are correlations between the majority of the variables we computed the the Pearson correlation coefficient (Rxy).

- Normalized Dataset

We used the min-max scaling method to normalize all input data and target variables. The Min-Max normalization is available as a feature within GeneXProTool

Table S1.  Normalized Training Set

| Cement | Water | Ceramic Fine Aggregate | W/C | Natural Coarse Aggregate | Natural Fine Aggregate | Superplasticizer | Age | Compressive Strength |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0 | 0.137559 | 1.49E-03 | 0.25 | 0.465385 | 1 | 0.3 | 0 | 0.467116358 |
| 0 | 0.137559 | 0.109134 | 0.25 | 0.465385 | 0.888372 | 0.2625 | 0 | 0.55143339 |
| 0 | 0.137559 | 0.269099 | 0.25 | 0.465385 | 0.722093 | 0.3 | 0 | 0.531197302 |
| 0 | 0.137559 | 0.429063 | 0.25 | 0.465385 | 0.555814 | 0.3 | 0 | 0.483979764 |
| 0 | 0.137559 | 0 | 0.25 | 0.465385 | 1 | 0.375 | 0 | 0.60539629 |
| 0 | 0.137559 | 0.104649 | 0.25 | 0.465385 | 0.888372 | 0.375 | 0 | 0.610455312 |
| 0 | 0.137559 | 0.261624 | 0.25 | 0.465385 | 0.722093 | 0.375 | 0 | 0.52613828 |
| 0 | 0.137559 | 0.418598 | 0.25 | 0.465385 | 0.555814 | 0.375 | 0 | 0.510961214 |
| 0 | 0.137559 | 1.49E-03 | 0.25 | 0.465385 | 1 | 0.3 | 0.058659 | 0.610455312 |
| 0 | 0.137559 | 0.109134 | 0.25 | 0.465385 | 0.888372 | 0.2625 | 0.058659 | 0.622259696 |
| 0 | 0.137559 | 0.269099 | 0.25 | 0.465385 | 0.722093 | 0.3 | 0.058659 | 0.645868465 |
| 0 | 0.137559 | 0.429063 | 0.25 | 0.465385 | 0.555814 | 0.3 | 0.058659 | 0.637436762 |
| 0 | 0.137559 | 0 | 0.25 | 0.465385 | 1 | 0.375 | 0.058659 | 0.693086003 |
| 0 | 0.137559 | 0.104649 | 0.25 | 0.465385 | 0.888372 | 0.375 | 0.058659 | 0.637436762 |
| 0 | 0.137559 | 0.261624 | 0.25 | 0.465385 | 0.722093 | 0.375 | 0.058659 | 0.539629005 |
| 0 | 0.137559 | 0.418598 | 0.25 | 0.465385 | 0.555814 | 0.375 | 0.058659 | 0.581787521 |
| 0 | 0.137559 | 1.49E-03 | 0.25 | 0.465385 | 1 | 0.3 | 1 | 0.779089376 |
| 0 | 0.137559 | 0.109134 | 0.25 | 0.465385 | 0.888372 | 0.2625 | 1 | 0.826306914 |
| 0 | 0.137559 | 0.269099 | 0.25 | 0.465385 | 0.722093 | 0.3 | 1 | 1 |
| 0 | 0.137559 | 0.429063 | 0.25 | 0.465385 | 0.555814 | 0.3 | 1 | 0.826306914 |
| 0 | 0.137559 | 0 | 0.25 | 0.465385 | 1 | 0.375 | 1 | 0.856661046 |
| 0 | 0.137559 | 0.104649 | 0.25 | 0.465385 | 0.888372 | 0.375 | 1 | 0.875210793 |
| 0 | 0.137559 | 0.261624 | 0.25 | 0.465385 | 0.722093 | 0.375 | 1 | 0.866779089 |
| 0 | 0.137559 | 0.418598 | 0.25 | 0.465385 | 0.555814 | 0.375 | 1 | 0.809443508 |
| 0.064 | 0.135662 | 0.11628 | 0 | 1 | 0.763721 | 0.383 | 0 | 0.084822934 |
| 0.064 | 0.153428 | 0.33721 | 0 | 1 | 0.572791 | 0.383 | 0 | 0.112310287 |
| 0.064 | 0.171108 | 0.55814 | 0 | 1 | 0.38186 | 0.383 | 0 | 0.179932546 |
| 0.064 | 0.188788 | 0.77907 | 0 | 1 | 0.19093 | 0.8426 | 0 | 0.202360877 |
| 0.064 | 0.206468 | 1 | 0 | 1 | 0 | 0.9192 | 0 | 0.179763912 |
| 0.064 | 0.465977 | 0.11628 | 0.5 | 1 | 0.763721 | 0.0383 | 0 | 1.69E-02 |
| 0.064 | 0.483743 | 0.33721 | 0.5 | 1 | 0.572791 | 0.0575 | 0 | 6.19E-02 |
| 0.064 | 0.501423 | 0.55814 | 0.5 | 1 | 0.38186 | 0.0575 | 0 | 6.75E-02 |
| 0.064 | 0.519103 | 0.77907 | 0.5 | 1 | 0.19093 | 0.0766 | 0 | 7.30E-02 |
| 0.064 | 0.536783 | 1 | 0.5 | 1 | 0 | 0.0766 | 0 | 8.99E-02 |
| 0.064 | 0.796292 | 0.11628 | 1 | 1 | 0.763721 | 0 | 0 | 0 |
| 0.064 | 0.814058 | 0.33721 | 1 | 1 | 0.572791 | 0 | 0 | 1.69E-02 |
| 0.064 | 0.831738 | 0.55814 | 1 | 1 | 0.38186 | 0.0192 | 0 | 0 |
| 0.064 | 0.849418 | 0.77907 | 1 | 1 | 0.19093 | 0.383 | 0 | 0 |
| 0.064 | 0.867098 | 1 | 1 | 1 | 0 | 0.383 | 0 | 0 |
| 0.064 | 0.135662 | 0.11628 | 0 | 1 | 0.763721 | 0.383 | 0.058659 | 0.337268128 |
| 0.064 | 0.153428 | 0.33721 | 0 | 1 | 0.572791 | 0.383 | 0.058659 | 0.424283305 |
| 0.064 | 0.171108 | 0.55814 | 0 | 1 | 0.38186 | 0.383 | 0.058659 | 0.460876897 |
| 0.064 | 0.188788 | 0.77907 | 0 | 1 | 0.19093 | 0.8426 | 0.058659 | 0.393423272 |
| 0.064 | 0.206468 | 1 | 0 | 1 | 0 | 0.9192 | 0.058659 | 0.354131535 |
| 0.064 | 0.465977 | 0.11628 | 0.5 | 1 | 0.763721 | 0.0383 | 0.058659 | 0.219224283 |
| 0.064 | 0.483743 | 0.33721 | 0.5 | 1 | 0.572791 | 0.0575 | 0.058659 | 0.264080944 |
| 0.064 | 0.501423 | 0.55814 | 0.5 | 1 | 0.38186 | 0.0575 | 0.058659 | 0.286677909 |
| 0.064 | 0.519103 | 0.77907 | 0.5 | 1 | 0.19093 | 0.0766 | 0.058659 | 0.275379427 |
| 0.064 | 0.536783 | 1 | 0.5 | 1 | 0 | 0.0766 | 0.058659 | 0.269814503 |
| 0.064 | 0.796292 | 0.11628 | 1 | 1 | 0.763721 | 0 | 0.058659 | 0.168634064 |
| 0.064 | 0.814058 | 0.33721 | 1 | 1 | 0.572791 | 0 | 0.058659 | 0.219224283 |
| 0.064 | 0.831738 | 0.55814 | 1 | 1 | 0.38186 | 0.0192 | 0.058659 | 0.219224283 |
| 0.064 | 0.849418 | 0.77907 | 1 | 1 | 0.19093 | 0.383 | 0.058659 | 0.219224283 |
| 0.064 | 0.867098 | 1 | 1 | 1 | 0 | 0.383 | 0.058659 | 0.168634064 |
| 0.064 | 0.135662 | 0.11628 | 0 | 1 | 0.763721 | 0.383 | 0.231844 | 0.523271501 |
| 0.064 | 0.153428 | 0.33721 | 0 | 1 | 0.572791 | 0.383 | 0.231844 | 0.595278246 |
| 0.064 | 0.171108 | 0.55814 | 0 | 1 | 0.38186 | 0.383 | 0.231844 | 0.607082631 |
| 0.064 | 0.188788 | 0.77907 | 0 | 1 | 0.19093 | 0.8426 | 0.231844 | 0.7306914 |
| 0.064 | 0.206468 | 1 | 0 | 1 | 0 | 0.9192 | 0.231844 | 0.652107926 |
| 0.064 | 0.465977 | 0.11628 | 0.5 | 1 | 0.763721 | 0.0383 | 0.231844 | 0.280944351 |
| 0.064 | 0.483743 | 0.33721 | 0.5 | 1 | 0.572791 | 0.0575 | 0.231844 | 0.356492411 |
| 0.064 | 0.501423 | 0.55814 | 0.5 | 1 | 0.38186 | 0.0575 | 0.231844 | 0.438448567 |
| 0.064 | 0.519103 | 0.77907 | 0.5 | 1 | 0.19093 | 0.0766 | 0.231844 | 0.49460371 |
| 0.064 | 0.536783 | 1 | 0.5 | 1 | 0 | 0.0766 | 0.231844 | 0.505902192 |
| 0.064 | 0.796292 | 0.11628 | 1 | 1 | 0.763721 | 0 | 0.231844 | 0.207925801 |
| 0.064 | 0.814058 | 0.33721 | 1 | 1 | 0.572791 | 0 | 0.231844 | 0.277403035 |
| 0.064 | 0.831738 | 0.55814 | 1 | 1 | 0.38186 | 0.0192 | 0.231844 | 0.25851602 |
| 0.064 | 0.849418 | 0.77907 | 1 | 1 | 0.19093 | 0.383 | 0.231844 | 0.354131535 |
| 0.064 | 0.867098 | 1 | 1 | 1 | 0 | 0.383 | 0.231844 | 0.403204047 |
| 0.064 | 0.135662 | 0.11628 | 0 | 1 | 0.763721 | 0.383 | 0.48324 | 0.532883642 |
| 0.064 | 0.153428 | 0.33721 | 0 | 1 | 0.572791 | 0.383 | 0.48324 | 0.681956155 |
| 0.064 | 0.171108 | 0.55814 | 0 | 1 | 0.38186 | 0.383 | 0.48324 | 0.798145025 |
| 0.064 | 0.188788 | 0.77907 | 0 | 1 | 0.19093 | 0.8426 | 0.48324 | 0.865598651 |
| 0.064 | 0.206468 | 1 | 0 | 1 | 0 | 0.9192 | 0.48324 | 0.84317032 |
| 0.064 | 0.465977 | 0.11628 | 0.5 | 1 | 0.763721 | 0.0383 | 0.48324 | 0.42158516 |
| 0.064 | 0.483743 | 0.33721 | 0.5 | 1 | 0.572791 | 0.0575 | 0.48324 | 0.52613828 |
| 0.064 | 0.501423 | 0.55814 | 0.5 | 1 | 0.38186 | 0.0575 | 0.48324 | 0.623946037 |
| 0.064 | 0.519103 | 0.77907 | 0.5 | 1 | 0.19093 | 0.0766 | 0.48324 | 0.769983137 |
| 0.064 | 0.536783 | 1 | 0.5 | 1 | 0 | 0.0766 | 0.48324 | 0.775716695 |
| 0.064 | 0.796292 | 0.11628 | 1 | 1 | 0.763721 | 0 | 0.48324 | 0.252951096 |
| 0.064 | 0.814058 | 0.33721 | 1 | 1 | 0.572791 | 0 | 0.48324 | 0.339460371 |
| 0.064 | 0.831738 | 0.55814 | 1 | 1 | 0.38186 | 0.0192 | 0.48324 | 0.359190556 |
| 0.064 | 0.849418 | 0.77907 | 1 | 1 | 0.19093 | 0.383 | 0.48324 | 0.466441821 |
| 0.064 | 0.867098 | 1 | 1 | 1 | 0 | 0.383 | 0.48324 | 0.477234401 |
| 0.064 | 0 | 0.11628 | 0 | 1 | 0.763721 | 0.383 | 0.058659 | 0.337268128 |
| 0.064 | 0 | 0.33721 | 0 | 1 | 0.572791 | 0.383 | 0.058659 | 0.42158516 |
| 0.064 | 0 | 0.55814 | 0 | 1 | 0.38186 | 0.383 | 0.058659 | 0.455311973 |
| 0.064 | 0 | 0.77907 | 0 | 1 | 0.19093 | 0.8426 | 0.058659 | 0.404721754 |
| 0.64 | 1 | 0.194349 | 1 | 0 | 0.697674 | 0 | 0.058659 | 0.302192243 |
| 0.64 | 1 | 0.493347 | 1 | 0 | 0.465116 | 0 | 0.058659 | 0.325632378 |
| 0.64 | 1 | 0.792346 | 1 | 0 | 0.232558 | 0 | 0.058659 | 0.268971332 |
| 1 | 0.56878 | 0 | 0.25 | 0.634615 | 0.732558 | 1 | 0.058659 | 0.398313659 |
| 1 | 0.56878 | 0.104649 | 0.25 | 0.634615 | 0.651163 | 1 | 0.058659 | 0.424957841 |
| 1 | 0.56878 | 0.209299 | 0.25 | 0.634615 | 0.569767 | 1 | 0.058659 | 0.46306914 |
| 1 | 0.56878 | 0.313948 | 0.25 | 0.634615 | 0.488372 | 1 | 0.058659 | 0.468802698 |

Table S2 Normalized Testing Set

| Cement | Water | Ceramic Fine Aggregate | W/C | Natural Coarse Aggregate | Natural Fine Aggregate | Superplasticizer | Age | Compressive Strength |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| -0.16 | 0.128935 | -5.16E-02 | 0.35 | 1.515385 | 0.762209 | 0.355 | 0.058659 | 0.669477234 |
| -0.16 | 0.128935 | 1.49E-03 | 0.35 | 1.515385 | 0.72093 | 0.355 | 0.058659 | 0.731871838 |
| -0.16 | 0.128935 | 5.46E-02 | 0.35 | 1.515385 | 0.679651 | 0.355 | 0.058659 | 0.801011804 |
| -0.16 | 0.128935 | 0.101659 | 0.35 | 1.515385 | 0.643023 | 0.355 | 0.058659 | 0.716694772 |
| -0.16 | 0.128935 | 0.204814 | 0.35 | 1.515385 | 0.562791 | 0.355 | 0.058659 | 0.725126476 |
| -0.16 | 0.128935 | 0.304978 | 0.35 | 1.515385 | 0.482558 | 0.355 | 0.058659 | 0.741989882 |
| -0.112 | 0.525658 | 8.52E-02 | 0.95 | -2.74692 | 0.59186 | 0 | 0.058659 | 0.401349073 |
| -0.112 | 0.525658 | 0.275078 | 0.95 | -2.74692 | 0.444186 | 0 | 0.058659 | 0.389544688 |
| -0.112 | 0.525658 | 0.316938 | 0.95 | -2.74692 | 0.295349 | 0 | 0.058659 | 0.355817875 |
| -0.112 | 0.525658 | 0.656301 | 0.95 | -2.74692 | 0.147674 | 0 | 0.058659 | 0.399662732 |
| -0.112 | 0.525658 | 0.846165 | 0.95 | -2.74692 | 0 | 0 | 0.058659 | 0.477234401 |
| 1.48 | 0.396292 | 3.41E-02 | -1.00E-01 | -0.4 | 0.971163 | 0.504 | 0 | 0.286677909 |
| 1.48 | 0.396292 | 0.172821 | -1.00E-01 | -0.4 | 0.863256 | 0.504 | 0 | 0.337268128 |
| 1.48 | 0.396292 | 0.311556 | -1.00E-01 | -0.4 | 0.755349 | 0.504 | 0 | 0.362563238 |
| 1.48 | 0.396292 | 0.450292 | -1.00E-01 | -0.4 | 0.647442 | 0.5208 | 0 | 0.370994941 |
| 1.48 | 0.396292 | 0.589027 | -1.00E-01 | -0.4 | 0.539535 | 0.6104 | 0 | 0.42158516 |
| 1.48 | 0.396292 | 0.727762 | -1.00E-01 | -0.4 | 0.431628 | 0.7 | 0 | 0.396290051 |
| 1.48 | 0.396292 | 0.866497 | -1.00E-01 | -0.4 | 0.323721 | 0.7896 | 0 | 0.370994941 |
| 1.48 | 0.396292 | 1.005232 | -1.00E-01 | -0.4 | 0.215814 | 0.8736 | 0 | 0.345699831 |
| 1.48 | 0.396292 | 1.143968 | -1.00E-01 | -0.4 | 0.107907 | 1.0304 | 0 | 0.303541315 |
| 1.48 | 0.396292 | 1.282703 | -1.00E-01 | -0.4 | 0 | 1.1872 | 0 | 0.286677909 |
| 1.48 | 0.396292 | 3.41E-02 | -1.00E-01 | -0.4 | 0.971163 | 0.504 | 0.058659 | 0.370994941 |
| 1.48 | 0.396292 | 0.172821 | -1.00E-01 | -0.4 | 0.863256 | 0.504 | 0.058659 | 0.387858347 |
| 1.48 | 0.396292 | 0.311556 | -1.00E-01 | -0.4 | 0.755349 | 0.504 | 0.058659 | 0.430016863 |
| 1.48 | 0.396292 | 0.450292 | -1.00E-01 | -0.4 | 0.647442 | 0.5208 | 0.058659 | 0.472175379 |
| 1.48 | 0.396292 | 0.589027 | -1.00E-01 | -0.4 | 0.539535 | 0.6104 | 0.058659 | 0.505902192 |
| 1.48 | 0.396292 | 0.727762 | -1.00E-01 | -0.4 | 0.431628 | 0.7 | 0.058659 | 0.480607083 |
| 1.48 | 0.396292 | 0.866497 | -1.00E-01 | -0.4 | 0.323721 | 0.7896 | 0.058659 | 0.438448567 |
| 1.48 | 0.396292 | 1.005232 | -1.00E-01 | -0.4 | 0.215814 | 0.8736 | 0.058659 | 0.396290051 |
| 1.48 | 0.396292 | 1.143968 | -1.00E-01 | -0.4 | 0.107907 | 1.0304 | 0.058659 | 0.387858347 |
| 1.48 | 0.396292 | 1.282703 | -1.00E-01 | -0.4 | 0 | 1.1872 | 0.058659 | 0.370994941 |
| 1.48 | 0.396292 | 3.41E-02 | -1.00E-01 | -0.4 | 0.971163 | 0.504 | 0.231844 | 0.396290051 |
| 1.48 | 0.396292 | 0.172821 | -1.00E-01 | -0.4 | 0.863256 | 0.504 | 0.231844 | 0.438448567 |
| 1.48 | 0.396292 | 0.311556 | -1.00E-01 | -0.4 | 0.755349 | 0.504 | 0.231844 | 0.480607083 |
| 1.48 | 0.396292 | 0.450292 | -1.00E-01 | -0.4 | 0.647442 | 0.5208 | 0.231844 | 0.522765599 |
| 1.48 | 0.396292 | 0.589027 | -1.00E-01 | -0.4 | 0.539535 | 0.6104 | 0.231844 | 0.556492411 |
| 1.48 | 0.396292 | 0.727762 | -1.00E-01 | -0.4 | 0.431628 | 0.7 | 0.231844 | 0.539629005 |
| 1.48 | 0.396292 | 0.866497 | -1.00E-01 | -0.4 | 0.323721 | 0.7896 | 0.231844 | 0.522765599 |
| 1.48 | 0.396292 | 1.005232 | -1.00E-01 | -0.4 | 0.215814 | 0.8736 | 0.231844 | 0.514333895 |
| 1.48 | 0.396292 | 1.143968 | -1.00E-01 | -0.4 | 0.107907 | 1.0304 | 0.231844 | 0.42158516 |
| 1.48 | 0.396292 | 1.282703 | -1.00E-01 | -0.4 | 0 | 1.1872 | 0.231844 | 0.387858347 |

- Example prediction.

Consider a concrete mix with C=375 kg/m³, W=150 kg/m³, CFA==250 kg/m³,
NCA=956 kg/m³, NFA==621 kg/m³, W/C=0.40, and curing age t=28 days.

Each variable is first normalized using the min–max values in Table S2.

The scaled values are then substituted into Eq. (5) to compute fk′

If output scaling is applied, the inverse transformation is used to recover
compressive strength in MPa.

fk'= t-C- CFA- t*G1C7G1C8+ C- NCAG2C5- CFA2W*G2C0

+W*G3C33* W-NFA+C+CFA+W*t*WW- WC

Important: All variables above are scaled to [0, 1] before substitution.

- Machine-readable equation (Python Code)

#------------------------------------------------------------------------

# Regression model generated by GeneXproTools 5.0 on 12/30/2025 9:35:40 PM

# GEP File: C:\Users\weahc\Desktop\Model10.Deployment.gep

# Training Records:  91

# Validation Records:   45

# Fitness Function:  RMSE

# Training Fitness:  711.357064601437

# Training R-square: 0.838416489002986

# Validation Fitness:   719.945716581774

# Validation R-square:  0.870033781038747

#------------------------------------------------------------------------

from math import *

def gepModel(d):

G1C7 = 2.1842531749944

G1C8 = -4.35019178767571

G2C5 = 4.22064129062341

G2C0 = -9.17555919281538

G3C3 = -0.297675714023064

Standardize(d)

y = 0.0

y = ((d[7]-d[0])-(d[2]-((d[7]*G1C7)/(G1C8*G1C8))))

y = y + (d[0]-(d[4]/(G2C5-((d[0]*d[0])*(d[1]*G2C0)))))

y = y + (d[1]*(d[0]-(pow(G3C3,3.0)*((d[1]-d[5])+d[0]))))

y = y + d[2]

y = y + (d[1]*(d[7]*(d[1]*(d[1]-d[3]))))

y = Reverse_Standardization(y)

return y

def Standardize(input):

AVERAGE_0 = 423.241758241758

STDEV_0 = 76.6075628206425

input[0] = (input[0] - AVERAGE_0) / STDEV_0

AVERAGE_1 = 178.21032967033

STDEV_1 = 29.8310925210798

input[1] = (input[1] - AVERAGE_1) / STDEV_1

AVERAGE_2 = 367.989230769231

STDEV_2 = 225.093631664844

input[2] = (input[2] - AVERAGE_2) / STDEV_2

AVERAGE_3 = 0.410772883626069

STDEV_3 = 7.59189716498191E-02

input[3] = (input[3] - AVERAGE_3) / STDEV_3

AVERAGE_4 = 962.797802197802

STDEV_4 = 200.444338617994

input[4] = (input[4] - AVERAGE_4) / STDEV_4

AVERAGE_5 = 453.110989010989

STDEV_5 = 243.11846881284

input[5] = (input[5] - AVERAGE_5) / STDEV_5

AVERAGE_7 = 76.1538461538462

STDEV_7 = 98.0723002094683

input[7] = (input[7] - AVERAGE_7) / STDEV_7

def Reverse_Standardization(modelOutput):

# Model standardization

MODEL_AVERAGE = 5.59752277970157E-02

MODEL_STDEV = 0.874152910221116

modelOutput = (modelOutput - MODEL_AVERAGE)/MODEL_STDEV

# Reverse standardization

TARGET_AVERAGE = 46.8889010989011

TARGET_STDEV = 12.7004324904967

return modelOutput * TARGET_STDEV + TARGET_AVERAGE