Supplementary Material

A Comprehensive Theoretical Investigation of Lead-Free Mixed Antimony-Bismuth Halide Double Perovskite (Cs₂AgBi₀.₇₅Sb₀.₂₅Br₆) Solar Cell using SCAPS-1D

Parwaz Asif *, Anupam Chetia, Dibyajyoti Saikia, Satyajit Sahu

Department of Physics, Indian Institute of Technology Jodhpur 342037, India

*Corresponding author E-mail: asif.1@alumni.iitj.ac.in;

Contributing authors: chetia.1@iitj.ac.in; saikia.2@iitj.ac.in; satyajit@iitj.ac.in

Table S1 The numerical parameters used for various electron transport materials (ETMs).

| Parameters | ZnO [1] | ZnSe [2] | STO [3] | IGZO [4] | CdS [5] | C60 [6],[7] | TiO2 [8], [9] | Cd0.5Zn0.5S [10] | PCBM [11] |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Thickness(µm) | 0.07 | 0.07 | 0.07 | 0.07 | 0.07 | 0.07 | 0.07 | 0.07 | 0.07 |
| Bandgap (eV) | 3.30 | 2.81 | 3.20 | 3.05 | 2.40 | 1.70 | 3.20 | 2.80 | 2.00 |
| Electron affinity(eV) | 4.00 | 4.09 | 4.00 | 4.16 | 4.20 | 3.90 | 3.90 | 3.80 | 3.90 |
| Dielectric permittivity | 9.0 | 8.6 | 8.7 | 10.0 | 10.0 | 4.20 | 9.00 | 10.0 | 3.90 |
| Effective density of states of CB (cm-3) | 3.7x 1018 | 2.2x 1018 | 1.7x 1019 | 5x 1018 | 2x 1018 | 8x 1019 | 1021 | 1018 | 2.5x 1021 |
| effective density of states of VB (cm-3) | 1.8x 1019 | 1.8x 1018 | 2x 1018 | 5x 1018 | 1.8 1019 | 8x 1019 | 2x 1020 | 1018 | 2.5x 1021 |
| Thermal velocity of electron(cm/s) | 107 | 107 | 107 | 107 | 107 | 107 | 107 | 107 | 107 |
| Thermal velocity of hole(cm/s) | 107 | 107 | 107 | 107 | 107 | 107 | 107 | 107 | 107 |
| Mobility of electron(cm2/Vs) | 100 | 400 | 5300 | 15 | 20 | 0.08 | 20 | 100 | 0.2 |
| Mobility of hole(cm2/Vs) | 25 | 110 | 660 | 0.1 | 10 | 0.0035 | 10 | 25 | 0.2 |
| Shallow uniform donor density ND (cm-3) | 5x 1017 | 5x 1017 | 5x 1017 | 5x 1017 | 1017 | 2.6x 1018 | 1017 | 1017 | 2.93x 1017 |
| Shallow uniform acceptor density NA (cm-3) | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 |

Table S2  Various cell parameter for simulated device with different ETMs.

| ETM | Voc(V) | Jsc(mA/cm2) | FF(%) | PCE(%) |
| --- | --- | --- | --- | --- |
| ZnO | 1.40011 | 15.278024 | 81.99 | 17.54 |
| ZnSe | 1.3393 | 15.438965 | 80.71 | 16.69 |
| STO | 1.3722 | 15.432828 | 81.14 | 17.18 |
| IGZO | 1.2491 | 15.414279 | 79.71 | 15.35 |
| CdS | 1.2317 | 15.409216 | 79.57 | 15.10 |
| C60 | 1.3787 | 15.797710 | 86.57 | 18.86 |
| TiO2 | 1.1720 | 15.311448 | 78.74 | 14.13 |
| Cd0.5Zn0.5S | 1.4321 | 15.389733 | 88.19 | 19.44 |
| PCBM | 1.3500 | 15.689894 | 81.66 | 17.30 |

Fig. S1 Variation of ETL Thickness on (a) Voc, (b) Jsc, (c) FF, and (d) PCE

Table S3 The numerical parameters used for various Hole transport materials (HTMs).

| Parameters | NiO [12] | CuI [13] | CuSCN [14] | SnS [15] | CuInSe2 [16] |
| --- | --- | --- | --- | --- | --- |
| Thickness(µm) | 0.07 | 0.07 | 0.07 | 0.07 | 0.07 |
| Bandgap (eV) | 3.80 | 3.10 | 3.60 | 1.60 | 1.00 |
| Electron affinity(eV) | 1.46 | 2.10 | 1.70 | 4.10 | 3.80 |
| Dielectric permittivity | 10.70 | 6.50 | 10 | 13.0 | 9.00 |
| Effective density of states of CB (cm-3) | 2.8x 1019 | 2.8 x 1019 | 2.2x1019 | 1.18 x 1018 | 1017 |
| effective density of states of VB (cm-3) | 1 x 1019 | 1x 1019 | 1.8x1018 | 4.46 x 1018 | 1019 |
| Thermal velocity of electron(cm/s) | 107 | 107 | 107 | 107 | 107 |
| Thermal velocity of hole(cm/s) | 107 | 107 | 107 | 107 | 107 |
| Mobility of electron(cm2/Vs) | 12 | 100 | 100 | 15 | 10-4 |
| Mobility of hole(cm2/Vs) | 2.8 | 43.9 | 25 | 100 | 10-4 |
| Shallow uniform donor density ND (cm-3) | 0 | 0 | 0 | 0 | 0 |
| Shallow uniform acceptor density NA (cm-3) | 1018 | 1018 | 1018 | 1.1 x 1016 | 1019 |

Table S4 Various cell parameter for simulated device with different HTMs.

| HTM | Voc(V) | Jsc(mA/cm2) | FF(%) | PCE(%) |
| --- | --- | --- | --- | --- |
| CuI | 1.4282 | 14.855680 | 87.56 | 18.58 |
| CuInSe2 | 1.2689 | 11.365478 | 80.06 | 11.55 |
| CuSCN | 1.4310 | 15.068992 | 88.17 | 19.01 |
| NiO | 1.4294 | 15.010441 | 88.00 | 18.88 |
| SnS | 1.1747 | 11.992886 | 80.94 | 11.40 |

Fig.  S2 Variation of HTL Thickness on (a) Voc, (b) Jsc, (c) FF, and (d) PCE

Fig.  S3  Energy Level diagram for optimized device.

References

[1]	D. Jalalian, A. Ghadimi, and A. Kiani, ‘Modeling of a high performance bandgap graded Pb-free HTM-free perovskite solar cell’, Eur. Phys. J. Appl. Phys., vol. 87, no. 1, p. 10101, 2019.

[2]	J. A. Owolabi, M. Y. Onimisi, J. A. Ukwenya, A. B. Bature, and U. R. Ushiekpan, ‘Investigating the effect of ZnSe (ETM) and Cu2O (HTM) on absorber layer on the performance of pervoskite solar cell using SCAPS-1D’, Am. J. Phys. Appl., vol. 8, no. 1, pp. 8–18, 2020.

[3]	S. Bishnoi and S. K. Pandey, ‘Device performance analysis for lead‐free perovskite solar cell optimisation’, IET Optoelectron., vol. 12, no. 4, pp. 185–190, 2018.

[4]	F. Azri, A. Meftah, N. Sengouga, and A. Meftah, ‘Electron and hole transport layers optimization by numerical simulation of a perovskite solar cell’, Sol. energy, vol. 181, pp. 372–378, 2019.

[5]	Y. Guo et al., ‘RF sputtered CdS films as independent or buffered electron transport layer for efficient planar perovskite solar cell’, Sol. Energy Mater. Sol. Cells, vol. 178, pp. 186–192, 2018.

[6]	X. Liu, K. Yan, D. Tan, X. Liang, H. Zhang, and W. Huang, ‘Solvent engineering improves efficiency of lead-free tin-based hybrid perovskite solar cells beyond 9%’, ACS Energy Lett., vol. 3, no. 11, pp. 2701–2707, 2018.

[7]	Z. Qirong et al., ‘A study on numerical simulation optimization of perovskite solar cell based on CuI and C60’, Mater. Res. Express, vol. 9, no. 3, p. 36401, 2022.

[8]	N. Pezhooli, J. Rahimi, F. Hasti, and A. Maleki, ‘Synthesis and evaluation of composite TiO2@ ZnO quantum dots on hybrid nanostructure perovskite solar cell’, Sci. Rep., vol. 12, no. 1, p. 9885, 2022.

[9]	Y. Gan et al., ‘Numerical investigation energy conversion performance of tin-based perovskite solar cells using cell capacitance simulator’, Energies, vol. 13, no. 22, p. 5907, 2020.

[10]	Y. H. Khattak, E. Vega, F. Baig, and B. M. Soucase, ‘Performance investigation of experimentally fabricated lead iodide perovskite solar cell via numerical analysis’, Mater. Res. Bull., vol. 151, p. 111802, 2022.

[11]	A. Raj, A. Anshul, V. Tuli, P. K. Singh, R. C. Singh, and M. Kumar, ‘Effect of appropriate ETL on quantum efficiency of double perovskite La2NiMnO6 based solar cell device via SCAPS simulation’, Mater. Today Proc., vol. 47, pp. 1656–1659, 2021.

[12]	R. R. Kumar and S. K. Pandey, ‘Performance evaluation and material parameter perspective of eco-friendly highly efficient CsSnGeI3 perovskite solar cell’, Superlattices Microstruct., vol. 135, p. 106273, 2019.

[13]	S. Pitchaiya et al., ‘A review on the classification of organic/inorganic/carbonaceous hole transporting materials for perovskite solar cell application’, Arab. J. Chem., vol. 13, no. 1, pp. 2526–2557, 2020.

[14]	M. Alla et al., ‘Optimized CH3NH3PbI3-XClX based perovskite solar cell with theoretical efficiency exceeding 30%’, Opt. Mater. (Amst)., vol. 124, p. 112044, 2022.

[15]	A. Mohandes, M. Moradi, and H. Nadgaran, ‘Numerical simulation of inorganic Cs 2 AgBiBr 6 as a lead-free perovskite using device simulation SCAPS-1D’, Opt. Quantum Electron., vol. 53, pp. 1–22, 2021.

[16]	R. Saha, K. Chakraborty, M. G. Choudhury, and S. Paul, ‘Simulation study of Formamidinium Lead Halide (FAPbX3; X= I and Br) Based Perovskite Solar Cells Using SCAPS-1D Device Simulator’, 2021.