Supporting Information

Theoretical insights into metal-doped nanostructured hematite catalyst supported by graphene underlayer for photoelectrochemical water splitting applications

Labanya Bhattacharya1, Maytal Caspary Toroker1,2,3*

1Department of Materials Science and Engineering,

Technion-Israel Institute of Technology, Haifa-3200003, Israel

2The Nancy and Stephen Grand Technion Energy Program,

Technion-Israel Institute of Technology, Haifa-3200003, Israel

3Resnick Sustainability Center for Catalysis,

Technion-Israel Institute of Technology, Haifa-3200003, Israel

*Email: maytalc@technion.ac.il

Table S1.

Corrections added to the free energy calculation of molecules involved in water oxidation

| Molecule | Etotal | ZPE | TS |
| --- | --- | --- | --- |
| H2 | -6.77 | 0.27 | 0.40 |
| O2 | -9.87 | 0.10 | 0.63 |
| H2O | -14.23 | 0.57 | 0.67 |

Table S2.

Zero Point Energy corrections ((∆ZPE-T∆S)1-5) added to the free energy calculation of water oxidation (equations (6)-(10) in manuscript)

| Reaction | Al doped hematite | Graphene-Al doped hematite | Graphitic-N_1 doped graphene-Al doped hematite | Graphitic-N_2 doped graphene-Al doped hematite | Graphitic-N_3 doped graphene-Al doped hematite |
| --- | --- | --- | --- | --- | --- |
| 1 | 0.761 | 0.751 | 0.682 | 0.756 | 0.753 |
| 2 | -0.343 | -0.339 | -0.213 | -0.290 | -0.298 |
| 3 | -0.361 | -0.435 | -0.546 | -0.453 | -0.505 |
| 4 | 0.369 | 0.445 | 0.554 | 0.463 | 0.462 |
| 5 | -1.016 | -1.011 | -1.068 | -1.067 | -1.000 |

Table S3.

Bader net charge (e) on the atoms of *OH intermediate

| Atoms | Hematite | Graphene-Hematite | Al doped hematite | Graphene-Al doped hematite | N doped graphene-Al doped hematite |
| --- | --- | --- | --- | --- | --- |
| O1 | -1.2266 | -1.2031 | -1.3408 | -1.3046 | -1.3031 |
| O2 | -1.1908 | -1.1919 | -1.3028 | -1.3002 | -1.3083 |
| O3 | -1.1907 | -1.2227 | -1.2957 | -1.3407 | -1.3431 |
| O4 | -1.2030 | -1.2289 | -1.3023 | -1.3249 | -1.3377 |
| O5 | -1.2013 | -1.2170 | -1.2998 | -1.3264 | -1.3012 |
| O6 | -1.2334 | -1.2117 | -1.3438 | -1.2923 | -1.2935 |
| Fe1 | +1.8649 | +1.8384 | +1.8717 | +1.861 | +1.8596 |
| Fe2/Al for Al doped system | +1.8651 | +1.8401 | +2.4748 | +2.4779 | +2.48 |
| H1 | +0.5758 | +0.6052 | +0.569 | +0.6038 | +0.5777 |
| H2 | +0.6124 | +0.6144 | +0.618 | +0.5912 | +0.604 |
| H3 | +0.5789 | +0.6151 | +0.5816 | +0.6141 | +0.6166 |
| H4 | +0.5714 | +0.5702 | +0.5778 | +0.5692 | +0.5763 |
| H5 | +0.5676 | +0.5805 | +0.5744 | +0.5729 | +0.5716 |
| H6 | +0.6096 | +0.5964 | +0.6181 | +0.5848 | +0.5874 |
| C1 | -- | +0.0668 |  | +0.1387 | +0.3756 |
| C2 | -- | -0.0013 |  | +0.0448 | +0.2095 |
| C3 | -- | +0.0606 |  | +0.1304 | +0.1228 |
| C4 | -- | -0.0005 |  | +0.0451 | +0.2857 |
| C5 | -- | -0.0521 |  | -0.1242 | +0.0842 |
| C6 | -- | -0.0005 |  | -0.0465 | +0.0566 |
| C7 | -- | -0.0535 |  | -0.1246 | -0.0211 |
| C8/N1 (for N doped systems) | -- | -0.0047 |  | -0.0500 | -2.0994 |

Table S4.

Bader net charge (e) on the atoms of *O intermediate

| Atoms | Hematite | Graphene-Hematite | Al doped hematite | Graphene-Al doped hematite | N doped graphene-Al doped hematite |
| --- | --- | --- | --- | --- | --- |
| O1 | -1.1138 | -1.1394 | -1.2208 | -1.2392 | -1.2276 |
| O2 | -1.1557 | -1.1035 | -1.2265 | -1.2516 | -1.2553 |
| O3 | -1.1753 | -1.147 | -1.2677 | -1.2906 | -1.2902 |
| O4 | -1.157 | -1.1287 | -1.2864 | -1.2793 | -1.2528 |
| O5 | -0.8914 | -1.1205 | -1.0049 | -1.2655 | -1.2886 |
| O6 | -1.1808 | -0.8871 | -1.2944 | -0.9868 | -1.0033 |
| Fe1 | 1.8356 | 1.6606 | 1.8337 | 1.8428 | 1.8318 |
| Fe2/Al for Al doped system | 1.8457 | 1.8452 | 2.4767 | 2.48 | 2.4793 |
| H1 | 0.6210 | 0.629 | 0.6275 | 0.6035 | 0.6252 |
| H2 | 0.5884 | 0.6165 | 0.612 | 0.6194 | 0.5892 |
| H3 | 0.5852 | 0.6247 | 0.573 | 0.6066 | 0.5976 |
| H4 | 0.6037 | 0.5594 | 0.5869 | 0.5677 | 0.5648 |
| H5 | 0.5945 | 0.5735 | 0.5909 | 0.5756 | 0.554 |
| H6 |  |  |  |  |  |
| C1 | -- | -0.0195 |  | 0.0049 | 0.4489 |
| C2 | -- | -0.046 |  | -0.0297 | 0.258 |
| C3 | -- | -0.0258 |  | -0.0023 | 0.1239 |
| C4 | -- | -0.045 |  | -0.0285 | 0.3616 |
| C5 | -- | 0.0335 |  | 0.0101 | -0.053 |
| C6 | -- | 0.0454 |  | 0.0297 | 0.0105 |
| C7 | -- | 0.0322 |  | 0.0089 | 0.0177 |
| C8/N1 (for N doped systems) | -- | 0.0424 |  | 0.0243 | -2.0917 |

Table S5.

Magnetization (units of Bohr Magneton) of the atoms of *OH intermediate

| Atoms | Hematite | Graphene-Hematite | Al doped hematite | Graphene-Al doped hematite | N doped graphene-Al doped hematite |
| --- | --- | --- | --- | --- | --- |
| O1 | 0.003 | -0.006 | 0.095 | 0.083 | 0.084 |
| O2 | -0.006 | 0.002 | 0.083 | 0.086 | 0.087 |
| O3 | 0.002 | -0.005 | 0.086 | 0.096 | 0.096 |
| O4 | 0.001 | -0.006 | 0.084 | 0.086 | 0.086 |
| O5 | -0.005 | 0.008 | 0.083 | 0.097 | 0.097 |
| O6 | 0.003 | 0.006 | 0.094 | 0.084 | 0.084 |
| Fe1 | 4.331 | 4.266 | 4.295 | 4.291 | 4.29 |
| Fe2/Al for Al doped system | -4.33 | -4.265 | 0.003 | 0.003 | 0.003 |
| H1 | 0.000 | -0.003 | 0.003 | 0.003 | 0.003 |
| H2 | 0.000 | 0.003 | 0.003 | 0.005 | 0.005 |
| H3 | 0.000 | 0.000 | 0.003 | 0.003 | 0.003 |
| H4 | 0.000 | 0.000 | 0.003 | 0.003 | 0.003 |
| H5 | 0.000 | -0.001 | 0.003 | 0.003 | 0.003 |
| H6 | 0.000 | 0.001 | 0.003 | 0.003 | 0.003 |
| C1 |  | 0.000 |  | 0.000 | 0.053 |
| C2 |  | 0.000 |  | 0.000 | 0.043 |
| C3 |  | 0.000 |  | 0.000 | 0.082 |
| C4 |  | 0.000 |  | 0.000 | 0.046 |
| C5 | -- | 0.000 |  | 0.000 | -0.001 |
| C6 | -- | 0.000 |  | 0.000 | -0.002 |
| C7 | -- | 0.000 |  | 0.000 | -0.001 |
| C8/N1 (for N doped systems) | -- | 0.000 |  | 0.000 | 0.061 |

Table S6.

Magnetization (units of Bohr Magneton) of the atoms of *O intermediate

| Atoms | Hematite | Graphene-Hematite | Al doped hematite | Graphene-Al doped hematite | N doped graphene-Al doped hematite |
| --- | --- | --- | --- | --- | --- |
| O1 | -0.103 | -0.085 | -0.016 | -0.006 | -0.003 |
| O2 | -0.096 | -0.059 | -0.012 | 0.022 | 0.021 |
| O3 | -0.01 | -0.028 | 0.071 | 0.05 | 0.051 |
| O4 | -0.031 | -0.044 | 0.057 | 0.049 | 0.049 |
| O5 | -0.042 | -0.019 | 0.053 | 0.074 | 0.075 |
| O6 | -0.029 | -0.051 | 0.06 | 0.056 | 0.052 |
| Fe1 | 3.639 | 3.572 | 3.659 | 3.621 | 3.692 |
| Fe2/Al for Al doped system | -4.269 | -4.235 | 0.009 | 0.008 | 0.008 |
| H1 | -0.002 | -0.001 | 0.003 | 0.003 | 0.003 |
| H2 | -0.002 | -0.002 | 0.003 | 0.003 | 0.003 |
| H3 | -0.001 | 0.000 | 0.001 | 0.002 | 0.002 |
| H4 | 0.000 | -0.001 | 0.002 | 0.002 | 0.002 |
| H5 | 0.002 | 0.000 | 0.002 | 0.002 | 0.002 |
| H6 |  |  |  |  |  |
| C1 | -- | 0.000 |  | 0.000 | 0.057 |
| C2 | -- | 0.000 |  | 0.000 | 0.051 |
| C3 | -- | 0.000 |  | 0.000 | 0.088 |
| C4 | -- | 0.000 |  | 0.000 | 0.052 |
| C5 | -- | 0.000 |  | 0.000 | 0.000 |
| C6 | -- | 0.000 |  | 0.000 | -0.002 |
| C7 | -- | 0.000 |  | 0.000 | 0.000 |
| C8/N1 (for N doped systems) | -- | 0.000 |  | 0.000 | 0.065 |

Table S7.

Spatial Grid density convergence test results for Graphene-Al doped Hematite system (*OH intermediate). Spatial spacing is denoted by 'dx'. Initial Total Energy is E0, Initial potential energy is V0 and Initial Kinetic energy is T0. 'Num' denotes numerically calculated energy values. 'Cal' denotes theoretically calculated energy values.

| Samples#, N | dx [Å] | E0num [eV] | T0num [eV] | T0cal [ev] | V0num [ev] | V0cal [ev] |
| --- | --- | --- | --- | --- | --- | --- |
| 2000 | 0.012808 | -2.76897 | 12.93043 | 12.9175 | -15.6994 | -15.6994 |
| 3000 | 0.008538 | -2.77328 | 12.92612 | 12.9175 | -15.6994 | -15.6994 |
| 4000 | 0.006404. | -2.77544 | 12.92396 | 12.9175 | -15.6994 | -15.6994 |
| 5000 | 0.005123 | -2.77673 | 12.92267 | 12.9175 | -15.6994 | -15.6994 |
| 6000 | 0.004269 | -2.77759 | 12.92181 | 12.9175 | -15.6994 | -15.6994 |
| 7000 | 0.003659 | -2.77821 | 12.92119 | 12.9175 | -15.6994 | -15.6994 |
| 8000 | 0.003202 | -2.77867 | 12.92073 | 12.9175 | -15.6994 | -15.6994 |
| 9000 | 0.002846 | -2.77903 | 12.92037 | 12.9175 | -15.6994 | -15.6994 |
| 10000 | 0.002562 | -2.77932 | 12.92008 | 12.9175 | -15.6994 | -15.6994 |
| 11000 | 0.002329 | -2.77955 | 12.91985 | 12.9175 | -15.6994 | -15.6994 |

Table S8. Valence Band Maxima (VBM) energy values for *OH intermediate. VBM energies are not referred to vacuum energy.

| System | VBM in eV |
| --- | --- |
| Hematite | -4.14 |
| Graphene-Hematite | -2.83 |
| Al doped hematite | -3.88 |
| Graphene-Al doped hematite | -2.78 |
| N doped graphene-Al doped hematite | -1.35 |

Table S9. Valence Band Maxima (VBM) energy values for *O intermediate. VBM energies are not referred to vacuum energy.

| System | VBM in eV |
| --- | --- |
| Hematite | -4.64 |
| Graphene-Hematite | -2.94 |
| Al doped hematite | -4.43 |
| Graphene-Al doped hematite | -2.76 |
| N doped graphene-Al doped hematite | -1.94 |

Table S10. Reaction activation energy (Ea), Gibbs free energy difference (∆G) and reorganization energy (λ) from NEB calculations and Marcus Theory for different dopants (Al, Ni and Co) in hematite. The zero-point energy corrections and entropic contributions are added to each parameter. Equations (8), (22), (23) and (24) are mentioned in the main manuscript. Core electrons of Ni and Co atoms such as Ni 1s2s2p3s3p and Co 1s2s2p3s3p are represented by PAW potential during DFT calculations. Ni and Co are doped in the same atomic site of Al in case of Al doped hematite.

| System | Ea (eV) from equation (22) | ∆G (eV) from equation (23) | λ (eV) from Marcus theory, equation (24) | ∆G (eV) from equation (8) | Ea (eV) from Marcus Theory equation (24) | Overpotential (V) from Table 1 |
| --- | --- | --- | --- | --- | --- | --- |
| Hematite | 0.66 | 0.13 | 2.37 | 1.88 | 1.91 | 0.77 |
| Al doped hematite | 0.75 | 0.19 | 2.61 | 2.07 | 2.10 | 0.96 |
| Ni doped hematite | 0.61 | 0.032 | 2.375 | 1.53 | 1.605 | 0.42 |
| Co doped hematite | 0.65 | -0.062 | 2.722 | 1.43 | 1.583 | 0.32 |

| - Hematite (side view) | - Hematite (top view) |
| --- | --- |
| - Graphene-Hematite (side view) | - Graphene-Hematite (top view) |
| - Al doped hematite (side view) | - Al doped hematite (top view) |
| - Graphene-Al doped hematite (side view) | - Graphene-Al doped hematite (top view) |
| - N doped Graphene-Al doped hematite (side view) | - N doped Graphene-Al doped hematite (top view) |
| Figure S1. Unit cell of *OH intermediate (side and top view along b and c axis, respectively) with atom numbers (a-b) Hematite, (c-d) Graphene-Hematite, (e-f) Al doped hematite, (g-h) Graphene-Al doped hematite, and (i-j) N doped Graphene-Al doped hematite, respectively. Fe1 is the active site. |  |

Figure S2. Convergence plots vs N, samples. Spatial Grid density convergence test for Graphene-Al doped Hematite (*OH intermediate). Wave propagates from hematite to graphene. Initial wavefunction is located at oxygen atom near the interface and the flux is measured at barrier.

Figure S3. Time convergence test results for Graphene-Al doped Hematite (*OH intermediate). Number of time steps = 200. Wave propagates from hematite to graphene. Initial wavefunction is located at oxygen atom near the interface and the flux is measured at barrier.

(a)

(b)

Figure S4. Projected density of states (states/eV/atom) for studied anode material Al-doped hematite below ~-6 eV.

(a)

(b)

Figure S5. Cumulative probability when wave propagates from hematite to graphene. Initial wavefunction located at oxygen atom near the interface and the flux is measured at iron atom. (a) is for *OH intermediate and (b) is for *O intermediate.

| Figure S6. Dynamics of charge propagation from Al doped Hematite to Graphene at different time steps in fsec for Graphene-Al doped Hematite (*OH intermediate). At each time step, the absolute value squared and the real part of the wave packet is shown in red and blue color respectively. Initial wavefunction located at oxygen atom near the interface. Flux is measured at barrier. Maximum flux is observed at t=0.2 fs and after t=0.4 fs the wavefunction begins to cross the edges. |  |
| --- | --- |

| Figure S7. Dynamics of charge propagation from Al doped Hematite to Graphene at different time steps in fsec for Graphene-Al doped Hematite (*O intermediate). At each time step, the absolute value squared and the real part of the wave packet is shown in red and blue color respectively. Initial wavefunction located at oxygen atom near the interface. Flux is measured at barrier. Maximum flux is observed at t=0.2 fs and after t=0.4 fs the wavefunction begins to cross the edges. |  |
| --- | --- |

| Figure S8. Dynamics of charge propagation from Graphene to Al doped Hematite at different time steps in fsec for Graphene-Al doped Hematite (*OH intermediate). At each time step, the absolute value squared and the real part of the wave packet is shown in red and blue color respectively. Initial wavefunction located at carbon atom near the interface. Flux is measured at barrier. Maximum flux is observed around t=0.2 fs and after t=0.4 fs the wavefunction begins to cross the edges. |  |
| --- | --- |

| Figure S9. Dynamics of charge propagation from Graphene to Al doped Hematite at different time steps in fsec for Graphene-Al doped Hematite (*O intermediate). At each time step, the absolute value squared and the real part of the wave packet is shown in red and blue color respectively. Initial wavefunction located at carbon atom near the interface. Flux is measured at barrier. Maximum flux is observed around t=0.2 fs and after t=0.4 fs the wavefunction begins to cross the edges. |  |
| --- | --- |

Figure S10. Electrostatic local potential along interface direction (Z-direction) of *O intermediate of Al-doped hematite and graphene supported heterostructures with respect to vacuum. Data for hematite and graphene-hematite are taken from our previous work [S1].

| Initial image: *OH intermediate | Transition state: H atom is between *O and Cl. | Final state: *O intermediate on the surface and H atom is captured by Cl. |
| --- | --- | --- |
| - Two Cl sinks both side of the hematite slab following N. Snir et al. [S2]. The computed reaction activation energy is 0.64 eV. Red, gold, white and green spheres represent oxygen, iron, hydrogen and chlorine atoms, respectively. Oxygen and hydrogen atoms of the surfaces both side of the slab are allowed to move in all three directions during initial and final image optimization and CI-NEB calculations (except H4 is fixed at c and allowed to move in a and b direction). Iron and chlorine atoms are fixed in all three directions. |  |  |
| Initial image: *OH intermediate | Transition state: H atom is between *O and Cl. | Final state: *O intermediate on the surface and H atom is captured by Cl. |
| - Two Cl sinks both side of the hematite slab. Second chlorine atom is placed just to balance the dipole moment created by the first chlorine atom. The computed reaction activation energy is 0.64 eV. Oxygen and hydrogen atoms of the surfaces both side of the slab are allowed to move in all three directions during initial and final image optimization and CI-NEB calculations. Iron and chlorine atoms are fixed in all three directions. |  |  |
| Initial image: *OH intermediate | Transition state: H atom is between *O and Cl. | Final state: *O intermediate on the surface and H atom is captured by Cl. |
| - One Cl sink is placed in one side of the hematite slab. Dipole correction has been considered. The computed reaction activation energy is 0.66 eV. Oxygen and hydrogen atoms of the surface (marked in black box) where deprotonation reaction takes place are allowed to move in all three directions during initial and final image optimization and CI-NEB calculations. All other atoms are fixed in all three directions. |  |  |
| Figure S11. Deprotonation of *OH intermediate of hematite monolayer considering (a) two chlorine sinks, (b) two chlorine sinks; Second chlorine atom is placed to balance the dipole moment created by the first chlorine atom and (c) one chlorine sink including dipole correction. |  |  |

| Initial image: *OH intermediate | Transition state: H atom is between *O and Cl. | Final state: *O intermediate on the surface and H atom is captured by Cl. |
| --- | --- | --- |
| - Graphene-Hematite. Selective dynamics constraints are the same as mentioned in Figure 11(c) including the carbon atoms in graphene are fixed in all three directions during initial and final image optimization and CI-NEB calculations. |  |  |
| Initial image: *OH intermediate | Transition state: H atom is between *O and Cl. | Final state: *O intermediate on the surface and H atom is captured by Cl. |
| (b) Al doped Hematite. Selective dynamics constraints are the same as mentioned in Figure 11(c) during initial and final image optimization and CI-NEB calculations |  |  |
| Initial image: *OH intermediate | Transition state: H atom is between *O and Cl. | Final state: *O intermediate on the surface and H atom is captured by Cl. |
| (c) Graphene- Al doped Hematite. Selective dynamics constraints are the same as mentioned in Figure 11(c) including the carbon atoms in graphene are fixed in all three directions during initial and final image optimization and CI-NEB calculations. |  |  |
| Initial image: *OH intermediate | Transition state: H atom is between *O and Cl. | Final state: *O intermediate on the surface and H atom is captured by Cl. |
| (d) N doped Graphene- Al doped Hematite. Selective dynamics constraints are the same as mentioned in Figure 11(c) including the carbon atoms in graphene are fixed in all three directions during initial and final image optimization and CI-NEB calculations. |  |  |
| Figure S12. Deprotonation of *OH intermediate of (a) Graphene-Hematite, (b) Al doped Hematite, and (c) Graphene- Al doped Hematite (d) N doped Graphene- Al doped Hematite |  |  |

Python module for the numerical simulation of wave function propagation

Y. Reichman, M. Caspary Toroker, A Numeric Approach for Investigating Electron Dynamics in Zinc-Blende Semiconductor Heterostructures, Adv Theory Simul (2023). https://doi.org/10.1002/adts.202300155.

INCAR used for geometry optimization of Graphene-Al doped Hematite:

SYSTEM = Graphene-Al doped Hematite

ISTART = 0

ICHARG = 2

PREC = Accurate

ALGO = Very_Fast

NPAR = 4

EDIFF = 1E-4

NELM = 200

MAGMOM = 6*0 1*4 1*0.12 6*0 8*0

LVTOT = .TRUE.

ISMEAR = 0

SIGMA = 0.05

EMIN = -8.5

EMAX = 5

NEDOS = 1500

LWAVE = .TRUE.

LCHARG = .FALSE.

ISPIN = 2

ISYM = 0

EDIFFG = -3.0E-2

LORBIT = 10

IBRION = 2

NSW = 50

ISIF = 2

POTIM = 0.3

LREAL = .FALSE.         # Real space projection

ENCUT = 700 eV

LDAU = .TRUE.

LDAUTYPE = 2

LDAUL = -1 2 -1 -1 -1

LDAUU = 0 4.3 0 0 0

LDAUJ = 0 0 0 0 0

LDAUPRINT = 0

IVDW = 20

LVDW_EWALD =.TRUE.

During Bader charge analysis. ICHARG =1 is taken which reads the charge density from CHGCAR outputted in geometry optimization. In INCAR, LCHARG = .TRUE., LAECHG = .TRUE. are also added.

INCAR used for calculating Zero-point energy (ZPE) corrections and entropic contribution

ISTART = 1

ICHARG = 1

PREC = Accurate

ALGO = Very_Fast

NPAR = 4

EDIFF = 1E-4

NELM = 200

MAGMOM = 6*0 1*4 1*0.12 6*0 8*0

LVTOT = .TRUE.

ISMEAR = 0

SIGMA = 0.05

EMIN = -8.5

EMAX = 5

NEDOS = 1500

LWAVE = .TRUE.

LCHARG = .FALSE.

ISPIN = 2

ISYM = 0

EDIFFG = -3.0E-2

LORBIT = 10

IBRION = 5      #ZPE and entropic calculations

NSW = 1         #ZPE and entropic calculations

ISIF = 2

POTIM = 0.3

NFREE = 2        #ZPE and entropic calculations

LREAL = .FALSE.         # Real space projection

ENCUT = 700 eV

LDAU = .TRUE.

LDAUTYPE = 2

LDAUL = -1 2 -1 -1 -1

LDAUU = 0 4.3 0 0 0

LDAUJ = 0 0 0 0 0

LDAUPRINT = 0

IVDW = 20

LVDW_EWALD =.TRUE.

VASP outputs of Zero-point energy (ZPE) corrections and entropic calculations are processed with the code available in https://github.com/ftherrien/VaspGibbs.git to calculate (∆ZPE-T∆S)1-5 values.

INCAR used for CI-NEB calculations for Graphene-Al doped hematite heterostructure

# This is one of the input files for a vasp DFT bulk calculation.

SYSTEM = Graphene-Al doped hematite

ISTART = 1

PREC = Accurate

ALGO = Very_Fast

NPAR = 4

EDIFF = 1E-4

NELM = 200

MAGMOM = 6*0 1*4 1*0.12 6*0 8*0 1*0

# DOS related values:

ISMEAR = 0

SIGMA = 0.05

NEDOS = 500

LWAVE = .TRUE.

LCHARG = .FALSE.

ISPIN = 2

ISYM = 0

EDIFFG = -3.0E-2

LORBIT = 10

IBRION = 3

NSW = 50

ISIF = 0

POTIM = 0

LDIPOL = .TRUE.

IDIPOL  = 3

LREAL = .FALSE.

ENCUT = 700 eV

LDAU = .TRUE.

LDAUTYPE = 2

LDAUL = -1 2 -1 -1 -1 -1

LDAUU = 0 4.3 0 0 0 0

LDAUJ = 0 0 0 0 0 0

LDAUPRINT = 0           ## 2

#VDW correction for graphene

IVDW = 20

LVDW_EWALD =.TRUE.

# NEB Calculations

IMAGES = 8

SPRING = -5

LCLIMB = .TRUE.

IOPT = 3

The relaxed geometries (CONTCAR outputted by VASP) and the total energy of the *OH intermediate of Al doped hematite, Graphene-Al doped hematite and N doped graphene- Al doped hematite are given according to the following order: title, lattice vectors in Cartesian coordinates, atom types and numbers, and atom locations in fractional coordinates.

*OH_ Al doped hematite

1.00000000000000

5.0980000496000004    0.0000000000000000    0.0000000000000000

-2.5490000248000002    4.4149975513999999    0.0000000000000000

0.0000000000000000    0.0000000000000000   25.6149997710999990

O    Fe   Al   H

6     1     1     6

Direct

0.6901238524363222  0.7360656003887627  0.3192470874727320

0.3043520230519192  0.0179809003962461  0.3192286843512449

0.0172654286355893  0.3541404904834309  0.3187446911819265

0.6897000001227411  0.0314595254986543  0.2356247808480774

0.0214404424687515  0.7356050783886516  0.2343963911679836

0.3056576452877664  0.3514926144467481  0.2338426965261817

0.3416151151035791  0.7005570264859671  0.2764708723056444

0.0054705365301473  0.0373558187383054  0.2767246217355890

0.0862786444305641  0.7967083327593656  0.1986874579182114

0.4991485284000703  0.3538294844543302  0.2324007889457604

0.7029219630978432  0.9853982626319748  0.1993407313980526

0.0844913905796361  0.3462479412137043  0.3538493531292701

0.2322208442760996  0.9416944630646285  0.3541017813571514

0.6887635471355651  0.5431544515217368  0.3210200124990266

Total Energy= -79.16890429 eV

*OH_ Graphene-Al doped hematite

1.00000000000000

5.0082168578999999    0.0000000000000000    0.0000000000000000

-2.5041084290000000    4.3372430266000004    0.0000000000000000

0.0000000000000000    0.0000000000000000   25.6149997710999990

O    Fe   Al   H    C

6     1     1     6     8

Direct

0.7110245982882404  0.6735746492183736  0.3345303562545752

0.3345596072181038  0.9713980793852528  0.3352592300997088

0.0378266398649956  0.3022564663982479  0.3362031896934354

0.7128733915176610  0.9564084172675180  0.2491898593497766

0.3283441583324702  0.2974000893862154  0.2502794244440167

0.0204903957847264  0.6622568492489762  0.2506587771516067

0.3565798483575264  0.6470399242749352  0.2918862297790596

0.0286855954311065  0.9874311348191753  0.2935944490402917

0.5455109136667033  0.3538064636328428  0.2494030757492851

0.7551408579694865  0.1531396354304562  0.2348031397895198

0.8427765894520007  0.3038973260109827  0.3377630024684422

0.2561589103748290  0.8946970709292188  0.3699752548691677

0.7002905068339587  0.7427638936328549  0.3694333062169193

0.0813433559158412  0.7452380580988844  0.2155907524044594

0.1670680542275775  0.3189213344260722  0.4642219198558806

0.1670009637852488  0.8187807367246265  0.4642780469853278

0.6671682223722826  0.3189356890549107  0.4642248851572646

0.6670762553424368  0.8188934761339013  0.4642311738044569

0.0005263060656375  0.9858555893054159  0.4642716853769926

0.0003123213938920  0.4852809009115617  0.4642592896056001

0.5005792930803779  0.9857760390669910  0.4642573989379954

0.5001865042806060  0.4852851177638371  0.4642634371308247

Total Energy = -154.39829169 eV

*OH_ N doped graphene-Al doped hematite

1.00000000000000

5.0082168578999999    0.0000000000000000    0.0000000000000000

-2.5041084290000000    4.3372430266000004    0.0000000000000000

0.0000000000000000    0.0000000000000000   25.6149997710999990

O    Fe   Al   H    C    N

6     1     1     6     7     1

Direct

0.7096740263813928  0.6722376515239716  0.3348284794107457

0.3349876786147519  0.9712974413870228  0.3352395940163007

0.0388377582017867  0.3024848809809697  0.3367068004950511

0.7133370189226511  0.9561107308261469  0.2493825073463753

0.3261934156404465  0.2961692800116396  0.2503978420704485

0.0186672549332343  0.6602540134551020  0.2510757903749763

0.3563283785874134  0.6467082450243637  0.2919145064202340

0.0277732543346048  0.9868783126881766  0.2940265020341073

0.5430545622648566  0.3519816702698222  0.2491594706334368

0.7572791119204538  0.1549023631824298  0.2356996531232483

0.8459046822508896  0.3081153248056481  0.3385156555862707

0.2626474475943041  0.8964462395552601  0.3702954156137608

0.6898117020785008  0.7357380312686743  0.3697252428560773

0.0793247045479077  0.7403325747182947  0.2158470890759077

0.1682040248288317  0.3207190802625632  0.4637687609275289

0.1684052333540293  0.8195980874740911  0.4636114579489643

0.6680758310981432  0.3200135608679702  0.4637352889937887

0.6672439976993871  0.8197933323253466  0.4635405058485134

0.0002315188791187  0.4863514495976489  0.4637987124447989

0.5020951893374672  0.9884826332650221  0.4637158318986394

0.5017335260296463  0.4863771823280061  0.4637599289762164

0.0017128173043659  0.9880448936685013  0.4638328331560970

Total Energy = -152.23336712 eV

The relaxed geometries (CONTCAR outputted by VASP) and the total energy of the initial state, transition state and final state from NEB calculations for hematite, Al doped hematite, Graphene-hematite, Graphene-Al doped hematite and N doped graphene- Al doped hematite are given according to the following order: title, lattice vectors in Cartesian coordinates, atom types and numbers, and atom locations in fractional coordinates.

Hematite

Initial state:

Hematite_Initial state

1.00000000000000

5.0980000496000004   0.0000000000000000   0.0000000000000000

-2.5490000247999998   4.4149975513999999   0.0000000000000000

0.0000000000000000   0.0000000000000000  25.6149997710999990

O    Fe   H    Cl

6  2  6  1

Selective dynamics

Direct

0.6740766762877044  0.7185456752957933  0.3215393424009534 F F F

0.3222995698639082  0.0231369641343520  0.3214666247348674 F F F

0.0180896557408801  0.3750866950027785  0.3219198286428835 F F F

0.6720352092274631  0.0341552189933221  0.2339151135178719 T T T

0.0242229829245717  0.7230136634937931  0.2333982519885388 T T T

0.3275817471758642  0.3781750637777839  0.2315847047344171 T T T

0.3412569463543775  0.7015897630606318  0.2765461206442055 F F F

0.0041295727295463  0.0404457524429134  0.2766691446156386 F F F

0.0780595839920000  0.7534219249967189  0.1961382889251797 T T T

0.5166964515285807  0.3695157489273340  0.2288032149804726 T T T

0.6705158510166465  0.9800658056369064  0.1972561827870697 T T T

0.1064543276942729  0.3694939614366746  0.3552833795558996 F F F

0.2344870568196811  0.9307311177776256  0.3549360335055596 F F F

0.6784994602312509  0.5277824997345917  0.3225114643694269 F F F

0.2339938879646368  0.5903573632047667  0.1176049485816790 F F F

Total Energy = -78.23345890 eV, Zero Point Energy corrections (ZPE-TS) = 1.034806 eV

Transition state:

Hematite_transition state

1.00000000000000

5.0980000496000004    0.0000000000000000    0.0000000000000000

-2.5490000247999998    4.4149975513999999    0.0000000000000000

0.0000000000000000    0.0000000000000000   25.6149997710999990

O    Fe   H    Cl

6     2     6     1

Selective dynamics

Direct

0.6740766762877044  0.7185456752957933  0.3215393424009534   F   F   F

0.3222995698639082  0.0231369641343520  0.3214666247348674   F   F   F

0.0180896557408374  0.3750866950027785  0.3219198286428835   F   F   F

0.6841455620659218  0.0277072571528549  0.2339973394013626   T   T   T

0.0886868302098023  0.7200328044732771  0.2259039944544483   T   T   T

0.3383007510717846  0.3684833798033793  0.2360826590746896   T   T   T

0.3412569463543207  0.7015897630606318  0.2765461206442055   F   F   F

0.0041295727295463  0.0404457524429134  0.2766691446156386   F   F   F

0.1529055551607854  0.6611090862716296  0.1763241465995264   T   T   T

0.5234579352209963  0.3563647049541032  0.2316039474094183   T   T   T

0.6678394307198801  0.9797302860537940  0.1966952495162104   T   T   T

0.1064543313751756  0.3694939614366746  0.3552833795558996   F   F   F

0.2344870568196384  0.9307311177776256  0.3549360335055596   F   F   F

0.6784994602312509  0.5277824997345917  0.3225114643694269   F   F   F

0.2339938806026964  0.5903573632047667  0.1176049485816790   F   F   F

Total Energy = -77.38131571 eV, Zero Point Energy corrections (ZPE-TS) = 0.845239 eV

Final state:

Hematite_final state

1.00000000000000

5.0980000496000004   0.0000000000000000   0.0000000000000000

-2.5490000247999998   4.4149975513999999   0.0000000000000000

0.0000000000000000   0.0000000000000000  25.6149997710999990

O    Fe   H    Cl

6  2  6  1

Selective dynamics

Direct

0.6740766762877044  0.7185456752957933  0.3215393424009534 F F F

0.3222995698639083  0.0231369641343520  0.3214666247348674 F F F

0.0180896557408183  0.3750866950027784  0.3219198286428835 F F F

0.6744086665217985  0.0200226309232579  0.2330234572719047 T T T

0.0631696180496058  0.7207602374205258  0.2392379686174950 T T T

0.3316455010354000  0.3709304644098972  0.2348868552456873 T T T

0.3412569463542929  0.7015897630606317  0.2765461206442055 F F F

0.0041295727295463  0.0404457524429134  0.2766691446156386 F F F

0.1053404561753202  0.6063717244340416  0.1602959886176007 T T T

0.5158193760831249  0.3560121456918233  0.2318082223510219 T T T

0.6477547989848857  0.9522112402229612  0.1966637187018034 T T T

0.1064543343199025  0.3694939614366746  0.3552833795558996 F F F

0.2344870568196166  0.9307311177776256  0.3549360335055596 F F F

0.6784994602312509  0.5277824997345917  0.3225114643694269 F F F

0.2339938747131581  0.5903573632047667  0.1176049485816790 F F F

Total Energy =  -78.03307374 eV,   Zero Point Energy corrections (ZPE-TS) = 0.961954 eV

Al doped Hematite

Initial state:

Al doped hematite_initial state

1.00000000000000

5.0980000496000004    0.0000000000000000    0.0000000000000000

-2.5490000248000002    4.4149975513999999    0.0000000000000000

0.0000000000000000    0.0000000000000000   25.6149997710999990

O    Fe   Al   H    Cl

6     1     1     6     1

Selective dynamics

Direct

0.6901238560239733  0.7360656261223752  0.3192470967821848   F   F   F

0.3043520152217027  0.0179808996665969  0.3192287087281471   F   F   F

0.0172654205521070  0.3541404904073389  0.3187446892430472   F   F   F

0.6907342309398175  0.0266613451022943  0.2360052300430698   T   T   T

0.0320021029757023  0.7401889801440307  0.2351232623728298   T   T   T

0.3085816937126369  0.3548457822359081  0.2350289658216049   T   T   T

0.3416151105828362  0.7005570530881116  0.2764708697749043   F   F   F

0.0054705361238589  0.0373558177733742  0.2767246365544480   F   F   F

0.0738789940957486  0.7592146197726385  0.1975519324258315   T   T   T

0.4993081369890159  0.3549019641190536  0.2297629670249513   T   T   T

0.6901174951320803  0.9910237220230741  0.1985805236976607   T   T   T

0.0844913795135724  0.3462479412961983  0.3538493513955174   F   F   F

0.2322208135829413  0.9416943788975871  0.3541017770858446   F   F   F

0.6887635588612895  0.5431544781354631  0.3210200071240052   F   F   F

0.2339938730568321  0.5903573632047667  0.1176049485816790   F   F   F

Total Energy = -79.98685881 eV, Zero Point Energy corrections (ZPE-TS) = 1.058524 eV

Transition state:

Al doped hematite_transition state

1.00000000000000

5.0980000496000004    0.0000000000000000    0.0000000000000000

-2.5490000247999998    4.4149975513999999    0.0000000000000000

0.0000000000000000    0.0000000000000000   25.6149997710999990

O    Fe   Al   H    Cl

6     1     1     6     1

Selective dynamics

Direct

0.6901238560239733  0.7360656261223752  0.3192470967821847   F   F   F

0.3043520152217027  0.0179808996665969  0.3192287087281471   F   F   F

0.0172654205521064  0.3541404904073389  0.3187446892430472   F   F   F

0.7018925496278949  0.0058626033798381  0.2352761180402762   T   T   T

0.0969358192322177  0.7317024037518921  0.2265169407550772   T   T   T

0.3120210860222051  0.3468050310260440  0.2380414294209625   T   T   T

0.3416151105828278  0.7005570530881116  0.2764708697749043   F   F   F

0.0054705361238588  0.0373558177733742  0.2767246365544480   F   F   F

0.1557519302399638  0.6671515382704217  0.1767150451789004   T   T   T

0.4952447879157513  0.3440902765550606  0.2279399454324429   T   T   T

0.6968077523252545  0.9838425554843132  0.1974205986029240   T   T   T

0.0844913795135724  0.3462479412961983  0.3538493513955175   F   F   F

0.2322208135829413  0.9416943788975871  0.3541017770858446   F   F   F

0.6887635588612895  0.5431544781354631  0.3210200071240053   F   F   F

0.2339938730568238  0.5903573632047667  0.1176049485816790   F   F   F

Total Energy = -79.04444562 eV,  Zero Point Energy corrections (ZPE-TS) = 0.864657 eV

Final state

Al doped hematite_final state

1.00000000000000

5.0980000496000004    0.0000000000000000    0.0000000000000000

-2.5490000248000002    4.4149975513999999    0.0000000000000000

0.0000000000000000    0.0000000000000000   25.6149997710999990

O    Fe   Al   H    Cl

6     1     1     6     1

Selective dynamics

Direct

0.6901238560239733  0.7360656261223752  0.3192470967821848   F   F   F

0.3043520152217027  0.0179808996665969  0.3192287087281471   F   F   F

0.0172654205521070  0.3541404904073389  0.3187446892430472   F   F   F

0.6963259096652161  0.0101590063654959  0.2354369566316660   T   T   T

0.0724779251962233  0.7365076966875258  0.2388650153850565   T   T   T

0.3100913484008578  0.3520286177914432  0.2372487999358063   T   T   T

0.3416151105828362  0.7005570530881116  0.2764708697749043   F   F   F

0.0054705361238589  0.0373558177733742  0.2767246365544480   F   F   F

0.1407857352156112  0.6489213186184607  0.1610460861160618   T   T   T

0.4975072898378411  0.3477502378615560  0.2311303948707380   T   T   T

0.6893264139529393  0.9807340440838915  0.1977670026592298   T   T   T

0.0844913795135724  0.3462479412961983  0.3538493513955174   F   F   F

0.2322208135829413  0.9416943788975871  0.3541017770858446   F   F   F

0.6887635588612895  0.5431544781354631  0.3210200071240052   F   F   F

0.2339938730568321  0.5903573632047667  0.1176049485816790   F   F   F

Total Energy = -79.72685144 eV,  Zero Point Energy corrections (ZPE-TS) = 0.992408 eV

Graphene-Hematite

Initial state

Graphene-Hematite_Initial state

1.00000000000000

5.0082168578999999    0.0000000000000000    0.0000000000000000

-2.5041084290000000    4.3372430266000004    0.0000000000000000

0.0000000000000000    0.0000000000000000   25.6149997710999990

O    Fe   H    C    Cl

6     2     6     8     1

Selective dynamics

Direct

0.6976631283975649  0.6492146849348543  0.3363840281865436   F   F   F

0.3540635706317516  0.9660570026403619  0.3372179567905178   F   F   F

0.0373229569720408  0.3140996097394009  0.3379423618331074   F   F   F

0.6911739070439680  0.9780258196344747  0.2494181989651096   T   T   T

0.3472426762560445  0.3086600199049983  0.2477670216685510   T   T   T

0.0291979113507423  0.6578181385614741  0.2487647540821882   T   T   T

0.3582273721089777  0.6428706645903048  0.2913401126952095   F   F   F

0.0322250686696677  0.9854547381336261  0.2928015589702255   F   F   F

0.5432190903141176  0.3063572162987924  0.2456703473413100   T   T   T

0.6915603958715479  0.9348492465488789  0.2122371028023124   T   T   T

0.8403651715473828  0.3135318458430945  0.3392430841949121   F   F   F

0.2561011612799717  0.8706268071310106  0.3701723515804218   F   F   F

0.6821497677939519  0.7244980930808680  0.3705992996615350   F   F   F

0.0833937726312612  0.6922566510737767  0.2112794563070182   T   T   T

0.1662684083029831  0.3280515371801442  0.4647158384295693   F   F   F

0.1662444324475700  0.8280113936375955  0.4647733569153445   F   F   F

0.6663798093957283  0.3280641435754248  0.4647429883419747   F   F   F

0.6663601994926722  0.8281518817302072  0.4647321402840987   F   F   F

0.9998077155007650  0.9950747489893956  0.4647403955642844   F   F   F

0.9995384813602755  0.4944500625968189  0.4647669494196833   F   F   F

0.4998469949066049  0.9950086475516287  0.4647792875810239   F   F   F

0.4994052647863825  0.4944134354124472  0.4647734165288568   F   F   F

0.2381887286982263  0.6009407639864719  0.1321067952855444   F   F   F

Total Energy = -153.25987998 eV,   Zero Point Energy corrections (ZPE-TS) = 0.968151 eV

Transition state

O    Fe   H    C    Cl

Graphene-hematite_transition state

5.0082168578999999    0.0000000000000000    0.0000000000000000

-2.5041084290000000    4.3372430266000004    0.0000000000000000

0.0000000000000000    0.0000000000000000   25.6149997710999990

O    Fe   H    C    Cl

6     2     6     8     1

Selective dynamics

Direct

0.6976631283975649  0.6492146849348543  0.3363840281865436   F   F   F

0.3540635706317730  0.9660570026403619  0.3372179567905178   F   F   F

0.0373229569720408  0.3140996097394009  0.3379423618331074   F   F   F

0.7077545091531476  0.9732806295065899  0.2492734984242304   T   T   T

0.3653045198118363  0.3163245102756491  0.2509822715281516   T   T   T

0.0994716630517161  0.6721419615767132  0.2423958190800022   T   T   T

0.3582273721089777  0.6428706645903048  0.2913401126952095   F   F   F

0.0322250686696677  0.9854547381336261  0.2928015589702255   F   F   F

0.5568103167789431  0.3085794490689366  0.2471679983153194   T   T   T

0.6970324331118860  0.9298918173013959  0.2118313887292018   T   T   T

0.8403651715473828  0.3135318458430945  0.3392430841949121   F   F   F

0.2561011612799717  0.8706268071310106  0.3701723515804218   F   F   F

0.6821497677939519  0.7244980930808680  0.3705992996615350   F   F   F

0.1632916652747198  0.6393095754162559  0.1920824837432562   T   T   T

0.1662684083029831  0.3280515371801442  0.4647158384295693   F   F   F

0.1662444324475700  0.8280113936375955  0.4647733569153445   F   F   F

0.6663798093957283  0.3280641435754248  0.4647429883419747   F   F   F

0.6663601994926722  0.8281518817302072  0.4647321402840987   F   F   F

0.9998077155007650  0.9950747489893956  0.4647403955642844   F   F   F

0.9995384813602755  0.4944500625968189  0.4647669494196833   F   F   F

0.4998469949066049  0.9950086475516287  0.4647792875810239   F   F   F

0.4994052647863825  0.4944134354124472  0.4647734165288568   F   F   F

0.2381887286982263  0.6009407639864719  0.1321067956325734   F   F   F

Total Energy = -152.61722942 eV, Zero Point Energy corrections (ZPE-TS) = 0.830039 eV

Final state

Graphene-hematite_final

1.00000000000000

5.0082168578999999    0.0000000000000000    0.0000000000000000

-2.5041084290000000    4.3372430266000004    0.0000000000000000

0.0000000000000000    0.0000000000000000   25.6149997710999990

O    Fe   H    C    Cl

6     2     6     8     1

Selective dynamics

Direct

0.6976631283975649  0.6492146849348543  0.3363840281865436   F   F   F

0.3540635706317516  0.9660570026403619  0.3372179567905178   F   F   F

0.0373229569720408  0.3140996097394009  0.3379423618331074   F   F   F

0.6998726306443928  0.9938785104076402  0.2503067034821882   T   T   T

0.3455190231990386  0.3142579117232955  0.2491516292853717   T   T   T

0.0441940016308280  0.7060799212773858  0.2538920143717078   T   T   T

0.3582273721089777  0.6428706645903048  0.2913401126952095   F   F   F

0.0322250686696677  0.9854547381336261  0.2928015589702255   F   F   F

0.5264064447644969  0.2874482122594770  0.2446828283297009   T   T   T

0.7154394564547673  0.9438439390701703  0.2139558296112938   T   T   T

0.8403651715473828  0.3135318458430945  0.3392430841949121   F   F   F

0.2561011612799717  0.8706268071310106  0.3701723515804218   F   F   F

0.6821497677939519  0.7244980930808680  0.3705992996615350   F   F   F

0.1303043108081212  0.6608879384476651  0.1738598320404492   T   T   T

0.1662684083029831  0.3280515371801442  0.4647158384295693   F   F   F

0.1662444324475700  0.8280113936375955  0.4647733569153445   F   F   F

0.6663798093957283  0.3280641435754248  0.4647429883419747   F   F   F

0.6663601994926722  0.8281518817302072  0.4647321402840987   F   F   F

0.9998077155007650  0.9950747489893956  0.4647403955642844   F   F   F

0.9995384813602755  0.4944500625968189  0.4647669494196833   F   F   F

0.4998469949066049  0.9950086475516287  0.4647792875810239   F   F   F

0.4994052647863825  0.4944134354124472  0.4647734165288568   F   F   F

0.2381887286982263  0.6009407639864719  0.1321067959101825   F   F   F

Total Energy =  -153.15656939 eV,  Zero Point Energy corrections (ZPE-TS) = 0.949389 eV

Graphene-Al doped hematite

Initial state

Graphene-Al doped hematite_initial

1.00000000000000

5.0082168578999999   0.0000000000000000   0.0000000000000000

-2.5041084290000000   4.3372430266000004   0.0000000000000000

0.0000000000000000   0.0000000000000000  25.6149997710999990

O    Fe   Al   H    C    Cl

6  1  1  6  8  1

Selective dynamics

Direct

0.7110245822858943  0.6735746263427984  0.3345303237389814 F F F

0.3345596491945955  0.9713981151530646  0.3352591991310092 F F F

0.0378266313267375  0.3022564649847794  0.3362032174880696 F F F

0.7071278698333288  0.9779746557869018  0.2520859888238505 T T T

0.3331464537484692  0.3052160808056072  0.2514108891617823 T T T

0.0362531148162262  0.6810998097388676  0.2516048610938810 T T T

0.3565798401556535  0.6470399499840624  0.2918862402425404 F F F

0.0286855865709441  0.9874311090557626  0.2935944497444396 F F F

0.5322652819971481  0.3120929850155321  0.2478931468422090 T T T

0.7088011966414882  0.9484173360066492  0.2144710214729599 T T T

0.8427765965859209  0.3038973211591625  0.3377630114508676 F F F

0.2561589180176398  0.8946970700514285  0.3699752688536933 F F F

0.7002905011314198  0.7427638770164577  0.3694333434145349 F F F

0.0756720424580024  0.6977346785125675  0.2137945525970792 T T T

0.1670680492228911  0.3189213275614691  0.4642219245465711 F F F

0.1670009493768347  0.8187807201995412  0.4642780423296244 F F F

0.6671681999787467  0.3189356922165345  0.4642248749662699 F F F

0.6670762301852307  0.8188934922985496  0.4642311632739577 F F F

0.0005262775623152  0.9858555794029158  0.4642716944084242 F F F

0.0003123060285688  0.4852809012756580  0.4642592966726085 F F F

0.5005792975451939  0.9857760666806924  0.4642573594873483 F F F

0.5001865030324737  0.4852851332266610  0.4642634391672829 F F F

0.2381887286982263  0.6009407639864719  0.1338986599121341 F F F

Total Energy = -155.45516267 eV, Zero Point Energy corrections (ZPE-TS) = 1.03276 eV

Transition state

Graphene-Al doped hematite_transition state

1.00000000000000

5.0082168578999999    0.0000000000000000    0.0000000000000000

-2.5041084290000000    4.3372430266000004    0.0000000000000000

0.0000000000000000    0.0000000000000000   25.6149997710999990

O    Fe   Al   H    C    Cl

6     1     1     6     8     1

Selective dynamics

Direct

0.7110245822858943  0.6735746263427984  0.3345303237389814   F   F   F

0.3345596491945955  0.9713981151530645  0.3352591991310093   F   F   F

0.0378266313267375  0.3022564649847793  0.3362032174880696   F   F   F

0.7208280637808517  0.9575592170566284  0.2512502513338600   T   T   T

0.3366003471546708  0.2994384579104423  0.2535195545377280   T   T   T

0.0999484672679969  0.6870494906876154  0.2444133141796881   T   T   T

0.3565798401556535  0.6470399499840623  0.2918862402425404   F   F   F

0.0286855865709441  0.9874311090557625  0.2935944497444396   F   F   F

0.5295019128522478  0.3028531801978867  0.2458116490918374   T   T   T

0.7197215798043550  0.9370758187930209  0.2133762424521993   T   T   T

0.8427765965859211  0.3038973211591623  0.3377630114508676   F   F   F

0.2561589180176667  0.8946970700514285  0.3699752688536933   F   F   F

0.7002905011314198  0.7427638770164577  0.3694333434145349   F   F   F

0.1602482867997722  0.6471721783659437  0.1940104950379968   T   T   T

0.1670680492228911  0.3189213275614690  0.4642219245465711   F   F   F

0.1670009493768348  0.8187807201995412  0.4642780423296244   F   F   F

0.6671681999787467  0.3189356922165345  0.4642248749662699   F   F   F

0.6670762301852307  0.8188934922985496  0.4642311632739577   F   F   F

0.0005262775623153  0.9858555794029157  0.4642716944084241   F   F   F

0.0003123060285690  0.4852809012756580  0.4642592966726085   F   F   F

0.5005792975451938  0.9857760666806924  0.4642573594873483   F   F   F

0.5001865030324737  0.4852851332266609  0.4642634391672829   F   F   F

0.2381887286982263  0.6009407639864719  0.1338986603285690   F   F   F

Total Energy = -154.72017940 eV, Zero Point Energy corrections (ZPE-TS) = 0.85232 eV

Final state

Graphene-Al doped hematite_final

1.00000000000000

5.0082168578999999   0.0000000000000000   0.0000000000000000

-2.5041084290000000   4.3372430266000004   0.0000000000000000

0.0000000000000000   0.0000000000000000  25.6149997710999990

O    Fe   Al   H    C    Cl

6  1  1  6  8  1

Selective dynamics

Direct

0.7110245822858943  0.6735746263427984  0.3345303237389814 F F F

0.3345596491945955  0.9713981151530646  0.3352591991310092 F F F

0.0378266313267375  0.3022564649847794  0.3362032174880696 F F F

0.7154505520787424  0.9557473964113044  0.2510558260500062 T T T

0.3328347629995321  0.3001309543396857  0.2527489325500270 T T T

0.0807721868974127  0.6803308880834109  0.2549241193936496 T T T

0.3565798401556535  0.6470399499840624  0.2918862402425404 F F F

0.0286855865709441  0.9874311090557626  0.2935944497444396 F F F

0.5274459481139999  0.3039947315714855  0.2465611663514053 T T T

0.7115613651511481  0.9308629463071654  0.2132714012315517 T T T

0.8427765965859209  0.3038973211591625  0.3377630114508676 F F F

0.2561589180176398  0.8946970700514285  0.3699752688536933 F F F

0.7002905011314198  0.7427638770164577  0.3694333434145349 F F F

0.1446377716052609  0.6198209409301043  0.1806618448251385 T T T

0.1670680492228911  0.3189213275614691  0.4642219245465711 F F F

0.1670009493768347  0.8187807201995412  0.4642780423296244 F F F

0.6671681999787467  0.3189356922165345  0.4642248749662699 F F F

0.6670762301852307  0.8188934922985496  0.4642311632739577 F F F

0.0005262775623152  0.9858555794029158  0.4642716944084242 F F F

0.0003123060285688  0.4852809012756580  0.4642592966726085 F F F

0.5005792975451939  0.9857760666806924  0.4642573594873483 F F F

0.5001865030324737  0.4852851332266610  0.4642634391672829 F F F

0.2381887286982263  0.6009407639864719  0.1338986605367722 F F F

Total Energy = -155.23095968 eV, Zero Point Energy corrections (ZPE-TS) = 0.996686 eV

N doped graphene-Al doped hematite

Initial state

N doped graphene-Al doped hematite_initial

1.00000000000000

5.0082168578999999   0.0000000000000000   0.0000000000000000

-2.5041084290000000   4.3372430266000004   0.0000000000000000

0.0000000000000000   0.0000000000000000  25.6149997710999990

O    Fe   Al   H    C    N    Cl

6  1  1  6  7  1  1

Selective dynamics

Direct

0.7096740007477393  0.6722376346260717  0.3348284959844747 F F F

0.3349877000104868  0.9712975026217094  0.3352395892147726 F F F

0.0388377682309837  0.3024848699862801  0.3367067873539824 F F F

0.7073278189981735  0.9765740825694920  0.2524329349932728 T T T

0.3313569726172716  0.3021284877615713  0.2518458629327540 T T T

0.0327571432580953  0.6772503922999604  0.2525108010490129 T T T

0.3563283681235774  0.6467082501020940  0.2919144928291715 F F F

0.0277732369451940  0.9868783355576412  0.2940264940192350 F F F

0.5285844809172033  0.3064633523496809  0.2476052316180457 T T T

0.7084803641457142  0.9445039666510624  0.2149170393014685 T T T

0.8459047079173203  0.3081153333590336  0.3385156691191185 F F F

0.2626474499679077  0.8964462279735130  0.3702954053781227 F F F

0.6898117064386611  0.7357380389868311  0.3697252571395708 F F F

0.0691401846898785  0.6891663300056621  0.2145986596739249 T T T

0.1682040243560721  0.3207190930895223  0.4637687504257926 F F F

0.1684052199633399  0.8195980788253507  0.4636114537622760 F F F

0.6680758595921148  0.3200135529615551  0.4637352824184688 F F F

0.6672440171198630  0.8197933436502183  0.4635404944409274 F F F

0.0002315420636521  0.4863514901201142  0.4637986719564111 F F F

0.5020951628419752  0.9884826540054020  0.4637158215164803 F F F

0.5017335414238246  0.4863771497382956  0.4637599289539196 F F F

0.0017128302817895  0.9880449176396198  0.4638328254214841 F F F

0.2381887436736179  0.6009407639864719  0.1362062543500926 F F F

Total Energy = -153.36673802 eV, Zero Point Energy corrections (ZPE-TS) = 1.039799 eV

Transition state

N doped graphene-Al doped hematite_transition state

1.00000000000000

5.0082168578999999    0.0000000000000000    0.0000000000000000

-2.5041084290000000    4.3372430266000004    0.0000000000000000

0.0000000000000000    0.0000000000000000   25.6149997710999990

O    Fe   Al   H    C    N    Cl

6     1     1     6     7     1     1

Selective dynamics

Direct

0.7096740007477393  0.6722376346260717  0.3348284959844747   F   F   F

0.3349877000104868  0.9712975026217093  0.3352395892147726   F   F   F

0.0388377682309837  0.3024848699862801  0.3367067873539824   F   F   F

0.7198609591060723  0.9604014950966341  0.2516235431740941   T   T   T

0.3341800372575817  0.2998382378698894  0.2536049396977271   T   T   T

0.0959146655135297  0.6888390013973669  0.2464966672816292   T   T   T

0.3563283681235774  0.6467082501020940  0.2919144928291715   F   F   F

0.0277732369451940  0.9868783355576412  0.2940264940192350   F   F   F

0.5278762498443914  0.3043018702675047  0.2460766276226012   T   T   T

0.7186266431187829  0.9356865681685022  0.2137923258407604   T   T   T

0.8459047079173203  0.3081153333590336  0.3385156691191185   F   F   F

0.2626474499679077  0.8964462279735130  0.3702954053781227   F   F   F

0.6898117064386611  0.7357380389868310  0.3697252571395708   F   F   F

0.1630777013302588  0.6443565210815969  0.1919541065671002   T   T   T

0.1682040243560721  0.3207190930895222  0.4637687504257926   F   F   F

0.1684052199633399  0.8195980788253507  0.4636114537622760   F   F   F

0.6680758595921148  0.3200135529615550  0.4637352824184688   F   F   F

0.6672440171198630  0.8197933436502183  0.4635404944409274   F   F   F

0.0002315420636521  0.4863514901201142  0.4637986719564111   F   F   F

0.5020951628419751  0.9884826540054020  0.4637158215164803   F   F   F

0.5017335414238246  0.4863771497382955  0.4637599289539196   F   F   F

0.0017128302817895  0.9880449176396197  0.4638328254214841   F   F   F

0.2381887436736179  0.6009407639864719  0.1362062543500926   F   F   F

Total Energy = -152.71868125 eV, Zero Point Energy corrections (ZPE-TS) = 0.84874 eV

Final state

N doped graphene-Al doped hematite_final

1.00000000000000

5.0082168578999999   0.0000000000000000   0.0000000000000000

-2.5041084290000000   4.3372430266000004   0.0000000000000000

0.0000000000000000   0.0000000000000000  25.6149997710999990

O    Fe   Al   H    C    N    Cl

6  1  1  6  7  1  1

Selective dynamics

Direct

0.7096740007477393  0.6722376346260717  0.3348284959844747 F F F

0.3349877000104868  0.9712975026217094  0.3352395892147726 F F F

0.0388377682309837  0.3024848699862801  0.3367067873539824 F F F

0.7153531257359234  0.9567676255602606  0.2513908935478852 T T T

0.3324023977857706  0.2995680679981305  0.2531301799350629 T T T

0.0780069423375593  0.6799608066486371  0.2553017689150323 T T T

0.3563283681235774  0.6467082501020940  0.2919144928291715 F F F

0.0277732369451940  0.9868783355576412  0.2940264940192350 F F F

0.5270695204751163  0.3033522476274442  0.2470893274298547 T T T

0.7116769477405001  0.9314853766485882  0.2136105171874618 T T T

0.8459047079173203  0.3081153333590336  0.3385156691191185 F F F

0.2626474499679077  0.8964462279735130  0.3702954053781227 F F F

0.6898117064386611  0.7357380389868311  0.3697252571395708 F F F

0.1434302170319484  0.6244474475956920  0.1826612510168815 T T T

0.1682040243560721  0.3207190930895223  0.4637687504257926 F F F

0.1684052199633399  0.8195980788253507  0.4636114537622760 F F F

0.6680758595921148  0.3200135529615551  0.4637352824184688 F F F

0.6672440171198630  0.8197933436502183  0.4635404944409274 F F F

0.0002315420636521  0.4863514901201142  0.4637986719564111 F F F

0.5020951628419752  0.9884826540054020  0.4637158215164803 F F F

0.5017335414238246  0.4863771497382956  0.4637599289539196 F F F

0.0017128302817895  0.9880449176396198  0.4638328254214841 F F F

0.2381887436736179  0.6009407639864719  0.1362062543500926 F F F

Total Energy = -153.08153799 eV, Zero Point Energy corrections (ZPE-TS) = 0.967994 eV

References:

[S1] Labanya Bhattacharya, Avi Cohen, Maytal Caspary Toroker, Theoretical understanding of graphene supported hematite photoanode for solar-driven water splitting applications, Catal Today 442 (2024) 114912. https://doi.org/10.1016/j.cattod.2024.114912.

[S2] N. Snir, M. Caspary Toroker, Kinetic Properties of Oxygen Evolution Reaction Catalysis in Hematite, Adv Theory Simul 6 (2023). https://doi.org/10.1002/adts.202300182.