SUPPORTING INFORMATION

Improving hydrodeoxygenation over Ni-Mo/Al2O3 by tuning the textural properties of the support via doping with lanthanoid group metals

Tove A. Kristensena,b,*, Jon Selimia,b, Jonas Elmroth Nordlandera, Omar Y. Abdelazizc,d, Christian P. Hulteberga,b, Sara Blomberga

aDivision of Chemical Engineering, Department of Process and Life Science Engineering, Lund University, SE-221 00 Lund, Sweden

bHulteberg Chemistry & Engineering AB, SE-212 25 Malmö, Sweden
cDepartment of Chemical Engineering, King Fahd University of Petroleum & Minerals, Dhahran 31261, Saudi Arabia

dInterdisciplinary Research Center for Refining & Advanced Chemicals, King Fahd University of Petroleum & Minerals, Dhahran 31261, Saudi Arabia

*E-mail: tove.kristensen@ple.lth.se

Number of pages: 3

Number of tables: 5

Number of figures: 1

Table S1. Experimental design matrix defining the amounts of La and Ce used for the preparation of the different supports, using impregnation method A-C, respectively.

| Sample # | La [wt%] | Ce [wt%] |
| --- | --- | --- |
| 1 | 5 | 5 |
| 2 | 2.5 | 5 |
| 3 | 2.5 | 0 |
| 4 | 0 | 0 |
| 5 | 2.5 | 2.5 |
| 6 | 0 | 2.5 |
| 7 | 5 | 0 |
| 8 | 5 | 2.5 |
| 9 | 2.5 | 2.5 |
| 10 | 0 | 5 |
| 11 | 2.5 | 2.5 |

Table S2. Regression models and fit statistics for the pore diameter (PD) and surface area (SA) generated for impregnation approach A.

| Property | Regression Model | Fit Statistics | Significant Term |
| --- | --- | --- | --- |
| Pore Diameter | PD=29.90-0.065A+1.35B-1.34A2 | Significant | B |
| Surface Area | SA=66.91-4.82A-1.82B | Significant | A |

Table S3. Regression models and fit statistics for the pore diameter (PD) and surface area (SA) generated for impregnation approach B.

| Property | Regression Model | Fit Statistics | Significant Term |
| --- | --- | --- | --- |
| Pore Diameter | PD=27.72-0.6983A+1.19B | Significant | A and B |
| Surface Area | SA=73-0.22A+0.28B-2.61AB-0.9B2-3AB2 | Significant | AB |

Table S4. Regression models and fit statistics for the pore diameter (PD) and surface area (SA) generated for impregnation approach C.

| Property | Regression Model | Fit Statistics | Significant Term |
| --- | --- | --- | --- |
| Pore Diameter | PD=31.83-0.0317A+1.72B | Significant | B |
| Surface Area | SA=59.61-3.06A-2.80B | Significant | A and B |

Table S5. Distribution of the carbon in the outgoing liquid and gas streams.

| Catalyst | Liquid [wt%] | Gas [wt%] |
| --- | --- | --- |
| NiMo/Aref.1_1 | 99.97 | 0.025 |
| NiMo/Aopt.5_0.9 | 99.98 | 0.018 |
| NiMo/Bref.5_3.3 | 99.98 | 0.016 |
| NiMo/Bopt.5_0 | 99.98 | 0.023 |
| NiMo/Cref.1_1 | 99.97 | 0.027 |
| NiMo/Copt.5_0 | 99.98 | 0.022 |
| NiMo/AAl2O3 | 99.98 | 0.022 |

Fig. S1 Measured adsorbed amount of NH3 per surface area determined for each catalyst, respectively