Supplementary material

Preparation of stacked 2D Fe3C/FeN-X carbon nanosheets and their catalytic performances for oxygen reduction reaction in microbial fuel cell

Decheng Lu1, 2, Hua Song1, Liuqingqing Yang2, *, Chunlei Zhang2

1College of Chemistry & Chemical Engineering, Northeast Petroleum University, Daqing, Heilongjiang, China.

2College of Chemistry and Materials Science, Shanghai Normal University, Shanghai, China.

* Corresponding Author

E-mail：monicaylqq@shnu.edu.cn (Dr. Liuqingqing Yang)

Table S1 Porosity property parameters of Fe3C/FeN-X-CNS

| Samples | SBET (m2.g-1) | Vp (cm3.g-1) | Dp (nm) |
| --- | --- | --- | --- |
| Fe3C@ZIF | 8.12 | 0.0025 | 0.57 |
| Fe3C/FeN-1-CNS | 8.09 | 0.0029 | 0.29 |
| Fe3C/FeN-2-CNS | 5.94 | 0.0022 | 0.15 |
| Fe3C/FeN-5-CNS | 4.47 | 0.0013 | 0.21 |
| Fe3C/FeN-10-CNS | 11.06 | 0.0043 | 0.71 |

Table S2 Percentage contents (at. %) of various chemical states of N in Fe3C/FeN-X-CNS

| Sample | Pyridinic N (at. %) | Pyrrole N (at. %) | Graphitic N (at. %) | Oxidized N (at. %) | FeN (at. %) |
| --- | --- | --- | --- | --- | --- |
| Fe3C/FeN-1-CNS | 398.3 eV (31.56) | 400.5 eV (24.16) | 401.6 eV (18.38) | 403.4 eV (7.38) | 399.4 eV (6.45) |
| Fe3C/FeN-2-CNS | 398.3 eV (38.73) | 400.5 eV (22.41) | 401.6 eV (18.37) | 403.4 eV (9.46) | 399.4 eV (8.36) |
| Fe3C/FeN-5-CNS | 398.3 eV (39.42) | 400.5 eV (20.44) | 401.6 eV (16.12) | 403.4 eV (11.61) | 399.4 eV (12.41) |
| Fe3C/FeN-10-CNS | 398.3 eV (39.06) | 400.5 eV (19.88) | 401.6 eV (16.45) | 403.4 eV (12.44) | 399.4 eV (12.17) |

Table S3 Percentage contents (at. %) of various chemical states of Fe in Fe3C/FeN-X-CNS

| Sample | Fe2+ 2p3/2 (at. %) | Fe3+ 2p3/2 (at. %) | Fe2+ 2p1/2 (at. %) | Fe3+ 2p1/2 (at. %) | Fe satellite (at. %) |
| --- | --- | --- | --- | --- | --- |
| Fe3C/FeN-1-CNS | 710.3 eV (39.87) | 712.5 eV (21.18) | 723.6 eV (7.32) | 725.3 eV (4.36) | 719.8 eV (27.27) |
| Fe3C/FeN-2-CNS | 710.3 eV (35.46) | 712.5 eV (22.29) | 723.6 eV (9.17) | 725.3 eV (7.47) | 719.8 eV (25.61) |
| Fe3C/FeN-5-CNS | 710.3 eV (30.45) | 712.5 eV (25.93) | 723.6 eV (13.49) | 725.3 eV (9.01) | 719.8 eV (21.12) |
| Fe3C/FeN-10-CNS | 710.3 eV (29.37) | 712.5 eV (25.56) | 723.6 eV (14.71) | 725.3 eV (9.19) | 719.8 eV (21.17) |