Supplementary Material

for

Volumetric and ultrasonic studies of molecular interactions in binary mixtures of N,N-dimethylacetamide with some polyethylene glycols at temperatures from 293.15 to 323.15 K

Nidhi and Anil Kumar Nain*

(a)

(b)

(c)

(d)

(e)

Fig. S1. Comparison of densities,  obtained in this work with the corresponding values available in the literature as function of temperature, T of pure (a) PEG 200, (b) PEG 300, (c) PEG 400, (d) PEG 600 and (e) DMA.

(a)

(b)

(c)

(d)

Fig. S2. Comparison of speed of sound, u obtained in this work with the corresponding values available in the literature as function of temperature, T of pure (a) PEG 200, (b) PEG 400, (c) PEG 600 and (d) DMA.

Table S1. Volume fractions, 1, of DMA in DMA + PEG 200/ PEG 300/ PEG 400/ PEG 600 binary mixture at temperatures, T/K = (293.15 − 323.15)

| x1 | T/K |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | 293.15 | 298.15 | 303.15 | 308.15 | 313.15 | 318.15 | 323.15 |

DMA + PEG 200

| 0.0000 | 0.0000 | 0.0000 | 0.0000 | 0.0000 | 0.0000 | 0.0000 | 0.0000 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.0584 | 0.0325 | 0.0326 | 0.0326 | 0.0327 | 0.0327 | 0.0327 | 0.0328 |
| 0.1152 | 0.0660 | 0.0660 | 0.0661 | 0.0662 | 0.0663 | 0.0663 | 0.0664 |
| 0.2003 | 0.1196 | 0.1197 | 0.1199 | 0.1200 | 0.1201 | 0.1203 | 0.1204 |
| 0.2790 | 0.1735 | 0.1737 | 0.1738 | 0.1740 | 0.1742 | 0.1744 | 0.1746 |
| 0.3756 | 0.2460 | 0.2462 | 0.2465 | 0.2467 | 0.2469 | 0.2472 | 0.2474 |
| 0.4655 | 0.3208 | 0.3211 | 0.3214 | 0.3216 | 0.3219 | 0.3222 | 0.3225 |
| 0.5320 | 0.3814 | 0.3817 | 0.3820 | 0.3823 | 0.3826 | 0.3829 | 0.3832 |
| 0.6027 | 0.4514 | 0.4517 | 0.4520 | 0.4523 | 0.4526 | 0.4530 | 0.4533 |
| 0.6652 | 0.5187 | 0.5190 | 0.5193 | 0.5196 | 0.5199 | 0.5203 | 0.5206 |
| 0.7327 | 0.5979 | 0.5982 | 0.5985 | 0.5988 | 0.5991 | 0.5994 | 0.5997 |
| 0.8046 | 0.6907 | 0.6910 | 0.6913 | 0.6915 | 0.6918 | 0.6921 | 0.6924 |
| 0.8708 | 0.7852 | 0.7854 | 0.7856 | 0.7858 | 0.7860 | 0.7863 | 0.7865 |
| 0.9294 | 0.8772 | 0.8773 | 0.8774 | 0.8776 | 0.8777 | 0.8778 | 0.8780 |
| 1.0000 | 1.0000 | 1.0000 | 1.0000 | 1.0000 | 1.0000 | 1.0000 | 1.0000 |

DMA + PEG 300

| 0.0000 | 0.0000 | 0.0000 | 0.0000 | 0.0000 | 0.0000 | 0.0000 | 0.0000 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.0712 | 0.0277 | 0.0277 | 0.0278 | 0.0278 | 0.0278 | 0.0279 | 0.0279 |
| 0.1422 | 0.0581 | 0.0581 | 0.0582 | 0.0583 | 0.0583 | 0.0584 | 0.0584 |
| 0.2123 | 0.0911 | 0.0912 | 0.0913 | 0.0914 | 0.0915 | 0.0916 | 0.0917 |
| 0.2813 | 0.1270 | 0.1272 | 0.1273 | 0.1274 | 0.1276 | 0.1277 | 0.1278 |
| 0.3584 | 0.1720 | 0.1721 | 0.1723 | 0.1725 | 0.1726 | 0.1728 | 0.1730 |
| 0.4216 | 0.2132 | 0.2134 | 0.2136 | 0.2138 | 0.2140 | 0.2142 | 0.2144 |
| 0.4970 | 0.2687 | 0.2689 | 0.2691 | 0.2694 | 0.2696 | 0.2698 | 0.2700 |
| 0.5616 | 0.3226 | 0.3229 | 0.3232 | 0.3234 | 0.3237 | 0.3239 | 0.3242 |
| 0.6525 | 0.4111 | 0.4114 | 0.4117 | 0.4120 | 0.4123 | 0.4125 | 0.4128 |
| 0.7472 | 0.5236 | 0.5239 | 0.5242 | 0.5245 | 0.5247 | 0.5250 | 0.5253 |
| 0.8004 | 0.5986 | 0.5988 | 0.5991 | 0.5994 | 0.5997 | 0.6000 | 0.6002 |
| 0.8667 | 0.7074 | 0.7076 | 0.7079 | 0.7081 | 0.7084 | 0.7086 | 0.7088 |
| 0.9311 | 0.8340 | 0.8342 | 0.8343 | 0.8345 | 0.8347 | 0.8348 | 0.8350 |
| 1.0000 | 1.0000 | 1.0000 | 1.0000 | 1.0000 | 1.0000 | 1.0000 | 1.0000 |

Table S1. Contd.

| x1 | T/K |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | 293.15 | 298.15 | 303.15 | 308.15 | 313.15 | 318.15 | 323.15 |

DMA + PEG 400

| 0.0000 | 0.0000 | 0.0000 | 0.0000 | 0.0000 | 0.0000 | 0.0000 | 0.0000 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.0732 | 0.0222 | 0.0222 | 0.0223 | 0.0223 | 0.0223 | 0.0223 | 0.0224 |
| 0.1472 | 0.0473 | 0.0473 | 0.0474 | 0.0474 | 0.0475 | 0.0476 | 0.0476 |
| 0.2055 | 0.0692 | 0.0693 | 0.0694 | 0.0694 | 0.0695 | 0.0696 | 0.0697 |
| 0.2649 | 0.0939 | 0.0940 | 0.0941 | 0.0942 | 0.0943 | 0.0944 | 0.0945 |
| 0.3485 | 0.1333 | 0.1334 | 0.1336 | 0.1337 | 0.1339 | 0.1340 | 0.1341 |
| 0.4253 | 0.1754 | 0.1756 | 0.1758 | 0.1760 | 0.1761 | 0.1763 | 0.1765 |
| 0.4985 | 0.2223 | 0.2225 | 0.2227 | 0.2229 | 0.2231 | 0.2233 | 0.2235 |
| 0.5833 | 0.2870 | 0.2872 | 0.2874 | 0.2877 | 0.2880 | 0.2882 | 0.2885 |
| 0.6520 | 0.3501 | 0.3504 | 0.3506 | 0.3509 | 0.3512 | 0.3515 | 0.3517 |
| 0.7287 | 0.4357 | 0.4360 | 0.4363 | 0.4366 | 0.4369 | 0.4372 | 0.4375 |
| 0.7974 | 0.5309 | 0.5312 | 0.5315 | 0.5318 | 0.5321 | 0.5324 | 0.5327 |
| 0.8693 | 0.6566 | 0.6569 | 0.6572 | 0.6574 | 0.6577 | 0.6580 | 0.6583 |
| 0.9322 | 0.7981 | 0.7983 | 0.7985 | 0.7987 | 0.7989 | 0.7991 | 0.7993 |
| 1.0000 | 1.0000 | 1.0000 | 1.0000 | 1.0000 | 1.0000 | 1.0000 | 1.0000 |

DMA + PEG 600

| 0.0000 | 0.0000 | 0.0000 | 0.0000 | 0.0000 | 0.0000 | 0.0000 | 0.0000 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.0718 | 0.0145 | 0.0145 | 0.0146 | 0.0146 | 0.0146 | 0.0146 | 0.0146 |
| 0.1430 | 0.0308 | 0.0308 | 0.0309 | 0.0309 | 0.0310 | 0.0310 | 0.0310 |
| 0.2128 | 0.0490 | 0.0490 | 0.0491 | 0.0491 | 0.0492 | 0.0493 | 0.0493 |
| 0.2912 | 0.0726 | 0.0727 | 0.0728 | 0.0728 | 0.0729 | 0.0730 | 0.0731 |
| 0.3702 | 0.1007 | 0.1008 | 0.1009 | 0.1010 | 0.1012 | 0.1013 | 0.1014 |
| 0.4450 | 0.1325 | 0.1326 | 0.1328 | 0.1329 | 0.1331 | 0.1332 | 0.1334 |
| 0.5072 | 0.1639 | 0.1641 | 0.1643 | 0.1644 | 0.1646 | 0.1648 | 0.1650 |
| 0.5785 | 0.2073 | 0.2075 | 0.2077 | 0.2079 | 0.2081 | 0.2083 | 0.2085 |
| 0.6511 | 0.2623 | 0.2625 | 0.2628 | 0.2630 | 0.2632 | 0.2635 | 0.2637 |
| 0.7207 | 0.3296 | 0.3298 | 0.3301 | 0.3304 | 0.3307 | 0.3310 | 0.3312 |
| 0.7998 | 0.4322 | 0.4325 | 0.4328 | 0.4331 | 0.4334 | 0.4337 | 0.4340 |
| 0.8701 | 0.5606 | 0.5609 | 0.5613 | 0.5616 | 0.5619 | 0.5622 | 0.5625 |
| 0.9385 | 0.7441 | 0.7443 | 0.7445 | 0.7448 | 0.7450 | 0.7452 | 0.7455 |
| 1.0000 | 1.0000 | 1.0000 | 1.0000 | 1.0000 | 1.0000 | 1.0000 | 1.0000 |

Table S2. Coefficients, Ai of equation (19) of  VmE, sE, LfE, uE, Ks,mE and ZE along with standard deviations,  for DMA + PEG 200/PEG 300/PEG 400/PEG 600 binary mixture at temperatures, T/K = (293.15 − 323.15)

| T/K | Ao | A1 | A2 | A3 | A4 |  |
| --- | --- | --- | --- | --- | --- | --- |

DMA + PEG 200

106VmE/m3 mol−1

| 293.15 | -3.3965 | 1.6021 | -0.6096 | 0.2691 |  | 0.0027 |
| --- | --- | --- | --- | --- | --- | --- |
| 298.15 | -3.5477 | 1.6261 | -0.6923 | 0.3042 |  | 0.0038 |
| 303.15 | -3.7029 | 1.6511 | -0.7754 | 0.3052 |  | 0.0052 |
| 308.15 | -3.8476 | 1.6922 | -0.8826 | 0.3052 |  | 0.0065 |
| 313.15 | -3.9874 | 1.7449 | -1.0007 | 0.2746 |  | 0.0067 |
| 318.15 | -4.1341 | 1.7837 | -1.0937 | 0.2744 |  | 0.0073 |
| 323.15 | -4.2768 | 1.8143 | -1.2154 | 0.2901 |  | 0.0077 |

1010sE/m2 N−1

| 293.15 | -0.7671 | 0.0822 | 0.0341 | -0.0425 |  | 0.00039 |
| --- | --- | --- | --- | --- | --- | --- |
| 298.15 | -0.8248 | 0.0760 | 0.0207 | -0.0337 |  | 0.00030 |
| 303.15 | -0.8867 | 0.0708 | 0.0095 | -0.0311 |  | 0.00048 |
| 308.15 | -0.9483 | 0.0696 | -0.0067 | -0.0298 |  | 0.00041 |
| 313.15 | -1.0134 | 0.0685 | -0.0505 | -0.0295 | 0.0511 | 0.00036 |
| 318.15 | -1.0795 | 0.0616 | -0.0914 | -0.0188 | 0.0805 | 0.00034 |
| 323.15 | -1.1515 | 0.0719 | -0.1327 | -0.0288 | 0.0883 | 0.00053 |

1011LfE/m

| 293.15 | -0.5876 | 0.2321 | -0.0972 | 0.0016 | 0.0390 | 0.00008 |
| --- | --- | --- | --- | --- | --- | --- |
| 298.15 | -0.6326 | 0.2431 | -0.0950 | 0.0096 | 0.0213 | 0.00012 |
| 303.15 | -0.6799 | 0.2556 | -0.0992 | 0.0153 | 0.0149 | 0.00024 |
| 308.15 | -0.7271 | 0.2658 | -0.1079 | 0.0260 | 0.0128 | 0.00020 |
| 313.15 | -0.7764 | 0.2751 | -0.1088 | 0.0412 |  | 0.00020 |
| 318.15 | -0.8264 | 0.2808 | -0.1174 | 0.0591 |  | 0.00023 |
| 323.15 | -0.8791 | 0.2896 | -0.1369 | 0.0775 |  | 0.00026 |

10−2uE/m s−1

| 293.15 | 1.1546 | -0.5187 | 0.2201 | 0.0378 | -0.1391 | 0.00051 |
| --- | --- | --- | --- | --- | --- | --- |
| 298.15 | 1.2126 | -0.5048 | 0.1831 | 0.0263 | -0.0745 | 0.00042 |
| 303.15 | 1.2714 | -0.4897 | 0.1713 | 0.0139 | -0.0590 | 0.00093 |
| 308.15 | 1.3231 | -0.4665 | 0.1760 | -0.0147 | -0.0604 | 0.00077 |
| 313.15 | 1.3797 | -0.4402 | 0.1526 | -0.0567 | -0.0274 | 0.00058 |
| 318.15 | 1.4339 | -0.4002 | 0.1369 | -0.1083 |  | 0.00044 |
| 323.15 | 1.4809 | -0.3680 | 0.1909 | -0.1478 | -0.0379 | 0.00064 |

1014Ks,mE/m5 N−1 mol−1

| 293.15 | -1.0155 | 0.4432 | -0.2116 | 0.0183 | 0.0881 | 0.00026 |
| --- | --- | --- | --- | --- | --- | --- |
| 298.15 | -1.1017 | 0.4584 | -0.2046 | 0.0336 | 0.0394 | 0.00042 |
| 303.15 | -1.1930 | 0.4751 | -0.2189 | 0.0470 | 0.0291 | 0.00068 |
| 308.15 | -1.2834 | 0.4895 | -0.2480 | 0.0748 | 0.0307 | 0.00063 |
| 313.15 | -1.3822 | 0.5056 | -0.2559 | 0.1095 |  | 0.00073 |
| 318.15 | -1.4842 | 0.5105 | -0.2846 | 0.1598 |  | 0.00080 |
| 323.15 | -1.5898 | 0.5258 | -0.3445 | 0.2069 |  | 0.00094 |

Table S2. Contd.

| T/K | Ao | A1 | A2 | A3 | A4 |  |
| --- | --- | --- | --- | --- | --- | --- |

10−5ZE/kg m−2 s−1

| 293.15 | 2.7241 | -0.8562 | 0.2917 | 0.0434 | -0.1803 | 0.0004 |
| --- | --- | --- | --- | --- | --- | --- |
| 298.15 | 2.7789 | -0.8353 | 0.2570 | 0.0248 | -0.1039 | 0.0007 |
| 303.15 | 2.8305 | -0.8122 | 0.2503 | 0.0115 | -0.0849 | 0.0010 |
| 308.15 | 2.8658 | -0.7805 | 0.2695 | -0.0186 | -0.0950 | 0.0009 |
| 313.15 | 2.8986 | -0.7448 | 0.2572 | -0.0586 | -0.0652 | 0.0011 |
| 318.15 | 2.9233 | -0.6921 | 0.2618 | -0.1118 | -0.0639 | 0.0012 |
| 323.15 | 2.9316 | -0.6449 | 0.3245 | -0.1517 | -0.1032 | 0.0012 |

DMA + PEG 300

106VmE /m3 mol−1

| 293.15 | -3.8957 | 1.7204 | -0.9322 | 0.0736 | 0.2263 | 0.0022 |
| --- | --- | --- | --- | --- | --- | --- |
| 298.15 | -4.0288 | 1.7596 | -1.1593 | 0.2156 | 0.1377 | 0.0023 |
| 303.15 | -4.1709 | 1.7475 | -1.3330 | 0.4446 |  | 0.0029 |
| 308.15 | -4.3190 | 1.7000 | -1.5656 | 0.7399 |  | 0.0039 |
| 313.15 | -4.4777 | 1.7028 | -1.6514 | 0.9219 | -0.2930 | 0.0038 |
| 318.15 | -4.6574 | 1.6511 | -1.6876 | 1.2144 | -0.6954 | 0.0030 |
| 323.15 | -4.8329 | 1.6512 | -1.8089 | 1.4641 | -1.0589 | 0.0024 |

1010sE/m2 N−1

| 293.15 | -0.9716 | 0.0055 | -0.0016 | -0.0142 | -0.0727 | 0.00043 |
| --- | --- | --- | --- | --- | --- | --- |
| 298.15 | -1.0234 | 0.0081 | -0.0309 | -0.0345 | -0.0607 | 0.00051 |
| 303.15 | -1.0736 | 0.0046 | -0.0718 | -0.0575 | -0.0393 | 0.00036 |
| 308.15 | -1.1236 | -0.0152 | -0.1339 | -0.0457 |  | 0.00085 |
| 313.15 | -1.1813 | -0.0292 | -0.1641 | -0.0516 |  | 0.00066 |
| 318.15 | -1.2404 | -0.0486 | -0.1965 | -0.0347 | -0.0351 | 0.00055 |
| 323.15 | -1.3053 | -0.0555 | -0.2570 | -0.0596 |  | 0.00077 |

1011LfE/m

| 293.15 | -0.9053 | 0.4835 | -0.2551 | 0.1500 | -0.0825 | 0.00032 |
| --- | --- | --- | --- | --- | --- | --- |
| 298.15 | -0.9529 | 0.5001 | -0.2670 | 0.1706 | -0.0975 | 0.00031 |
| 303.15 | -1.0047 | 0.5146 | -0.2748 | 0.1878 | -0.1136 | 0.00019 |
| 308.15 | -1.0572 | 0.5273 | -0.2576 | 0.2068 | -0.1639 | 0.00044 |
| 313.15 | -1.1120 | 0.5435 | -0.2643 | 0.2223 | -0.1777 | 0.00040 |
| 318.15 | -1.1696 | 0.5557 | -0.2685 | 0.2475 | -0.2020 | 0.00056 |
| 323.15 | -1.2353 | 0.5713 | -0.2748 | 0.2742 | -0.2261 | 0.00061 |

10−2 uE/m s−1

| 293.15 | 1.4359 | -0.9740 | 0.5525 | -0.3341 | 0.2046 | 0.00107 |
| --- | --- | --- | --- | --- | --- | --- |
| 298.15 | 1.4673 | -0.9503 | 0.5389 | -0.3555 | 0.2277 | 0.00105 |
| 303.15 | 1.5007 | -0.9141 | 0.5107 | -0.3694 | 0.2534 | 0.00054 |
| 308.15 | 1.5376 | -0.8775 | 0.3958 | -0.3768 | 0.3978 | 0.00132 |
| 313.15 | 1.5708 | -0.8480 | 0.3775 | -0.3779 | 0.3853 | 0.00112 |
| 318.15 | 1.6039 | -0.8045 | 0.3493 | -0.4026 | 0.4037 | 0.00133 |
| 323.15 | 1.6387 | -0.7629 | 0.3213 | -0.4202 | 0.4183 | 0.00138 |

Table S2. Contd.

| T/K | Ao | A1 | A2 | A3 | A4 |  |
| --- | --- | --- | --- | --- | --- | --- |

1014Ks,mE/m5 N−1 mol−1

| 293.15 | -1.4562 | 0.6391 | -0.3612 | 0.1812 | -0.1039 | 0.00084 |
| --- | --- | --- | --- | --- | --- | --- |
| 298.15 | -1.5498 | 0.6477 | -0.3896 | 0.2265 | -0.1455 | 0.00077 |
| 303.15 | -1.6487 | 0.6423 | -0.4126 | 0.2789 | -0.1859 | 0.00044 |
| 308.15 | -1.7610 | 0.6349 | -0.3637 | 0.3295 | -0.3245 | 0.00109 |
| 313.15 | -1.8758 | 0.6332 | -0.3805 | 0.3775 | -0.3658 | 0.00082 |
| 318.15 | -1.9984 | 0.6143 | -0.3933 | 0.4583 | -0.4321 | 0.00102 |
| 323.15 | -2.1321 | 0.6020 | -0.4101 | 0.5382 | -0.5108 | 0.00129 |

10−5ZE/kg m−2 s−1

| 293.15 | 4.5661 | -2.0787 | 0.9324 | -0.3469 | 0.1127 | 0.0011 |
| --- | --- | --- | --- | --- | --- | --- |
| 298.15 | 4.5884 | -2.0442 | 0.9340 | -0.3950 | 0.1571 | 0.0011 |
| 303.15 | 4.6165 | -1.9906 | 0.9186 | -0.4429 | 0.2015 | 0.0006 |
| 308.15 | 4.6389 | -1.9338 | 0.8154 | -0.4869 | 0.3595 | 0.0015 |
| 313.15 | 4.6596 | -1.8870 | 0.7916 | -0.5156 | 0.3943 | 0.0010 |
| 318.15 | 4.6809 | -1.8206 | 0.7571 | -0.5784 | 0.4596 | 0.0012 |
| 323.15 | 4.7058 | -1.7606 | 0.7307 | -0.6303 | 0.5178 | 0.0015 |

DMA + PEG 400

106VmE /m3 mol−1

| 293.15 | -4.9104 | 2.2625 | -1.4286 | 0.3890 |  | 0.0037 |
| --- | --- | --- | --- | --- | --- | --- |
| 298.15 | -5.0615 | 2.2894 | -1.6752 | 0.5745 | -0.2328 | 0.0023 |
| 303.15 | -5.2260 | 2.2727 | -1.8236 | 0.9235 | -0.6356 | 0.0056 |
| 308.15 | -5.3959 | 2.2329 | -1.9510 | 1.4144 | -1.1116 | 0.0073 |
| 313.15 | -5.5542 | 2.2020 | -2.0461 | 1.9409 | -1.7333 | 0.0083 |
| 318.15 | -5.7223 | 2.1311 | -2.0211 | 2.4550 | -2.5665 | 0.0066 |
| 323.15 | -5.9106 | 2.0889 | -1.9844 | 2.8720 | -3.3500 | 0.0075 |

1010sE/m2 N−1

| 293.15 | -1.1751 | -0.3778 | -0.0763 | -0.0072 | -0.0697 | 0.00046 |
| --- | --- | --- | --- | --- | --- | --- |
| 298.15 | -1.2183 | -0.4171 | -0.1443 | -0.0069 | -0.0564 | 0.00068 |
| 303.15 | -1.2601 | -0.4560 | -0.2096 | -0.0256 | -0.0511 | 0.00077 |
| 308.15 | -1.3023 | -0.4904 | -0.3644 | -0.0768 | 0.1328 | 0.00064 |
| 313.15 | -1.3640 | -0.5331 | -0.3776 | -0.0742 |  | 0.00072 |
| 318.15 | -1.4182 | -0.5684 | -0.4556 | -0.0963 |  | 0.00058 |
| 323.15 | -1.4696 | -0.6009 | -0.5777 | -0.1518 | 0.0512 | 0.00081 |

1011LfE/m

| 293.15 | -1.1677 | 0.6957 | -0.3555 | 0.1704 | -0.0774 | 0.00019 |
| --- | --- | --- | --- | --- | --- | --- |
| 298.15 | -1.2345 | 0.7143 | -0.3404 | 0.1827 | -0.1182 | 0.00037 |
| 303.15 | -1.3032 | 0.7278 | -0.3333 | 0.1980 | -0.1416 | 0.00054 |
| 308.15 | -1.3790 | 0.7386 | -0.3029 | 0.2378 | -0.1865 | 0.00071 |
| 313.15 | -1.4526 | 0.7580 | -0.3041 | 0.2419 | -0.2256 | 0.00081 |
| 318.15 | -1.5292 | 0.7716 | -0.2937 | 0.2684 | -0.2683 | 0.00090 |
| 323.15 | -1.6138 | 0.7746 | -0.2759 | 0.3163 | -0.3131 | 0.00097 |

Table S2. Contd.

| T/K | Ao | A1 | A2 | A3 | A4 |  |
| --- | --- | --- | --- | --- | --- | --- |

10−2uE/m s−1

| 293.15 | 1.9334 | -1.3134 | 0.5480 | -0.1029 | 0.0401 | 0.0008 |
| --- | --- | --- | --- | --- | --- | --- |
| 298.15 | 1.9855 | -1.2507 | 0.4024 | -0.0919 | 0.1621 | 0.0012 |
| 303.15 | 2.0318 | -1.1707 | 0.3053 | -0.0844 | 0.1937 | 0.0018 |
| 308.15 | 2.0912 | -1.0801 | 0.1227 | -0.1552 | 0.2828 | 0.0020 |
| 313.15 | 2.1450 | -1.0288 | 0.0716 | -0.0898 | 0.3484 | 0.0019 |
| 318.15 | 2.1911 | -0.9545 | -0.0075 | -0.1041 | 0.3941 | 0.0018 |
| 323.15 | 2.2380 | -0.8337 | -0.1117 | -0.1937 | 0.4433 | 0.0018 |

1014Ks,mE/m5 N−1 mol−1

| 293.15 | -2.2081 | 0.7140 | -0.2297 | 0.0315 | -0.0839 | 0.00069 |
| --- | --- | --- | --- | --- | --- | --- |
| 298.15 | -2.3484 | 0.6787 | -0.1720 | 0.0682 | -0.2005 | 0.00094 |
| 303.15 | -2.4921 | 0.6192 | -0.1451 | 0.1286 | -0.2698 | 0.00124 |
| 308.15 | -2.6560 | 0.5405 | -0.0338 | 0.3055 | -0.3703 | 0.00172 |
| 313.15 | -2.8287 | 0.4980 | -0.0175 | 0.2984 | -0.5579 | 0.00157 |
| 318.15 | -3.0009 | 0.4272 | 0.0323 | 0.4001 | -0.7145 | 0.00155 |
| 323.15 | -3.1911 | 0.3045 | 0.1034 | 0.5934 | -0.8639 | 0.00191 |

10−5ZE/kg m−2 s−1

| 293.15 | 6.0508 | -3.1902 | 1.3611 | -0.4149 | 0.1401 | 0.0009 |
| --- | --- | --- | --- | --- | --- | --- |
| 298.15 | 6.1101 | -3.1122 | 1.2347 | -0.4414 | 0.2820 | 0.0012 |
| 303.15 | 6.1626 | -3.0082 | 1.1347 | -0.4904 | 0.3753 | 0.0017 |
| 308.15 | 6.2297 | -2.8902 | 0.9395 | -0.6360 | 0.5358 | 0.0022 |
| 313.15 | 6.2741 | -2.8078 | 0.8744 | -0.6296 | 0.6939 | 0.0023 |
| 318.15 | 6.3135 | -2.6992 | 0.7706 | -0.7078 | 0.8370 | 0.0023 |
| 323.15 | 6.3554 | -2.5443 | 0.6393 | -0.8508 | 0.9733 | 0.0025 |

DMA + PEG 600

106VmE /m3 mol−1

| 293.15 | -6.6078 | 2.3582 | -0.8023 | 0.3148 |  | 0.0070 |
| --- | --- | --- | --- | --- | --- | --- |
| 298.15 | -6.8020 | 2.3490 | -1.0506 | 0.4840 |  | 0.0079 |
| 303.15 | -7.0101 | 2.3312 | -1.2605 | 0.6973 |  | 0.0083 |
| 308.15 | -7.2256 | 2.3223 | -1.5298 | 0.8584 |  | 0.0093 |
| 313.15 | -7.4453 | 2.3338 | -1.8286 | 0.9698 |  | 0.0108 |
| 318.15 | -7.6761 | 2.3400 | -2.0625 | 1.1357 |  | 0.0115 |
| 323.15 | -7.9443 | 2.3616 | -1.9828 | 1.2845 | -0.6200 | 0.0118 |

1010sE/m2 N−1

| 293.15 | -1.5758 | -0.7514 | -0.1384 | -0.0460 | 0.3542 | 0.00102 |
| --- | --- | --- | --- | --- | --- | --- |
| 298.15 | -1.6425 | -0.8361 | -0.1293 | 0.0815 | 0.1243 | 0.00074 |
| 303.15 | -1.7210 | -0.8688 | -0.1651 | -0.0521 | 0.2153 | 0.00103 |
| 308.15 | -1.8029 | -0.9508 | -0.1269 | 0.0397 |  | 0.00130 |
| 313.15 | -1.8805 | -1.0487 | -0.0978 | 0.1506 | -0.3020 | 0.00088 |
| 318.15 | -1.9609 | -1.0810 | -0.2296 | -0.0049 | -0.1364 | 0.00082 |
| 323.15 | -2.0509 | -1.1672 | -0.2800 | 0.0205 | -0.1934 | 0. 00124 |

Table S2. Contd.

| T/K | Ao | A1 | A2 | A3 | A4 |  |
| --- | --- | --- | --- | --- | --- | --- |

1011LfE/m

| 293.15 | -1.4710 | 1.2301 | -0.8928 | 0.5734 | -0.1983 | 0.00074 |
| --- | --- | --- | --- | --- | --- | --- |
| 298.15 | -1.5510 | 1.2792 | -0.9162 | 0.5823 | -0.2190 | 0.00053 |
| 303.15 | -1.6336 | 1.3358 | -0.9499 | 0.5925 | -0.2266 | 0.00076 |
| 308.15 | -1.7156 | 1.3896 | -0.9834 | 0.6042 | -0.2393 | 0.00085 |
| 313.15 | -1.8043 | 1.4251 | -1.0290 | 0.6474 | -0.2038 | 0.00045 |
| 318.15 | -1.9018 | 1.4805 | -1.0101 | 0.6614 | -0.2882 | 0.00034 |
| 323.15 | -2.0053 | 1.5469 | -1.0249 | 0.6694 | -0.3227 | 0.00050 |

10−2uE/m s−1

| 293.15 | 2.3463 | -2.7305 | 2.1012 | -0.5015 | -0.5860 | 0.0043 |
| --- | --- | --- | --- | --- | --- | --- |
| 298.15 | 2.4152 | -2.7226 | 2.0305 | -0.3947 | -0.5709 | 0.0039 |
| 303.15 | 2.4815 | -2.7382 | 1.9942 | -0.2930 | -0.6029 | 0.0043 |
| 308.15 | 2.5384 | -2.7382 | 1.9658 | -0.2094 | -0.6284 | 0.0052 |
| 313.15 | 2.6100 | -2.6596 | 1.9726 | -0.2523 | -0.8239 | 0.0056 |
| 318.15 | 2.6945 | -2.6509 | 1.7362 | -0.1670 | -0.5784 | 0.0051 |
| 323.15 | 2.7623 | -2.6543 | 1.6200 | -0.0623 | -0.5372 | 0.0052 |

1014Ks,mE/m5 N−1 mol−1

| 293.15 | -3.4628 | 1.8272 | -0.7782 | -0.1778 | 0.7134 | 0.00227 |
| --- | --- | --- | --- | --- | --- | --- |
| 298.15 | -3.6939 | 1.8457 | -0.7602 | -0.2482 | 0.6171 | 0.00196 |
| 303.15 | -3.9356 | 1.8917 | -0.7720 | -0.3086 | 0.5947 | 0.00188 |
| 308.15 | -4.1862 | 1.9290 | -0.7914 | -0.3685 | 0.5432 | 0.00306 |
| 313.15 | -4.4744 | 1.8319 | -0.9009 | -0.1822 | 0.7832 | 0.00335 |
| 318.15 | -4.7926 | 1.8560 | -0.6489 | -0.2439 | 0.3729 | 0.00373 |
| 323.15 | -5.1150 | 1.9021 | -0.5468 | -0.3046 | 0.2160 | 0.00409 |

10−5ZE/kg m−2 s−1

| 293.15 | 7.8689 | -6.1029 | 4.0155 | -1.7200 |  | 0.0024 |
| --- | --- | --- | --- | --- | --- | --- |
| 298.15 | 7.9397 | -6.0712 | 3.9546 | -1.6275 |  | 0.0019 |
| 303.15 | 8.0064 | -6.0647 | 3.8965 | -1.5342 |  | 0.0021 |
| 308.15 | 8.0505 | -6.0348 | 3.8505 | -1.4595 |  | 0.0029 |
| 313.15 | 8.1125 | -5.9188 | 3.7429 | -1.5198 |  | 0.0030 |
| 318.15 | 8.1782 | -5.8788 | 3.6272 | -1.4428 |  | 0.0027 |
| 323.15 | 8.2435 | -5.8557 | 3.3881 | -1.3397 | 0.2467 | 0.0028 |

Table S3. Partial molar volumes, 106Vm,1/(m3 mol−1) of DMA as a function of mole fraction, x1 of DMA in DMA + PEG 200/ PEG 300/ PEG 400/ PEG 600 binary mixture at temperatures, T/K = (293.15 − 323.15)

| x1 | T/K |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | 293.15 | 298.15 | 303.15 | 308.15 | 313.15 | 318.15 | 323.15 |

DMA + PEG 200

| 0.0000 | 90.427 | 90.643 | 90.877 | 91.130 | 91.398 | 91.654 | 91.900 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.0584 | 90.370 | 90.630 | 90.898 | 91.181 | 91.467 | 91.734 | 92.019 |
| 0.1152 | 90.326 | 90.617 | 90.914 | 91.220 | 91.532 | 91.816 | 92.131 |
| 0.2003 | 90.305 | 90.626 | 90.952 | 91.287 | 91.627 | 91.943 | 92.289 |
| 0.2790 | 90.346 | 90.685 | 91.030 | 91.382 | 91.744 | 92.085 | 92.447 |
| 0.3756 | 90.473 | 90.824 | 91.182 | 91.546 | 91.922 | 92.287 | 92.666 |
| 0.4655 | 90.660 | 91.017 | 91.381 | 91.751 | 92.129 | 92.507 | 92.895 |
| 0.5320 | 90.828 | 91.194 | 91.561 | 91.934 | 92.314 | 92.697 | 93.089 |
| 0.6027 | 91.024 | 91.397 | 91.772 | 92.152 | 92.536 | 92.925 | 93.323 |
| 0.6652 | 91.206 | 91.586 | 91.969 | 92.356 | 92.746 | 93.139 | 93.541 |
| 0.7327 | 91.406 | 91.796 | 92.187 | 92.583 | 92.981 | 93.380 | 93.789 |
| 0.8046 | 91.611 | 92.012 | 92.416 | 92.824 | 93.235 | 93.645 | 94.065 |
| 0.8708 | 91.798 | 92.212 | 92.630 | 93.053 | 93.479 | 93.904 | 94.337 |
| 0.9294 | 91.956 | 92.382 | 92.814 | 93.250 | 93.688 | 94.130 | 94.576 |
| 1.0000 | 92.140 | 92.581 | 93.026 | 93.475 | 93.928 | 94.386 | 94.849 |

DMA + PEG 300

| 0.0000 | 89.986 | 90.177 | 90.365 | 90.554 | 90.669 | 90.777 | 90.907 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.0712 | 89.858 | 90.115 | 90.375 | 90.633 | 90.858 | 91.070 | 91.295 |
| 0.1422 | 89.846 | 90.143 | 90.444 | 90.744 | 91.031 | 91.306 | 91.591 |
| 0.2123 | 89.906 | 90.229 | 90.559 | 90.886 | 91.212 | 91.524 | 91.846 |
| 0.2813 | 90.007 | 90.349 | 90.699 | 91.043 | 91.391 | 91.728 | 92.074 |
| 0.3584 | 90.157 | 90.514 | 90.877 | 91.238 | 91.600 | 91.956 | 92.319 |
| 0.4216 | 90.299 | 90.664 | 91.035 | 91.406 | 91.776 | 92.143 | 92.515 |
| 0.4970 | 90.490 | 90.863 | 91.240 | 91.618 | 91.995 | 92.373 | 92.754 |
| 0.5616 | 90.669 | 91.048 | 91.431 | 91.814 | 92.197 | 92.584 | 92.966 |
| 0.6525 | 90.944 | 91.329 | 91.717 | 92.107 | 92.497 | 92.893 | 93.283 |
| 0.7472 | 91.257 | 91.647 | 92.040 | 92.435 | 92.833 | 93.235 | 93.635 |
| 0.8004 | 91.444 | 91.838 | 92.235 | 92.635 | 93.037 | 93.443 | 93.850 |
| 0.8667 | 91.675 | 92.078 | 92.485 | 92.895 | 93.308 | 93.724 | 94.144 |
| 0.9311 | 91.907 | 92.324 | 92.746 | 93.170 | 93.599 | 94.031 | 94.467 |
| 1.0000 | 92.140 | 92.581 | 93.026 | 93.475 | 93.928 | 94.386 | 94.849 |

Table S3. Contd.

| x1 | T/K |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | 293.15 | 298.15 | 303.15 | 308.15 | 313.15 | 318.15 | 323.15 |

DMA + PEG 400

| 0.0000 | 88.964 | 89.017 | 89.071 | 89.209 | 89.337 | 89.425 | 89.547 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.0732 | 88.994 | 89.178 | 89.377 | 89.609 | 89.839 | 90.050 | 90.278 |
| 0.1472 | 89.067 | 89.332 | 89.605 | 89.897 | 90.184 | 90.466 | 90.757 |
| 0.2055 | 89.150 | 89.447 | 89.750 | 90.074 | 90.393 | 90.709 | 91.031 |
| 0.2649 | 89.247 | 89.569 | 89.890 | 90.236 | 90.572 | 90.909 | 91.249 |
| 0.3485 | 89.418 | 89.757 | 90.095 | 90.456 | 90.810 | 91.165 | 91.523 |
| 0.4253 | 89.608 | 89.951 | 90.298 | 90.668 | 91.034 | 91.399 | 91.764 |
| 0.4985 | 89.823 | 90.173 | 90.529 | 90.902 | 91.272 | 91.643 | 92.014 |
| 0.5833 | 90.114 | 90.469 | 90.833 | 91.205 | 91.580 | 91.955 | 92.327 |
| 0.6520 | 90.384 | 90.745 | 91.114 | 91.488 | 91.866 | 92.245 | 92.621 |
| 0.7287 | 90.723 | 91.092 | 91.467 | 91.842 | 92.224 | 92.608 | 92.989 |
| 0.7974 | 91.054 | 91.430 | 91.810 | 92.193 | 92.580 | 92.970 | 93.361 |
| 0.8693 | 91.421 | 91.811 | 92.203 | 92.599 | 92.999 | 93.401 | 93.807 |
| 0.9322 | 91.770 | 92.180 | 92.594 | 93.012 | 93.432 | 93.857 | 94.285 |
| 1.0000 | 92.140 | 92.581 | 93.026 | 93.475 | 93.928 | 94.386 | 94.849 |

DMA + PEG 600

| 0.0000 | 88.035 | 88.170 | 88.248 | 88.381 | 88.372 | 88.537 | 88.662 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.0718 | 87.842 | 88.036 | 88.209 | 88.391 | 88.526 | 88.780 | 88.970 |
| 0.1430 | 87.814 | 88.054 | 88.288 | 88.513 | 88.734 | 89.038 | 89.276 |
| 0.2128 | 87.906 | 88.179 | 88.456 | 88.720 | 88.986 | 89.312 | 89.586 |
| 0.2912 | 88.098 | 88.404 | 88.712 | 89.015 | 89.317 | 89.654 | 89.957 |
| 0.3702 | 88.368 | 88.698 | 89.028 | 89.359 | 89.686 | 90.021 | 90.342 |
| 0.4450 | 88.687 | 89.030 | 89.371 | 89.715 | 90.057 | 90.397 | 90.732 |
| 0.5072 | 88.990 | 89.338 | 89.686 | 90.035 | 90.385 | 90.732 | 91.071 |
| 0.5785 | 89.370 | 89.724 | 90.077 | 90.430 | 90.787 | 91.143 | 91.486 |
| 0.6511 | 89.797 | 90.154 | 90.511 | 90.868 | 91.230 | 91.598 | 91.951 |
| 0.7207 | 90.238 | 90.599 | 90.961 | 91.323 | 91.691 | 92.070 | 92.434 |
| 0.7998 | 90.767 | 91.137 | 91.510 | 91.883 | 92.261 | 92.654 | 93.034 |
| 0.8701 | 91.246 | 91.633 | 92.022 | 92.414 | 92.809 | 93.217 | 93.618 |
| 0.9385 | 91.726 | 92.134 | 92.545 | 92.960 | 93.378 | 93.803 | 94.229 |
| 1.0000 | 92.140 | 92.581 | 93.026 | 93.475 | 93.928 | 94.386 | 94.849 |

Table S4. Partial molar volumes, 106Vm,2/(m3 mol−1) of PEGs as a function of mole fraction, x1 of DMA in DMA + PEG 200/ PEG 300/ PEG 400/ PEG 600 binary mixture at temperatures, T/K = (293.15 − 323.15)

| x1 | T/K |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | 293.15 | 298.15 | 303.15 | 308.15 | 313.15 | 318.15 | 323.15 |

DMA + PEG 200

| 0.0000 | 169.873 | 170.481 | 171.090 | 171.701 | 172.312 | 172.927 | 173.544 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.0584 | 169.774 | 170.370 | 170.967 | 171.567 | 172.166 | 172.770 | 173.376 |
| 0.1152 | 169.675 | 170.262 | 170.849 | 171.439 | 172.031 | 172.625 | 173.221 |
| 0.2003 | 169.516 | 170.090 | 170.665 | 171.244 | 171.819 | 172.404 | 172.987 |
| 0.2790 | 169.350 | 169.917 | 170.484 | 171.054 | 171.624 | 172.199 | 172.771 |
| 0.3756 | 169.109 | 169.666 | 170.227 | 170.790 | 171.355 | 171.922 | 172.488 |
| 0.4655 | 168.854 | 169.401 | 169.954 | 170.510 | 171.070 | 171.628 | 172.187 |
| 0.5320 | 168.650 | 169.191 | 169.735 | 170.284 | 170.839 | 171.391 | 171.942 |
| 0.6027 | 168.424 | 168.954 | 169.490 | 170.030 | 170.577 | 171.119 | 171.662 |
| 0.6652 | 168.223 | 168.741 | 169.264 | 169.792 | 170.326 | 170.855 | 171.387 |
| 0.7327 | 168.014 | 168.514 | 169.019 | 169.527 | 170.041 | 170.551 | 171.064 |
| 0.8046 | 167.798 | 168.276 | 168.756 | 169.240 | 169.725 | 170.212 | 170.700 |
| 0.8708 | 167.618 | 168.072 | 168.530 | 168.991 | 169.451 | 169.911 | 170.366 |
| 0.9294 | 167.469 | 167.895 | 168.339 | 168.782 | 169.221 | 169.654 | 170.070 |
| 1.0000 | 167.297 | 167.685 | 168.118 | 168.545 | 168.979 | 169.369 | 169.723 |

DMA + PEG 300

| 0.0000 | 247.797 | 248.697 | 249.601 | 250.517 | 251.441 | 252.378 | 253.325 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.0712 | 247.635 | 248.520 | 249.409 | 250.310 | 251.214 | 252.129 | 253.056 |
| 0.1422 | 247.463 | 248.334 | 249.209 | 250.094 | 250.983 | 251.883 | 252.794 |
| 0.2123 | 247.283 | 248.145 | 249.010 | 249.885 | 250.766 | 251.653 | 252.551 |
| 0.2813 | 247.097 | 247.950 | 248.809 | 249.675 | 250.548 | 251.425 | 252.315 |
| 0.3584 | 246.883 | 247.727 | 248.577 | 249.436 | 250.302 | 251.167 | 252.050 |
| 0.4216 | 246.697 | 247.534 | 248.378 | 249.230 | 250.090 | 250.948 | 251.824 |
| 0.4970 | 246.463 | 247.292 | 248.129 | 248.973 | 249.825 | 250.673 | 251.544 |
| 0.5616 | 246.244 | 247.070 | 247.902 | 248.740 | 249.585 | 250.427 | 251.288 |
| 0.6525 | 245.906 | 246.721 | 247.543 | 248.370 | 249.203 | 250.034 | 250.882 |
| 0.7472 | 245.514 | 246.306 | 247.104 | 247.906 | 248.713 | 249.519 | 250.338 |
| 0.8004 | 245.283 | 246.050 | 246.822 | 247.599 | 248.378 | 249.158 | 249.947 |
| 0.8667 | 244.986 | 245.703 | 246.423 | 247.148 | 247.873 | 248.599 | 249.332 |
| 0.9311 | 244.723 | 245.357 | 245.992 | 246.630 | 247.267 | 247.900 | 248.545 |
| 1.0000 | 244.485 | 244.974 | 245.461 | 245.949 | 246.432 | 246.895 | 247.398 |

Table S4. Contd.

| x1 | T/K |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | 293.15 | 298.15 | 303.15 | 308.15 | 313.15 | 318.15 | 323.15 |

DMA + PEG 400

| 0.0000 | 320.479 | 321.635 | 322.800 | 323.959 | 325.129 | 326.313 | 327.506 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.0732 | 320.216 | 321.346 | 322.488 | 323.630 | 324.782 | 325.942 | 327.110 |
| 0.1472 | 319.959 | 321.076 | 322.205 | 323.328 | 324.465 | 325.612 | 326.765 |
| 0.2055 | 319.762 | 320.867 | 321.985 | 323.102 | 324.234 | 325.374 | 326.520 |
| 0.2649 | 319.560 | 320.661 | 321.770 | 322.875 | 323.995 | 325.126 | 326.268 |
| 0.3485 | 319.259 | 320.353 | 321.452 | 322.539 | 323.648 | 324.764 | 325.889 |
| 0.4253 | 318.950 | 320.040 | 321.125 | 322.199 | 323.292 | 324.392 | 325.499 |
| 0.4985 | 318.599 | 319.683 | 320.761 | 321.826 | 322.910 | 323.994 | 325.084 |
| 0.5833 | 318.081 | 319.164 | 320.234 | 321.291 | 322.368 | 323.443 | 324.518 |
| 0.6520 | 317.539 | 318.615 | 319.682 | 320.734 | 321.805 | 322.876 | 323.938 |
| 0.7287 | 316.766 | 317.805 | 318.845 | 319.875 | 320.922 | 321.978 | 323.016 |
| 0.7974 | 315.863 | 316.831 | 317.803 | 318.761 | 319.735 | 320.728 | 321.707 |
| 0.8693 | 314.645 | 315.483 | 316.301 | 317.079 | 317.852 | 318.662 | 319.459 |
| 0.9322 | 313.288 | 313.950 | 314.532 | 315.023 | 315.463 | 315.913 | 316.382 |
| 1.0000 | 311.488 | 311.802 | 311.919 | 311.853 | 311.652 | 311.417 | 311.258 |

DMA + PEG 600

| 0.0000 | 483.674 | 485.381 | 487.102 | 488.842 | 490.593 | 492.363 | 494.157 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.0718 | 483.370 | 485.057 | 486.755 | 488.474 | 490.198 | 491.943 | 493.714 |
| 0.1430 | 483.050 | 484.717 | 486.394 | 488.088 | 489.793 | 491.520 | 493.268 |
| 0.2128 | 482.726 | 484.375 | 486.037 | 487.710 | 489.395 | 491.103 | 492.833 |
| 0.2912 | 482.336 | 483.971 | 485.620 | 487.277 | 488.950 | 490.642 | 492.355 |
| 0.3702 | 481.915 | 483.539 | 485.179 | 486.827 | 488.491 | 490.164 | 491.863 |
| 0.4450 | 481.491 | 483.106 | 484.736 | 486.375 | 488.029 | 489.693 | 491.386 |
| 0.5072 | 481.108 | 482.717 | 484.342 | 485.974 | 487.618 | 489.278 | 490.960 |
| 0.5785 | 480.626 | 482.229 | 483.845 | 485.471 | 487.105 | 488.754 | 490.423 |
| 0.6511 | 480.087 | 481.677 | 483.280 | 484.894 | 486.513 | 488.148 | 489.800 |
| 0.7207 | 479.523 | 481.090 | 482.669 | 484.257 | 485.852 | 487.459 | 489.082 |
| 0.7998 | 478.828 | 480.345 | 481.870 | 483.404 | 484.945 | 486.494 | 488.055 |
| 0.8701 | 478.172 | 479.607 | 481.047 | 482.497 | 483.948 | 485.412 | 486.882 |
| 0.9385 | 477.545 | 478.844 | 480.144 | 481.461 | 482.753 | 484.082 | 485.418 |
| 1.0000 | 477.005 | 478.125 | 479.235 | 480.387 | 481.451 | 482.615 | 483.789 |

Table S5. Partial molar isentropic compressibilities, 1014Ks,m,1/(m5 N−1 mol−1) of DMA as a function of mole fraction, x1 of DMA in DMA + PEG 200/ PEG 300/ PEG 400/ PEG 600 binary mixture at temperatures, T/K = (293.15 − 323.15)

| x1 | T/K |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | 293.15 | 298.15 | 303.15 | 308.15 | 313.15 | 318.15 | 323.15 |

DMA + PEG 200

| 0.0000 | 3.812 | 3.883 | 3.972 | 4.081 | 4.193 | 4.309 | 4.447 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.0584 | 3.784 | 3.871 | 3.966 | 4.075 | 4.187 | 4.309 | 4.433 |
| 0.1152 | 3.772 | 3.868 | 3.968 | 4.078 | 4.192 | 4.317 | 4.441 |
| 0.2003 | 3.773 | 3.876 | 3.982 | 4.098 | 4.216 | 4.345 | 4.478 |
| 0.2790 | 3.790 | 3.898 | 4.009 | 4.130 | 4.254 | 4.386 | 4.530 |
| 0.3756 | 3.827 | 3.940 | 4.059 | 4.187 | 4.316 | 4.456 | 4.615 |
| 0.4655 | 3.876 | 3.996 | 4.120 | 4.255 | 4.392 | 4.539 | 4.706 |
| 0.5320 | 3.923 | 4.048 | 4.177 | 4.316 | 4.459 | 4.612 | 4.782 |
| 0.6027 | 3.981 | 4.112 | 4.246 | 4.390 | 4.540 | 4.700 | 4.873 |
| 0.6652 | 4.041 | 4.176 | 4.317 | 4.465 | 4.619 | 4.784 | 4.961 |
| 0.7327 | 4.113 | 4.255 | 4.400 | 4.554 | 4.713 | 4.884 | 5.065 |
| 0.8046 | 4.198 | 4.344 | 4.497 | 4.656 | 4.822 | 4.999 | 5.187 |
| 0.8708 | 4.279 | 4.431 | 4.590 | 4.757 | 4.930 | 5.112 | 5.310 |
| 0.9294 | 4.353 | 4.511 | 4.676 | 4.850 | 5.030 | 5.219 | 5.426 |
| 1.0000 | 4.442 | 4.608 | 4.782 | 4.964 | 5.154 | 5.353 | 5.574 |

DMA + PEG 300

| 0.0000 | 3.413 | 3.473 | 3.529 | 3.548 | 3.618 | 3.684 | 3.754 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.0712 | 3.424 | 3.500 | 3.574 | 3.643 | 3.725 | 3.867 | 3.896 |
| 0.1422 | 3.434 | 3.521 | 3.609 | 3.699 | 3.791 | 3.919 | 3.989 |
| 0.2123 | 3.452 | 3.548 | 3.646 | 3.745 | 3.847 | 3.978 | 4.066 |
| 0.2813 | 3.481 | 3.582 | 3.686 | 3.790 | 3.902 | 4.035 | 4.145 |
| 0.3584 | 3.522 | 3.629 | 3.744 | 3.858 | 3.978 | 4.112 | 4.245 |
| 0.4216 | 3.566 | 3.680 | 3.800 | 3.920 | 4.048 | 4.186 | 4.335 |
| 0.4970 | 3.630 | 3.751 | 3.879 | 4.008 | 4.145 | 4.290 | 4.450 |
| 0.5616 | 3.697 | 3.822 | 3.956 | 4.094 | 4.236 | 4.390 | 4.556 |
| 0.6525 | 3.807 | 3.939 | 4.080 | 4.231 | 4.381 | 4.546 | 4.720 |
| 0.7472 | 3.944 | 4.082 | 4.230 | 4.388 | 4.548 | 4.724 | 4.902 |
| 0.8004 | 4.033 | 4.174 | 4.326 | 4.487 | 4.652 | 4.833 | 5.016 |
| 0.8667 | 4.155 | 4.303 | 4.459 | 4.625 | 4.796 | 4.981 | 5.174 |
| 0.9311 | 4.286 | 4.441 | 4.605 | 4.777 | 4.956 | 5.144 | 5.350 |
| 1.0000 | 4.442 | 4.608 | 4.782 | 4.964 | 5.154 | 5.353 | 5.574 |

Table S5. Contd.

| x1 | T/K |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | 293.15 | 298.15 | 303.15 | 308.15 | 313.15 | 318.15 | 323.15 |

DMA + PEG 400

| 0.0000 | 2.748 | 2.693 | 2.681 | 2.807 | 2.606 | 2.566 | 2.606 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.0732 | 2.787 | 2.793 | 2.807 | 2.889 | 2.813 | 2.876 | 2.847 |
| 0.1472 | 2.834 | 2.868 | 2.901 | 2.957 | 2.955 | 3.004 | 3.029 |
| 0.2055 | 2.876 | 2.922 | 2.969 | 3.021 | 3.052 | 3.117 | 3.154 |
| 0.2649 | 2.926 | 2.984 | 3.044 | 3.103 | 3.156 | 3.228 | 3.290 |
| 0.3485 | 3.017 | 3.084 | 3.164 | 3.240 | 3.315 | 3.406 | 3.498 |
| 0.4253 | 3.119 | 3.204 | 3.300 | 3.394 | 3.487 | 3.591 | 3.715 |
| 0.4985 | 3.234 | 3.335 | 3.446 | 3.560 | 3.667 | 3.789 | 3.938 |
| 0.5833 | 3.394 | 3.508 | 3.632 | 3.765 | 3.890 | 4.031 | 4.198 |
| 0.6520 | 3.538 | 3.665 | 3.800 | 3.946 | 4.081 | 4.234 | 4.409 |
| 0.7287 | 3.716 | 3.853 | 3.997 | 4.153 | 4.301 | 4.464 | 4.647 |
| 0.7974 | 3.888 | 4.032 | 4.184 | 4.343 | 4.501 | 4.674 | 4.861 |
| 0.8693 | 4.078 | 4.227 | 4.385 | 4.551 | 4.718 | 4.897 | 5.092 |
| 0.9322 | 4.252 | 4.406 | 4.570 | 4.742 | 4.918 | 5.104 | 5.309 |
| 1.0000 | 4.442 | 4.608 | 4.782 | 4.964 | 5.154 | 5.353 | 5.574 |

DMA + PEG 600

| 0.0000 | 2.639 | 2.447 | 2.325 | 2.170 | 2.296 | 1.988 | 1.825 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.0718 | 2.286 | 2.187 | 2.121 | 2.036 | 2.024 | 1.811 | 1.808 |
| 0.1430 | 2.117 | 2.072 | 2.040 | 2.002 | 1.953 | 1.854 | 1.852 |
| 0.2128 | 2.057 | 2.042 | 2.032 | 2.019 | 1.981 | 1.917 | 1.931 |
| 0.2912 | 2.067 | 2.074 | 2.078 | 2.087 | 2.076 | 2.031 | 2.047 |
| 0.3702 | 2.126 | 2.146 | 2.168 | 2.192 | 2.212 | 2.201 | 2.220 |
| 0.4450 | 2.229 | 2.265 | 2.296 | 2.337 | 2.390 | 2.403 | 2.441 |
| 0.5072 | 2.343 | 2.395 | 2.442 | 2.494 | 2.574 | 2.616 | 2.670 |
| 0.5785 | 2.528 | 2.596 | 2.659 | 2.724 | 2.824 | 2.895 | 2.976 |
| 0.6511 | 2.774 | 2.860 | 2.937 | 3.031 | 3.137 | 3.234 | 3.348 |
| 0.7207 | 3.054 | 3.158 | 3.257 | 3.362 | 3.480 | 3.602 | 3.745 |
| 0.7998 | 3.424 | 3.543 | 3.667 | 3.792 | 3.929 | 4.070 | 4.235 |
| 0.8701 | 3.778 | 3.917 | 4.055 | 4.203 | 4.362 | 4.519 | 4.708 |
| 0.9385 | 4.142 | 4.293 | 4.453 | 4.619 | 4.794 | 4.972 | 5.175 |
| 1.0000 | 4.442 | 4.608 | 4.782 | 4.964 | 5.154 | 5.353 | 5.574 |

Table S6. Partial molar isentropic compressibilities, 1014Ks,m,2/(m5 N−1 mol−1) of PEGs as a function of mole fraction, x1 of DMA in DMA + PEG 200/ PEG 300/ PEG 400/ PEG 600 binary mixture at temperatures, T/K = (293.15 − 323.15)

| x1 | T/K |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | 293.15 | 298.15 | 303.15 | 308.15 | 313.15 | 318.15 | 323.15 |

DMA + PEG 200

| 0.0000 | 5.749 | 5.881 | 6.012 | 6.141 | 6.272 | 6.404 | 6.536 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.0584 | 5.712 | 5.838 | 5.965 | 6.090 | 6.216 | 6.343 | 6.470 |
| 0.1152 | 5.675 | 5.798 | 5.920 | 6.039 | 6.161 | 6.283 | 6.404 |
| 0.2003 | 5.618 | 5.735 | 5.850 | 5.964 | 6.079 | 6.192 | 6.302 |
| 0.2790 | 5.564 | 5.676 | 5.785 | 5.891 | 5.999 | 6.104 | 6.206 |
| 0.3756 | 5.490 | 5.595 | 5.698 | 5.795 | 5.894 | 5.989 | 6.084 |
| 0.4655 | 5.410 | 5.507 | 5.602 | 5.694 | 5.784 | 5.870 | 5.958 |
| 0.5320 | 5.341 | 5.432 | 5.521 | 5.607 | 5.692 | 5.772 | 5.854 |
| 0.6027 | 5.255 | 5.340 | 5.421 | 5.501 | 5.580 | 5.654 | 5.730 |
| 0.6652 | 5.167 | 5.245 | 5.322 | 5.395 | 5.465 | 5.533 | 5.603 |
| 0.7327 | 5.058 | 5.130 | 5.196 | 5.261 | 5.322 | 5.381 | 5.439 |
| 0.8046 | 4.926 | 4.987 | 5.044 | 5.095 | 5.144 | 5.190 | 5.229 |
| 0.8708 | 4.792 | 4.840 | 4.883 | 4.921 | 4.952 | 4.980 | 4.994 |
| 0.9294 | 4.666 | 4.697 | 4.727 | 4.747 | 4.757 | 4.761 | 4.748 |
| 1.0000 | 4.516 | 4.513 | 4.521 | 4.515 | 4.485 | 4.445 | 4.393 |

DMA + PEG 300

| 0.0000 | 8.449 | 8.688 | 8.922 | 9.189 | 9.454 | 9.726 | 10.007 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.0712 | 8.378 | 8.610 | 8.836 | 9.094 | 9.351 | 9.614 | 9.884 |
| 0.1422 | 8.307 | 8.533 | 8.753 | 9.004 | 9.252 | 9.505 | 9.766 |
| 0.2123 | 8.239 | 8.460 | 8.673 | 8.918 | 9.158 | 9.400 | 9.651 |
| 0.2813 | 8.171 | 8.384 | 8.589 | 8.827 | 9.060 | 9.295 | 9.536 |
| 0.3584 | 8.087 | 8.293 | 8.491 | 8.724 | 8.947 | 9.171 | 9.402 |
| 0.4216 | 8.011 | 8.213 | 8.404 | 8.626 | 8.843 | 9.060 | 9.284 |
| 0.4970 | 7.908 | 8.104 | 8.289 | 8.500 | 8.709 | 8.918 | 9.131 |
| 0.5616 | 7.806 | 7.995 | 8.175 | 8.377 | 8.580 | 8.782 | 8.988 |
| 0.6525 | 7.627 | 7.809 | 7.981 | 8.176 | 8.369 | 8.563 | 8.761 |
| 0.7472 | 7.376 | 7.546 | 7.709 | 7.896 | 8.078 | 8.262 | 8.447 |
| 0.8004 | 7.196 | 7.355 | 7.509 | 7.690 | 7.863 | 8.038 | 8.211 |
| 0.8667 | 6.914 | 7.055 | 7.191 | 7.357 | 7.512 | 7.668 | 7.820 |
| 0.9311 | 6.565 | 6.674 | 6.784 | 6.915 | 7.048 | 7.169 | 7.288 |
| 1.0000 | 6.083 | 6.140 | 6.200 | 6.259 | 6.352 | 6.418 | 6.477 |

Table S6. Contd.

| x1 | T/K |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | 293.15 | 298.15 | 303.15 | 308.15 | 313.15 | 318.15 | 323.15 |

DMA + PEG 400

| 0.0000 | 11.010 | 11.291 | 11.578 | 11.868 | 12.191 | 12.512 | 12.852 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.0732 | 10.887 | 11.156 | 11.430 | 11.715 | 12.014 | 12.317 | 12.640 |
| 0.1472 | 10.768 | 11.025 | 11.286 | 11.557 | 11.840 | 12.129 | 12.438 |
| 0.2055 | 10.673 | 10.922 | 11.172 | 11.431 | 11.703 | 11.982 | 12.271 |
| 0.2649 | 10.572 | 10.815 | 11.054 | 11.301 | 11.563 | 11.824 | 12.100 |
| 0.3485 | 10.424 | 10.650 | 10.874 | 11.099 | 11.349 | 11.595 | 11.842 |
| 0.4253 | 10.274 | 10.488 | 10.699 | 10.902 | 11.140 | 11.369 | 11.597 |
| 0.4985 | 10.112 | 10.314 | 10.514 | 10.702 | 10.927 | 11.142 | 11.358 |
| 0.5833 | 9.902 | 10.086 | 10.274 | 10.449 | 10.661 | 10.866 | 11.070 |
| 0.6520 | 9.702 | 9.881 | 10.065 | 10.236 | 10.436 | 10.633 | 10.832 |
| 0.7287 | 9.447 | 9.621 | 9.801 | 9.972 | 10.164 | 10.353 | 10.552 |
| 0.7974 | 9.184 | 9.356 | 9.532 | 9.700 | 9.884 | 10.067 | 10.260 |
| 0.8693 | 8.870 | 9.030 | 9.199 | 9.359 | 9.528 | 9.693 | 9.870 |
| 0.9322 | 8.560 | 8.694 | 8.849 | 8.986 | 9.127 | 9.261 | 9.400 |
| 1.0000 | 8.185 | 8.258 | 8.385 | 8.468 | 8.555 | 8.625 | 8.682 |

DMA + PEG 600

| 0.0000 | 16.614 | 17.068 | 17.538 | 18.047 | 18.575 | 19.109 | 19.677 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.0718 | 16.476 | 16.907 | 17.358 | 17.844 | 18.355 | 18.860 | 19.405 |
| 0.1430 | 16.322 | 16.738 | 17.174 | 17.644 | 18.134 | 18.627 | 19.153 |
| 0.2128 | 16.166 | 16.569 | 16.991 | 17.445 | 17.908 | 18.390 | 18.902 |
| 0.2912 | 15.987 | 16.377 | 16.783 | 17.223 | 17.646 | 18.105 | 18.596 |
| 0.3702 | 15.785 | 16.157 | 16.551 | 16.975 | 17.362 | 17.803 | 18.269 |
| 0.4450 | 15.564 | 15.920 | 16.294 | 16.703 | 17.072 | 17.478 | 17.922 |
| 0.5072 | 15.334 | 15.677 | 16.040 | 16.431 | 16.795 | 17.176 | 17.593 |
| 0.5785 | 15.018 | 15.342 | 15.685 | 16.054 | 16.409 | 16.758 | 17.147 |
| 0.6511 | 14.617 | 14.924 | 15.241 | 15.599 | 15.935 | 16.259 | 16.623 |
| 0.7207 | 14.141 | 14.432 | 14.731 | 15.060 | 15.383 | 15.695 | 16.037 |
| 0.7998 | 13.509 | 13.780 | 14.056 | 14.359 | 14.666 | 14.965 | 15.280 |
| 0.8701 | 12.893 | 13.154 | 13.406 | 13.689 | 13.985 | 14.265 | 14.566 |
| 0.9385 | 12.325 | 12.565 | 12.805 | 13.065 | 13.352 | 13.582 | 13.858 |
| 1.0000 | 11.893 | 12.111 | 12.339 | 12.575 | 12.878 | 13.001 | 13.242 |

Table S7. Excess partial molar volumes, 106Vm,1E/(m3 mol−1) of DMA as a function of mole fraction, x1 of DMA in DMA + PEG 200/ PEG 300/ PEG 400/ PEG 600 binary mixture at temperatures, T/K = (293.15 − 323.15)

| x1 | T/K |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | 293.15 | 298.15 | 303.15 | 308.15 | 313.15 | 318.15 | 323.15 |

DMA + PEG 200

| 0.0000 | -1.713 | -1.938 | -2.149 | -2.344 | -2.531 | -2.733 | -2.949 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.0584 | -1.770 | -1.951 | -2.127 | -2.294 | -2.462 | -2.652 | -2.830 |
| 0.1152 | -1.814 | -1.963 | -2.112 | -2.255 | -2.396 | -2.571 | -2.718 |
| 0.2003 | -1.835 | -1.955 | -2.074 | -2.187 | -2.302 | -2.444 | -2.560 |
| 0.2790 | -1.794 | -1.896 | -1.996 | -2.093 | -2.184 | -2.301 | -2.402 |
| 0.3756 | -1.667 | -1.756 | -1.843 | -1.929 | -2.007 | -2.100 | -2.183 |
| 0.4655 | -1.480 | -1.563 | -1.645 | -1.724 | -1.799 | -1.880 | -1.954 |
| 0.5320 | -1.312 | -1.387 | -1.465 | -1.540 | -1.615 | -1.689 | -1.760 |
| 0.6027 | -1.116 | -1.184 | -1.254 | -1.322 | -1.393 | -1.462 | -1.526 |
| 0.6652 | -0.934 | -0.994 | -1.057 | -1.118 | -1.183 | -1.248 | -1.308 |
| 0.7327 | -0.734 | -0.785 | -0.838 | -0.891 | -0.947 | -1.007 | -1.060 |
| 0.8046 | -0.529 | -0.569 | -0.610 | -0.651 | -0.694 | -0.742 | -0.784 |
| 0.8708 | -0.343 | -0.369 | -0.395 | -0.422 | -0.450 | -0.482 | -0.512 |
| 0.9294 | -0.184 | -0.199 | -0.212 | -0.225 | -0.240 | -0.256 | -0.273 |
| 1.0000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 |

DMA + PEG 300

| 0.0000 | -2.155 | -2.403 | -2.660 | -2.921 | -3.260 | -3.609 | -3.942 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.0712 | -2.282 | -2.465 | -2.651 | -2.842 | -3.070 | -3.316 | -3.554 |
| 0.1422 | -2.294 | -2.438 | -2.582 | -2.731 | -2.897 | -3.080 | -3.258 |
| 0.2123 | -2.234 | -2.351 | -2.467 | -2.589 | -2.716 | -2.862 | -3.003 |
| 0.2813 | -2.133 | -2.232 | -2.327 | -2.431 | -2.537 | -2.658 | -2.775 |
| 0.3584 | -1.983 | -2.067 | -2.149 | -2.236 | -2.328 | -2.431 | -2.530 |
| 0.4216 | -1.841 | -1.916 | -1.990 | -2.069 | -2.152 | -2.243 | -2.334 |
| 0.4970 | -1.650 | -1.718 | -1.785 | -1.857 | -1.933 | -2.014 | -2.095 |
| 0.5616 | -1.472 | -1.533 | -1.595 | -1.661 | -1.731 | -1.803 | -1.883 |
| 0.6525 | -1.196 | -1.252 | -1.309 | -1.368 | -1.431 | -1.494 | -1.565 |
| 0.7472 | -0.884 | -0.934 | -0.986 | -1.039 | -1.095 | -1.152 | -1.214 |
| 0.8004 | -0.696 | -0.743 | -0.791 | -0.840 | -0.891 | -0.943 | -0.999 |
| 0.8667 | -0.466 | -0.503 | -0.541 | -0.580 | -0.620 | -0.662 | -0.705 |
| 0.9311 | -0.233 | -0.256 | -0.280 | -0.304 | -0.330 | -0.356 | -0.382 |
| 1.0000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 |

Table S7. Contd.

| x1 | T/K |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | 293.15 | 298.15 | 303.15 | 308.15 | 313.15 | 318.15 | 323.15 |

DMA + PEG 400

| 0.0000 | -3.176 | -3.564 | -3.955 | -4.266 | -4.592 | -4.961 | -5.302 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.0732 | -3.146 | -3.402 | -3.649 | -3.865 | -4.089 | -4.336 | -4.571 |
| 0.1472 | -3.073 | -3.249 | -3.420 | -3.578 | -3.744 | -3.920 | -4.092 |
| 0.2055 | -2.990 | -3.133 | -3.275 | -3.400 | -3.535 | -3.677 | -3.818 |
| 0.2649 | -2.893 | -3.012 | -3.136 | -3.239 | -3.356 | -3.478 | -3.600 |
| 0.3485 | -2.722 | -2.824 | -2.930 | -3.019 | -3.119 | -3.221 | -3.326 |
| 0.4253 | -2.532 | -2.629 | -2.728 | -2.806 | -2.894 | -2.987 | -3.085 |
| 0.4985 | -2.317 | -2.408 | -2.497 | -2.573 | -2.657 | -2.743 | -2.835 |
| 0.5833 | -2.027 | -2.112 | -2.193 | -2.270 | -2.349 | -2.432 | -2.522 |
| 0.6520 | -1.756 | -1.836 | -1.911 | -1.987 | -2.062 | -2.142 | -2.227 |
| 0.7287 | -1.417 | -1.489 | -1.559 | -1.633 | -1.704 | -1.779 | -1.860 |
| 0.7974 | -1.086 | -1.151 | -1.216 | -1.281 | -1.348 | -1.417 | -1.487 |
| 0.8693 | -0.719 | -0.770 | -0.823 | -0.875 | -0.930 | -0.986 | -1.042 |
| 0.9322 | -0.370 | -0.400 | -0.431 | -0.463 | -0.496 | -0.530 | -0.564 |
| 1.0000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 |

DMA + PEG 600

| 0.0000 | -4.106 | -4.410 | -4.778 | -5.094 | -5.557 | -5.850 | -6.187 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.0718 | -4.298 | -4.545 | -4.817 | -5.084 | -5.402 | -5.606 | -5.879 |
| 0.1430 | -4.326 | -4.527 | -4.738 | -4.962 | -5.194 | -5.348 | -5.573 |
| 0.2128 | -4.234 | -4.402 | -4.570 | -4.755 | -4.942 | -5.074 | -5.263 |
| 0.2912 | -4.042 | -4.176 | -4.313 | -4.459 | -4.611 | -4.732 | -4.892 |
| 0.3702 | -3.772 | -3.883 | -3.998 | -4.116 | -4.242 | -4.365 | -4.507 |
| 0.4450 | -3.453 | -3.551 | -3.655 | -3.760 | -3.872 | -3.989 | -4.117 |
| 0.5072 | -3.150 | -3.242 | -3.340 | -3.439 | -3.544 | -3.654 | -3.778 |
| 0.5785 | -2.770 | -2.857 | -2.949 | -3.044 | -3.142 | -3.244 | -3.363 |
| 0.6511 | -2.343 | -2.427 | -2.515 | -2.607 | -2.698 | -2.789 | -2.898 |
| 0.7207 | -1.902 | -1.982 | -2.065 | -2.151 | -2.237 | -2.316 | -2.415 |
| 0.7998 | -1.373 | -1.443 | -1.516 | -1.592 | -1.668 | -1.733 | -1.815 |
| 0.8701 | -0.894 | -0.948 | -1.004 | -1.061 | -1.120 | -1.170 | -1.231 |
| 0.9385 | -0.414 | -0.447 | -0.481 | -0.515 | -0.551 | -0.583 | -0.620 |
| 1.0000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 |

Table S8. Excess partial molar volumes, 106Vm,2E/(m3 mol−1) of PEGs as a function of mole fraction, x1 of DMA in DMA + PEG 200/ PEG 300/ PEG 400/ PEG 600 binary mixture at temperatures, T/K = (293.15 − 323.15)

| x1 | T/K |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | 293.15 | 298.15 | 303.15 | 308.15 | 313.15 | 318.15 | 323.15 |

DMA + PEG 200

| 0.0000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.0584 | -0.099 | -0.111 | -0.123 | -0.134 | -0.147 | -0.157 | -0.169 |
| 0.1152 | -0.197 | -0.219 | -0.241 | -0.262 | -0.281 | -0.302 | -0.323 |
| 0.2003 | -0.356 | -0.390 | -0.425 | -0.457 | -0.493 | -0.523 | -0.558 |
| 0.2790 | -0.523 | -0.564 | -0.606 | -0.646 | -0.688 | -0.727 | -0.773 |
| 0.3756 | -0.764 | -0.814 | -0.863 | -0.910 | -0.957 | -1.005 | -1.056 |
| 0.4655 | -1.019 | -1.080 | -1.136 | -1.191 | -1.243 | -1.299 | -1.357 |
| 0.5320 | -1.223 | -1.290 | -1.355 | -1.416 | -1.473 | -1.536 | -1.602 |
| 0.6027 | -1.449 | -1.527 | -1.600 | -1.671 | -1.735 | -1.808 | -1.882 |
| 0.6652 | -1.649 | -1.740 | -1.826 | -1.909 | -1.986 | -2.072 | -2.157 |
| 0.7327 | -1.859 | -1.966 | -2.071 | -2.174 | -2.272 | -2.376 | -2.481 |
| 0.8046 | -2.075 | -2.205 | -2.334 | -2.461 | -2.587 | -2.715 | -2.845 |
| 0.8708 | -2.255 | -2.409 | -2.560 | -2.709 | -2.862 | -3.016 | -3.178 |
| 0.9294 | -2.404 | -2.585 | -2.751 | -2.919 | -3.092 | -3.273 | -3.474 |
| 1.0000 | -2.575 | -2.796 | -2.972 | -3.156 | -3.333 | -3.558 | -3.821 |

DMA + PEG 300

| 0.0000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.0712 | -0.162 | -0.177 | -0.192 | -0.207 | -0.227 | -0.248 | -0.269 |
| 0.1422 | -0.334 | -0.363 | -0.393 | -0.423 | -0.458 | -0.495 | -0.531 |
| 0.2123 | -0.513 | -0.552 | -0.592 | -0.632 | -0.675 | -0.725 | -0.774 |
| 0.2813 | -0.699 | -0.747 | -0.792 | -0.842 | -0.893 | -0.952 | -1.010 |
| 0.3584 | -0.914 | -0.970 | -1.024 | -1.081 | -1.139 | -1.210 | -1.275 |
| 0.4216 | -1.100 | -1.163 | -1.223 | -1.287 | -1.351 | -1.430 | -1.500 |
| 0.4970 | -1.334 | -1.405 | -1.472 | -1.544 | -1.616 | -1.705 | -1.781 |
| 0.5616 | -1.552 | -1.627 | -1.699 | -1.777 | -1.856 | -1.950 | -2.037 |
| 0.6525 | -1.891 | -1.976 | -2.058 | -2.147 | -2.237 | -2.344 | -2.443 |
| 0.7472 | -2.283 | -2.391 | -2.497 | -2.611 | -2.728 | -2.858 | -2.986 |
| 0.8004 | -2.514 | -2.647 | -2.779 | -2.918 | -3.063 | -3.219 | -3.377 |
| 0.8667 | -2.811 | -2.994 | -3.178 | -3.369 | -3.568 | -3.778 | -3.993 |
| 0.9311 | -3.074 | -3.340 | -3.610 | -3.887 | -4.174 | -4.478 | -4.780 |
| 1.0000 | -3.311 | -3.723 | -4.140 | -4.568 | -5.009 | -5.482 | -5.927 |

Table S8. Contd.

| x1 | T/K |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | 293.15 | 298.15 | 303.15 | 308.15 | 313.15 | 318.15 | 323.15 |

DMA + PEG 400

| 0.0000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.0732 | -0.232 | -0.257 | -0.279 | -0.298 | -0.317 | -0.340 | -0.360 |
| 0.1472 | -0.464 | -0.501 | -0.536 | -0.572 | -0.607 | -0.645 | -0.681 |
| 0.2055 | -0.645 | -0.692 | -0.736 | -0.778 | -0.820 | -0.866 | -0.910 |
| 0.2649 | -0.837 | -0.888 | -0.938 | -0.985 | -1.037 | -1.091 | -1.141 |
| 0.3485 | -1.117 | -1.173 | -1.229 | -1.286 | -1.346 | -1.406 | -1.464 |
| 0.4253 | -1.397 | -1.463 | -1.530 | -1.587 | -1.652 | -1.720 | -1.783 |
| 0.4985 | -1.696 | -1.767 | -1.841 | -1.902 | -1.976 | -2.049 | -2.118 |
| 0.5833 | -2.099 | -2.181 | -2.269 | -2.337 | -2.419 | -2.503 | -2.584 |
| 0.6520 | -2.485 | -2.580 | -2.680 | -2.759 | -2.852 | -2.948 | -3.043 |
| 0.7287 | -2.989 | -3.110 | -3.235 | -3.343 | -3.461 | -3.584 | -3.710 |
| 0.7974 | -3.519 | -3.685 | -3.853 | -4.006 | -4.171 | -4.342 | -4.516 |
| 0.8693 | -4.163 | -4.405 | -4.657 | -4.896 | -5.150 | -5.410 | -5.674 |
| 0.9322 | -4.784 | -5.134 | -5.513 | -5.869 | -6.252 | -6.643 | -7.032 |
| 1.0000 | -5.538 | -6.073 | -6.690 | -7.239 | -7.851 | -8.471 | -9.069 |

DMA + PEG 600

| 0.0000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.0718 | -0.304 | -0.325 | -0.347 | -0.368 | -0.395 | -0.420 | -0.443 |
| 0.1430 | -0.624 | -0.664 | -0.708 | -0.754 | -0.800 | -0.843 | -0.889 |
| 0.2128 | -0.948 | -1.007 | -1.065 | -1.132 | -1.198 | -1.259 | -1.324 |
| 0.2912 | -1.338 | -1.411 | -1.482 | -1.565 | -1.644 | -1.721 | -1.802 |
| 0.3702 | -1.759 | -1.842 | -1.923 | -2.016 | -2.103 | -2.199 | -2.294 |
| 0.4450 | -2.183 | -2.276 | -2.366 | -2.467 | -2.565 | -2.669 | -2.771 |
| 0.5072 | -2.565 | -2.664 | -2.760 | -2.868 | -2.975 | -3.085 | -3.197 |
| 0.5785 | -3.047 | -3.152 | -3.257 | -3.371 | -3.489 | -3.609 | -3.734 |
| 0.6511 | -3.587 | -3.704 | -3.822 | -3.948 | -4.080 | -4.215 | -4.357 |
| 0.7207 | -4.151 | -4.291 | -4.433 | -4.585 | -4.741 | -4.903 | -5.075 |
| 0.7998 | -4.846 | -5.037 | -5.232 | -5.439 | -5.649 | -5.868 | -6.102 |
| 0.8701 | -5.501 | -5.774 | -6.055 | -6.345 | -6.645 | -6.951 | -7.275 |
| 0.9385 | -6.128 | -6.537 | -6.958 | -7.381 | -7.841 | -8.280 | -8.739 |
| 1.0000 | -6.668 | -7.257 | -7.867 | -8.455 | -9.143 | -9.748 | -10.368 |

Table S9. Excess partial molar isentropic compressibilities, 1014Ks.m,1E/(m5 N−1 mol−1) of DMA as a function of mole fraction, x1 of DMA in DMA + PEG 200/ PEG 300/ PEG 400/ PEG 600 binary mixture at temperatures, T/K = (293.15 − 323.15)

| x1 | T/K |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | 293.15 | 298.15 | 303.15 | 308.15 | 313.15 | 318.15 | 323.15 |

DMA + PEG 200

| 0.0000 | -0.630 | -0.725 | -0.809 | -0.883 | -0.962 | -1.044 | -1.127 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.0584 | -0.658 | -0.737 | -0.815 | -0.889 | -0.967 | -1.044 | -1.141 |
| 0.1152 | -0.669 | -0.740 | -0.813 | -0.886 | -0.962 | -1.036 | -1.133 |
| 0.2003 | -0.669 | -0.732 | -0.799 | -0.866 | -0.938 | -1.008 | -1.096 |
| 0.2790 | -0.652 | -0.710 | -0.773 | -0.834 | -0.901 | -0.967 | -1.044 |
| 0.3756 | -0.615 | -0.668 | -0.722 | -0.777 | -0.838 | -0.897 | -0.959 |
| 0.4655 | -0.565 | -0.612 | -0.661 | -0.709 | -0.762 | -0.814 | -0.868 |
| 0.5320 | -0.519 | -0.560 | -0.605 | -0.648 | -0.695 | -0.741 | -0.792 |
| 0.6027 | -0.461 | -0.496 | -0.536 | -0.574 | -0.614 | -0.653 | -0.701 |
| 0.6652 | -0.401 | -0.432 | -0.465 | -0.499 | -0.535 | -0.569 | -0.613 |
| 0.7327 | -0.328 | -0.353 | -0.382 | -0.410 | -0.442 | -0.470 | -0.509 |
| 0.8046 | -0.244 | -0.264 | -0.285 | -0.308 | -0.332 | -0.355 | -0.387 |
| 0.8708 | -0.162 | -0.177 | -0.192 | -0.207 | -0.224 | -0.241 | -0.264 |
| 0.9294 | -0.089 | -0.097 | -0.106 | -0.115 | -0.124 | -0.134 | -0.148 |
| 1.0000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 |

DMA + PEG 300

| 0.0000 | -1.029 | -1.135 | -1.252 | -1.416 | -1.537 | -1.669 | -1.820 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.0712 | -1.018 | -1.108 | -1.207 | -1.321 | -1.429 | -1.486 | -1.678 |
| 0.1422 | -1.008 | -1.087 | -1.173 | -1.266 | -1.363 | -1.434 | -1.585 |
| 0.2123 | -0.989 | -1.059 | -1.136 | -1.219 | -1.307 | -1.375 | -1.508 |
| 0.2813 | -0.961 | -1.026 | -1.096 | -1.174 | -1.253 | -1.318 | -1.429 |
| 0.3584 | -0.920 | -0.979 | -1.038 | -1.106 | -1.176 | -1.241 | -1.329 |
| 0.4216 | -0.876 | -0.928 | -0.981 | -1.044 | -1.106 | -1.167 | -1.239 |
| 0.4970 | -0.812 | -0.857 | -0.902 | -0.956 | -1.009 | -1.063 | -1.124 |
| 0.5616 | -0.745 | -0.786 | -0.826 | -0.870 | -0.918 | -0.963 | -1.018 |
| 0.6525 | -0.635 | -0.669 | -0.702 | -0.733 | -0.773 | -0.807 | -0.854 |
| 0.7472 | -0.498 | -0.525 | -0.552 | -0.576 | -0.606 | -0.630 | -0.672 |
| 0.8004 | -0.409 | -0.434 | -0.456 | -0.477 | -0.502 | -0.520 | -0.558 |
| 0.8667 | -0.287 | -0.305 | -0.323 | -0.339 | -0.358 | -0.373 | -0.400 |
| 0.9311 | -0.156 | -0.167 | -0.176 | -0.188 | -0.198 | -0.209 | -0.224 |
| 1.0000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 |

Table S9. Contd.

| x1 | T/K |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | 293.15 | 298.15 | 303.15 | 308.15 | 313.15 | 318.15 | 323.15 |

DMA + PEG 400

| 0.0000 | -1.693 | -1.915 | -2.100 | -2.157 | -2.548 | -2.787 | -2.968 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.0732 | -1.655 | -1.815 | -1.975 | -2.075 | -2.341 | -2.478 | -2.727 |
| 0.1472 | -1.608 | -1.740 | -1.881 | -2.007 | -2.199 | -2.350 | -2.545 |
| 0.2055 | -1.566 | -1.686 | -1.813 | -1.943 | -2.102 | -2.236 | -2.420 |
| 0.2649 | -1.516 | -1.624 | -1.737 | -1.861 | -1.998 | -2.125 | -2.284 |
| 0.3485 | -1.425 | -1.524 | -1.618 | -1.724 | -1.839 | -1.947 | -2.076 |
| 0.4253 | -1.323 | -1.404 | -1.481 | -1.570 | -1.668 | -1.762 | -1.859 |
| 0.4985 | -1.208 | -1.273 | -1.336 | -1.404 | -1.487 | -1.565 | -1.636 |
| 0.5833 | -1.048 | -1.100 | -1.149 | -1.199 | -1.265 | -1.322 | -1.376 |
| 0.6520 | -0.904 | -0.943 | -0.981 | -1.018 | -1.073 | -1.119 | -1.165 |
| 0.7287 | -0.726 | -0.755 | -0.784 | -0.811 | -0.853 | -0.889 | -0.927 |
| 0.7974 | -0.554 | -0.576 | -0.598 | -0.621 | -0.653 | -0.680 | -0.713 |
| 0.8693 | -0.364 | -0.381 | -0.397 | -0.413 | -0.436 | -0.456 | -0.482 |
| 0.9322 | -0.190 | -0.201 | -0.211 | -0.223 | -0.236 | -0.249 | -0.265 |
| 1.0000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 |

DMA + PEG 600

| 0.0000 | -1.803 | -2.161 | -2.457 | -2.794 | -2.859 | -3.365 | -3.749 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.0718 | -2.156 | -2.421 | -2.661 | -2.928 | -3.131 | -3.543 | -3.766 |
| 0.1430 | -2.325 | -2.536 | -2.742 | -2.962 | -3.202 | -3.500 | -3.722 |
| 0.2128 | -2.384 | -2.566 | -2.750 | -2.946 | -3.173 | -3.437 | -3.643 |
| 0.2912 | -2.375 | -2.534 | -2.704 | -2.877 | -3.078 | -3.322 | -3.527 |
| 0.3702 | -2.316 | -2.462 | -2.613 | -2.772 | -2.942 | -3.152 | -3.354 |
| 0.4450 | -2.213 | -2.343 | -2.486 | -2.627 | -2.764 | -2.950 | -3.133 |
| 0.5072 | -2.099 | -2.213 | -2.339 | -2.470 | -2.580 | -2.737 | -2.904 |
| 0.5785 | -1.913 | -2.012 | -2.123 | -2.240 | -2.331 | -2.459 | -2.598 |
| 0.6511 | -1.668 | -1.748 | -1.845 | -1.933 | -2.017 | -2.120 | -2.226 |
| 0.7207 | -1.388 | -1.450 | -1.524 | -1.602 | -1.674 | -1.751 | -1.829 |
| 0.7998 | -1.018 | -1.065 | -1.115 | -1.172 | -1.225 | -1.283 | -1.339 |
| 0.8701 | -0.664 | -0.690 | -0.727 | -0.761 | -0.792 | -0.834 | -0.866 |
| 0.9385 | -0.300 | -0.314 | -0.329 | -0.345 | -0.360 | -0.382 | -0.399 |
| 1.0000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 |

Table S10. Excess partial molar isentropic compressibilities, 1014Ks.m,2E/(m5 N−1 mol−1) of PEGs as a function of mole fraction, x1 of DMA in DMA + PEG 200/ PEG 300/ PEG 400/ PEG 600 binary mixture at temperatures, T/K = (293.15 − 323.15)

| x1 | T/K |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | 293.15 | 298.15 | 303.15 | 308.15 | 313.15 | 318.15 | 323.15 |

DMA + PEG 200

| 0.0000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.0584 | -0.037 | -0.042 | -0.047 | -0.051 | -0.056 | -0.061 | -0.067 |
| 0.1152 | -0.074 | -0.083 | -0.092 | -0.102 | -0.111 | -0.121 | -0.132 |
| 0.2003 | -0.131 | -0.145 | -0.162 | -0.177 | -0.194 | -0.212 | -0.234 |
| 0.2790 | -0.185 | -0.205 | -0.227 | -0.250 | -0.273 | -0.300 | -0.331 |
| 0.3756 | -0.259 | -0.286 | -0.314 | -0.346 | -0.378 | -0.415 | -0.453 |
| 0.4655 | -0.339 | -0.373 | -0.410 | -0.447 | -0.489 | -0.534 | -0.578 |
| 0.5320 | -0.408 | -0.448 | -0.491 | -0.534 | -0.581 | -0.632 | -0.682 |
| 0.6027 | -0.494 | -0.541 | -0.591 | -0.640 | -0.692 | -0.750 | -0.806 |
| 0.6652 | -0.582 | -0.635 | -0.691 | -0.746 | -0.807 | -0.871 | -0.933 |
| 0.7327 | -0.691 | -0.751 | -0.816 | -0.880 | -0.950 | -1.023 | -1.097 |
| 0.8046 | -0.823 | -0.893 | -0.968 | -1.045 | -1.128 | -1.214 | -1.308 |
| 0.8708 | -0.957 | -1.041 | -1.129 | -1.220 | -1.320 | -1.424 | -1.542 |
| 0.9294 | -1.083 | -1.183 | -1.286 | -1.394 | -1.516 | -1.643 | -1.788 |
| 1.0000 | -1.233 | -1.367 | -1.491 | -1.626 | -1.787 | -1.959 | -2.143 |

DMA + PEG 300

| 0.0000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.0712 | -0.070 | -0.078 | -0.086 | -0.095 | -0.103 | -0.112 | -0.123 |
| 0.1422 | -0.142 | -0.155 | -0.170 | -0.185 | -0.202 | -0.221 | -0.241 |
| 0.2123 | -0.210 | -0.228 | -0.250 | -0.271 | -0.296 | -0.325 | -0.356 |
| 0.2813 | -0.278 | -0.303 | -0.334 | -0.362 | -0.394 | -0.431 | -0.471 |
| 0.3584 | -0.362 | -0.395 | -0.431 | -0.465 | -0.507 | -0.554 | -0.605 |
| 0.4216 | -0.437 | -0.475 | -0.518 | -0.563 | -0.611 | -0.665 | -0.723 |
| 0.4970 | -0.541 | -0.584 | -0.633 | -0.689 | -0.745 | -0.808 | -0.876 |
| 0.5616 | -0.643 | -0.692 | -0.747 | -0.812 | -0.874 | -0.943 | -1.019 |
| 0.6525 | -0.822 | -0.879 | -0.942 | -1.013 | -1.085 | -1.163 | -1.245 |
| 0.7472 | -1.073 | -1.142 | -1.213 | -1.293 | -1.375 | -1.464 | -1.560 |
| 0.8004 | -1.253 | -1.333 | -1.413 | -1.499 | -1.591 | -1.688 | -1.796 |
| 0.8667 | -1.534 | -1.633 | -1.731 | -1.832 | -1.941 | -2.058 | -2.187 |
| 0.9311 | -1.884 | -2.013 | -2.138 | -2.273 | -2.406 | -2.556 | -2.719 |
| 1.0000 | -2.366 | -2.548 | -2.722 | -2.930 | -3.102 | -3.308 | -3.530 |

Table S10. Contd.

| x1 | T/K |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | 293.15 | 298.15 | 303.15 | 308.15 | 313.15 | 318.15 | 323.15 |

DMA + PEG 400

| 0.0000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.0732 | -0.123 | -0.135 | -0.148 | -0.153 | -0.177 | -0.194 | -0.211 |
| 0.1472 | -0.242 | -0.266 | -0.292 | -0.311 | -0.351 | -0.383 | -0.414 |
| 0.2055 | -0.337 | -0.369 | -0.407 | -0.438 | -0.488 | -0.530 | -0.580 |
| 0.2649 | -0.438 | -0.476 | -0.525 | -0.567 | -0.629 | -0.688 | -0.752 |
| 0.3485 | -0.586 | -0.641 | -0.705 | -0.769 | -0.843 | -0.916 | -1.010 |
| 0.4253 | -0.736 | -0.803 | -0.880 | -0.966 | -1.052 | -1.143 | -1.255 |
| 0.4985 | -0.898 | -0.977 | -1.065 | -1.167 | -1.265 | -1.370 | -1.494 |
| 0.5833 | -1.108 | -1.205 | -1.304 | -1.419 | -1.530 | -1.646 | -1.781 |
| 0.6520 | -1.308 | -1.410 | -1.514 | -1.632 | -1.755 | -1.879 | -2.019 |
| 0.7287 | -1.563 | -1.670 | -1.777 | -1.897 | -2.027 | -2.159 | -2.300 |
| 0.7974 | -1.826 | -1.935 | -2.046 | -2.168 | -2.307 | -2.445 | -2.591 |
| 0.8693 | -2.140 | -2.261 | -2.379 | -2.509 | -2.664 | -2.819 | -2.982 |
| 0.9322 | -2.450 | -2.597 | -2.729 | -2.882 | -3.064 | -3.250 | -3.452 |
| 1.0000 | -2.825 | -3.033 | -3.194 | -3.400 | -3.637 | -3.887 | -4.169 |

DMA + PEG 600

| 0.0000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 | 0.000 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.0718 | -0.138 | -0.161 | -0.180 | -0.203 | -0.220 | -0.249 | -0.272 |
| 0.1430 | -0.292 | -0.330 | -0.365 | -0.402 | -0.441 | -0.482 | -0.524 |
| 0.2128 | -0.448 | -0.499 | -0.547 | -0.601 | -0.667 | -0.718 | -0.775 |
| 0.2912 | -0.627 | -0.691 | -0.755 | -0.824 | -0.929 | -1.004 | -1.081 |
| 0.3702 | -0.829 | -0.911 | -0.987 | -1.072 | -1.213 | -1.306 | -1.408 |
| 0.4450 | -1.050 | -1.148 | -1.244 | -1.344 | -1.503 | -1.631 | -1.756 |
| 0.5072 | -1.280 | -1.390 | -1.498 | -1.616 | -1.780 | -1.933 | -2.085 |
| 0.5785 | -1.596 | -1.726 | -1.853 | -1.992 | -2.166 | -2.351 | -2.530 |
| 0.6511 | -1.997 | -2.144 | -2.297 | -2.448 | -2.640 | -2.850 | -3.054 |
| 0.7207 | -2.473 | -2.636 | -2.807 | -2.986 | -3.192 | -3.414 | -3.640 |
| 0.7998 | -3.105 | -3.288 | -3.482 | -3.687 | -3.909 | -4.144 | -4.397 |
| 0.8701 | -3.721 | -3.914 | -4.132 | -4.357 | -4.590 | -4.844 | -5.111 |
| 0.9385 | -4.289 | -4.502 | -4.733 | -4.982 | -5.223 | -5.527 | -5.819 |
| 1.0000 | -4.721 | -4.957 | -5.199 | -5.472 | -5.697 | -6.107 | -6.435 |