## Supporting Information

A Systematic Review on Life Cycle Assessment (LCA) of Metal Organic Frameworks (MOFs) and MXenes

Andrei Ungureanu1,2, Antonella Sola1,2, Anna Maria Ferrari1,2 and Roberto Rosa1,2

1Department of Sciences and Methods for Engineering, University of Modena and Reggio Emilia, via Amendola 2, 42122 Reggio Emilia, Italy

2Interdepartmental Center En&Tech, University of Modena and Reggio Emilia, Tecnopolo di Reggio Emilia, Piazzale Europa 1, 42123 Reggio Emilia, Italy

Number of pages: 21

Number of Tables: 4

Table S1	LCA of MOFs and MXenes: A chronological literature review focused on study scope, system boundaries, scale, functional unit (FU) and key findings.

|  | Author and Year | Study Scope | System Boundaries | Scale and functional unit | Key Findings |
| --- | --- | --- | --- | --- | --- |
| 1. | Grande et al. (2017) [25] | To assess the environmental impacts of CPO-27-Ni MOF production and optimizing a methodology for eco-design of MOF materials for CCS technologies | Cradle-to-gate | Lab-scale (scale-up framework) FU: 1 kg of CPO-27-Ni MOF powder | CPO-27-Ni synthesis impact dominated by solvent use; switching to water-based synthesis reduced GHG emissions from 1136.2 to 12.3 kg CO₂ eq., and significantly lowered freshwater toxicity and resource depletion. |
| 2. | Garcia-Palacin et al. (2020) [65] | Eco-balance methodology applied to ZIF-8 nanoparticle synthesis from recycled mother liquors, evaluating different deprotonators, washing steps, and drying procedures. | Cradle-to-gate | Lab-scale (synthesis of ZIF-8 nanocrystals). | Recycling mother liquors reduced solvent use for washing, improving environmental impacts. Using NH₄OH as a deprotonator had lower environmental impacts than NaOH. |
| 3. | Hu et al. (2021) [31] | Assessing the overall environmental impact of approximately 50 diverse MOFs for post-combustion CCS and comparing them to MEA scrubbing technology. | Cradle-to-gate for CCS process, comprising MOF production (precursors, solvents, electricity) and MOF use (CO2 separation, MOF regeneration, CO2 compression). Includes solvent and metal recycling. | Lab-scale (scale-up framework). FU: 1 t CO2 | Solvent type and quantity are major contributors to MOF environmental impacts, particularly EUP. Organic solvents like DMF and DMA exhibit high EUP, often exceeding that of MEA, even with high recycling rates. Enhancing solvent recycling and selecting greener alternatives are essential for improving MOF sustainability. Five MOFs were identified as more environmentally favourable than MEA. |
| 4. | Ntouros et al. (2021) [29] | Environmental performance assessment of five different synthetic routes of ZIF-8 nanomaterials, investigating different solvents and synthetic steps. | Cradle-to-gate | Lab-scale (scale-up) FU: 1 kg of produced ZIF-8 powder. | DMF and MeOH contributed over 85% of environmental impacts as solvents/washing agents. Electricity (up to 13%) was another hotspot, especially with fossil-based energy. De-ionized water showed minimal impact (<2%). |
| 5. | Pioquinto-García et al. (2021) [30] | Environmental assessment of MOF DUT-4 synthesis, evaluating the effect of different solvents. The main application was siloxane removal for biogas purification (Not included in the LCA). | Cradle-to-gate | Lab-scale including mixing, synthesis, cleaning, solvent exchange, and drying. FU: 1 g of DUT-4 | Solvothermal synthesis showed the highest environmental impacts due to organic solvents (DMF, DCM, hexane) used in synthesis, washing, and solvent exchange. Chemical reagent production accounted for 79.1–91.1% of total environmental damage. |
| 6. | Mohamed and Bicer (2022) [28] | Computational screening to select and evaluate MOFs as nitrogen fixation photocatalysts, integrating LCA to quantify and compare materials from an environmental perspective. | Cradle-to-gate | Lab-scale FU: 1 g of MOF material. | Environmental burden ranked as Fe₂Cl₂(BBTA) > Zn₂(mDOBDC) > Fe₂(mDOBDC) > Ni-BTP, mainly due to solvent use. Fe₂Cl₂(BBTA) had the highest impact due to more chemical steps and solvent consumption. Reducing solvent use and incorporating waste materials (e.g., plastics) can significantly lower impacts. |
| 7. | Carvalho et al. (2022) [37] | Environmental-economic assessment comparing Na-ion coin cells with Ti1Al1TiC1.85 MXene as anode material (SIB) with Li-ion batteries (LIBs). | Cradle-to-gate | Lab-scale for Na-ion battery, compared to industrial LIBs. FU: 1 kWh of battery capacity. | SIBs have lower environmental performance than LIBs when compared by energy density, due to lower efficiency. By mass, SIBs are promising alternatives, using fewer critical raw materials, but they still consume more natural resources over their life cycle, even at industrial scale. |
| 8. | Yang et al. (2022) [60] | To evaluate the environmental impacts of synthesizing vanadium-based MOFs (MIL-47) on CNT fibres from gasification waste for Zn-ion batteries, and to identify process hotspots and improvements for a sustainable, closed-loop battery fabrication route. | Cradle-to-gate | Lab-scale FU: 1.0 kg fibre-shaped ZIBs. | Fabrication of w-MIL-47@CNT cathodes was the main environmental hotspot, dominating 13 of 17 impact categories. Methanol recovery, replacing Argon with N₂, and reducing the amounts of NH₄Cl significantly lowered impacts. |
| 9. | Rico-Barragán et al. (2023) [55] | To develop a cleaner synthesis route for MIL-101(Cr) by evaluating its environmental (via LCA), technical (adsorption performance), and economic feasibility, aiming to optimize MOF production for toluene capture in a sustainable framework. | Cradle-to-gate | Lab-scale FU: 1 g of MIL-101(Cr). | The major impacts were driven by DMF and chromium nitrate use. DMF also raised synthesis costs by 30–35%. A cleaner MIL-101(Cr) synthesis using PET and no DMF, reduced environmental impacts by 64% and was 34% more cost-effective. |
| 10. | Dadashi Firouzjaei et al. (2023) [34] | Assessing the cumulative energy demand (CED) and environmental impacts of lab-scale synthesis of Ti3C2Tx MXene, with a focus on its application for electromagnetic interference (EMI) shielding. | Cradle-to-gate | Two lab-scale sizes: small (19.2 g per batch, g-Ti3C2Tx) and large (800 g per batch, kg-Ti3C2Tx). | Producing 1 kg of Ti3C2Tx MXene required ~1/9 the energy of lab-scale (g-level) production, showing strong scale-up benefits. However, MXene production still had much higher energy demand than Al or Cu foil (CED: 17.364 vs 0.517 and 1.131 GJ-eq). Titanium was the main contributor (~75%) to environmental impact, followed by Al and LiCl. Reducing equipment energy use, synthesis time, and switching to renewables are key to improving sustainability. |
| 11. | De Miranda et al. (2023) [56] | Comparing hydrothermal production of MIL-53(Al) with different reaction times and proposing a more sustainable synthesis route including Al recovery and solvent volume reduction. The main goal was separation and COCNT capture (not included in the LCA). | Cradle-to-gate | Lab-scale FU: 1 kg of MIL-53(Al). | Reducing reaction time from 72h to 24h lowered electricity consumption by 66.7%. Additional measures—Al recovery and reduced solvent volume—led to major environmental improvements: MD (−77.1%), FET (−70.4%), PM (−65%), CC (−44.7%), and HT (−43.3%). |
| 12. | Escobar-Hernandez et al. (2023) [58] | Studying the sustainability of MOF technology through potential industrial production at large scale, specifically a comparative LCA of four different ZIF-67 synthesis routes (solvothermal vs. reactive extrusion). | Cradle-to-grave | Lab-scale (scale-up framework) FU: 1 kg ZIF-67 | Reactive extrusion synthesis was found to be several orders of magnitude (∼3−5) lower than the traditional solvothermal reaction in terms of environmental and health impacts. Solvents (methanol, DMF, and TEA) were significant contributors to environmental impacts in solvothermal synthesis. |
| 13. | Chang et al. (2024) [59] | Comparing the production cost and LCA of MIL-100(Fe)-ore synthesized from iron ore concentrates with traditional MIL-100(Fe) produced from elemental iron and iron salts. | Cradle-to-gate | Lab-scale FU: 1 mg of produced MIL-100(Fe) powder. | Synthesis of MIL-100(Fe) with iron ore concentrates greatly reduced the synthesis cost and reduced the environmental impacts compared to the traditional method. |
| 14. | Dutta et al. (2024) [24] | LCA of 10 industrially produced and widely explored MOFs across 18 diverse environmental impact categories, comparing different synthetic methods of each MOF. | Cradle-to-gate | lab-scale (scale-up framework) FU: 1 kg of MOF | The washing step is a major contributor to MOF environmental impacts due to high organic solvent use, often accounting for 80–90% of total impact. Organic solvents outweigh other factors like energy use and chemical toxicity. Minimizing or replacing them with greener alternatives (e.g., water) is strongly recommended for improving sustainability. Mechanochemical synthesis shows lower impacts but still requires solvent optimization. |
| 15. | Ghaedi et al. (2024) [61] | LCA and cost analysis of biochar (BC), UiO-67, and UBC (UiO-67/biochar) composites with varying MOF-to-biochar ratios. | Cradle-to-gate | Lab-scale FU: 1 kg MOF, MOF/biochar composites | Pure UiO-67 had the highest cost (67.58 $/kg) and CO₂ emissions (195.41 kg CO₂-eq/kg) compared to biochar (0.4 $/kg, 0.32 kg CO₂-eq/kg). Increasing MOF content in composites raised both cost and emissions. The optimal MOF-to-composite ratio for sorption with minimal cost and emissions was 61–62%. |
| 16. | Hansen et al. (2024) [26] | Applied the SSbD framework on Ti3C2Tx MXenes, including a prospective LCA. | Cradle-to-gate | Prospective LCA to assess impacts at future large-scale production. FU: 1 kg of Ti3C2Tx powder. | Ti powder production is a major environmental hotspot due to the energy-intensive Kroll process. Using more sustainable Ti sources and increasing recycled content are key to reducing impacts. Switching to low-carbon electricity has a smaller but still positive effect. |
| 17. | Mohtar et al. (2024) [66] | Evaluating the carbon footprint of preserving cinematographic and photographic films using MIL-100(Fe). LCA of the new MOF-based solution compared to the classical method. | Cradle-to-grave | Lab-scale FU: 1 package unit stored for 100 years under five different scenarios. | LCA results indicated a reduction of the carbon footprint related to movie film preservation by approximately 50% when considering the current EU energy mix, and about 40% considering the 2030 EU energy mix, when using MIL-100(Fe). |
| 18. | Tao and Brander (2024) [32] | Consequential LCA (CLCA) of coal-fired power generation in the US, comparing MEA-based and Mg-MOF-74-based carbon capture. Aims to address gaps in full life cycle, systemic effects in plants, and comparative reduction potential. | Cradle-to-grave for the full system. | Lab-scale (scale-up framework) FU: 1 kg of Mg-MOF-74 | Carbon capture greatly reduces emissions from coal power (e.g., 779.5 to 50.1 Mt CO2e for MEA; 61.1 Mt CO2e for Mg-MOF-74 by 2050). MOF-74 shows higher environmental impacts than MEA due to the emissions associated with solvent use and washing stage and to a lesser extent, the ligand preparation. Metal and energy contributions are minor. Variations in adsorption and degradation affect results by 4–6%. |
| 19. | Ungureanu et al. (2024) [36] | Systematic LCA comparison among seven different synthetic pathways of the same Ti3C2Tx MXene, differing in MAX phase precursors, etching, and delamination procedures. | Cradle-to-gate | Lab-scale FU: 1 g Ti3C2Tx MXene | The earliest reported Ti3C2Tx synthesis had the lowest environmental impact across all categories. In contrast, newer methods the highest impacts, mainly due to high electricity use during etching and delamination and MAX phase production. Using alternative MAX phase raw materials (e.g., from recycled materials) could reduce impacts by up to 30%. |
| 20. | Zu et al. (2024) [40] | To assess the environmental impact of using cathodic polarization to enhance the stability and reusability of Ti3C2Tx MXene catalysts in Fenton-like water purification, aiming to support the development of efficient and sustainable advanced oxidation processes. | Cradle-to-gate | Lab-scale FU: Removal of 1 μmol contaminant (i.e., carbamazepine). | Ti3C2 hydrogel catalysts had the highest environmental impact in one-off systems (>99% normalized impact). Reusing MXene is critical to reducing environmental burden in Fenton-like reactions. Extending Ti3C2 lifespan further lowers environmental impacts. |
| 21. | Wang et al. (2025) [33] | Systematically evaluating the environmental impacts of MOF-74 series adsorbents (Co-MOF-74, Mg-MOF-74, Ni-MOF-74, Zn-MOF-74) in CO2 capture and comparing results with MEA-based chemical absorption technology. | Cradle-to-gate for the whole system Cradle-to-grave for MOF, considering raw material extraction, manufacturing, use, recycling, and disposal. | Large-scale commercial application. FU: 1 t of CO2 captured | Mg-MOF-74 had the highest environmental impact among four adsorbents, with Zn-MOF-74 performing best (average impacts 40% lower). DMF used in synthesis contributed up to 80% of impacts. Heat-related GWP stemmed mainly from energy use in carbon capture. MOF yield and CO2 capture energy were key uncertainty factors. Ni-MOF-74 showed high uncertainty due to ethanol use. |
| 22. | Jia et al. (2025) [27] | Assessing the environmental impacts of different preparation methods for ZIF-8 hydrogen-selective membranes to identify the most environmentally friendly method. | Cradle-to-gate | Lab-scale FU: 1 cm² membrane | The second repair growth method for ZIF-8 membranes showed the lowest environmental impact across all categories, due to low energy use and room-temperature processing, outperforming seed growth, plasma-assisted, and sol-gel methods. |
| 23. | Zu et al. (2025) [39] | To quantify the environmental impacts of reductant-driven Fenton-like advanced oxidation processes compared to conventional systems, and to identify how reductant choice and system design influence sustainability in water purification technologies. | Cradle-to-gate | Lab-scale synthesis for MoS2 and MXene. FU: Reduction of 2 μM CBZ concentration by one order of magnitude in 100 mL wastewater using the proposed AOPs. | Reductant-driven Fenton-like systems showed varied environmental impacts. Hydroxylamine and ascorbic acid reduced impacts compared to Fe/PMS, while MoS2 and MXene increased them due to energy- and chemical-intensive synthesis. MoS2 had the highest impact, mainly from MoO2. MXene had moderate impact, which dropped further with renewable energy and sludge regeneration. |
| 24. | Srivastava et al. (2025) | NiMoSe/Ti3C2Tx@CC electrocatalysts for hydrogen evolution reaction (HER) in acidic media. | Cradle-to-gate | Lab-scale FU: 1 mg cm−2 loading of electrocatalysts. | The electrocatalyst showed high environmental impacts in categories such as global warming potential, acidification, and resource use (fossil and metals). |
| 25. | Meng et al. (2025) [67] | To evaluate the environmental impacts of piezo-photocatalytic BM-1 heterojunctions for selective 1O2 generation and pretreatment of antibiotic wastewater. | Not specified (assumed cradle-to-gate) | Lab-scale, with discussion of industrial scale-up potential. FU: 4.5 ton of 5ppm ofloxacin (OFX) wastewater. | The BM-1 heterojunction exhibited significantly lower environmental impacts than MIL-88A(Fe) and V-BiOIO3 across both preparation and application stages, likely due to its superior piezo-photocatalytic activity. Its lower energy demand and elimination of H₂O₂ transport enhance sustainability. The system shows strong potential for scalable, eco-friendly antibiotic wastewater pretreatment. |
| 26. | Wu et al. (2025) [57] | To evaluate the industrial-scale potential of using ZIF-8 biochar (ZB) as an adsorbent for the selective recovery of precious metals, by conducting LCA alongside testing two different remediation methods. | Not specified (assumed cradle-to-gate) | Lab-scale FU: the input and output data required to treat 1 kg of pure water | The LCA results for MOFs were not detailed. |

Table S2	Methodological approaches for LCA across the reviewed studies

|  | Author and Year | Software | Database | Method | Impact Categories covered |
| --- | --- | --- | --- | --- | --- |
| 1. | Grande et al. (2017) [1] | Simapro | Ecoinvent | ILCD | CC, PMFP, FEP, FETP, and RD (mineral, fossil and renewable). |
| 2. | Garcia-Palacin et al. (2020) [2] | - | - | Eco-balance | - |
| 3. | Hu et al. (2021) [3] | - | Ecoinvent | TRACI | 10 midpoint1 |
| 4. | Ntouros et al. (2021) [4] | Simapro | Ecoinvent | ReCipe | 18 midpoint2, 3 endpoint3 |
| 5. | Pioquinto-García et al. (2021) [5] | Simapro | Ecoinvent | ReCiPe | CC, FD, PM |
| 6. | Mohamed and Bicer (2022) [6] | GaBi | Nuss and Eckelman | ReCipe | GW, ED, AP, FEP |
| 7. | Carvalho et al. (2022) [7] | Simapro | Ecoinvent | EF | 16 midpoint4 |
| 8. | Yang et al. (2022) [8] | GaBi | Ecoinvent | ReCiPe | 18 midpoint (without LU) |
| 9. | Rico-Barragán et al. (2023) [9] | Simapro | Ecoinvent | ReCiPe | Midpoint (focused on CC, FD, MD, PM and HT) and endpoint3 |
| 10. | Dadashi Firouzjaei et al. (2023) [10] | openLCA | Ecoinvent | TRACI, CED | 10 midpoint1 |
| 11. | De Miranda et al. (2023) [11] | Umberto | Ecoinvent | ReCiPe | 18 mindpoint2 |
| 12. | Escobar-Hernandez et al. (2023) [12] | openLCA | Agrylife, Ecoinvent, and ILCD | TRACI | 10 midpoint1 |
| 13. | Chang et al. (2024) [13] | - | Ecoinvent | ReCiPe | 18 midpoint2 |
| 14. | Dutta et al. (2024) [14] | openLCA | Ecoinvent | ReCiPe | 18 midpoint2 |
| 15. | Ghaedi et al. (2024) [15] | - | - | - | Climate Change |
| 16. | Hansen et al. (2024) [16] | openLCA | Ecoinvent | EF | 16 midpoint (focused on GW, FE, AP, OD, WU, MR) |
| 17. | Mohtar et al. (2024) [17] | - | - | - | GWP (carbon footprint) |
| 18. | Tao and Brander (2024) [18] | - | Ecoinvent | ReCiPe | GWP |
| 19. | Ungureanu et al. (2024) [19] | Simapro | Ecoinvent | ReCiPe | 18 midpoint2 and 3 endpoint3 |
| 20. | Zu et al. (2024) [20] | - | Ecoinvent | ReCiPe, CED | 3 endpoint3 |
| 21. | Wang et al. (2025) [21] | - | Ecoinvent | ReCipe | AP, EUP, ME, GWP, OD, HT, FE |
| 22. | Jia et al. (2025) [22] | - | Ecoinvent | ReCiPe | 12 midpoint: GWP, FDP, FETP, FEP, HTP, METP, MEP, ODP, PMFP, POFP, TAP, and TETP |
| 23. | Zu et al. (2025) [23] | Simapro | Ecoinvent | ReCiPe, CED | 18 midpoint2 and 3 endpoint3 |
| 24. | Srivastava et al. (2025) | GaBi | Thinkstep | EF | AP, GWP, FEP, HTC, PM, RU-F, RU-MM, WU |
| 25. | Meng et al. (2025) [24] | - | - | ReCiPe | 18 midpoint2 |
| 26. | Wu et al. (2025) [25] | openLCA | Ecoinvent | ReCiPe | FETP, FEP, GWP, HTNC, MEP, MRS, WC |

1TRACI midpoint indicators: OD, GWP, Smog, AP, EP, HTC, HTNC, RE, ETP, FD

2ReCiPe midpoint indicators: GWP, ODP, IR, OF-HH, OF-TE, PMFP, IR, TAP, FEP, MEP, TETP, METP, HTC, HTNC, LU, MRS, FRS, WU

3Recipe endpoint indicators: human health, ecosystems, and resources

4EF midpoint indicators: AP, CC, FETP, PM, MEP, FEP, TEP, HTC, HTNC, IR, LU, OD, POF, RU-F, RU-MM

Table S3	  LCA of MOFs case studies identified within the 26 studies reviewed.

| MOF | Method | metal salt | ligand | reaction solvent | washing/ exchange | main conditions | Experimental reference | LCA reference |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| CPO-27-Ni | Solvothermal | Ni(NO3)2·6H2O | DHTA | DMF-EtOH-H2O | MeOH | 110°C, 70 h | - | Grande et al. [1] |
| CPO-27-Ni | Solvothermal | Ni(OAc)2·4H2O | DHTA | THF-H2O | H2O | 110°C, 70 h | - | Grande et al. [1] |
| CPO-27-Ni | Solvothermal | Ni(OAc)2·4H2O | DHTA | H2O | H2O, THF | 110°C, 70 h | - | Grande et al. [1] |
| CPO-27-Ni | Solvothermal | Ni(OAc)2·4H2O | DHTA | H2O | H2O | 110°C, 70 h | - | Grande et al. [1] |
| ZIF-8 | RT | Zn(NO3)2·6H2O | MeIM | MeOH | MeOH | RT, 30 min | - | García-Palacín et al [2] |
| ZIF-8 | RT | Zn(NO3)2·6H2O | MeIM | H2O | MeOH | RT, 24 h; 80°C, 14 h | Şahin et al. [26] | Ntouros et al. [4] |
| ZiF-8 | RT | Zn(NO3)2·6H2O | MeIM | H2O | MeOH | RT, 24 h; 40°C, 24 h | Kida et al. [27] | Ntouros et al. [4] |
| ZIF-8 | solvothermal | Zn(NO3)2·6H2O | MeIM | DMF | DMF | 140oC, 24 h | Lee et al. [28] | Ntouros et al. [4] |
| ZIF-8 | solvothermal | Zn(NO3)2·6H2O | MeIM | MeOH | MeOH | RT, 24 h | Lee et al. [28] | Ntouros et al. [4] |
| ZIF-8 | - | Zn(NO3)2·4H2O | MeIM | MeOH | MeOH | 60oC, 1 h | Tsai et al. [29] | Ntouros et al. [4] |
| SIFSIX-3-Cu | RT | CuSiF6 | PZ | MeOH | MeOH | RT, 24 h | Shekhah et al. [30] | Hu et al. [3] |
| SIFSIX-3-Zn | RT | ZnSiF6 | PZ | MeOH | - | RT, 3 days | Forrest et al. [31] | Hu et al. [3] |
| YANBAR01 | solvothermal | Co(NO3)2·6H2O | FM | DMF | - | 100°C, 48 h | Li et al. [32] | Hu et al. [3] |
| NIHBEM | RT | Fe(ClO4)2·6H2O | FM | MeOH | MeOH | RT, 7 days | Wang et al. [33] | Hu et al. [3] |
| REJVOS | solvothermal | Mg(NO3)2·6H2O | FM | DMF | - | 100°C, 40 h | Rood et al. [34] | Hu et al. [3] |
| ATIBOU01 | solvothermal | Mn(NO3)2·6H2O | FM | DMF | - | 100 °C, 24 h | Li et al. [32] | Hu et al. [3] |
| XOBXIW | - | Ni(NO3)2·6H2O | FM | H2O | - | - | - | Hu et al. [3]* |
| TEVZIE | RT | Zn(NO3)2·6H2O | FM | MeOH-TEA | MeOH | RT, 3 days | Wang et al. [35] | Hu et al. [3] |
| ZIF-2 | solvothermal | Zn(NO3)2·6H2O | IM | DMF |  | 85 °C, 3 days | Park et al. [36] | Hu et al. [3] |
| ZIF-6 | solvothermal | Zn(NO3)2·6H2O | IM | DMF |  | 85 °C, 3 days | Park et al. [36] | Hu et al. [3] |
| ZIF-90 | solvothermal | Zn(NO3)2·6H2O | 2-FIM | DMF |  | 18 h, 100°C | Morris et al. [37] | Hu et al. [3] |
| ZIF-77 | solvothermal | Zn(NO3)2·6H2O | 2-nIM | DMF |  | 72 h, 100 °C | Banerjee et al. [38] | Hu et al. [3] |
| CEYPUT | RT | Co(NO3)2·6H2O | IN | DMF | - | RT | Li et al. [39] | Hu et al. [3] |
| CAXXEG | Solvothermal | Ni(AcO)2·6H2O | IN | EtOH-H2O | EtOH | 140°C, 96 h | Chen et al. [40] | Hu et al. [3] |
| HOGSIG | solvothermal | Ni(NO3)2·6H2O | IN | EtOH, urea, H2O | - | 140°C, 2 days | Hu et al. [41] | Hu et al. [3] |
| NOCKUM | solvothermal | Ca(NO3)2·4H2O | BDC | DEF | - | 110°C, 4 days | Williams et al. [42] | Hu et al. [3] |
| MOXDIN01 | solvothermal | CoCl2 | BDC | DMF-MeOH | - | 160°C, 2 days | Luo et al. [43] | Hu et al. [3] |
| KIFJUF | solvothermal | Mg(NO3)2·6H2O | BDC | DMA | - | 120°C, 18 h | Davies et al. [44] | Hu et al. [3] |
| FIJDIM02 |  | Mn(NO3)2·6H2O | BDC | DEF | - | 102°C, 3 days | Poulsen et al. [45] | Hu et al. [3] |
| XISVUR | reflux | ZnO | BDC | DMSO | - | Reflux, 4 h | Zevaco et al. [46] | Hu et al. [3] |
| IRMOF-1 | solvothermal | Zn(NO3)2·6H2O | BDC | DEF | - | 85-105°C | Eddaudi et al. [47] | Hu et al. [3] |
| IRMOF-6 | solvothermal | Zn(NO3)2·6H2O | BDC | DEF | - | 85-105°C | Eddaudi et al. [47] | Hu et al. [3] |
| IRMOF-7 | solvothermal | Zn(NO3)2·6H2O | BDC | DEF | - | 85-105°C | Eddaudi et al. [47] | Hu et al. [3] |
| ZAZBUZ | - | CuCl2·6H2O | BDC | DMF | - | - | - | Hu et al. [3]* |
| REDROI | solvothermal | Zn(NO3)2·6H2O | BDC | DMF | - | 80°C, 1 day | Liao et al. [47] | Hu et al. [3] |
| DAXNOG | solvothermal | Zn(NO3)2·6H2O | BDC | DMF | - | 108°C, 4 days | Clausen et al. [48] | Hu et al. [3] |
| CIFJAE | solvothermal | Mn(NO3)2 | BDC | DMA | - | 90°C, 75 h | Yang et al. [49] | Hu et al. [3] |
| MOF-74-Co | solvothermal | Co(NO3)2·6H2O | DHTA | DMF-EtOH- H2O | - | 120°C, 18 h | Kapelewski et al. [50] | Hu et al. [3] |
| MOF-74-Mg | solvothermal | Mg(NO3)2·6H2O | DHTA | DMF-EtOH- H2O | - | 120°C, 8 h | Kapelewski et al. [50] | Hu et al. [3] |
| MOF-74-Ni | solvothermal | Ni(NO3)2·6H2O | DHTA | DMF-EtOH- H2O | - | 120°C, 18 h | Kapelewski et al. [50] | Hu et al. [3] |
| MOF-74-Zn |  | Ni(NO3)2·6H2O | DHTA | DMF-EtOH- H2O | - | - | - | Hu et al. [3]* |
| TECTUS | solvothermal | Ca(NO3)2·4H2O | BTC | DMF-H2O | - | 85°C, 48 h | Mallick et al.[51] | Hu et al. [3] |
| CIFMEL | solvothermal | CoCl2·6H2O | BTC | DMF | - | 120 °C, 2 days | Li et al. [52] | Hu et al. [3] |
| XAVQIU01 | solvothermal | CoCl2·6H2O | BTC | DMSO | - | 160 °C, 3 days | Luo et al. [53] | Hu et al. [3] |
| CuBTC CuHKUST-1 | solvothermal | Cu(NO3)2·2.5H2O | BTC | DMF-EtOH- H2O | - | 70°C, 24 h | Song et al. [54] | Hu et al. [3] |
| XEKCAT01 |  | Mg(NO3)2·6H2O | BTC | DMF | EtOH | 127°C, 3 days | Łuczyńska-Szymczak [55] | Hu et al. [3] |
| CADPII |  | ZnCl2 | BTC | H2O | H2O | 170°C, 5 days | Fu et al. [56] | Hu et al. [3] |
| XOHLEM |  | Zn(NO3)2·6H2O | BTC | [EMI]Br |  | 160°C, 5 days | Xu et al. [57] | Hu et al. [3] |
| XIHSEN |  | Co(NO3)2·6H2O | NDC | DMF-EtOH | DMF-EtOH | 105°C, 3 days | Kim et al. [58] | Hu et al. [3] |
| ISUCUV |  | FeCl2·4H2O | NDC | DMF | - | 160°C, 72 h | Wang et al. [59] | Hu et al. [3] |
| LEVNOQ |  | Mg(NO3)2·6H2O | NDC | DMF | - | 100°C, 24 h | Senkovska et al. [60] | Hu et al. [3] |
| LIXWAR01 |  | Mn(NO3)2 | NDC | DMF | - | 110°C, 48h | Senkovska et al. [60] | Hu et al. [3] |
| QAQSAD |  | Zn(NO3)2·6H2O | NDC | DMF-MeOH | - | 120°C, 67 h | Yang et al. [49] | Hu et al. [3] |
| SUJNUH | RT | CuSO4·5H2O | NDC | KOH, H2O | - | RT, 48 h | Kanoo et al .[61] | Hu et al. [3] |
| RIHJUO |  | Co(NO3)2·6H2O | BZT | Acetonitrile-H2O | - | 150 °C, 5 days | Zhang et al. [62] | Hu et al. [3] |
| LETROT |  | Zn(NO3)2·6H2O | BZT | DMF-H2O | - | 140°C, 3 days | Xiao et al. [63] | Hu et al.[3] |
| PURQEZ |  | Zn(NO3)2 | BZT | MeOH-NaOH- H2O | - | RT | Zeng et al. [64] | Hu et al.[3] |
| DUT-4 | Solvothermal | Al(NO3)3·9H2O | NDC | DMF | DMF | 120°C, 24 h | - | Pioquinto-García et al. [5] |
| DUT-4 | Solvothermal | Al(NO3)3·9H2O | NDC | DMF/DCM | DMF-DCM | 120°C, 24 h | - | Pioquinto-García et al. [5] |
| DUT-4 | Solvothermal | Al(NO3)3·9H2O | NDC | DMF/DCM-H | DMF-DCM-H | 120°C, 24 h | - | Pioquinto-García et al. [5] |
| DUT-4 | Hydrothermal | Al(NO3)3·9H2O | NDC | H2O/H2O | H2O | 120°C, 24 h | - | Pioquinto-García et al. [5] |
| ZIF-67 | Solvothermal | Co(NO3)2·6H2O | MeIM | MeOH | MeOH | - | - | Escobar-Hernandez et al. [65] |
| ZIF-67 | Solvothermal | Co(NO3)2·6H2O | MeIM | DMF | DMF | - | - | Escobar-Hernandezet al. [65] |
| ZIF-67 | Solvothermal | Co(NO3)2·6H2O | MeIM | TEA | TEA | - | - | Escobar-Hernandezet al. [65] |
| ZIF-67 | Reactive extrusion | Co(NO3)2·6H2O | MeIM | - | - | - | - | Escobar-Hernandezet al. [65] |
| MIL-101(Cr) | Hydrothermal | Cr(NO3)3·9H2O | BDC | H2O | EtOH-H2O, DMF | 215 °C, 8 h | - | Rico-Barragán et al. [65] |
| MIL-101(Cr) | Hydrothermal | Cr(NO3)3·9H2O | BDC | H2O | EtOH-H2O, DMF | 215 °C, 8 h | - | Rico-Barragán et al. [65] |
| MIL-101(Cr) | Hydrothermal | Cr(NO3)3·9H2O | BDC | H2O, HNO3. AcOH | EtOH-H2O, DMF | 215 °C, 8 h | - | Rico-Barragán et al. [65] |
| MIL-101(Cr) | Hydrothermal | Cr(NO3)3·9H2O | BDC | H2O, HNO3. AcOH | EtOH-H2O, DMF | 215 °C, 8 h | - | Rico-Barragán et al. [65] |
| MIL-101(Cr) | Hydrothermal | Cr(NO3)3·9H2O | PET | H2O, HNO3. AcOH | EtOH-H2O, DMF | 215 °C, 8 h | - | Rico-Barragán et al. [65] |
| MIL-53(Cr) | Hydrothermal | Cr(NO3)3·9H2O | PET | H2O, HNO3. AcOH | EtOH-H2O, DMF | 215 °C, 8 h | - | Rico-Barragán et al. [65] |
| MIL-101(Cr) | Hydrothermal | Cr(NO3)3·9H2O | PET | H2O, HNO3. AcOH | EtOH-H2O | 215 °C, 8 h | - | Rico-Barragán et al. [65] |
| MiL-53 (Al) | Hydrothermal | Al(NO3)3·9H2O | BDC | H2O | Ethanol-DMF | 220 °C, 24 h; 150°C, 15 h | - | De Miranda et al. [11] |
| MiL-53 (Al) | Hydrothermal | Al(NO3)3·9H2O | BDC | H2O | Ethanol-DMF | 220 °C, 48 h; 150°C, 15 h | - | De Miranda et al. [11] |
| MiL-53 (Al) | Hydrothermal | Al(NO3)3·9H2O | BDC | H2O | Ethanol-DMF | 220 °C, 72 h; 150°C, 15 h | - | De Miranda et al. [11] |
| Ni-BTP | Reflux | Ni(OAc)2·4H2O | BTP | DMF | MeOH | reflux, 16 h | Colombo et al. [66] | Mohamed et al. [6] |
| Fe2Cl2(BBTA) | Solvothermal | FeCl2 | BBTA | DMF | DMF, MeOH | 100 °C, 24 h; 120 °C, 12 h (5 times); 60°C, 12 h; 180°C, 7 days | Reed et al. [67] | Mohamed et al. [6] |
| Fe2(mDOBDC) | Solvothermal | FeCl2 | mDOBDC | MeOH-DMF | DMF, MeOH | 120 °C, 18 h; 70 °C, 24 h; 70°C, 4 days; 150°C, 12 h | Kapelewski et al. [50] | Mohamed et al. [6] |
| Zn2(mDOBDC) | Solvothermal | ZnCl2 | mDOBDC | MeOH-DMF | DMF | 120 °C, 18 h; 70 °C, 24 h; 70°C, 4 days; 150°C, 12 h | Kapelewski et al. [50] | Mohamed et al. [6] |
| MIL-100(Fe)–ore | Hydrothermal | Fe-ore | BTC | H2O, HNO3, HF | H2O | 140-160 °C, 24 h | - | Chang et al. [13] |
| MOF-74-Mg | Solvothermal | Mg(NO3)2·6H2O | DHTA | DMF-EtOH-H2O | MeOH | - | Glover et al. [68] | Tao and Brander [18] |
| MOF-74-Mg | Solvothermal | Mg(NO3)2·6H2O | DOBDC | DMF-EtOH-H2O | DMF-EtOH | 120 °C, 24 h; 130°C, 16h | Oh et al. [69] | Dutta et al. [14] |
| MOF-74-Mg | RT | Mg(OAc)2·4H2O | DOBDC | DMF | - | 20 h | Diaz-Garcia et al. [70] | Dutta et al. [14] |
| MOF-74-Mg | MW | Mg(NO3)2·6H2O | DOBDC | DMF-EtOH-H2O | MeOH | 100 °C, 90 min | Wu et al. [71] | Dutta et al. [14] |
| CAU-10 (Al) | Solvothermal | Al2(SO4)3·18H2O | 1,3-BDC | H2O-DMF | H2O | 135 °C, 12 h | Lenzen et al. [72] | Dutta et al. [14] |
| CAU-10 (Al) | MW | Al2(SO4)3·18H2O NaAlO2 | Na2BDC | EtOH-H2O | EtOH-H2O | 100 °C, 12 h; 80 °C, 12 h | Lenzen et al. [72] | Dutta et al. [14] |
| CAU-10 (Al) | Reflux | Al2(SO4)3·18H2O NaAlO2 | 1,3-BDC | EtOH-H2O | H2O | Reflux, 16 h; Reflux, 8 h; 100°C, 12 h | Lenzen et al. [72] | Dutta et al. [14] |
| MIL-53 (Al) | Solvothermal | Al(NO3)3·9H2O | 1,3-BDC | H2O-MeOH | - | 150°C, 12 h; 65°C, 12 h | Zornoza et al. [73] | Dutta et al. [14] |
| MIL-53 (Al) | Continuous flow MW | Al(NO3)3·9H2O | 1,3-BDC | H2O-DMF | DMF-EtOH | 200W, 34 min; 70°C, 12 h | Taddei et al. [74] | Dutta et al. [14] |
| MIL-53 (Al) | Microfluidic | Al(NO3)3·9H2O | Na2BDC | H2O | EtOH | 250°C, 20 min | Bayliss et al. [75] | Dutta et al. [14] |
| MIL-53 (Fe) | Solvothermal | FeCl2·6H2O | H2BDC | DMF | MeOH | 150°C, 72 h | Faustini et al. [76] | Dutta et al. [14] |
| MIL-53 (Fe) | Cont. flow MW | FeCl2·6H2O | BDC | DMF | DMF-EtOH | 150°C, 15 min (600 W); 60°C, 1 h | Oh et al. [69] | Dutta et al. [14] |
| HKUST-1 (Cu) | Solvothermal | Cu(NO3)2·6H2O | 1,3,5-BTC | H2O-EtOH | - | 180°C, 24 h | Chui et al. [77] | Dutta et al. [14] |
| HKUST-1 (Cu) | RT | Cu(NO3)2·6H2O | 1,3,5-BTC | H2O-EtOH | - | 180°C, 24 h | Zhuang et al. [78] | Dutta et al. [14] |
| HKUST-1 (Cu) | Microfluidic | Cu(NO3)2·6H2O | 1,3,5-BTC | EtOH | EtOH | 180°C, 1.2 min; 40°C, 8 h | Rubio Martinez et al. [79] | Dutta et al. [14] |
| HKUST-1 (Cu) | MW | Cu(NO3)2·6H2O | 1,3,5-BTC | EtOH | - | 160 W, 20 min | McKinstry et al. [80] | Dutta et al. [14] |
| HKUST-1 (Cu) | Mechanochemical | Cu(OAc)2·H2O | 1,3,5-BTC | - | EtOH | - | Klimakow et al. [81]. | Dutta et al. [14] |
| MOF-5 (Zn) | Solvothermal | Zn(NO3)2·6H2O | BDC | DMF-H2O | DMF | 120°C, 48 h | Chen et al. [82] | Dutta et al. [14] |
| MOF-5 (Zn) | RT | Zn(NO3)2·6H2O | BDC | DMF-TEA | DMF | Stir 2.5 h; 120°C, 8 h; 120°C, 6h | Tranchemotagne et al. [83] | Dutta et al. [14] |
| MOF-5 (Zn) | Microfluidic | Zn(NO3)2·6H2O | BDC | DMF | EtOH | 80°C, 12 min; 80°C, 12 h | Faustini et al. [76] | Dutta et al. [14] |
| MOF-5 (Zn) | MW | Zn(NO3)2·6H2O | BDC | NMP | NMP-CHCl3 | 95-135°C, 10-60 min; 100°C, 24 h | Vakili et al. [84] | Dutta et al. [14] |
| MOF-5 (Zn) | Mechanochemical | Et2Zn | BDC | THF- Benzamide/DEF | H2O/ THF | -78°C/RT, 20 h | Prochowicz et al. [85] | Dutta et al. [14] |
| UiO-66 (Zr) | Solvothermal | ZrCl4 | BDC | DMF-HCl | DMF-EtOH | 80°C, 12 h; 150°C, 3 h | Katz et al. [86] | Dutta et al. [14] |
| UiO-66 (Zr) | Solvothermal | ZrCl4 | BDC | DMF-FA | acetone | 120°C, 24 h | Ren et al. [87] | Dutta et al. [14] |
| UiO-66 (Zr) | MW | ZrCl4 | BDC | DMF-H2O | - | 200 W, 3 min 80 W, 15 min | Taddei et al. [88] | Dutta et al. [14] |
| UiO-66 (Zr) | Microfluidic | ZrCl4 | BDC | DMF | DMF-EtOH | 130 °C, 10 min; 40 °C, 8 h | Rubio-Martinez et al. [79] | Dutta et al. [14] |
| UiO-66 (Zr) | Mechanochemical | Zr(PrO)4 | BDC | MAA, H2O, MeOH | iPrOH/MeOH | 75 min | Uzarevic et al. [89] | Dutta et al. [14] |
| UiO-67 (Zr) | Solvothermal | ZrCl4 | H2BPDC | DMF-HCl | DMF-EtOH | 80°C, 12 h; 150 °C, 3h | Katz et al. [86] | Dutta et al. [14] |
| UiO-67 (Zr) | Solvothermal | ZrCl4 | H2BPDC | DMF-BA | DMF-EtOH | 120°C, 24 h; 120 °C, 8 h | Vakili et al. [84] | Dutta et al. [14] |
| UiO-67 (Zr) | Microfluidic | ZrCl4 | H2BPDC | DMF-BA-silicon oil, H2O | DMF/DMF-MeOH | 2.5 h, stirring; 100°C, 12 h | Bailey et al. [90] | Dutta et al. [14] |
| UiO-67 (Zr) | MW | ZrCl4 | H2BPDC | DMF | DMF-EtOH | 120 °C (150 W, 12 h); 120°C, 8 h | Vakili et al. [84] | Dutta et al. [14] |
| MI (Zr) | Mechanochemical | Zr(PrO)4 | BDC | MAA, DMF, H2O | DMF | 260 min | Fidelli et al. [91] | Dutta et al. [14] |
| MOF-808 (Zr) | Solvothermal | ZrCl4 | 1,3-BTC | DMF-AA | Acetone/ CHCl3 | 120 °C, 72 h; 50°C, 72 h; 120°C, 24 h | Xu et al. [92] | Dutta et al. [14] |
| MOF-808 (Zr) | MW | ZrCl4 | 1,3-BTC | FA-H2O | Acetone/H2O | 95°C, 2h | Gonzales et al. [93] | Dutta et al. [14] |
| MOF-808 (Zr) | Microfluidic | ZrCl4 | 1,3-BTC | FA-DMF | DMF-MeOH | 150°C, 60 min | Bagi et al. [94] | Dutta et al. [14] |
| NU-1000 (Zr) | solvothermal | ZrOCl2·8H2O | H4TBAPy | BA-DMF | DMF, DMF-HCl, DMF, acetone | 120 °C, 16 h; 100 °C, 12 h | Wang et al. [95] | Dutta et al. [14] |
| NU-1000 (Zr) | RT | ZrCl4 | H4TBAPy | OmimBr, AA, DMF | acetone | RT | Zhang et al. [96] | Dutta et al. [14] |
| MOF-74-Zn | solvothermal | Zn(NO3)2·6H2O | DHTA | H2O-DMF | - | - | - | Wang et al. [21] |
| MOF-74-Ni | solvothermal | Ni(NO3)2·6H2O | DHTA | H2O-DMF | - | - | - | Wang et al. [21] |
| MOF-74-Mg | solvothermal | Mg(NO3)2·6H2O | DHTA | H2O-DMF | - | - | - | Wang et al. [21] |
| MOF-74-Co | solvothermal | Co(NO3)2·6H2O | DHTA | H2O-DMF | - | - | - | Wang et al. [21] |
| MIL-47@CNT | hydrothermal | V2O3 | BDC | DMF | MeOH | 180°C, 10-34 h | - | Yang et al. [8] |
| MIL-100(Fe) | reflux | FeCl3 | Ta4Hz | iPrOH | EtOH | Reflux, 1 day | Severino et al. [97] | Mohtar et al. [17] |
| MIL-88A (Fe) | RT | FeCl3·6H2O | Fumaric Acid | EtOH-H2O | EtOH-H2O | RT, 24 h; 60°C 12 h | - | Meng et al. [24] |
| UiO-67 (Zr)/BC | solvothermal | ZrCl4 | BPDC | DMF-AA | DMF | 120°C, 24 h | - | Ghaedi et al. [15] |
| ZnCo-ZB/BC | RT | Co(NO3)2·6H2O Zn(NO3)2·6H2O | MeIM | MeOH | MeOH | 60°C, 12 h; 900°C, 1h | - | Wu et al. [25] |
| ZiF-8 hallow fibres | RT | Zn(NO3)2·6H2O | MeIM | H2O | MeOH | RT | - | Jia et al. [22] |

*These case studies were not included because the reference for the experimental procedure was not accessible.

| Entry | MAX phase Synthesis | Etching Conditions | Delamination Conditions | Experimental reference | LCA Reference |
| --- | --- | --- | --- | --- | --- |
| 1. | Ti, Al, C + TiC, high temperature | HFaq | - | - | Carvalho et al. [7] |
| 2. | Ti, Al, C (3:1:1), 1400C, 2 h | 37 wt% HCl + H2O + 48 wt% HF (6:3:1 vol ratio), 35C, 24 h | 0.47 M LiClaq | - | Dadashi Firouzjaei et al. [10] |
| 3. | Ti2AlC, TiC (1:1), 1350C, 2 h | HFaq (50 wt%), 2 h | Sonication in CH3OH | Naguib et al., [98] | Ungureanu et al. [19] |
| 4. | Ti, Al, TiC (3:1.1:1.8), 1650C, 2 h | LiF in 37 wt% HClaq, 40 h | Washing/ centrifugation | Shuck et al. [99] | Ungureanu et al. [19] |
| 5. | TiC, Ti, Al (2:1.25:2.2), 1380C, 2 h | 12 M HClaq + H2O + 50 wt% HFaq (6:3:1 vol ratio), 35C, 24 h | 0.5 M LiClaq | Mathis et al. [100] | Ungureanu et al. [19] |
| 6. | TiC, Ti , Al (2:1:1), 1400C, 2 h | 12 M HClaq + H2O + 49 wt% HFaq (6:3:1 vol ratio), 35C, 24 h | 1.18 M LiClaq | Shuck et al. [101] | Ungureanu et al. [19] |
| 7. | TiO2 (anatase), Al (secondary), C (tire derived), 1350C, 1 h | LiF in 9M HClaq, 40C, 24 h | Washing/ centrifugation | Jolly et al. [102] | Ungureanu et al. [19] |
| 8. | TiC, Ti, Al (2:1:1), 1450C, 2 h | 0.5 M LiFaq, 100 min/100 mg MAX Phase | Surface acoustic waves | El Ghazaly et al. [103] | Ungureanu et al. [19] |
| 9. | Ti, Al, C (3:1:1), 1400C, 2 h | 37 wt% HCl + H2O + 48 wt% HF (6:3:1 vol ratio), 35C, 24 h | 0.47 M LiClaq | Dadashi Firouzjaei et al. [10] | Ungureanu et al. [19] |
| 10. | Ti, Al, C, 625 °C, 3 h | HF (49%) + HCl (37%) (1:6 ratio) + H2O | LiCl, H2O | Shuck et al. [101] | Hansen et al. [16] |
| 11. | Ti, Al, C, 1400 °C, 2 h | HCl-LiF, 35°C, 48 h | DI water, sonication, 30 min | - | Zu et al. [20] and [23] |
| 12. | - | HFaq, 24 h | TMAOH, H2O, 12 h | Alhabeb et al. [104] | Srivastava et al. [105] |

Table S4	LCA of MXenes case studies identified within the 26 studies reviewed

### References

[1]	C. A. Grande, R. Blom, A. Spjelkavik, V. Moreau, and J. Payet, “Life-cycle assessment as a tool for eco-design of metal-organic frameworks (MOFs),” Sustainable Materials and Technologies, vol. 14, pp. 11–18, Dec. 2017, doi: 10.1016/j.susmat.2017.10.002.

[2]	M. García-Palacín et al., “Sized-Controlled ZIF-8 Nanoparticle Synthesis from Recycled Mother Liquors: Environmental Impact Assessment,” ACS Sustainable Chem. Eng., vol. 8, no. 7, pp. 2973–2980, Feb. 2020, doi: 10.1021/acssuschemeng.9b07593.

[3]	J. Hu, X. Gu, L.-C. Lin, and B. R. Bakshi, “Toward Sustainable Metal–Organic Frameworks for Post-Combustion Carbon Capture by Life Cycle Assessment and Molecular Simulation,” ACS Sustainable Chem. Eng., vol. 9, no. 36, pp. 12132–12141, Sept. 2021, doi: 10.1021/acssuschemeng.1c03473.

[4]	V. Ntouros, I. Kousis, D. Papadaki, A. L. Pisello, and M. N. Assimakopoulos, “Life Cycle Assessment on Different Synthetic Routes of ZIF-8 Nanomaterials,” Energies, vol. 14, no. 16, p. 4998, Aug. 2021, doi: 10.3390/en14164998.

[5]	S. Pioquinto-García et al., “Environmental assessment of metal-organic framework DUT-4 synthesis and its application for siloxane removal,” Journal of Environmental Chemical Engineering, vol. 9, no. 6, p. 106601, Dec. 2021, doi: 10.1016/j.jece.2021.106601.

[6]	A. M. O. Mohamed and Y. Bicer, “The Search for Efficient and Stable Metal-Organic Frameworks for Photocatalysis: Atmospheric Fixation of Nitrogen,” Applied Surface Science, vol. 583, p. 152376, May 2022, doi: 10.1016/j.apsusc.2021.152376.

[7]	M. L. Carvalho, G. Mela, A. Temporelli, E. Brivio, and P. Girardi, “Sodium-Ion Batteries with Ti1 Al1 TiC1.85 MXene as Negative Electrode: Life Cycle Assessment and Life Critical Resource Use Analysis,” Sustainability (Switzerland), vol. 14, no. 10, 2022, doi: 10.3390/su14105976.

[8]	J. Yang et al., “Eco-friendly synthesis of vanadium metal-organic frameworks from gasification waste for wearable Zn-ion batteries,” Energy Storage Materials, vol. 53, pp. 352–362, Dec. 2022, doi: 10.1016/j.ensm.2022.09.009.

[9]	A. A. Rico-Barragán, J. R. Álvarez, S. Pioquinto-García, J. Rodríguez-Hernández, P. Rivas-García, and N. E. Dávila-Guzmán, “Cleaner production of metal-organic framework MIL-101(Cr) for toluene adsorption,” Sustainable Production and Consumption, vol. 40, pp. 159–168, Sept. 2023, doi: 10.1016/j.spc.2023.06.011.

[10]	M. Dadashi Firouzjaei, S. K. Nemani, M. Sadrzadeh, E. K. Wujcik, M. Elliott, and B. Anasori, “Life‐Cycle Assessment of Ti3 C2 T x  MXene Synthesis,” Advanced Materials, vol. 35, no. 31, p. 2300422, Aug. 2023, doi: 10.1002/adma.202300422.

[11]	J. L. De Miranda et al., “A case study for an eco-design of aluminum terephthalate metal-organic framework- MIL-53(Al) for CO2 and methane adsorption,” Sustainable Materials and Technologies, vol. 37, p. e00689, Sept. 2023, doi: 10.1016/j.susmat.2023.e00689.

[12]	H. U. Escobar-Hernandez, Y. Quan, M. I. Papadaki, and Q. Wang, “Life Cycle Assessment of Metal–Organic Frameworks: Sustainability Study of Zeolitic Imidazolate Framework-67,” ACS Sustainable Chem. Eng., vol. 11, no. 10, pp. 4219–4225, Mar. 2023, doi: 10.1021/acssuschemeng.2c07276.

[13]	M. Chang, C. Tang, C.-C. Wang, and C. Zhao, “From ore to MOF: A case of MIL-100(Fe) production from iron ore concentrates,” Progress in Natural Science: Materials International, vol. 34, no. 1, pp. 66–73, Feb. 2024, doi: 10.1016/j.pnsc.2024.01.013.

[14]	S. Dutta, M. Walden, A. Sinelshchikova, R. Ettlinger, E. Lizundia, and S. Wuttke, “Cradle‐to‐Gate Environmental Impact Assessment of Commercially Available Metal‐Organic Frameworks Manufacturing,” Adv Funct Materials, vol. 34, no. 52, p. 2410751, Dec. 2024, doi: 10.1002/adfm.202410751.

[15]	S. Ghaedi, H. Rajabi, M. Hadi Mosleh, P. Babakhani, and M. Sedighi, “UiO-67 metal-organic framework loaded on hardwood biochar for sustainable management of environmental boron contaminations,” Journal of Environmental Chemical Engineering, vol. 12, no. 6, 2024, doi: 10.1016/j.jece.2024.114511.

[16]	S. F. Hansen et al., “Maximizing the safety and sustainability of MXenes,” Sci Rep, vol. 14, no. 1, Dec. 2024, doi: 10.1038/s41598-024-82063-w.

[17]	A. A. Mohtar et al., “Iron(III) based Metal-Organic Frameworks in cellulose acetate film preservation: Fundamental aspects and first application,” Journal of Cultural Heritage, vol. 66, pp. 236–243, 2024, doi: 10.1016/j.culher.2023.11.013.

[18]	Y. Tao and M. Brander, “A comparative prospective life cycle assessment of coal-fired power plants in the US with MEA/MOF-based carbon capture,” Journal of Cleaner Production, vol. 456, p. 142418, June 2024, doi: 10.1016/j.jclepro.2024.142418.

[19]	A. Ungureanu et al., “Systematic Life Cycle Environmental Impact Comparison of Alternative Synthetic Strategies for Ti3 C2 T x  MXene,” ACS Sustainable Chem. Eng., vol. 12, no. 15, pp. 5893–5906, Apr. 2024, doi: 10.1021/acssuschemeng.3c08491.

[20]	D. Zu et al., “Cathodic polarization sustaining MXene-mediated fenton-like reactions: Performance, reaction mechanisms, and life cycle assessment,” Chemical Engineering Journal, vol. 487, 2024, doi: 10.1016/j.cej.2024.150503.

[21]	P. Wang, Z. Pan, Z. Liu, L. Shang, M. R. Soltanian, and Z. Zhang, “Life cycle assessment of CO2 capture through pressure swing adsorption using MOF-74,” Gas Science and Engineering, vol. 133, p. 205497, Jan. 2025, doi: 10.1016/j.jgsce.2024.205497.

[22]	S. Jia, J. Tan, Z. Zhou, and S. Zhang, “A sustainable method to prepare ultra-thin MOF hollow fiber membranes for H2 separation,” Journal of Membrane Science, vol. 721, 2025, doi: 10.1016/j.memsci.2025.123794.

[23]	D. Zu et al., “Comparative life cycle assessment of Fenton-like systems: Insights into the environmental benefits of reductant-driven strategies,” Water Research, vol. 279, 2025, doi: 10.1016/j.watres.2025.123489.

[24]	L. Meng et al., “Orbital hybridization-driven singlet oxygen generation in piezo-photocatalytic self-fenton system: Synergistic band engineering and spin-state modulation for sustainable water remediation,” Applied Catalysis B: Environmental, vol. 377, 2025, doi: 10.1016/j.apcatb.2025.125521.

[25]	Y. Wu et al., “Insight into the mechanism of pyrolysis temperature on the performance of biochar-based MOF materials in capacitive deionization for heavy metal removal,” Desalination, vol. 609, 2025, doi: 10.1016/j.desal.2025.118856.

[26]	F. Şahin, B. Topuz, and H. Kalıpçılar, “Synthesis of ZIF-7, ZIF-8, ZIF-67 and ZIF-L from recycled mother liquors,” Microporous and Mesoporous Materials, vol. 261, pp. 259–267, May 2018, doi: 10.1016/j.micromeso.2017.11.020.

[27]	K. Kida, M. Okita, K. Fujita, S. Tanaka, and Y. Miyake, “Formation of high crystalline ZIF-8 in an aqueous solution,” CrystEngComm, vol. 15, no. 9, p. 1794, 2013, doi: 10.1039/c2ce26847g.

[28]	Y.-R. Lee, M.-S. Jang, H.-Y. Cho, H.-J. Kwon, S. Kim, and W.-S. Ahn, “ZIF-8: A comparison of synthesis methods,” Chemical Engineering Journal, vol. 271, pp. 276–280, July 2015, doi: 10.1016/j.cej.2015.02.094.

[29]	C.-W. Tsai, J. W. Niemantsverdriet, and E. H. G. Langner, “Enhanced CO2 adsorption in nano-ZIF-8 modified by solvent assisted ligand exchange,” Microporous and Mesoporous Materials, vol. 262, pp. 98–105, May 2018, doi: 10.1016/j.micromeso.2017.11.024.

[30]	O. Shekhah et al., “Made-to-order metal-organic frameworks for trace carbon dioxide removal and air capture,” Nat Commun, vol. 5, no. 1, p. 4228, June 2014, doi: 10.1038/ncomms5228.

[31]	K. A. Forrest et al., “Computational Studies of CO2 Sorption and Separation in an Ultramicroporous Metal–Organic Material,” J. Phys. Chem. C, vol. 117, no. 34, pp. 17687–17698, Aug. 2013, doi: 10.1021/jp405781c.

[32]	K. Li et al., “Multifunctional Microporous MOFs Exhibiting Gas/Hydrocarbon Adsorption Selectivity, Separation Capability and Three‐Dimensional Magnetic Ordering,” Adv Funct Materials, vol. 18, no. 15, pp. 2205–2214, Aug. 2008, doi: 10.1002/adfm.200800058.

[33]	Z. ‐M. Wang, Y. ‐J. Zhang, T. Liu, M. Kurmoo, and S. Gao, “[Fe3 (HCOO)6 ]: A Permanent Porous Diamond Framework Displaying H2 /N2 Adsorption, Guest Inclusion, and Guest‐Dependent Magnetism,” Adv Funct Materials, vol. 17, no. 9, pp. 1523–1536, June 2007, doi: 10.1002/adfm.200600676.

[34]	J. A. Rood, B. C. Noll, and K. W. Henderson, “Synthesis, Structural Characterization, Gas Sorption and Guest-Exchange Studies of the Lightweight, Porous Metal−Organic Framework α-[Mg3 (O2 CH)6 ],” Inorg. Chem., vol. 45, no. 14, pp. 5521–5528, July 2006, doi: 10.1021/ic060543v.

[35]	Z. Wang et al., “[Zn3(HCOO)6]: A Porous Diamond Framework Conformable to Guest Inclusion,” Aust. J. Chem., vol. 59, no. 9, p. 617, 2006, doi: 10.1071/CH06176.

[36]	K. S. Park et al., “Exceptional chemical and thermal stability of zeolitic imidazolate frameworks,” Proc. Natl. Acad. Sci. U.S.A., vol. 103, no. 27, pp. 10186–10191, July 2006, doi: 10.1073/pnas.0602439103.

[37]	W. Morris, C. J. Doonan, H. Furukawa, R. Banerjee, and O. M. Yaghi, “Crystals as Molecules: Postsynthesis Covalent Functionalization of Zeolitic Imidazolate Frameworks,” J. Am. Chem. Soc., vol. 130, no. 38, pp. 12626–12627, Sept. 2008, doi: 10.1021/ja805222x.

[38]	R. Banerjee et al., “High-Throughput Synthesis of Zeolitic Imidazolate Frameworks and Application to CO2 Capture,” Science, vol. 319, no. 5865, pp. 939–943, Feb. 2008, doi: 10.1126/science.1152516.

[39]	Z. Li et al., “A chiral porous cobalt–organic framework based on reinforced sinusoidal-like SBUs involving in situ-generated formate,” New J. Chem., vol. 37, no. 8, p. 2473, 2013, doi: 10.1039/c3nj00236e.

[40]	Q. Chen, W. Xue, J.-B. Lin, R.-B. Lin, M.-H. Zeng, and X.-M. Chen, “Highly-connected, porous coordination polymers based on [M4(μ3-OH)2] (M = CoII and NiII) clusters: different networks, adsorption and magnetic properties,” Dalton Trans., vol. 41, no. 14, p. 4199, 2012, doi: 10.1039/c2dt12022d.

[41]	B.-W. Hu, J.-P. Zhao, E. C. Sañudo, F.-C. Liu, Y.-F. Zeng, and X.-H. Bu, “Nickel(ii)–azido ferromagnetic chains in a 3D porous metal–organic framework with breathing guest molecules,” Dalton Trans., no. 41, p. 5556, 2008, doi: 10.1039/b812402g.

[42]	C. A. Williams, A. J. Blake, C. Wilson, P. Hubberstey, and M. Schröder, “Novel Metal−Organic Frameworks Derived from Group II Metal Cations and Aryldicarboxylate Anionic Ligands,” Crystal Growth & Design, vol. 8, no. 3, pp. 911–922, Mar. 2008, doi: 10.1021/cg700731d.

[43]	F. Luo, Y. Che, and J. Zheng, “Trinuclear Cobalt Based Porous Coordination Polymers Showing Unique Topological and Magnetic Variety upon Different Dicarboxylate-like Ligands,” Crystal Growth & Design, vol. 9, no. 2, pp. 1066–1071, Feb. 2009, doi: 10.1021/cg800895g.

[44]	R. P. Davies, R. J. Less, P. D. Lickiss, and A. J. P. White, “Framework materials assembled from magnesium carboxylate building units,” Dalton Trans., no. 24, p. 2528, 2007, doi: 10.1039/b705028c.

[45]	R. D. Poulsen, A. Bentien, M. Chevalier, and B. B. Iversen, “Synthesis, Physical Properties, Multitemperature Crystal Structure, and 20 K Synchrotron X-ray Charge Density of a Magnetic Metal Organic Framework Structure, Mn3 (C8 O4 H4 )3 (C5 H11 ON)2,” J. Am. Chem. Soc., vol. 127, no. 25, pp. 9156–9166, June 2005, doi: 10.1021/ja051233z.

[46]	T. A. Zevaco, D. Männle, O. Walter, and E. Dinjus, “An easy way to achieve three‐dimensional metal–organic coordination polymers: synthesis and crystal structure of dizinc diisophthalate bis‐dimethylsulfoxide monohydrate: [Zn2 (ip)4 (DMSO)2 (H2 O)·3 DMSO] n ,” Applied Organom Chemis, vol. 21, no. 11, pp. 970–977, Nov. 2007, doi: 10.1002/aoc.1325.

[47]	M. Eddaoudi et al., “Systematic Design of Pore Size and Functionality in Isoreticular MOFs and Their Application in Methane Storage,” Science, vol. 295, no. 5554, pp. 469–472, Jan. 2002, doi: 10.1126/science.1067208.

[48]	H. F. Clausen, R. D. Poulsen, A. D. Bond, M.-A. S. Chevallier, and B. B. Iversen, “Solvothermal synthesis of new metal organic framework structures in the zinc–terephthalic acid–dimethyl formamide system,” Journal of Solid State Chemistry, vol. 178, no. 11, pp. 3342–3351, Nov. 2005, doi: 10.1016/j.jssc.2005.08.013.

[49]	S.-Y. Yang, H.-B. Yuan, X.-B. Xu, and R.-B. Huang, “Influential factors on assembly of first-row transition metal coordination polymers,” Inorganica Chimica Acta, vol. 403, pp. 53–62, July 2013, doi: 10.1016/j.ica.2013.03.042.

[50]	M. T. Kapelewski et al., “M2 ( m -dobdc) (M = Mg, Mn, Fe, Co, Ni) Metal–Organic Frameworks Exhibiting Increased Charge Density and Enhanced H2 Binding at the Open Metal Sites,” J. Am. Chem. Soc., vol. 136, no. 34, pp. 12119–12129, Aug. 2014, doi: 10.1021/ja506230r.

[51]	A. Mallick, T. Kundu, and R. Banerjee, “Correlation between coordinated water content and proton conductivity in Ca–BTC-based metal–organic frameworks,” Chem. Commun., vol. 48, no. 70, p. 8829, 2012, doi: 10.1039/c2cc34006b.

[52]	P.-Z. Li et al., “Co(II)-tricarboxylate metal–organic frameworks constructed from solvent-directed assembly for CO2 adsorption,” Microporous and Mesoporous Materials, vol. 176, pp. 194–198, Aug. 2013, doi: 10.1016/j.micromeso.2013.03.052.

[53]	F. Luo, Y. Che, and J. Zheng, “Rarely Decorated Rutile Frameworks Built from Triangular Organic Spacers and Distorted Octahedral Co3 Building Blocks,” Eur J Inorg Chem, vol. 2007, no. 24, pp. 3906–3910, Aug. 2007, doi: 10.1002/ejic.200700285.

[54]	X. Song, S. Jeong, D. Kim, and M. S. Lah, “Transmetalations in two metal–organic frameworks with different framework flexibilities: Kinetics and core–shell heterostructure,” CrystEngComm, vol. 14, no. 18, p. 5753, 2012, doi: 10.1039/c2ce26115d.

[55]	K. Łuczyńska-Szymczak, W. Starosta, and J. Leciejewicz, “Poly[bis(μ6 -benzene-1,3,5-tricarboxylato-κ7 O1 , O1′ : O1′ : O3 : O3′ : O5 : O5′ )tetrakis(dimethylformamide-κ O )trimagnesium(II)],” Acta Crystallogr E Struct Rep Online, vol. 68, no. 6, pp. m852–m853, June 2012, doi: 10.1107/S1600536812023240.

[56]	Y. Fu, G. Li, F. Liao, M. Xiong, and J. Lin, “Two novel transition metal–organic frameworks based on 1,3,5-benzenetricarboxylate ligand: Syntheses, structures and thermal properties,” Journal of Molecular Structure, vol. 1004, no. 1–3, pp. 252–256, Oct. 2011, doi: 10.1016/j.molstruc.2011.08.013.

[57]	L. Xu, E.-Y. Choi, and Y.-U. Kwon, “Ionothermal synthesis of a 3D Zn–BTC metal-organic framework with distorted tetranuclear [Zn4(μ4-O)] subunits,” Inorganic Chemistry Communications, vol. 11, no. 10, pp. 1190–1193, Oct. 2008, doi: 10.1016/j.inoche.2008.07.001.

[58]	S. H. Kim, H. S. Huh, and S. W. Lee, “Cobalt(II) coordination polymers based on dicarboxylates and dipyridyl-type ligands: [CoL1.5(NO3)2], [Co1.5(bpdc)1.5(dma)]·(dma)·(EtOH), [Co1.5(ndc)1.5(dma)2], [Co3(ndc)3(dmf)4], and [CoL(bpdc)]·(EtOH) (bpdcH2=biphenyl-4,4′-dicarboxylic acid, ndcH2=2,6-naphthalene dicarboxylic acid, L=pyCHNC10H6NCHpy),” Journal of Molecular Structure, vol. 841, no. 1–3, pp. 78–87, Sept. 2007, doi: 10.1016/j.molstruc.2006.11.065.

[59]	X.-F. Wang, Y.-B. Zhang, W.-X. Zhang, W. Xue, H.-L. Zhou, and X.-M. Chen, “Buffering additive effect in the formation of metal–carboxylate frameworks with slightly different linear M3(RCOO)6 clusters,” CrystEngComm, vol. 13, no. 12, p. 4196, 2011, doi: 10.1039/c1ce05190c.

[60]	I. Senkovska and S. Kaskel, “Solvent‐Induced Pore‐Size Adjustment in the Metal‐Organic Framework [Mg3 (ndc)3 (dmf)4 ] (ndc = naphthalenedicarboxylate),” Eur J Inorg Chem, vol. 2006, no. 22, pp. 4564–4569, Nov. 2006, doi: 10.1002/ejic.200600635.

[61]	P. Kanoo, K. L. Gurunatha, and T. K. Maji, “Versatile functionalities in MOFs assembled from the same building units: interplay of structural flexibility, rigidity and regularity,” J. Mater. Chem., vol. 20, no. 7, pp. 1322–1331, 2010, doi: 10.1039/B917029D.

[62]	X. Zhang, Z. Hao, W. Zhang, and X. Chen, “Dehydration‐Induced Conversion from a Single‐Chain Magnet into a Metamagnet in a Homometallic Nanoporous Metal–Organic Framework,” Angew Chem Int Ed, vol. 46, no. 19, pp. 3456–3459, May 2007, doi: 10.1002/anie.200604284.

[63]	J. Xiao, Y. Wu, M. Li, B. Liu, X. Huang, and D. Li, “Crystalline Structural Intermediates of a Breathing Metal–Organic Framework That Functions as a Luminescent Sensor and Gas Reservoir,” Chemistry A European J, vol. 19, no. 6, pp. 1891–1895, Feb. 2013, doi: 10.1002/chem.201203515.

[64]	H. Zeng, T. Li, Z. Yan, S. Luo, and F. Li, “Two Porous Metal−Organic Frameworks Showing Different Behaviors to Sodium Cation,” Crystal Growth & Design, vol. 10, no. 2, pp. 475–478, Feb. 2010, doi: 10.1021/cg901114e.

[65]	Y. Quan, R. Shen, R. Ma, Z. Zhang, and Q. Wang, “Sustainable and Efficient Manufacturing of Metal-Organic Framework-Based Polymer Nanocomposites by Reactive Extrusion,” ACS Sustainable Chem. Eng., vol. 10, no. 22, pp. 7216–7222, June 2022, doi: 10.1021/acssuschemeng.2c01720.

[66]	V. Colombo et al., “High thermal and chemical stability in pyrazolate-bridged metal–organic frameworks with exposed metal sites,” Chem. Sci., vol. 2, no. 7, p. 1311, 2011, doi: 10.1039/c1sc00136a.

[67]	D. A. Reed et al., “A spin transition mechanism for cooperative adsorption in metal–organic frameworks,” Nature, vol. 550, no. 7674, pp. 96–100, Oct. 2017, doi: 10.1038/nature23674.

[68]	T. Grant Glover, G. W. Peterson, B. J. Schindler, D. Britt, and O. Yaghi, “MOF-74 building unit has a direct impact on toxic gas adsorption,” Chemical Engineering Science, vol. 66, no. 2, pp. 163–170, Jan. 2011, doi: 10.1016/j.ces.2010.10.002.

[69]	H. Oh et al., “Efficient synthesis for large-scale production and characterization for hydrogen storage of ligand exchanged MOF-74/174/184-M (M = Mg2+, Ni2+),” International Journal of Hydrogen Energy, vol. 42, no. 2, pp. 1027–1035, Jan. 2017, doi: 10.1016/j.ijhydene.2016.08.153.

[70]	M. Díaz-García, Á. Mayoral, I. Díaz, and M. Sánchez-Sánchez, “Nanoscaled M-MOF-74 Materials Prepared at Room Temperature,” Crystal Growth & Design, vol. 14, no. 5, pp. 2479–2487, May 2014, doi: 10.1021/cg500190h.

[71]	X. Wu et al., “Microwave synthesis and characterization of MOF-74 (M=Ni, Mg) for gas separation,” Microporous and Mesoporous Materials, vol. 180, pp. 114–122, Nov. 2013, doi: 10.1016/j.micromeso.2013.06.023.

[72]	D. Lenzen et al., “Scalable Green Synthesis and Full‐Scale Test of the Metal–Organic Framework CAU‐10‐H for Use in Adsorption‐Driven Chillers,” Advanced Materials, vol. 30, no. 6, p. 1705869, Feb. 2018, doi: 10.1002/adma.201705869.

[73]	B. Zornoza et al., “Caffeine Encapsulation in Metal Organic Framework MIL-53(Al) at Pilot Plant Scale for Preparation of Polyamide Textile Fibers with Cosmetic Properties,” ACS Appl. Mater. Interfaces, vol. 14, no. 19, pp. 22476–22488, May 2022, doi: 10.1021/acsami.2c04293.

[74]	M. Taddei, D. A. Steitz, J. A. van Bokhoven, and M. Ranocchiari, “Continuous‐Flow Microwave Synthesis of Metal–Organic Frameworks: A Highly Efficient Method for Large‐Scale Production,” Chemistry A European J, vol. 22, no. 10, pp. 3245–3249, Mar. 2016, doi: 10.1002/chem.201505139.

[75]	P. A. Bayliss et al., “Synthesis of metal–organic frameworks by continuous flow,” Green Chem., vol. 16, no. 8, pp. 3796–3802, 2014, doi: 10.1039/C4GC00313F.

[76]	M. Faustini et al., “Microfluidic Approach toward Continuous and Ultrafast Synthesis of Metal–Organic Framework Crystals and Hetero Structures in Confined Microdroplets,” J. Am. Chem. Soc., vol. 135, no. 39, pp. 14619–14626, Oct. 2013, doi: 10.1021/ja4039642.

[77]	S. S.-Y. Chui, S. M.-F. Lo, J. P. H. Charmant, A. G. Orpen, and I. D. Williams, “A Chemically Functionalizable Nanoporous Material [Cu3 (TMA)2 (H2 O)3 ] n ,” Science, vol. 283, no. 5405, pp. 1148–1150, Feb. 1999, doi: 10.1126/science.283.5405.1148.

[78]	J. Zhuang, D. Ceglarek, S. Pethuraj, and A. Terfort, “Rapid Room‐Temperature Synthesis of Metal–Organic Framework HKUST‐1 Crystals in Bulk and as Oriented and Patterned Thin Films,” Adv Funct Materials, vol. 21, no. 8, pp. 1442–1447, Apr. 2011, doi: 10.1002/adfm.201002529.

[79]	M. Rubio-Martinez et al., “Versatile, High Quality and Scalable Continuous Flow Production of Metal-Organic Frameworks,” Sci Rep, vol. 4, no. 1, p. 5443, June 2014, doi: 10.1038/srep05443.

[80]	C. McKinstry, E. J. Cussen, A. J. Fletcher, S. V. Patwardhan, and J. Sefcik, “Scalable continuous production of high quality HKUST-1 via conventional and microwave heating,” Chemical Engineering Journal, vol. 326, pp. 570–577, Oct. 2017, doi: 10.1016/j.cej.2017.05.169.

[81]	M. Klimakow, P. Klobes, A. F. Thünemann, K. Rademann, and F. Emmerling, “Mechanochemical Synthesis of Metal−Organic Frameworks: A Fast and Facile Approach toward Quantitative Yields and High Specific Surface Areas,” Chem. Mater., vol. 22, no. 18, pp. 5216–5221, Sept. 2010, doi: 10.1021/cm1012119.

[82]	B. Chen et al., “Synthesis and characterization of the interpenetrated MOF-5,” J. Mater. Chem., vol. 20, no. 18, p. 3758, 2010, doi: 10.1039/b922528e.

[83]	D. J. Tranchemontagne, J. R. Hunt, and O. M. Yaghi, “Room temperature synthesis of metal-organic frameworks: MOF-5, MOF-74, MOF-177, MOF-199, and IRMOF-0,” Tetrahedron, vol. 64, no. 36, pp. 8553–8557, Sept. 2008, doi: 10.1016/j.tet.2008.06.036.

[84]	R. Vakili, S. Xu, N. Al-Janabi, P. Gorgojo, S. M. Holmes, and X. Fan, “Microwave-assisted synthesis of zirconium-based metal organic frameworks (MOFs): Optimization and gas adsorption,” Microporous and Mesoporous Materials, vol. 260, pp. 45–53, Apr. 2018, doi: 10.1016/j.micromeso.2017.10.028.

[85]	D. Prochowicz et al., “A mechanochemical strategy for IRMOF assembly based on pre-designed oxo-zinc precursors,” Chem. Commun., vol. 51, no. 19, pp. 4032–4035, 2015, doi: 10.1039/C4CC09917F.

[86]	M. J. Katz et al., “A facile synthesis of UiO-66, UiO-67 and their derivatives,” Chem. Commun., vol. 49, no. 82, p. 9449, 2013, doi: 10.1039/c3cc46105j.

[87]	J. Ren, H. W. Langmi, B. C. North, M. Mathe, and D. Bessarabov, “Modulated synthesis of zirconium-metal organic framework (Zr-MOF) for hydrogen storage applications,” International Journal of Hydrogen Energy, vol. 39, no. 2, pp. 890–895, Jan. 2014, doi: 10.1016/j.ijhydene.2013.10.087.

[88]	M. Taddei et al., “Efficient microwave assisted synthesis of metal–organic framework UiO-66: optimization and scale up,” Dalton Trans., vol. 44, no. 31, pp. 14019–14026, 2015, doi: 10.1039/C5DT01838B.

[89]	K. Užarević et al., “Mechanochemical and solvent-free assembly of zirconium-based metal–organic frameworks,” Chem. Commun., vol. 52, no. 10, pp. 2133–2136, 2016, doi: 10.1039/C5CC08972G.

[90]	T. Bailey, M. Pinto, N. Hondow, and K.-J. Wu, “Continuous microfluidic synthesis of zirconium-based UiO-67 using a coiled flow invertor reactor,” MethodsX, vol. 8, p. 101246, 2021, doi: 10.1016/j.mex.2021.101246.

[91]	A. M. Fidelli et al., “Green and rapid mechanosynthesis of high-porosity NU- and UiO-type metal–organic frameworks,” Chem. Commun., vol. 54, no. 51, pp. 6999–7002, 2018, doi: 10.1039/C8CC03189D.

[92]	J. Xu et al., “Optimized synthesis of Zr( iv ) metal organic frameworks (MOFs-808) for efficient hydrogen storage,” New J. Chem., vol. 43, no. 10, pp. 4092–4099, 2019, doi: 10.1039/C8NJ06362A.

[93]	L. González, R. Gil-San-Millán, J. A. R. Navarro, C. R. Maldonado, E. Barea, and F. J. Carmona, “Green synthesis of zirconium MOF-808 for simultaneous phosphate recovery and organophosphorus pesticide detoxification in wastewater,” J. Mater. Chem. A, vol. 10, no. 37, pp. 19606–19611, 2022, doi: 10.1039/D2TA02074B.

[94]	S. Bagi, S. Yuan, S. Rojas-Buzo, Y. Shao-Horn, and Y. Román-Leshkov, “A continuous flow chemistry approach for the ultrafast and low-cost synthesis of MOF-808,” Green Chem., vol. 23, no. 24, pp. 9982–9991, 2021, doi: 10.1039/D1GC02824C.

[95]	T. C. Wang et al., “Scalable synthesis and post-modification of a mesoporous metal-organic framework called NU-1000,” Nat Protoc, vol. 11, no. 1, pp. 149–162, Jan. 2016, doi: 10.1038/nprot.2016.001.

[96]	P. Zhang et al., “A New Route for the Rapid Synthesis of Metal–Organic Frameworks at Room Temperature,” CCS Chem, vol. 5, no. 6, pp. 1462–1469, May 2023, doi: 10.31635/ccschem.022.202202155.

[97]	M. I. Severino et al., “MOFs with Open Metal(III) Sites for the Environmental Capture of Polar Volatile Organic Compounds,” Angew Chem Int Ed, vol. 62, no. 6, p. e202211583, Feb. 2023, doi: 10.1002/anie.202211583.

[98]	M. Naguib et al., “Two‐Dimensional Nanocrystals Produced by Exfoliation of Ti3 AlC2,” Advanced Materials, vol. 23, no. 37, pp. 4248–4253, Oct. 2011, doi: 10.1002/adma.201102306.

[99]	C. E. Shuck et al., “Effect of Ti3 AlC2 MAX Phase on Structure and Properties of Resultant Ti3 C2 T x  MXene,” ACS Appl. Nano Mater., vol. 2, no. 6, pp. 3368–3376, June 2019, doi: 10.1021/acsanm.9b00286.

[100]	T. S. Mathis et al., “Modified MAX Phase Synthesis for Environmentally Stable and Highly Conductive Ti3 C2 MXene,” ACS Nano, vol. 15, no. 4, pp. 6420–6429, Apr. 2021, doi: 10.1021/acsnano.0c08357.

[101]	C. E. Shuck et al., “Scalable Synthesis of Ti3 C2 T x  MXene,” Adv Eng Mater, vol. 22, no. 3, p. 1901241, Mar. 2020, doi: 10.1002/adem.201901241.

[102]	S. Jolly, M. P. Paranthaman, and M. Naguib, “Synthesis of Ti3C2Tz MXene from low-cost and environmentally friendly precursors,” Materials Today Advances, vol. 10, p. 100139, June 2021, doi: 10.1016/j.mtadv.2021.100139.

[103]	A. E. Ghazaly et al., “Ultrafast, One-Step, Salt-Solution-Based Acoustic Synthesis of Ti3 C2 MXene,” ACS Nano, vol. 15, no. 3, pp. 4287–4293, Mar. 2021, doi: 10.1021/acsnano.0c07242.

[104]	M. Alhabeb et al., “Guidelines for Synthesis and Processing of Two-Dimensional Titanium Carbide (Ti3 C2 T x  MXene),” Chem. Mater., vol. 29, no. 18, pp. 7633–7644, Sept. 2017, doi: 10.1021/acs.chemmater.7b02847.

[105]	N. Srivastava, M. Saquib, P. Arora, and A. C. Bhosale, “Investigation of NiMoSe/Ti3C2Tx on Carbon Cloth as an Effective Electrocatalyst for the Hydrogen Evolution Reaction in an Acidic Medium,” Energy and Fuels, vol. 39, no. 12, pp. 5719–5729, 2025, doi: 10.1021/acs.energyfuels.4c05965.