Electrocatalytic Detection and Adsorptive Removal of Rose Bengal Dye from Wastewater

Maria Khana, Afzal Shaha*, Mohsin Javeda

aDepartment of Chemistry Quaid-i-Azam University, Islamabad 45320, Pakistan

Correspondence*: afzals_qau@yahoo.com

Supporting Information

Table S1: Chemicals catalog listing and associated purity standards and suppliers.

| S. No. | Chemicals | Purity (%) | Supplier |
| --- | --- | --- | --- |
| 1. | Acetone | 99 | Riedel-deHaen |
| 2. | Ammonia solution | 25% | Merck |
| 3. | Bismuth nitrate pentahydrate | ˃99 | Sigma Aldrich |
| 4. | Dimethylformamide | 99 | Riedel-deHaen |
| 5. | Disodium hydrogen phosphate dihydrate | ˃99 | Merck |
| 6. | Ethanol | 99.8 | Riedel-deHaen |
| 7. | Iron nitrate nonahydrate | >99 | Sigma Aldrich |
| 8. | Potassium chloride | 99 | Sigma Aldrich |
| 9. | Potassium hexacyanoferrate | ˃99 | Sigma Aldrich |
| 10. | Rose bengal | Extra pure | Sigma Aldrich |
| 11. | Sodium hydroxide | 97 | Fluka |
| 12. | Sodium dihydrogen phosphate monohydrate | ˃99 | Merck |
| 13. | Sulfuric acid | 98 | Merck |
| 14. | Zinc nitrate hexahydrate | 98 | Sigma Aldrich |

Table S2: Parameters obtained from CV analysis.

| Working electrode | Electroactive surface area (cm2) | Peak separation (mV) |
| --- | --- | --- |
| Bare GCE | 0.035 | 105 |
| Fe-ZnO/GCE | 0.053 | 93 |
| MWCNTs/GCE | 0.087 | 90 |
| Fe-ZnO/MWCNTs/GCE | 0.112 | 85 |

Table S3: Parameters obtained from recovery of RB in distilled and tap water.

| Sample | Spiked amount (µM) | Found (n=3) (µM) | RSD (%) | Recovery (%) |
| --- | --- | --- | --- | --- |
| Distilled water | 15 | 14.97 | 1.42 | 99.8 |
| Tap water | 15 | 14.26 | 4.30 | 95.1 |

Figure S1: Equivalent circuit used for assessment of EIS parameters.

Figure S2: (A) Bar graph between Ip vs various supporting electrolytes, (B) SWVs of RB were recorded in NaOH solution with concentrations ranging from 0.1 M to 0.4 M by using Fe-ZnO/MWCNTs as a modifier, and (C) Ip vs various concentration of NaOH as electrolyte.

Figure S3: (A) Impact of deposition potential on SWV peak current of 30 µM RB, (B) Ip vs deposition potential, (C) The impact of accumulation time on the anodic peak current of 30 µM RB, and (D) Ip vs deposition time.

Figure S4: (A) SWVs of 20 µM RB using different modified GCEs in 0.2 M NaOH, and (B) SWVs showing repeatability for electroanalysis of 20 µM RB at different time intervals

Figure S5: (A) Linear calibration curve of absorbance vs concentration for RB, (B) pseudo-first-order kinetic, (C) Intraparticle diffusion kinetics, and (D) Elovich model.