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Fig. 1 X-ray diffractograms of fine clay fractions (<0.2m); Ca=Ca saturated; Ca-EG=Ca saturated plus ethylene glycol vapour; CaGLV=Ca-saturated plus glycerol vapour; Li=Li-saturated and heated to 250oC (16h), LiGLV=Li-saturated and heated to 250oC plus glycerol vapour; K-saturated and heated to 25, 110, 300, 550oC. K300EG= K-saturated plus ethylene glycol vapour and heated to 300oC; Sm=Smectite, B-N = beidellite-nontronite; V+Ch = vermiculite plus chlorite; M = mica; Mt = montmorillonite; K = Kaolinite; F = Feldspars.  
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