Supplementary Data

Effect of CNT Dispersion and Content on the Properties and Fuel Cell Performance of Bipolar Plates

# Seon Ho Leea,b,1, Song Mi Lee a,b,1, Seungjoo Park a,b, Doo-Hwan Jungb,*, Young-Seak Leea,c,*

# aDepartment of Chemical Engineering and Applied Chemistry, Chungnam National University, Daejeon 34134, Republic of Korea

# bHigh Temperature Electolysis Laboratory, Korea Institute of Energy Research, Daejeon 34129, Republic of Korea

# cInstitute of Carbon Fusion Technology (InCFT), Chungnam National University, 99 Daehak-ro, Yuseong-gu, Daejeon, 34134, Korea

* Corresponding author at: High Temperature Electrolysis Laboratory, Korea Institute of Energy Research (KIER), Daejeon 34129, Republic of Korea.

** Corresponding author at: Institute of Carbon Fusion Technology (InCFT), Chungnam National University, Daejeon 34134, Republic of Korea.

E-mail addresses: youngslee@cnu.ac.kr (Y.-S. Lee), doohwan@kier.re.kr (D.-H. Jung).

1 These authors contributed equally to this paper.

Table S1. Specification of synthetic graphite and MWCNT.

|  | SG | LG | CNT |
| --- | --- | --- | --- |
| Bulk Density (g/cc) | 0.07 | 0.42 | 0.08~0.13 |
| Particle size(D50) (μm) | 3.4 | 5.0 | Dia. 10–15 nm /Length 60–80 μm |
| Particle size(D90) (μm) | 5.8~7.1 | 63.0~100.0 | - |
| BET (m2/g) | 26 | 3 | 155-195 |
| Powder Resistivity (Ω·cm) | 1.55~2.25 | 1.55~2.25 | ~0.021 |
| Moisture Content (%) | 0.10~0.50 | 0.10~0.50 | - |
| Ash (% max) | 0.06~0.10 | 0.06~0.10 | - |