Supporting Information

Site-Selective Ru Doping in Spinel Co3O4 Unlocks Dual-Site Synergy for Acidic Water Electrolysis

Yumeng Wang1, Yaling Zhang1, Shiyao Chen1, Yameng Fan2, Jian Peng3, Tofik Ahmed Shifa4, Yaping Li1*, Alberto Vomiero4, Fengmei Wang1*, and Xiaoming Sun1*

1State Key Laboratory of Chemical Resource Engineering, College of Chemistry, Beijing University of Chemical Technology, Beijing 100029, P. R. China.

2School of Science, RMIT University, Melbourne, VIC 3000, Australia

3Eastern Institute for Advanced Study, Eastern Institute of Technology, Ningbo, 315200, China.

4Department of Molecular Sciences and Nanosystems, Ca’ Foscari University of Venice Via Torino 155,30172 Venezia Mestre, Italy.

Correspondence: Yaping Li, E-mail:liyp@mail.buct.edu.cn.

Fengmei Wang: wangfm@buct.edu.cn.

Xiaoming Sun: sunxm@mail.buct.edu.cn

Experimental Section

Materials. Cobalt(Ⅱ) nitrate (Co(NO3)2·6H2O, AR), was purchased from Shanghai Aladdin Biochemical Technology Co., Ltd. Ruthenium tri-chloride hydrate (RuCl3·xH2O, content (as Ru) % 35.0−38.0) was purchased from Shenyang Nonferrous Metals Research Institute Co., Ltd. and no further purification was required. Carbon cloth was purchased from Toray Industries, Inc.

Catalyst Preparation. Oct-RuxCo3-xO4 with Ru substituted at the octahedral sites of Co₃O₄, was prepared through electrodeposition followed by cation exchange. Briefly, 1.41 g of Co(NO3)₂·6H₂O was dissolved in 100 mL of deionized water to form the electrolyte. A standard three-electrode system was employed, consisting of an Ag/AgCl electrode as reference electrode, a graphite rod as counter electrode, and a carbon cloth (2 × 2 cm², precleaned by ethanol and deionized water) as the working electrode. Electrodeposition was performed at −1 V (vs. Ag/AgCl electrode) for 15 min to deposit a Co(OH)2 precursor onto the carbon cloth (i.e., Co(OH)₂/CC). The resulting Co(OH)2/CC was thoroughly rinsed with deionized water dried at 80 °C for 12 h, and then calcined in air at 300 °C for 3 h to obtain Co₃O₄/CC. For cation exchange, the Co₃O₄/CC precursor was immersed in an aqueous solution of RuCl3 (0.3 mg/mL) in a glass vial, which was heated at 60 °C for 9 h. The product was repeatedly washed with deionized water and annealed at 300 °C for 3 h in a tube furnace, yielding Oct-Ru0.13Co2.87O4/CC with partial substitution of octahedral Co by Ru. The Ru content in the Oct-RuxCo3-xO4 was tuned by varying the concentration of RuCl₃ solution and quantified by Inductively Coupled Plasma Mass spectrometry (ICP-MS). As a comparison, Co₃O₄/CC sample was prepared under the same procedure, except for the absence of cation exchange treatment. Tet-RuxCo3-xO4 with Ru substitution at tetrahedral Co sites, was synthesized through a one-step electrodeposition method. The electrolyte was prepared by dissolving different ratio of RuCl₃·xH₂O and Co(NO3)2·6H2O in 100 mL deionized water. Using the same three-electrode configuration, cyclic electrodeposition was conducted between −1.2 V and −0.2 V (vs. Ag/AgCl) for 80 cycles. The as-obtained RuCo(OH)ₓ/CC precursor was washed extensively with deionized water and annealed at 300 °C for 3 h under inert atmosphere to produce Tet-RuxCo3-xO4/CC.

Structural Characterizations. The morphology of the samples characterized by scanning electron microscope (SEM，JEM 2100F, Japan) at an acceleration voltage of 5 kV. The elemental information was observed by energy dispersive X-ray spectroscopy (EDS) equipped with the SEM. The content of the elements in the samples was analyzed quantitatively by ICP-MS (iCAP 7400, Thermo Fisher). The crystal characteristics of the samples was tasted by Rigaku D/max 2500 X-ray diffractometer, the angle range of the test is 10-90° and the scan rate was 10° min-1. The chemical states of different element of the samples were collected by an X-ray photoelectron spectrometer (ESCALAB 250). The Raman spectra of the samples were collected by using a LabRAM Odyssey equipped with a diode laser operating at 633 nm. Microstructure observation was characterized by high-resolution transmission electron microscopy (HR-TEM) using a double aberration-corrected field emission gun transmission electron microscope Titan 80−300 at a voltage of 200 kV. The K-edge XAS spectra of Ru and Co were acquired at the 1W1B station of the Beijing Institute of High Energy Physics.

Electrocatalyst Characterizations. The electrochemical tests were performed in a three-electrode system at room temperature (25℃) in O2-saturated 0.5 M H2SO4 electrolyte solution in an electrochemical workstation (Chenhua, CHI760E). The catalyst on CC was cut into a 1×1cm2 film as the working electrode, while a platinum sheet and a saturated calomel electrode (SCE) served as the counter and reference electrodes, respectively. All the potentials shown in our research were calibrated with the reversible hydrogen electrode (RHE). The cyclic voltammetry (CV) curve tests were recorded in a potential window ranging from 0.8 V to 1.8 V vs SCE at a scan rate of 50 mV s−1. Then the Linear sweep voltammetry (LSV) curve of the catalyst was performed at a scan rate of 5 mV s−1 in the voltage range of 0.8 V to 1.8V vs SCE. A chronopotentiometry (CP) test was performed at a room temperature @ 10 mA·cm-2. The solution resistance (Rs) was collected by electrochemical impedance spectra (EIS) in the frequency range from 0.01 Hz to 10 kHz at the potential of 1.5 V.

The Membrane Electrode Assembly of PEM device was prepared by the catalyst coating membrane (CCM) method. The 20 wt % commercial platinum carbon catalyst powder was first dispersed in a mixture of isopropyl alcohol, deionized water and Nafion solution (5 wt %). The ink was sprayed onto the Nafion 117 proton exchange membrane. The catalyst on CC was hot-pressed onto the proton exchange membrane at 120 °C. Titanium felt and carbon paper were used as gas diffusion layers for the anode and cathode, respectively.

Theoretical Calculations. All DFT calculations were performed using the Viena Ab initio Simulation Package (VASP). The projector augmented wave (PAW) pseudopotential with the PBE generalized gradient approximation (GGA) exchange correlation function was utilized in the computations.1 The cutoff energy of the plane waves basis set was 450 eV and a Monkhorst-pack mesh of 2×2×1 was used in K- sampling.2 All structures were spin polarized and all atoms were fully relaxed with the energy convergence tolerance of 10-4 eV per atom, and the final force on each atom was < 0.05 eV Å-1. In order to improve the accuracy of model calculation, the DFT+U calculation method was used to describe the correlation of 3d transition metal system. According to previous work, the U value could be selected as 3.3 for Co3 and 2.0 for Ru.4

The adsorption energy of reaction intermediates, can be computed using the following Equation5:

ΔGads =Eads- E*+ ΔEZPE – TΔS

Where Eads is the calculated adsorption energy for the OH*, O*, OOH*, O*- OH*, O*- O* intermediates, and E* is the binding energy of the corresponding intermediates, ΔEZPE is the zero-point energy change, ΔS is the entropy change, T is the temperature (T = 298.15 K). The values of ΔEZPE and ΔS were obtained by vibration frequency calculation.

Fig S1. SEM images of (a) Oct-Ru0.08Co2.92O4,(b) Oct-Ru0.47Co2.53O4 and (c)Oct-Ru0.59Co2.41O4 (d) Co3O4 nanosheet arrays synthesized on the carbon cloth.

Fig S2. SEM images of (a) Tet-Ru0.07Co2.93O4 and (b)Tet-Ru0.42Co2.58O4 nanosheet arrays synthesized on the carbon cloth.

Fig S3. SEM images of Co3O4 nanosheet arrays synthesized on the carbon cloth.

Fig S4.HR-TEM images of the Co3O4 sample.

Fig S5. The EDS mapping images of the Oct-RuxCo3-xO4 samples. (a) Oct-Ru0.08Co2.92O4; (b) Oct-Ru0.47Co2.53O4 and (c) Oct-Ru0.59Co2.41O4.

Fig S6. The EDS mapping images of the Tet-RuxCo3-xO4 samples. (a) Tet-Ru0.07Co2.92O4; (b) Tet-Ru0.18Co2.53O4 and (c) Tet-Ru0.42Co2.58O4.

Fig S7. The EDS spectra collected from Oct-RuxCo3-xO4 samples. (a) Oct-Ru0.08Co2.92O4; (b) Oct-Ru0.13Co2.87O4; (c) Oct-Ru0.47Co2.53O4 and (d) Oct-Ru0.59Co2.41O4.

Fig S8. The EDS spectra collected from Oct-RuxCo3-xO4 samples. (a) Tet-Ru0.07Co2.92O4; (b) Tet-Ru0.18Co2.53O4; (c) Tet-Ru0.42Co2.58O4.

Fig S9. Full XPS survey spectra collected from theOct-Ru0.13Co2.87O4 sample.

Fig S10. Full XPS survey spectra collected from the Tet-Ru0.18Co2.82O4 sample.

Fig S11. O 1s scan analysis of the Oct-Ru0.13Co2.87O4 and Tet-Ru0.18Co2.82O4, compared with the Co3O4 and RuO2 as the references.

Fig S12. Co K-edge EXAFS spectra of the Oct-Ru0.13Co2.87O4 compared with the Co3O4 sample.

Fig S13. Ru K-edge EXAFS spectra of the Oct-Ru0.13Co2.87O4 and Tet-Ru0.18Co2.82O4 samples with the RuO2, Ru foil and RuCl3 as the references.

Fig S14. Co L-edge XAS spectra of the Oct-Ru0.13Co2.87O4, Tet-Ru0.18Co2.82O4 and Co3O4 sample.

Fig S15. Ru K-edge EXAFS spectra in K space of the (a) Oct-Ru0.13Co2.87O4, (b) Tet-Ru0.18Co2.82O4 and (c) RuO2 sample.

Fig S16. Tafel plots of various Oct-RuxCo3-xO4 (x=0.08, 0.13, 0.47, 0.59) and Co3O4 electrodes.

Fig S17. Tafel plots of various Tet-RuxCo3-xO4 (x=0.07, 0.18, 0.42) electrodes, compared with the Co3O4 electrode.

Fig S18. Electrochemical double-layer capacitance (Cdl) of Oct-RuxCo3-xO4 and Co3O4. (a-c) Representative CV curves collected at different scan rates of 2-10 mV s⁻¹ under the potential range of 1.044 -1.144 V vs. RHE of Oct-RuxCo3-xO4 (x=0.13, 0.47, 0.59). (d) Cdl values calculated from the CV curves.

Fig S19. Electrochemical double-layer capacitance (Cdl) of Oct-RuxCo3-xO4 and Co3O4. (a-c) Representative CV curves collected at different scan rates of 2-10 mV s⁻¹ under the potential range of 1.044 -1.144 V vs. RHE of Oct-RuxCo3-xO4 (x=0.07, 0.18, 0.42). (d) Cdl values calculated from the CV curves.

Fig S20. LSV curves normalized to ECSA of (a) Oct-RuxCo3-xO4, (b) Tet-RuxCo3-xO4 and Co3O4 samples. The electrochemically active surface area (ECSA) of the catalysts was estimated from the electrochemical double-layer capacitance (Cdl) of the catalytic surface using a specific equation (ECSA=Cdl/Cs), whereas Cs value is 0.035 mF cm−2 in acid electrolyte.

Fig S21. EIS plots collected from various Oct-RuxCo3-xO4 (x=0.08, 0.13, 0.47, 0.59) and Co3O4 electrodes, inset, the simulative equivalent circuit.

Fig S22. EIS plots collected from various Tet-RuxCo3-xO4 (x=0.08, 0.18, 0.42) electrodes, compared with the Co3O4 electrode, inset, the simulative equivalent circuit.

Fig S23. XRD pattern collected from Tet-Ru0.18Co2.82O4 sample after the stability test at 10 mA cm-2 for 50 h.

Fig S24. Raman pattern collected from Tet-Ru0.18Co2.82O4 sample after the stability test at 10 mA cm-2 for 50 h.

Fig S25. XRD spectra of (a) Oct-Ru0.13Co2.87O4 and (b) Oct-Ru0.59Co2.41O4 after the stability test at 10 mA cm-2 for 240 h and 135h .

Fig S26. Raman spectra collected from fresh Oct-Ru0.13Co2.87O4, Oct-Ru0.13Co2.87O4 and Oct-Ru0.59Co2.41O4 sample after the stability test at 10 mA cm-2 for 240 h and 135h.

Fig S27. (a) Ru 3p and (b) Co 2p XPS spectra collected from the fresh Oct-Ru0.13Co2.87O4 catalyst and the sample after the stability test at 10 mA cm-2 for 240 h.

Fig S28. (a) The EDS mapping images, (b) and inset the EDS result of the Oct-Ru0.13Co2.87O4 sapmle after the stability test at 10 mA cm-2 for 240 h.

Fig S29. Bader charge distribution calculated from Co3O4 model.

Fig S30. Bader charge density calculated on (a)Oct-Ru0.13Co2.87O4 (b)Tet-Ru0.13Co2.87O4 (c) and (d) Co3O4 models (bule ball: Co or Ru, red ball: O)

Fig S31. Co 3d, O 2p, and Ru 4d PDOS spectra of Oct-Ru0.13Co2.87O4, Tet-Ru0.13Co2.87O4 and Co3O4 models.

Table S1 The ratio of Co and Ru in various Oct-RuxCo3-xO4 (x=0.07, 0.13, 0.47, 0.59) measured through ICP-OES.

|  |  | Oct-Ru0.08Co2.92O4 | Oct-Ru0.13Co2.87O4 | Oct-Ru0.47Co2.53O4 | Oct-Ru0.59Co2.41O4 |
| --- | --- | --- | --- | --- | --- |
| ppm | Ru | 0.289 | 0.236 | 1.326 | 3.183 |
|  | Co | 6.137 | 3.049 | 4.154 | 7.571 |

Table S2 The ratio of Co and Ru in various Tet-RuxCo3-xO4 (x=0.08, 0.18,0.42)measured by ICP-OES.

|  | Tet-Ru0.08Co2.92O4 |  | Tet-Ru0.18Co2.82O4 | Tet-Ru0.42Co2.58O4 |
| --- | --- | --- | --- | --- |
| ppm | Ru | 0.112 | 0.497 | 1.821 |
|  | Co | 2.752 | 4.522 | 6.532 |

Table S3. Comparison of overpotential and stability @10mA cm-2 of the Oct-Ru0.13Co2.87O4 electrocatalyst with and other reported acidic OER electrocatalysts.

| Electrocatalyst | Electrolyte | overpotential (mV @ 10 mA cm-2) | Stability (h @ 10 mA cm-2) | Reference |
| --- | --- | --- | --- | --- |
| Oct-Ru0.13Co2.87O4 | 0.5 M H2SO4 | 240 | 234 | This work |
| IrOx-B | 0.1 M HClO4 | 292 | 10 | [6] |
| Ir-doped WO3 | 0.5 M H2SO4 | 258 | 60 | [7] |
| Ir SAs-NiCo2O4 NSs | 0.5 M H2SO4 | 240 | 70 | [8] |
| Ir-MnO2 | 0.5 M H2SO4 | 280 | 100 | [9] |
| Ir0.06Co2.94O4 | 0.1 M HClO4 | 300 | 200 | [10] |
| RuCu | 0.5 M H2SO4 | 270 | 20 | [11] |
| IrSAE-CMO | 0.5 M H2SO4 | 235 | 25 | [12] |
| Ir0.3Mo0.7O8 | 0.1 M HClO4 | 345 | 11 | [13] |
| Ir-Co3O4 | 0.5 M H2SO4 | 236 | 30 | [14] |
| Ru-SA/Ti3C2Tx | 0.1 M HClO4 | 290 | 32 | [15] |
| IrO2/MnO2 | 0.5 M H2SO4 | 310 | 80 | [16] |
| La3IrO7-SLD | 0.1 M HClO4 | 296 | 17 | [17] |
| LaMn-Co3O4 | 0.5 M H2SO4 | 353 | 80 | [18] |
| PdCu/Ir/C | 0.5 M H2SO4 | 283 | 15 | [19] |
| IrBa-Co3O4 | 0.5 M H2SO4 | 295 | 100 | [20] |

REFERENCE

1	Perdew, J. P. et al. Atoms, molecules, solids, and surfaces: Applications of the generalized gradient approximation for exchange and correlation. Physical Review B 46, 6671-6687, doi:10.1103/PhysRevB.46.6671 (1992).

2	Monkhorst, H. J. & Pack, J. D. Special points for Brillouin-zone integrations. Physical Review B 13, 5188-5192, doi:10.1103/PhysRevB.13.5188 (1976).

3	Wang, L., Maxisch, T. & Ceder, G. Oxidation energies of transition metal oxides within the GGA+U framework. Physical Review B 73, 195107, doi:10.1103/PhysRevB.73.195107 (2006).

4	Yang, H.-C., Gong, B.-C., Liu, K. & Lu, Z.-Y. J. J. o. P. C. M. Quasi-degenerate magnetic states in α-RuCl3. 31, 025803 (2018).

5	Rossmeisl, J., Logadottir, A. & Nørskov, J. K. Electrolysis of water on (oxidized) metal surfaces. Chemical Physics 319, 178-184, doi:10.1016/j.chemphys.2005.05.038 (2005).

6	Cheng, Z., Pi, Y., Shao, Q. & Huang, X. Boron-doped amorphous iridium oxide with ultrahigh mass activity for acidic oxygen evolution reaction. Science China Materials 64, 2958-2966, doi:10.1007/s40843-021-1687-5 (2021).

7	Li, P., Duan, X., Kuang, Y. & Sun, X. Iridium in Tungsten Trioxide Matrix as an Efficient Bi-Functional Electrocatalyst for Overall Water Splitting in Acidic Media. Small 17, 2102078, doi:10.1002/smll.202102078 (2021).

8	Yin, J. et al. Iridium Single Atoms Coupling with Oxygen Vacancies Boosts Oxygen Evolution Reaction in Acid Media. Journal of the American Chemical Society 142, 18378-18386, doi:10.1021/jacs.0c05050 (2020).

9	Sun, Y., Chen, J., Liu, L., Chi, H. & Han, H. The mechanism of OER activity and stability enhancement in acid by atomically doped iridium in γ-MnO2. Chinese Journal of Catalysis 69, 99-110, doi:10.1016/S1872-2067(24)60201-9 (2025).

10	Shan, J. et al. Short-Range Ordered Iridium Single Atoms Integrated into Cobalt Oxide Spinel Structure for Highly Efficient Electrocatalytic Water Oxidation. Journal of the American Chemical Society 143, 5201-5211, doi:10.1021/jacs.1c01525 (2021).

11	Li, Y. et al. Donutlike RuCu Nanoalloy with Ultrahigh Mass Activity for Efficient and Robust Oxygen Evolution in Acid Solution. ACS Applied Energy Materials 2, 7483-7489, doi:10.1021/acsaem.9b01459 (2019).

12	Kumar, A. et al. Iridium Single-Atom-Ensembles Stabilized on Mn-Substituted Spinel Oxide for Durable Acidic Water Electrolysis. Advanced Materials 36, 2401648, doi:10.1002/adma.202401648 (2024).

13	Tariq, M. et al. Unraveling the Beneficial Electrochemistry of IrO2/MoO3 Hybrid as a Highly Stable and Efficient Oxygen Evolution Reaction Catalyst. ACS Sustainable Chemistry & Engineering 6, 4854-4862, doi:10.1021/acssuschemeng.7b04266 (2018).

14	Zhu, Y. et al. Iridium single atoms incorporated in Co3O4 efficiently catalyze the oxygen evolution in acidic conditions. Nature Communications 13, 7754, doi:10.1038/s41467-022-35426-8 (2022).

15	Peng, X. et al. Trifunctional Single-Atomic Ru Sites Enable Efficient Overall Water Splitting and Oxygen Reduction in Acidic Media. Small 16, 2002888, doi:10.1002/smll.202002888 (2020).

16	Wang, F. et al. IrO2/MnO2 metal oxide-support interaction enables robust acidic water oxidation. Journal of Colloid and Interface Science 683, 160-169, doi:10.1016/j.jcis.2024.12.033 (2025).

17	Qin, Q. et al. Gettering La Effect from La3IrO7 as a Highly Efficient Electrocatalyst for Oxygen Evolution Reaction in Acid Media. Advanced Energy Materials 11, 2003561, doi:10.1002/aenm.202003561 (2021).

18	Chong, L. et al. La- and Mn-doped cobalt spinel oxygen evolution catalyst for proton exchange membrane electrolysis. Science 380, 609-616, doi:10.1126/science.ade1499 (2023).

19	Li, M. et al. Exclusive Strain Effect Boosts Overall Water Splitting in PdCu/Ir Core/Shell Nanocrystals. Angewandte Chemie International Edition 60, 8243-8250, doi:10.1002/anie.202016199 (2021).

20	Huo, M. et al. Barium-induced compressive strain engineering in low-iridium Co3O4 spinel for high-efficiency acidic oxygen evolution. Chemical Engineering Journal 519, 165555, doi:10.1016/j.cej.2025.165555 (2025).