Electronic Structure Engineering and Photocatalytic Potential of MA2N4 Two-Dimensional Materials: A First-Principles Perspective

Dan Hong, a, Qi-Jun Liu c, Tao Jiang a, Hui Liu a, Zheng-Tang Liu d, Yu-Lan Ren ,b

a School of Intelligent Medicine, Chengdu University of Traditional Chinese Medicine, Chengdu 611137, China

b School of Chinese Classics, Chengdu University of Traditional

Chinese Medicine, Chengdu 610075, China

c School of Physical Science and Technology, Southwest Jiaotong University, Key Laboratory of Advanced Technologies of Materials, Ministry of Education of China, Chengdu 610031, People’s Republic of China

d State Key Laboratory of Solidification Processing, Northwestern Polytechnical University, Xi’an 710072, People’s Republic of China

Correspondence about the paper at the following address and e-mail address:

Dan Hong E-mail: 18382927860@163.com

Yu-Lan Ren E-mail: renxg2468@163.com

School of Intelligent Medicine, School of Chinese Classics, Chengdu University of Traditional Chinese Medicine, Chengdu 611137, China

1. Band structures and density of states

The calculated electronic properties (including band structures and density of states) by HSE06 for MA2N4 (M= Ti, Zr, Hf, V, Nb, Ta, Cr, Mo and W, A is Si) are depicted in Figure S1. It can be seen that the minimum of conduction band (CBM) and maximum of valence band (VBM) VSi2N4, NbSi2N4 and TaSi2N4 all through the Fermi level, implying that the metallic properties of them. All the rest of materials have band gaps, and which are all indirect band gaps. On the whole, the band gaps of VI group are smaller than the IV group materials, which can be contributed to more extra d electrons in the outermost shell of VI group metal. It can be seen from the partial density of states (PDOS) that the CBM and VBM are mainly made up by the d orbitals of the metal elements, and there are little contributions of electrons from A and N elements.

Moreover, we classify the 9 original materials (exclude the VSi2N4, NbSi2N4 and TaSi2N4 by considering the characteristics of their band gaps) according to the size of their band gap, which as follows: small band gap (CrSi2N4 with 0.522 eV), big band gap (MoSi2N4 with 2.61 eV, WSi2N4 with 2.16 eV, TiSi2N4 with 2.907 eV, ZrSi2N4 with 2.532 eV and HfSi2N4 with 3.101 eV) to investigate their specific photoelectric performance. Firstly, we calculate and plot the optical spectra of the polycrystalline for the origin 6 materials in Figure S2. It can be observed that the reflectivity is arranged from high to low as CrSi2N4, MoSi2N4, TiSi2N4, WSi2N4, ZrSi2N4 and HfSi2N4, and the absorption coefﬁcient, ranked by the list from the high to low, is CrSi2N4, ZrSi2N4, MoSi2N4, TiSi2N4, WSi2N4 and HfSi2N4. Therein, the approximate absorption coefﬁcients for MoSi2N4, TiSi2N4, WSi2N4 can be attributed to the closer values of their band gap. Due to the smallest band gap, the reflectivity and absorption coefﬁcient of CrSi2N4 are the highest in these 6 original materials, respectively. Nevertheless, HfSi2N4 owns the minimum reflectivity and absorption coefﬁcient, which corresponds to the greatest band gap. Hence, it can be intuitively understood that CrSi2N4 and HfSi2N4 have the minimum and maximum transmissivity, respectively. The band gaps of the remaining 4 materials range from 2.16 to 2.907 eV, meaning a certain part of the 4 materials is transparent in the visible light (VIS) region and which is consistent with the analysis of the reflectivity and absorption coefficient.

2. Effective masses of carriers

Effective masses of the 6 original materials were calculated, which are depicted in Figure S3. It can be seen that CrSi2N4, MoSi2N4 and WSi2N4 exhibit the lighter hole and electron effective mass corresponding to the higher curvature of band structures that can be seen in Figure S1, which suggests a strong capacity of hole and electron mobility. The remaining TiSi2N4, ZrSi2N4, and HfSi2N4 have a more localized band distribution near the Fermi level, resulting in a greater effective mass. Thus, the carrier mobility and electrical conductivity of VI group are superior to those of IV group. Moreover, the greater discrepancy between mh/me and 1, the greater the difference in electron-hole mobility, indicating a lower recombination rate of electron-hole pairs. It can be observed that CrSi2N4, MoSi2N4 and WSi2N4 also generally have more excellent mh/me value than other three materials, reflecting the lower recombination rate of electron-hole pairs for them. The more preeminent carrier mobility and carrier recombination, which suggests CrSi2N4, MoSi2N4 and WSi2N4 not only have better electrical conductivity (which can be effectively applied in transparent conductive device), but also can be reasonably used in photocatalysts.

To sum up, CrSi2N4 has excellent conductivity with the unsatisfactory transparency in visible light range yet. MoSi2N4 and WSi2N4 have certain transparency with promising conductivity and degradation ability, making them can be effectively applied in transparent conductive devices and photocatalysts.  Although HfSi2N4 owns the splendid transparency, the imperfect carrier effective mass makes it difficult to as an n-type transparent electrical device, it can be considered as a potential p-type transparent conductive material yet. Moreover, it also can be reasonably used as a photocatalyst. TiSi2N4 and ZrSi2N4 have weaker photocatalytic properties than HfSi2N4, but they still can be used as photocatalysts and they also can be considered as the potential for making p-type conductors.

Figure S1 The calculated band structures and density of states for MA2N4 by HSE06, therein, M= Ti, Zr, Hf, V, Nb, Ta, Cr, Mo and W, A is Si.

Figure S2 Reflectivity, absorption coefﬁcient, Imaginary and real parts of the dielectric function for 6 original materials by HSE06.

Figure S3. The calculated effective mass with band gaps of 6 original materials.

(a) CrC2N4                                        (b) CrC2N4

(c) CrGe2N4                                        (d) MoC2N4

(e) MoSi2N4                                        (f) MoGe2N4

(g) WC2N4                                        (h) WSi2N4

(i) WGe2N4                                        (j) TiC2N4

(k) TiSi2N4                                        (l) ZrSi2N4

(m) ZrGe2N4                                        (n) ZrSn2N4

(o) ZrPb2N4                                        (p) HfSi2N4

(q) HfGe2N4

Figure S4 The calculated phonon spectra of 17 kinds of MA2N4.

Figure S5. The calculated lattice parameter for CrA2N4, MoA2N4, WA2N4, TiA2N4, ZrA2N4 and HfA2N4.

Figure S6. The calculated band structures and density of states of A-site-substituted MA2N4.

(a)

(b)

(c)

(d)

(e)

(f)

Figure S7. The partial charge density of (111) plane for CrA2N4 (a), MoA2N4 (b), WA2N4 (c), TiA2N4 (d), ZrA2N4 (e) and HfA2N4 (f).

(a)

(b)

(c)

(d)

(e)

(f)

Figure S8. The calculated reffectivity, absorption coefffcient (α), complex dielectric function of CrA2N4 (a), MoA2N4 (b), WA2N4 (c), TiA2N4 (d), ZrA2N4 (e) and HfA2N4 (f).

Table S1. The calculated lattice parameters and band gaps by GGA-PBE and HSE06 for MSi2N4 (M= Ti, Zr, Hf, V, Nb, Ta, Cr, Mo and W).

| MA2N4 |  | Lattice parameters (Å) | Eg (GGA-PBE) (eV) | Eg (HSE06) (eV) |
| --- | --- | --- | --- | --- |
| TiSi2N4 | This work | 2.926 2.932 [35] 2.93 [36] | 1.649 1.61 [35] 1.62 [37] | 2.907 2.74 [35] |
| ZrSi2N4 | This work | 3.028 3.022[35] 3.04 [36] | 1.622 1.56 [35] 1.15 [39] | 2.532 2.94 [35] 2.73 [39] |
| HfSi2N4 | This work | 3.052 3.022 [35] 3.02 [36] | 1.364 1.77 [35] 1.61 [38] 1.03 [39] | 3.101 3.25 [35] 3.02 [39] |
| VSi2N4 | This work | 2.877 2.883 [35] | Half-metal | Half-metal |
| NbSi2N4 | This work | 2.961 2.965 [35] | metal metal [35] | metal |
| TaSi2N4 | This work | 2.993 2.967 [35] | metal metal [35] | metal |
| CrSi2N4 | This work | 2.839 2.844 [35] 2.84 [36] | 0.511 0.49 [35] | 0.522 0.99 [35] |
| MoSi2N4 | This work | 2.902 2.909 [35] 2.91 [36] 2.94 [10] | 1.754 1.72 [35] 1.78 [40] 1.94 [10] | 2.610 2.21 [35] 2.22 [42] 2.298 [43] |
| WSi2N4 | This work | 2.907 2.912 [35] 2.91 [35] | 2.094 2.19 [35] 2.00 [40] | 2.160 2.51 [35] 2.68 [41] 2.56 [42] 2.608 [43] |

Table S2. The calculated bond populations of the screened materials mentioned above.

| Materials | Bond | Population | Length |
| --- | --- | --- | --- |
| CrC2N4 | C-N1 | 0.61 | 1.444 |
|  | C-N2 | 2.22 | 1.527 |
|  | Cr-N1 | 1.09 | 1.862 |
| CrSi2N4 | Si-N1 | 0.43 | 1.718 |
|  | Si-N2 | 2.00 | 1.723 |
|  | Cr-N1 | 1.19 | 1.957 |
| CrGe2N4 | Ge-N1 | 0.43 | 1.838 |
|  | Ge-N2 | 1.91 | 1.794 |
|  | Cr-N1 | 1.22 | 2.023 |
| MoC2N4 | C-N1 | 0.66 | 1.416 |
|  | C-N2 | 2.18 | 1.569 |
|  | Mo-N1 | 1.04 | 2.021 |
| MoSi2N4 | Si-N1 | 0.47 | 1.729 |
|  | Si-N2 | 2.05 | 1.745 |
|  | Mo-N1 | 1.20 | 2.102 |
| MoGe2N4 | Ge-N1 | 0.46 | 1.833 |
|  | Ge-N2 | 1.94 | 1.822 |
|  | Mo-N1 | 1.21 | 2.108 |
| WC2N4 | C-N1 | 0.65 | 1.399 |
|  | C-N2 | 2.18 | 1.568 |
|  | W-N1 | 1.10 | 2.012 |
| WSi2N4 | Si-N1 | 0.47 | 1.719 |
|  | Si-N2 | 2.02 | 1.714 |
|  | W-N1 | 1.27 | 2.050 |
| WGe2N4 | Ge-N1 | 0.53 | 1.824 |
|  | Ge-N2 | 1.89 | 1.816 |
|  | W-N1 | 1.24 | 2.090 |
| TiC2N4 | C-N1 | 0.57 | 1.511 |
|  | C-N2 | 2.22 | 1.547 |
|  | Ti-N1 | 1.03 | 1.900 |
| TiSi2N4 | Si-N1 | 0.45 | 1.722 |
|  | Si-N2 | 2.01 | 1.708 |
|  | Ti-N1 | 1.22 | 2.009 |
| ZrSi2N4 | Si-N1 | 0.42 | 1.671 |
|  | Si-N2 | 2.12 | 1.759 |
|  | Zr-N1 | 1.11 | 2.140 |
| ZrGe2N4 | Ge-N1 | 0.49 | 1.794 |
|  | Ge-N2 | 1.99 | 1.838 |
|  | Zr-N1 | 1.10 | 2.175 |
| ZrSn2N4 | Sn-N1 | 0.36 | 1.933 |
|  | Sn-N2 | 1.85 | 1.935 |
|  | Zr-N1 | 1.17 | 2.183 |
| ZrPb2N4 | Pb-N1 | 0.23 | 1.977 |
|  | Pb-N2 | 1.36 | 2.006 |
|  | Zr-N1 | 1.12 | 2.217 |
| HfSi2N4 | Si-N1 | 0.45 | 1.721 |
|  | Si-N2 | 2.09 | 1.760 |
|  | Hf-N1 | 1.46 | 2.082 |
| HfGe2N4 | Ge-N1 | 0.44 | 1.840 |
|  | Ge-N2 | 1.94 | 1.858 |
|  | Hf-N1 | 1.42 | 2.112 |

Table S3 The calculated bond populations Mulliken charges of the screened materials mentioned above.

| Materials |  | Charge (e) |
| --- | --- | --- |
| CrC2N4 | Cr | 1.05 |
|  | C | 0.43 |
|  | N1 | -0.60 |
|  | N2 | -0.36 |
| CrSi2N4 | Cr | 0.96 |
|  | Si | 1.85 |
|  | N1 | -0.92 |
|  | N2 | -1.40 |
| CrGe2N4 | Cr | 0.94 |
|  | Ge | 1.57 |
|  | N1 | -0.83 |
|  | N2 | -1.21 |
| MoC2N4 | Mo | 1.15 |
|  | C | 0.45 |
|  | N1 | -0.65 |
|  | N2 | -0.37 |
| MoSi2N4 | Mo | 1.04 |
|  | Si | 1.84 |
|  | N1 | -0.96 |
|  | N2 | -1.39 |
| MoGe2N4 | Mo | 1.06 |
|  | Ge | 1.57 |
|  | N1 | -0.90 |
|  | N2 | -1.21 |
| WC2N4 | W | 1.29 |
|  | C | 0.46 |
|  | N1 | -0.73 |
|  | N2 | -0.37 |
| WSi2N4 | W | 1.20 |
|  | Si | 1.93 |
|  | N1 | -1.06 |
|  | N2 | -1.47 |
| WGe2N4 | W | 1.24 |
|  | Ge | 1.58 |
|  | N1 | -0.95 |
|  | N2 | -1.25 |
| TiC2N4 | Ti | 1.17 |
|  | C | 0.43 |
|  | N1 | -0.67 |
|  | N2 | -0.35 |
| TiSi2N4 | Ti | 1.14 |
|  | Si | 1.94 |
|  | N1 | -1.03 |
|  | N2 | -1.48 |
| ZrSi2N4 | Zr | 1.30 |
|  | Si | 1.88 |
|  | N1 | -1.12 |
|  | N2 | -1.41 |
| ZrGe2N4 | Zr | 1.33 |
|  | Ge | 1.58 |
|  | N1 | -1.02 |
|  | N2 | -1.23 |
| ZrSn2N4 | Zr | 1.30 |
|  | Sn | 1.81 |
|  | N1 | -1.06 |
|  | N2 | -1.40 |
| ZrPb2N4 | Zr | 1.41 |
|  | Pb | 1.32 |
|  | N1 | -0.97 |
|  | N2 | -1.05 |
| HfSi2N4 | Hf | 1.44 |
|  | Si | 1.83 |
|  | N1 | -1.15 |
|  | N2 | -1.40 |
| HfGe2N4 | Hf | 1.49 |
|  | Ge | 1.48 |
|  | N1 | -1.07 |
|  | N2 | -1.16 |

Table S4 The calculated mh/me for CrA2N4, MoA2N4, WA2N4, TiA2N4, ZrA2N4 and HfA2N4.

| Materials | mh/me | mh/me-1 |
| --- | --- | --- |
| CrC2N4 | 1.924 | 0.924 |
| CrSi2N4 | 0.391 | 0.609 |
| CrGe2N4 | 0.426 | 0.574 |
| MoC2N4 | 3.329 | 2.329 |
| MoSi2N4 | 0.878 | 0.122 |
| MoGe2N4 | 0.438 | 0.562 |
| WC2N4 | 1.640 | 0.640 |
| WSi2N4 | 0.286 | 0.714 |
| WGe2N4 | 0.496 | 0.504 |
| TiC2N4 | 2.066 | 1.066 |
| TiSi2N4 | 0.460 | 0.119 |
| ZrSi2N4 | 1.238 | 0.238 |
| ZrGe2N4 | 1.520 | 0.520 |
| ZrSn2N4 | 0.471 | 0.529 |
| ZrPb2N4 | 0.361 | 0.639 |
| HfSi2N4 | 0.924 | 0.076 |
| HfGe2N4 | 1.236 | 0.236 |

Corresponding author. E-mail: 18382927860@163.com

Corresponding author. E-mail: renxg2468@163.com