Supplementary Information

Investigating the removal efficiency of methylene blue dye and the reusability of NaBO3 modified biomass ash geopolymer

Table S1 Proportion materials for BAG, H2O2@BAG, and NaBO3@BAG preparation.

| Sample name | BA a (%wt) | H2O2 b (%wt) | NaBO3 c (%wt) | L/B d | Conc. NaOH e (M) | NS/NH f | T (C°) g |
| --- | --- | --- | --- | --- | --- | --- | --- |
| BAG | 100 | 0 | 0 | 0.6 | 12.5 | 1 | 60 |
| 0.5 wt% H2O2@BAG | 99.50 | 0.50 | 0 | 0.6 | 12.5 | 1 | 60 |
| 0.75 wt% H2O2@BAG | 99.25 | 0.75 | 0 | 0.6 | 12.5 | 1 | 60 |
| 1 wt% H2O2@BAG | 99.00 | 1.00 | 0 | 0.6 | 12.5 | 1 | 60 |
| 0.5 wt% NaBO3@BAG | 99.50 | 0 | 0.50 | 0.6 | 12.5 | 1 | 60 |
| 0.75 wt% NaBO3@BAG | 99.25 | 0 | 0.75 | 0.6 | 12.5 | 1 | 60 |
| 1 wt% NaBO3@BAG | 99.00 | 0 | 1.00 | 0.6 | 12.5 | 1 | 60 |

a Biomass ash

b Hydrogen peroxide

c Sodium perborate

d Ratio of alkaline solution to biomass ash

e Concentration of NaOH

f Ratio of Na2SiO3 to NaOH

g Curing temperature

Fig. S1 Determination of the point of zero charges (pHpzc) of the BAG, 0.75 wt% H2O2@BAG, and 0.75 wt% NaBO3@BAG materials