# SUPPORTING INFORMATION FOR:

Cepeda-Kato, J., Zhengyang, Z. & Matsubae, K. Article title: Environmental Trade-offs from Renewable Energy Adoption in Chile’s Copper Production: A Life Cycle Assessment. Journal of Industrial Ecology.

Supporting Information S1: This document provides a detailed description of the scenario configurations used in this study. It includes the assumptions and parameters applied to model electricity, fuel, and water supply systems under both the business-as-usual and renewables-led scenarios, as well as the integration of ore grade decline into the analysis. The document outlines the methodological choices, boundary conditions, and system design considerations that underpin the life cycle assessment, thereby ensuring transparency and reproducibility of the results presented in the main text.

The objective of this study was to assess and quantify the environmental trade-offs associated with integrating energy transition strategies into copper production in Chile, using 1 ton of copper cathode as the functional unit for both pyrometallurgical ([P]Cu) and hydrometallurgical ([H]Cu) production routes. Two scenarios were evaluated: a business-as-usual (BAU) scenario, reflecting production conditions in 2023, and a renewables-led scenario, representing a projected future in 2050 in which copper production relies predominantly on renewable energy sources and is fully supplied with desalinated seawater. Within the renewables-led scenario, variations in green hydrogen production technologies and delivery pathways were also examined. A complete description of the scenarios and their variations is provided in Table S1-1.

In addition to modeling electricity, fuel, and water supply in the future scenario, the analysis incorporated the effect of declining ore grades to better represent current trends in mineral production. Information on ore grade projections and changes in energy inputs is provided in Section 1.

Details on system design and core datasets for Stages 1 through 4 are presented in Sections 2–5, respectively, while comprehensive datasets and life cycle inventories are included in Supporting Information S4.

The LCIA was performed by using SimaPro v9.5 software (PRé Sustainability, 2023) and applied the ReCiPe 2016-Hierarchist impact assessment method (Jolliet, Saadé-Sbeih, Shaked, & Crettaz, 2020). The 17 indicators included in the analysis were:

- Global warming (GWP)

- Stratospheric ozone depletion (ODP)

- Ionizing radiation (IRP)

- Tropospheric ozone formation (human health) (HOFP)

- Fine particulate matter formation (FPMF)

- Tropospheric ozone formation (ecosystems) (EOFP)

- Terrestrial acidification (TAP)

- Freshwater eutrophication (FEP)

- Terrestrial ecotoxicity (TETP)

- Freshwater ecotoxicity (FETP)

- Marine ecotoxicity (METP)

- Human carcinogenic toxicity (HTPc)

- Human non-carcinogenic toxicity (HTPnc)

- Land use (LOP)

- Mineral resource scarcity (MRS)

- Fossil resource scarcity (FFS)

- Water consumption (WCP)

Table S1-1 Scenarios settings

| Scenario |  | Metallurgical route | Year | Stage 1: Electricity supply |  | Stage 2: Open pit haul trucks fuel supply |  |  | Stage 3: Water supply | Ore grade |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | Matrix | Energy sources | Type of Fuel | Hydrogen electrolyzer technology | Hydrogen transportation |  |  |
| BAU | BAU [P]Cu | Pyrometallurgy | 2023 | Hybrid | Wind 12.20%, Solar 22.2%, Concentration Solar Plant (CSP) 0.0%, Run-of-River (ROR) Hydropower 15.3%, Storage Hydropower 7.6%, Biofuel 3.9%, Geothermal 0.7%, Coal 25.4%, Liquid Natural Gas (LNG) 6.6%, Diesel 6.1%. | Diesel | - | - | 61% Freshwater and 39% desalinated seawater | 0.58% |
|  | BAU [H]Cu | Hydrometallurgy |  |  |  | Diesel | - | - | 83% Freshwater and 17% desalinated seawater |  |
| Renewables-led | Renewables-led [P]Cu (AEL, Road) | Pyrometallurgy | 2050 | Full renewable | Wind 41.0%, Solar 31.7%, Concentration Solar Plant (CSP) 17.00%, Run-of-River (ROR) Hydropower 6.0%, Storage Hydropower 2.9%, Biofuel 1.0%, Geothermal 0%, Coal 0%, Liquid Natural Gas (LNG) 0%, Diesel 0%. | Hydrogen | Alkaline electrolyzer | Road tankers with gaseous tanks | 100% desalinated seawater | 0.50% |
|  | Renewables-led [P]Cu (AEL, Pipeline) |  |  |  |  |  |  | Pipeline |  |  |
|  | Renewables-led [P]Cu (PEMEL, Road) |  |  |  |  |  | Proton exchange membrane electrolyzer | Road tankers with gaseous tanks |  |  |
|  | Renewables-led [P]Cu (PEMEL, Pipeline) |  |  |  |  |  |  | Pipeline |  |  |
|  | Renewables-led [H]Cu (AEL, Road) | Hydrometallurgy |  |  |  |  | Alkaline electrolyzer | Road tankers with gaseous tanks |  |  |
|  | Renewables-led [H]Cu (AEL, Pipeline) |  |  |  |  |  |  | Pipeline |  |  |
|  | Renewables-led [H]Cu (PEMEL, Road) |  |  |  |  |  | Proton exchange membrane electrolyzer | Road tankers with gaseous tanks |  |  |
|  | Renewables-led [H]Cu (PEMEL, Pipeline) |  |  |  |  |  |  | Pipeline |  |  |

# Copper Ore Grade

The Chilean Copper Commission (2024b) and the Mining Council of Chile (2024) have historically documented ore grades. The recorded values represent the average ore grade throughout various stages of the copper cathode production process for the pyrometallurgical and hydrometallurgical methods. Figure S1-1 illustrates the trend of ore grades over time, clearly showing a consistent decline over the past 24 years.

Figure S1-1: Copper ore grade trend in the temporal line, from 2002 to 2023.

The decline in ore grade cannot be attributed solely to the depletion of high-grade mineral deposits. Other key factors include the development of larger economies of scale, which allow for the profitable extraction of lower-grade ores, and technological advancements in extraction processes that enhance efficiency and feasibility (Northey, Mohr, Mudd, Weng, & Giurco, 2014). Based on this information, the relationship between ore grade and cumulative production was established using the work of (Lagos, Peters, Videla, & Jara, 2018) to forecast the copper ore grade by the year 2050.

The cumulative copper production in Chile from 2004 to 2023 was sourced from the Chilean Copper Commission, (2024b) while the projection for copper production from 2024 to 2033 was obtained from the Chilean Copper Commission (2022). From 2033 to 2050, a steady increase was assumed to align with the government’s production target of 9,000 Mtons by 2050 (Ministry of Mining Chile, 2021) (Table S1-2). Based on this data, a power function was developed (Figure S1-2), enabling the forecast that the ore grade will decline to 0.50% by 2050. This projection aligns with the findings of Northey et al. (2014) for individual countries in the year 2050.

Table S1-2 Cumulated copper production 2006-2023, and projection from 2024-2050.

| Year | Cumulated production (kton) | Reference |
| --- | --- | --- |
| 2004 | 5,413 | (Cochilco, 2024c) |
| 2005 | 10,733 |  |
| 2006 | 16,094 |  |
| 2007 | 21,651 |  |
| 2008 | 26,978 |  |
| 2009 | 32,373 |  |
| 2010 | 37,792 |  |
| 2011 | 43,055 |  |
| 2012 | 48,488 |  |
| 2013 | 54,264 |  |
| 2014 | 60,026 |  |
| 2015 | 65,798 |  |
| 2016 | 71,350 |  |
| 2017 | 76,854 |  |
| 2018 | 82,685 |  |
| 2019 | 88,473 |  |
| 2020 | 94,206 |  |
| 2021 | 99,831 |  |
| 2022 | 105,161 |  |
| 2023 | 110,412 |  |
| 2024 | 116,303 | (Cochilco, 2022) |
| 2025 | 122,693 |  |
| 2026 | 129,424 |  |
| 2027 | 136,380 |  |
| 2028 | 143,469 |  |
| 2029 | 150,580 |  |
| 2030 | 157,715 |  |
| 2031 | 164,588 |  |
| 2032 | 171,229 |  |
| 2033 | 177,810 |  |
| 2034 | 184,522 | A steady increase reaching 9,000 Mtons by 2050 (Ministry of Mines Chile, 2021) |
| 2035 | 191,369 |  |
| 2036 | 198,353 |  |
| 2037 | 205,476 |  |
| 2038 | 212,742 |  |
| 2039 | 220,154 |  |
| 2040 | 227,713 |  |
| 2041 | 235,424 |  |
| 2042 | 243,289 |  |
| 2043 | 251,311 |  |
| 2044 | 259,494 |  |
| 2045 | 267,840 |  |
| 2046 | 276,353 |  |
| 2047 | 285,037 |  |
| 2048 | 293,894 |  |
| 2049 | 302,928 |  |
| 2050 | 312,143 |  |

Figure S1-2: Copper ore grade trend by cumulative production, from 2002 to 2023.

Copper ore grade is closely linked to greenhouse gas (GHG) emissions due to its significant impact on energy consumption. Declining ore grades greatly influence environmental impacts, particularly when they fall below 1%. Norgate & Jahanshahi (2006, 2010) developed a power function that correlates copper ore grade with embodied energy, specifically for the stages of concentrating, smelting, and leaching (Figure S1-3). However, the effect of ore grade on energy requirements is mainly confined to the initial stages of the mining process, such as mining and beneficiation (Harmsen, Roes, & Patel, 2013). Using the projected ore grade of 0.50% and the power function, it was estimated that energy requirements for mining and beneficiation activities in the Renewables-led scenario would rise by 22%.

Figure S1-3: Effect of ore grade and grind size on the embodied energy of copper production (Redraw fromNorgate & Jahanshahi (2010))

# Stage 1: Electricity Mix

The electricity matrices for BAU and renewables-led scenarios were derived from Chile’s Long-Term Energy Planning (Ministry of Energy, 2021). In the BAU system, approximately 39% of the energy is generated from fossil fuels, while 61% comes from renewable sources. In contrast, the renewables-led scenario features a fully renewable electricity mix, primarily dominated by wind power (41%) and solar PV (31.7%). The primary data for this analysis were obtained from Ecoinvent 3.8 (Table S1-3). The sole exception was solar PV generation, as representative data specific to the Chilean context were unavailable.

In Chile, the performance of solar technologies is primarily driven by large-scale solar plants rather than urban rooftop installations. Data for such large-scale solar infrastructure were obtained from Smith, Sekar, Mirletz, Heath, and Margolis (2024). Solar PV systems are assumed to be imported from China by direct shipping. Finally, regarding solar energy potential, the average annual solar irradiation is estimated at 2,400 [kWh/m2] (Molina, Falvey, & Rondanelli, 2017).

Table S1-3 Electricity Mix BAU and Renewables-led scenario.

| Energy source | BAU Scenario(2023) | Renewables-led Scenario (2050) | Ecoivent data source |
| --- | --- | --- | --- |
| Wind | 12.20% | 41.00% | Electricity, high voltage {CL}¦ electricity production, wind, 1-3MW turbine, onshore ¦ Cut-off, U |
| Solar | 22.20% | 31.70% | (Smith et al., 2024) |
| Concentration Solar Plant (CSP) | 0% | 17.00% | S.1 Electricity, high voltage {RoW}¦ electricity production, solar tower power plant, 20 MW ¦ Cut-off, U |
| Run-of-River (ROR) Hydropower | 15.30% | 6.00% | Electricity, high voltage {CL}¦ electricity production, hydro, run-of-river ¦ Cut-off, U |
| Storage Hydropower | 7.60% | 2.90% | Electricity, high voltage {CL}¦ electricity production, hydro, reservoir, alpine region ¦ Cut-off, U |
| Biofuel | 3.90% | 1.00% | Electricity, high voltage {CL}¦ heat and power co-generation, biogas, gas engine ¦ Cut-off, U |
| Geothermal | 0.70% | 0% | Electricity, high voltage {CL}¦ electricity production, deep geothermal ¦ Cut-off, U Electricity, high voltage {CL}¦ heat and power co-generation, wood chips, 6667 kW ¦ Cut-off, U |
| Coal | 25.40% | 0% | Electricity, high voltage {CL}¦ electricity production, hard coal ¦ Cut-off, U |
| Liquid Natural Gas (LNG) | 6.60% | 0% | Electricity, high voltage {CL}¦ electricity production, natural gas, combined cycle power plant ¦ Cut-off, U |
| Diesel | 6.10% | 0% | Electricity, high voltage {CL}¦ electricity production, oil ¦ Cut-off, U |

# Stage 2: Green Hydrogen Production

Alkaline (AEL) and Proton exchange membrane (PEMEL) electrolyzer technologies were selected for this study due to their advanced technological development and maturity in market production (Lotrič, Sekavčnik, Kuštrin, & Mori, 2021). The inventory was developed for a 50 MW hydrogen plant. The electrolyzers are assumed to be imported from China. Hydrogen production is based on current projects in Chile, with an operational capacity of 7,300 hrs/yr (Evaluation Commission Antofagasta Region, 2022). Details on the design and production parameters are presented in Table S1-4.

Table S1-4 Hydrogen plant operation design.

| Parameter | Unit | AEL Plant | PEMEL Plant | Reference |
| --- | --- | --- | --- | --- |
| Capacity | MW | 50 | 50 | - |
| Efficiency | kWh/kgH2 | 50 | 60 | (Khan et al., 2024) |
| Electrolyzer lifetime | hrs | 100,000 | 80,000 | (Khan et al., 2024) |
| Annual working hours | Hrs/yr | 7,300 | 7,300 | (Evaluation Commission Antofagasta Region, 2022) |
| BOP Lifetime | yrs | 30 | 30 | (Delpierre, Quist, Mertens, Prieur-Vernat, & Cucurachi, 2021) |
| Capacity Factor (solar) | % | 40 | 40 | (Khan et al., 2024) |
| Deionised water | l/kgH2 | 10 | 10 | (Ellersdorfer, Omar, Taylor, Daiyan, & Leslie, 2023) |
| Water, Cooling system | l/kgH2 | 40 | 40 | (Ellersdorfer et al., 2023) |
| Nitrogen | g/kgH2 | 0.3 | - | (Koj, Wulf, Schreiber, & Zapp, 2017) |
| Potassium Hidroxide | Kg/kgH2 | 0.0025 | - | (Delpierre et al., 2021) |
| Stack and BOP component transportation from Factory to port in China | tkm | 1,873,497 | 969,050 | - |
| Stack and BOP component transportation from Port in China to port in Chile | tkm | 9,667 | 5,000 | - |
| Stack and BOP component transportation from port in Chile to Plant location | tkm | 9,667 | 5,000 | - |

The Life Cycle Inventory of stack components was scaled to match the plant’s projected capacity, while the Balance of Plant (BOP) materials were adjusted proportionately. Stack and BOP components were replaced based on their respective lifespan. Data for the LCI of AEL systems were sourced from (Koj et al., 2017; Krishnan, Corona, Kramer, Junginger, & Koning, 2024). For PEMEL systems, data were drawn from Bareiß, de la Rua, Möckl, and Hamacher (2019), Delpierre, Quist, Mertens, Prieur-Vernat, and Cucurachi (2021) and Krishnan et al. (2024) (Tables S1-5 and S1-6).

Table S1-5 Construction materials AEL hydrogen plant.

| Structure | Material | Unit | Value | Reference |
| --- | --- | --- | --- | --- |
| Balance of Plant (1MWp) | Low alloyes steel | t | 4.8 | (Krishnan et al., 2024) |
|  | High alloyed steel | t | 1.9 |  |
|  | Aluminum | t | 0.1 |  |
|  | Copper | t | 0.1 |  |
|  | Plastic | t | 0.3 |  |
|  | Electronic material | t | 1.1 |  |
|  | Process material | t | 0.2 |  |
|  | Concrete | t | 5.6 |  |
| Cell stack Framework (6MWp) | Copper | t | 2 | (Koj et al., 2017) |
|  | Unalloyed steel | t | 200 |  |
| Cells (6MWp) | Nickel | t | 19 |  |
|  | Aluminum | kg | 450 |  |
|  | Calendered rigid plastic | kg | 780 |  |
|  | Polytetrafluoroethylene | kg | 78 |  |
|  | Acrylonitrile butadiene styrene | kg | 160 |  |
|  | Polyphenylene sulfide | kg | 340 |  |
|  | Polysulfones | kg | 260 |  |
|  | N-Methyl-2-pyrrolidone | t | 1.3 |  |
|  | Aniline | kg | 49 |  |
|  | Acetic anhydride | kg | 54 |  |
|  | Terephthalic acid | kg | 88 |  |
|  | Nitric acid | kg | 33 |  |
|  | Hydrochloric acid | kg | 130 |  |
|  | Graphite | kg | 430 |  |
|  | Lubricating oil | kg | 0.48 |  |
|  | Zirconium oxide | t | 1.1 |  |
|  | Carbon monoxide | kg | 150 |  |
|  | Decarbonized water | t | 11 |  |
|  | Deionized water | t | 86 |  |
|  | Industrial machine production | kg | 0.16 |  |
|  | Plaster mixing | kg | 780 |  |
| Energy (6MWp) | Electricity | GJ | 36 |  |
|  | Heat | GJ | 88 |  |
|  | Steam | MJ | 700 |  |

Table S1-6 Construction materials PEMEL hydrogen plant.

| Structure | Material | Unit | Value | Reference |
| --- | --- | --- | --- | --- |
| Balance of Plant (1MWp) | Low alloyes steel | t | 4.8 | (Bareiß et al., 2019; Delpierre et al., 2021; Khan et al., 2024; Krishnan et al., 2024) |
|  | High alloyed steel | t | 1.9 |  |
|  | Aluminum | t | 0.1 |  |
|  | Copper | t | 0.1 |  |
|  | Plastic | t | 0.3 |  |
|  | Electronic material | t | 1.1 |  |
|  | Process material | t | 0.2 |  |
|  | Concrete | t | 5.6 |  |
| Stack (1MWp) | Titanium | kg | 13.85 |  |
|  | Aluminium | kg | 54 |  |
|  | Stainless steel | kg | 40 |  |
|  | Copper | kg | 0.9 |  |
|  | Nafion | kg | 2 |  |
|  | Activated carbon | kg | 4.5 |  |
|  | Iridium | kg | 0.037 |  |
| Platinum (1MWp) | Platinum | kg | 0.01 |  |
|  | Cast iron | kg | 12 |  |
|  | Silicon, metallurgical grade | kg | 1.05 |  |
|  | Graphite | kg | 1.7 |  |
| Energy (1MWp) | Electricity | kWh | 9,969.9 |  |
| Nafion (1kg) | Tetrafluoroethylene | kg | 0.85 |  |
|  | sulfuric acid | kg | 0.15 |  |

Two transportation options—road tankers and pipelines—were designed to transport hydrogen over 200 km to the mining site. The hydrogen production plant is assumed to be near the coast, which is considered the most conservative scenario. The transportation route spans an elevation gain from sea level to 2,500 meters above sea level, terminating in the foothills where copper mines are typically located in Chile. The pipeline design is based on natural gas pipeline standards, with modifications to accommodate hydrogen transport. It features a Galvalume coating to prevent hydrogen diffusion (Wulf et al., 2018). The hydrogen operates at a pressure of 100 bar with a diameter of 200 mm.

For road transportation, EUROVI trucks with a capacity of 40 tons were considered. Each truck can transport 1,100 kg of hydrogen distributed in 100 kg gaseous hydrogen tanks. The tanks are constructed from fiber-reinforced composites with a polymer liner and transport hydrogen at a pressure of 500 bar (Wulf et al., 2018). The design specifications and construction materials for both transportation methods are detailed in Tables S1-7, S1-8, and S1-9.

A fuel station was considered in the Mining Site to deliver the hydrogen to the mining haul trucks in the Open Pit at a pressure of 700 bar. The design and materials are referenced from the studies of Burkhardt, Patyk, Tanguy, and Retzke (2016) and Wulf et al. (2018) (Table S1-10).

Table S1-7 Transportation infrastructure operation design.

| Structure | Parameter | Unit | Value | Reference |
| --- | --- | --- | --- | --- |
| Pipeline | Design capacity | kg/day | 850 | (Reuß et al., 2017; Tsiklios, Hermesmann, & Müller, 2022; Wulf et al., 2018) |
|  | Diameter | mm | 200 |  |
|  | Distance | km | 200 |  |
|  | Adicional material for maintenance | km | 10 |  |
|  | Lifetime | year | 40 |  |
|  | Flow velocity | m/s | 10-20 |  |
|  | Pressure level in | bar | 100 |  |
|  | Pressure level out | bar | 70 |  |
|  | Losses | % | 0.013 |  |
|  | Electricity for compression (from 30bar to 100 bar) | kWh | 0.6 |  |
| Gaseous Hydrogen tank, truck transportation | Storage capacity per tank | kgH2 | 100 | (Wulf et al., 2018) |
|  | Storage capacity per truck | kgH2 | 1,100 |  |
|  | Pressure level | bar | 500 |  |
|  | Losses | % | 0 |  |
|  | Electricity for compression (from 30bar to 500 bar) | kWh/kgH2 | 2.1 |  |
| Hydrogen Fuel Station | Pressure level max | bar | 880 | (Akhtar, Dickson, & Liu, 2021; Burkhardt et al., 2016; Wulf et al., 2018) |
|  | Pressure level out | bar | 700 |  |
|  | Losses | % | 0.005 |  |
|  | Electricity for compression (from 100 bar to 700 bar) | kWh/kgH2 | 1.6 |  |
|  | Electricity for compression (from 500 bar to 700 bar) | kWh/kgH2 | 0.5 |  |
|  | Electricity precooling | kWh/kgH2 | 4 |  |

Table S1-8 Construction materials pipeline.

| Structure |  | Material | Unit | Value | Reference |
| --- | --- | --- | --- | --- | --- |
| Pipeline (1km) |  | Primary aluminum | kg | 64.8 | (Wulf et al., 2018) |
|  |  | Pipeline decommissioning | kg | 10,900 |  |
|  |  | Silica sand | t | 225 |  |
|  |  | Steel, low alloyed | kg | 21,800 |  |
|  |  | Silicon | g | 1,900 |  |
|  |  | Zinc | kg | 51.1 |  |
|  |  | Drawing of pipe steel | kg | 21,800 |  |
|  |  | Excavation, hydraulic digger | m3 | 1,200 |  |
|  |  | Excavation, skid-steer loader | m3 | 9,000 |  |
|  |  | Zinc coating | kg | 21,800 |  |
|  |  | Transport train | tkm | 4,390 |  |
|  |  | Transport lorry | tkm | 13,600 |  |
| Galvalume Coat (1ton) | Inputs | Waste dust from unalloyed electric steel production, landfill | kg | 14.7 |  |
|  |  | Waste sludge from steel rolling, landfill | g | 90.6 |  |
|  |  | Waste mineral oil, hazardous waste incineration | g | 160 |  |
|  |  | Deionized water | kg | 200 |  |
|  |  | Inorganic chemicals | kg | 1.5 |  |
|  |  | Aluminum sulphate powder | mg | 906 |  |
|  |  | Ammonia | g | 30.6 |  |
|  |  | Heat from mineral oil | MJ | 768 |  |
|  |  | Heat in chemical industry | MJ | 20.1 |  |
|  |  | Hydrochloric acid , 30 % | kg | 22.2 |  |
|  |  | Heat from CHP | kg | 768 |  |
|  |  | Rolling mill production | pcs | 1.63E-10 |  |
|  |  | Soda ash, light, crystalline, heptahydrate | kg | 1,000 |  |
|  |  | Sodium hydroxide, without water, in 50% solution state | g | 380 |  |
|  |  | Transport lorry | tkm | 8.04 |  |
|  |  | Electricity | MJ | 73.2 |  |
|  | Outputs | Ammonia | g | 43.6 |  |
|  |  | Arsenic | μg | 190 |  |
|  |  | Biological oxygen demand (BOD), fresh water | g | 13.2 |  |
|  |  | Cadmium | mg | 1.31 |  |
|  |  | Chemical oxygen demand (COD), fresh water | g | 132 |  |
|  |  | Chloride, fresh water | g | 1.88 |  |
|  |  | Chromium (+VI), fresh water | mg | 7.6 |  |
|  |  | Dust (>PM10) | g | 157 |  |
|  |  | Dust (PM2,5-10) | kg | 7.62 |  |
|  |  | Hydrocarbons fresh water | mg | 119 |  |
|  |  | Hydrogen chloride air | g | 18.3 |  |
|  |  | Iron, air | g | 1.4 |  |
|  |  | Iron, fresh water | g | 5.65 |  |
|  |  | Lead, air | mg | 3.4 |  |
|  |  | Lead, fresh water | mg | 1.51 |  |
|  |  | Nickel, fresh water | mg | 1 |  |
|  |  | Oil ,fresh water | mg | 104 |  |
|  |  | Phosphorus, fresh water | mg | 90 |  |
|  |  | Solids (suspended) fresh water | mg | 224 |  |
|  |  | Total dissolved organic bound carbon (TOC) DOC, fresh water | mg | 297 |  |
|  |  | Total organic bound carbon (TOC) fresh water | mg | 297 |  |
|  |  | Waste heat air | MJ | 7.56 |  |
|  |  | Zinc, air | g | 27.5 |  |
|  |  | Zinc, fresh water | g | 1.9 |  |

Table S1-9 Construction materials gaseous hydrogen tank.

| Structure | Material | Unit | Value | Reference |
| --- | --- | --- | --- | --- |
| High pressure tank (1 tank, capacity 10kgH2) | Rolling aluminum sheets | kg | 6 | (Wulf et al., 2018) |
|  | Aluminum | kg | 6 |  |
|  | Rolling of chromium steel sheets | kg | 9 |  |
|  | Chromium steel | kg | 9 |  |
|  | Carbon fiber | kg | 71.4 |  |
|  | Epoxy resin | kg | 30.6 |  |
|  | Electricity | kWh | 4.5 |  |
|  | Rolling steel sheets | kg | 9 |  |
|  | Steel, low alloyed | kg | 9 |  |
| Carbon Fiber (1kg) | Acrylonitrile | kg | 2.25 |  |
|  | Vinyl acetate | kg | 0.2 |  |
|  | Resin | kg | 1.07 |  |
|  | Heat | kWh | 175 |  |
|  | Electricity | kWh | 26.2 |  |
| Resin (1kg) | Epoxy resin | g | 420 | (Akhtar et al., 2021) |
|  | Styrene | g | 400 |  |
|  | Acrylic acid | g | 180 |  |

Table S1-10 Construction materials fuel station.

| Structure | Material | Unit | Value | Reference |
| --- | --- | --- | --- | --- |
| Fuel Station (850kg/d) | Low alloy steel | t | 26.60 | (Wulf et al., 2018) |
|  | High alloy steel | t | 5.21 |  |
|  | Cast iron | t | 2.94 |  |
|  | Copper | t | 1.18 |  |
|  | Aluminum | kg | 499 |  |
|  | Polymer | kg | 372 |  |
|  | electronics | kg | 64 |  |
|  | Concrete | t | 210 |  |
|  | Recycling Concrete | t | 210 |  |

# Stage 3: Reverse Osmosis Seawater Desalination

Seawater desalination was modeled by assuming the use of reverse osmosis technology to produce potable water quality for mining operations and deionized water for hydrogen production. This process involves seawater intake and subsequent brine discharge into the ocean. Under the BAU scenario, 39% of the total water consumption was assumed to be sourced from desalinated seawater in [P]Cu and 17% in [H]Cu line (Cochilco, 2024c), while under the renewables-led scenario, 100% of water demand was assumed to be met through desalination. The model also accounted for the transportation of water to the mine site, ensuring a comprehensive assessment of water-related impacts.

Seawater desalination employs reverse osmosis (RO) technology to produce tap-quality water for mining operations and deionized water for hydrogen production. This process involves seawater intake and the disposal back into the sea. The desalinated water is transported through a 200 km length of high-density polyethylene (HDPE) pipeline, elevating it from sea level to an altitude of 2,500 meters above sea level to supply the mining site.

Seawater is desalinated using a polyamide membrane. The RO module lasts 5 years. The system requires 2.5 liters of seawater to produce 1 liter of tap water, generating 1.5 liters of brine as a byproduct, which is discharged into the sea. The data for this process were sourced from Ecoinvent, and the electricity sources were modified to the Chilean electricity mix. The plant generates tap water quality for mine activities and deionized water for green hydrogen production.

The pipeline's design and materials were based on a representative project in Chile approved by the government in 2019 (Evaluation Commission Republic of Chile, 2021). Additionally, the pumping system's capacity and electricity consumption were calculated using assumptions provided by the Chilean Copper Commission (2024). The information is presented in Tables S1-11 and S1-12.

Table S1-11 Seawater desalination plant data source.

| Structure | BAU Scenario(2023) | Renewables-led Scenario (2050 | Comments | References |
| --- | --- | --- | --- | --- |
| Reverse Osmosis Seawater Desalination Plant | Electricity, high voltage {CL}¦ electricity production, wind, 1-3MW turbine, onshore ¦ Cut-off, U | Electricity, high voltage {CL}¦ electricity production, wind, 1-3MW turbine, onshore ¦ Cut-off, U | Each data source was configurate to the respective electricity matrix of each scenario. | (Wernet et al., 2016) |

Table S1-12 Desalinated water pipe design.

| Parameter | Unit | Pipeline | Reference |
| --- | --- | --- | --- |
| Lenght | km | 200 | (Evaluation Commission Republic of Chile, 2021) |
| Hight difference | m | 2,500 |  |
| Diameter | mm | 2,000 |  |
| Wall thickness | mm | 10 |  |
| Lifetime | yrs | 30 |  |
| Material | - | HDPE |  |
| Density | Kg/m3 | 955 |  |
| Volume of Water | l/s | 1,000 |  |
| Pump capacity | MWp | 85 | (Cochilco, 2024b) |
| Electricity consumption | kWh/l | 0.028 | (White, 1998) |

# Stage 4 Copper production

Chile’s copper production system comprises two primary processing pathways: pyrometallurgy ([P]Cu) and hydrometallurgy ([H]Cu). Sulfide ores extracted from underground and open-pit operations are processed through the [P]Cu line, while oxide ores and low-grade sulfide ores are processed through the [H]Cu line. The two production lines differ markedly in their process design, material and energy inputs, and water requirements. According to (Castro-Molinare, Korre, & Durucan, 2014), both production lines begin with shared upstream operations, including blasting, excavation, and ore transportation. In the [P]Cu line, the extracted ore proceeds to the beneficiation stage, undergoing grinding, flotation, thickening, and filtering. This yields copper concentrate and valuable byproducts such as molybdenum, gold, and silver. Tailings—a byproduct of this stage—are stored in dedicated dams near the mine site. The concentrate then undergoes smelting—comprising melting, converting, and pyro-refining—to produce copper anodes. This stage is thermally intensive and generates both gaseous emissions and solid slag. In Chile, sulfur-rich gases from the smelting process are partially captured and converted into sulfuric acid, a commercial byproduct. The anodes are subsequently refined electrochemically by using sulfuric acid and an electrical current to produce 99.99% pure copper cathodes. Anodic slime, rich in precious metals such as gold and silver, is also recovered during this step. The life cycle inventory for the [P]Cu line includes the following stages: open-pit mining, underground mining, concentration, smelting, electrolytic refining, and services.

In contrast, the [H]Cu process begins with heap leaching, where crushed ore is irrigated with a solution of water and sulfuric acid. This leaches copper from oxide minerals into the pregnant leach solution, which is collected and transferred to the solvent extraction stage. Here, copper is separated by using an organic phase comprising paraffin and resin, followed by stripping with a weak acid solution. The resulting electrolyte is sent to the electrowinning stage, where copper is recovered as 99.99% pure cathodes. The life cycle inventory for the [H]Cu line is structured around open-pit mining, heap leaching/solvent extraction/electrowinning, and services.

Electricity, fuel, and water consumption data for the business-as-usual (BAU) scenario in 2023 were sourced from (Cochilco, 2024c). Input allocation was performed using a combination of mass allocation—based on production line and deposit type (Cochilco, 2024c; Mining Council of Chile, 2024)— and economic allocation (Ardente & Cellura, 2012), particularly for by-products of the [P]Cu route. onomic allocation factors were derived from 2023 market prices (Cochilco, 2024a, 2024d; London Metal Exchange, 2024). The increase in energy input associated with ore grade decline was incorporated according to the information provided in Section 1.

The allocation factors are reported in Table S1-13. Electricity, fuel, and water consumption data for both the BAU and renewables-led scenarios, after applying allocation procedures and accounting for the effect of ore grade decline, are presented in Tables S1-14 and S1-15.

Table S1-13 Allocation procedures Copper production process.

| Stage | Type Allocation | Product | Weight |
| --- | --- | --- | --- |
| Production Line | Mass | [P]Cu Copper Cathodes | 75% |
|  |  | [H]Cu Copper Cathodes | 15% |
| Deposit ([P]Cu) | Mass | Open pit | 84% |
|  |  | Underground | 16% |
| Concentration | Economic | Copper | 88.5% |
|  |  | Molybdenum | 6.2% |
|  |  | Gold | 3.7% |
|  |  | Silver | 1.6% |
| Smelting | Economic | Copper | 96.3% |
|  |  | Sulfuric Acid | 3.7% |
| Electro-refining | Economic | Copper | 94.4% |
|  |  | Gold | 2.5% |
|  |  | Silver | 3.1% |

Note: [P]Cu = Pyrometallurgy line, [H]Cu = Hydrometallurgy line.

Table S1-14 Energy consumption copper production.

| Line | Process | Unit | Electricity |  | Fuel |  | References |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | BAU | Renewables-led | BAU | Renewables-led |  |
| [P]Cu | Open Pit | MJ/t Cu | 487 | 555 | 7,866 | 8,967 | (Cochilco, 2024c) |
|  | Underground Mine | MJ/t Cu | 422 | 481 | 249 | 284 |  |
|  | Concentrating Plant | MJ/t Cu | 11,565 | 13,184 | 465 | 530 |  |
|  | Smelter | MJ/t Cu | 4,770 | 4,770 | 4,974 | 4,974 |  |
|  | Electrolytic Refining | MJ/t Cu | 1,284 | 1,284 | 2,033 | 2,033 |  |
|  | Services | MJ/t Cu | 2,774 | 2,774 | 456 | 456 |  |
| [H]Cu | Open pit | MJ/t Cu | 189 | 216 | 3,056 | 3,484 |  |
|  | Lx/Sx/Ew | MJ/t Cu | 12,956 | 12,956 | 3,342 | 3,342 |  |
|  | Services | MJ/t Cu | 2,774 | 2,774 | 456 | 456 |  |

Note: BAU = Business-as-usual, [P]Cu = Pyrometallurgy line, [H]Cu = Hydrometallurgy line, Lx/Sx/Ew = Leaching/ Solvent Extraction/ Electro-winning.

Table S1-15 Water consumption in copper production.

| Line | Process | Unit | Fresh Water |  | Desalinated Seawater |  | References |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | BAU | Renewables-led | BAU | Renewables-led |  |
| [P]Cu | Mine | m3/t Cu | 2.72 | 0.00 | 9.34 | 12.06 | (Cochilco, 2024c) |
|  | Concentrating Plant | m3/t Cu | 46.20 | 0.00 | 28.39 | 74.59 |  |
|  | Smelter& Refinery | m3/t Cu | 2.10 | 0.00 | 0.00 | 2.10 |  |
|  | Other & Services | m3/t Cu | 5.72 | 0.00 | 0.00 | 5.72 |  |
| [H]Cu | Mine | m3/t Cu | 0.93 | 0.00 | 3.18 | 4.11 |  |
|  | Lx/Sx/Ew | m3/t Cu | 8.40 | 0.00 | 0.00 | 8.40 |  |
|  | Other & Services | m3/t Cu | 5.72 | 0.00 | 0.00 | 5.72 |  |

Note: BAU = Business-as-usual, [P]Cu = Pyrometallurgy line, [H]Cu = Hydrometallurgy line, Lx/Sx/Ew = Leaching/ Solvent Extraction/ Electro-winning.

For copper production, material datasets from Ecoinvent were adapted to reflect Chile’s context. For example, the hydrometallurgical line was modified to consider sulfuric acid heap leaching and was configured to share the same mining infrastructure as the pyrometallurgical line. These adaptations ensured a consistent representation of site-level operations across both production pathways.

- Copper concentrate, sulfide ore {CL}| copper mine operation and beneficiation, sulfide ore | Cut-off, U

- Copper, anode {CL}| smelting of copper concentrate, sulfide ore | Cut-off, U

- Copper, cathode {GLO}| electrorefining of copper, anode | Cut-off, U

- Copper, cathode {GLO}| copper production, cathode, solvent extraction and electrowinning process | Cut-off, U

Detailed information on the datasets and life cycle inventories is provided in Supporting Information S4.

References

Akhtar, M. S., Dickson, R., & Liu, J. J. (2021). Life Cycle Assessment of Inland Green Hydrogen Supply Chain Networks with Current Challenges and Future Prospects. ACS Sustainable Chemistry and Engineering, 9(50), 17152–17163. https://doi.org/10.1021/acssuschemeng.1c06769

Ardente, F., & Cellura, M. (2012). Economic Allocation in Life Cycle Assessment: The State of the Art and Discussion of Examples. Journal of Industrial Ecology, 16(3), 387–398. https://doi.org/10.1111/j.1530-9290.2011.00434.x

Bareiß, K., de la Rua, C., Möckl, M., & Hamacher, T. (2019). Life cycle assessment of hydrogen from proton exchange membrane water electrolysis in future energy systems. Applied Energy, 237, 862–872. https://doi.org/10.1016/j.apenergy.2019.01.001

Burkhardt, J., Patyk, A., Tanguy, P., & Retzke, C. (2016). Hydrogen mobility from wind energy – A life cycle assessment focusing on the fuel supply. Applied Energy, 181, 54–64. https://doi.org/10.1016/j.apenergy.2016.07.104

Castro-Molinare, J., Korre, A., & Durucan, S. (2014). Sustainability Analysis of Copper Extraction and Processing using Life Cycle Analysis Methods: A Case Study in the North of Chile. In Computer Aided Chemical Engineering (Vol. 33, pp. 1861–1866). Elsevier B.V. https://doi.org/10.1016/B978-0-444-63455-9.50145-8

Cochilco. (2022). Copper projection in Chile 2022-2033. Santiago, Chile.

Cochilco. (2024a). Chilean sulfuric acid market. Projection to 2023. Santiago, Chile.

Cochilco. (2024b). Projection of electrical energy consumption in copper mining 2023-2034. Santiago, Chile. Retrieved from https://www.cochilco.cl/web/informe-proyeccion-del-consumo-de-energia-electrica-en-la-mineria-del-cobre-2023-2034/#:~:text=Se%20estima%20el%20consumo%20el%C3%A9ctrico,en%20el%20mismo%20periodo%20analizado.

Cochilco. (2024c). Yearbook: Copper and Other Mineral Statistics 2004-2023. Santiago, Chile. Retrieved from https://www.cochilco.cl/web/anuario-de-estadisticas-del-cobre-y-otros-minerales/

Cochilco. (2024d, December). Historical Metal Prices.

Delpierre, M., Quist, J., Mertens, J., Prieur-Vernat, A., & Cucurachi, S. (2021). Assessing the environmental impacts of wind-based hydrogen production in the Netherlands using ex-ante LCA and scenarios analysis. Journal of Cleaner Production, 299. https://doi.org/10.1016/j.jclepro.2021.126866

Ellersdorfer, P., Omar, A., Taylor, R. A., Daiyan, R., & Leslie, G. (2023). Multi-effect distillation: a sustainable option to large-scale green hydrogen production using solar energy. International Journal of Hydrogen Energy, 48(81), 31491–31505. https://doi.org/10.1016/j.ijhydene.2023.04.261

Evaluation Commission Antofagasta Region, R. of C. HyEx Project - Green Hydrogen Production. , Pub. L. No. RCA 202202001118 (2022). Chile.

Evaluation Commission Republic of Chile. Infrastructure development and improvement of the productive capacity of Collahuasi. , Pub. L. No. RCA 20219900112 (2021). Chile.

Harmsen, J. H. M., Roes, A. L., & Patel, M. K. (2013). The impact of copper scarcity on the efficiency of 2050 global renewable energy scenarios. Energy, 50(1), 62–73. https://doi.org/10.1016/j.energy.2012.12.006

Jolliet, O., Saadé-Sbeih, M., Shaked, S., & Crettaz, P. (2020). Environmental Life Cycle Assessment (2nd edition). CRC Predd.

Khan, M. H. A., Sitaraman, T., Haque, N., Leslie, G., Saydam, S., Daiyan, R., … Kara, S. (2024). Strategies for life cycle impact reduction of green hydrogen production – Influence of electrolyser value chain design. International Journal of Hydrogen Energy, 62, 769–782. https://doi.org/10.1016/j.ijhydene.2024.01.081

Koj, J. C., Wulf, C., Schreiber, A., & Zapp, P. (2017). Site-dependent environmental impacts of industrial hydrogen production by alkalinewater electrolysis. Energies, 10(7). https://doi.org/10.3390/en10070860

Krishnan, S., Corona, B., Kramer, G. J., Junginger, M., & Koning, V. (2024). Prospective LCA of alkaline and PEM electrolyser systems. International Journal of Hydrogen Energy, 55, 26–41. https://doi.org/10.1016/j.ijhydene.2023.10.192

Lagos, G., Peters, D., Videla, A., & Jara, J. J. (2018). The effect of mine aging on the evolution of environmental footprint indicators in the Chilean copper mining industry 2001–2015. Journal of Cleaner Production, 174, 389–400. https://doi.org/10.1016/j.jclepro.2017.10.290

London Metal Exchange. (2024, December). LME Copper Official Prices curve.

Lotrič, A., Sekavčnik, M., Kuštrin, I., & Mori, M. (2021). Life-cycle assessment of hydrogen technologies with the focus on EU critical raw materials and end-of-life strategies. International Journal of Hydrogen Energy, 46(16), 10143–10160. https://doi.org/10.1016/j.ijhydene.2020.06.190

Mining Council of Chile. (2024). Updated Mining Figures. Santiago, Chile. Retrieved from https://consejominero.cl/wp-content/uploads/2024/05/20240527-CAM.pdf

Ministry of Energy, C. (2021). Long-Term Energy Planning.

Ministry of Mines Chile. National Mining Policy 2050. , (2021). Chile.

Ministry of Mining Chile. (2021). Chilean Mining Policy 2050.

Molina, A., Falvey, M., & Rondanelli, R. (2017). A solar radiation database for Chile. Scientific Reports, 7(1). https://doi.org/10.1038/s41598-017-13761-x

Norgate, T., & Jahanshahi, S. (2006). Energy and greenhouse gas implications of deteriorating quality ore reserves.

Norgate, T., & Jahanshahi, S. (2010). Low grade ores - Smelt, leach or concentrate? Minerals Engineering, 23(2), 65–73. https://doi.org/10.1016/j.mineng.2009.10.002

Northey, S., Mohr, S., Mudd, G. M., Weng, Z., & Giurco, D. (2014). Modelling future copper ore grade decline based on a detailed assessment of copper resources and mining. Resources, Conservation and Recycling, 83, 190–201. https://doi.org/10.1016/j.resconrec.2013.10.005

PRé Sustainability. (2023). SimaPro.

Reuß, M., Grube, T., Robinius, M., Preuster, P., Wasserscheid, P., & Stolten, D. (2017). Seasonal storage and alternative carriers: A flexible hydrogen supply chain model. Applied Energy, 200, 290–302. https://doi.org/10.1016/j.apenergy.2017.05.050

Smith, B. L., Sekar, A., Mirletz, H., Heath, G., & Margolis, R. (2024). An Updated Life Cycle Assessment of Utility-Scale Solar Photovoltaic Systems Installed in the United States. Retrieved from www.nrel.gov/publications.

Tsiklios, C., Hermesmann, M., & Müller, T. E. (2022). Hydrogen transport in large-scale transmission pipeline networks: Thermodynamic and environmental assessment of repurposed and new pipeline configurations. Applied Energy, 327. https://doi.org/10.1016/j.apenergy.2022.120097

Wernet, G., Bauer, C., Steubing, B., Reinhard, J., Moreno-Ruiz, E., & Weidema, B. (2016). The ecoinvent database version 3 (part I): overview and methodology. International Journal of Life Cycle Assessment, 21(9), 1218–1230. https://doi.org/10.1007/s11367-016-1087-8

White, F. M. (1998). Fluid Mechanics (4th ed.; J. P. Holman & J. Lloyd, Eds.). McGraw-Hill Science Engineering.

Wulf, C., Reuß, M., Grube, T., Zapp, P., Robinius, M., Hake, J. F., & Stolten, D. (2018). Life Cycle Assessment of hydrogen transport and distribution options. Journal of Cleaner Production, 199, 431–443. https://doi.org/10.1016/j.jclepro.2018.07.180