Supplementary Material

HMDSO plasma treatment of cellulose fibers influences the performance of extruded fiber cement composites under accelerated aging

Laís Salviano de Oliveira Schiavi, Mateus Aquino Gonçalves, Adriana de Oliveira Delgado-Silva, Elidiane Cipriano Rangel, Teodorico de Castro Ramalho, Rafael Farinassi Mendes, Lívia Elisabeth Vasconcellos de Siqueira Brandão Vaz

S1. FTIR band assignments used for the interpretation of HMDSO-derived coatings

Fourier-transform infrared spectroscopy was used to support the identification of chemical groups associated with HMDSO-derived plasma coatings deposited on reference substrates and cellulose fibers. The interpretation of the spectra was based on absorption bands commonly reported for organosilicon and silica-like films obtained from HMDSO-containing plasma environments. Because cellulose also exhibits absorption bands in some of these spectral regions, the assignments were interpreted together with wettability measurements and SEM/EDS results.

Table S1. Main FTIR absorption bands used for the interpretation of HMDSO-derived plasma coatings.

| Absorption Range (cm-1) | Assignment | References |
| --- | --- | --- |
| 3664 – 3774 | O-H | [1] |
| 3500 - 3700 | Si-O-H | [1, 2] |
| 2958 | C-H | [3] |
| 1170 - 1200 | Si–O–Si | [1, 2, 4–6] |
| 1200 - 1275 | Si(CH3)x | [1, 3] |
| 1255 | mono-substituted (Si(CH3)3) | [1, 3] |
| 1265 | di-substituted (Si(CH3)2) | [1, 3] |
| 1275 | tri-substituted (Si(CH3)) | [1, 3] |
| 1030 | Si–O–C | [1, 4–6] |
| 779 – 806 | Si(CH3) | [1, 2, 4–6] |
| 736 | Si–O–Si | [1, 2] |
| 690 – 700 | Si-H | [1] |
| 480 | O–Si–O | [1, 2] |

S2. QTAIM atomic properties for the cellulose–HMDSO interaction

Quantum Theory of Atoms in Molecules (QTAIM) analysis was used to evaluate the proposed hydrogen-bond interaction between cellulose and HMDSO. According to the criteria proposed by Koch and Popelier, hydrogen-bond formation is associated with a decrease in the first atomic dipole moment, M1(H), and atomic volume, V(H), together with an increase in the atomic charge, q(H), and atomic energy, E(H), of the hydrogen atom involved in the interaction.

In Table S2, H1 represents the reference hydrogen atom, whereas H2 corresponds to the hydrogen atom involved in the proposed cellulose–HMDSO hydrogen-bond interaction. Relative to H1, H2 exhibited an increase in q(H) and E(H), accompanied by decreases in M1(H) and V(H). This behavior is consistent with the Koch and Popelier criteria and supports the interpretation of a hydrogen-bond-assisted interaction in the simplified cellulose–HMDSO model.

Table S2. Atomic properties obtained from QTAIM calculations for the hydrogen atoms used to evaluate the cellulose–HMDSO interaction according to the Koch and Popelier criteria.

| Atom | q(H) | M1(H) | V(H) | E(H) |
| --- | --- | --- | --- | --- |
| H1 | +0.006031 | +0.156027 | +47.774140 | -0.620045 |
| H2 | +0.502016 | +0.146183 | +24.434133 | -0.415224 |

q(H), atomic charge of the hydrogen atom; M1(H), first atomic dipole moment; V(H), atomic volume; E(H), atomic energy. H1 is the reference hydrogen atom and H2 is the hydrogen atom involved in the proposed hydrogen-bond interaction. Values are reported in atomic units where applicable.

S3. Supplementary references

1. 	de Freitas ASM, Maciel CC, Rodrigues JS, et al (2021) Organosilicon films deposited in low-pressure plasma from hexamethyldisiloxane — A review. Vacuum 194:110556. https://doi.org/10.1016/J.VACUUM.2021.110556

2. 	Grill A, Neumayer DA (2003) Structure of low dielectric constant to extreme low dielectric constant SiCOH films: Fourier transform infrared spectroscopy characterization. J Appl Phys 94:6697–6707. https://doi.org/10.1063/1.1618358

3. 	Vendemiatti C, Hosokawa RS, Rangel RCC, et al (2015) Wettability and surface microstructure of polyamide 6 coated with SiOXCYHZ films. Surf Coat Technol 275:32–40. https://doi.org/10.1016/j.surfcoat.2015.03.051

4. 	Navascués P, Buchtelová M, Zajícková L, et al (2024) Polymerization mechanisms of hexamethyldisiloxane in low-pressure plasmas involving complex geometries. Appl Surf Sci 645:158824. https://doi.org/10.1016/J.APSUSC.2023.158824

5. 	Dufour T (2023) From Basics to Frontiers: A Comprehensive Review of Plasma-Modified and Plasma-Synthesized Polymer Films. Polymers 2023, Vol 15, Page 3607 15:3607. https://doi.org/10.3390/POLYM15173607

6. 	Jang HJ, Jung EY, Parsons T, et al (2021) A Review of Plasma Synthesis Methods for Polymer Films and Nanoparticles under Atmospheric Pressure Conditions. Polymers 13:2267. https://doi.org/10.3390/POLYM13142267