S2. Additional Figures and Tables
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Figure S1. Release profiles of DOX and MMC from RGD-DMPLN (Med) in PBS, pH =7.4 using a dialysis method at 37 (C over 72 h (n=3). DOX and MMC concentrations were determined spectrophotometrically at 480 nm and 364 nm, respectively. Free DOX and MMC solutions were used as a reference to differentiate the effect of dialysis membrane barrier and nanocarrier barrier on the measured drug release profiles[4]. Data are reported as mean ± SD (n=3).
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