Supplementary Information for

Controlled On-chip Fabrication of Large-scale Perovskite Single Crystal Arrays for High-performance Laser and Photodetector Integration

Zhangsheng Xu1, 2, Xun Han1, 3*, Wenqiang Wu1, 4, Fangtao Li1, Ru Wang1 ,4, Hui Lu1, 2, Qiuchun Lu1, 5, Binghui Ge6, Ningyan Cheng6, Xiaoyi Li7, Guangjie Yao8, Hao Hong8, Kaihui Liu8,9 and Caofeng Pan1,2 *

1CAS Center for Excellence in Nanoscience, Beijing Key Laboratory of Micro-nano Energy and Sensor, Beijing Institute of Nanoenergy and Nanosystems, Chinese Academy of Sciences, Beijing, 101400, China

2School of Nanoscience and Technology, University of Chinese Academy of Sciences, Beijing, 100049, China

3College of Mechatronics and Control Engineering, Shenzhen University, Shenzhen, 518060, China

4College of Physics and Optoelectronic Engineering, Shenzhen University, Shenzhen, 518060, China

5Center on Nanoenergy Research, School of Physical Science and Technology, Guangxi University, Nanning, 530004, China

6Information Materials and Intelligent Sensing Laboratory of Anhui Province, Key Laboratory of Structure and Functional Regulation of Hybrid Materials of Ministry of Education, Institutes of Physical Science and Information Technology, Anhui University, Hefei, 230601, China

7College of Materials Science and Engineering, Ocean University of China, Qingdao, 266100, China

8State Key Laboratory for Mesoscopic Physics, Frontiers Science Centre for Nano-optoelectronics, School of Physics, Peking University, Beijing, 100871, China

9Songshan Lake Materials Laboratory, Dongguan, 523808, China

These authors contributed equally: Zhangsheng Xu, Xun Han, Wenqiang Wu.

*Corresponding author. Email: Xun Han (hanxun@szu.edu.cn; tel:+8618810869039 ); Caofeng Pan (cfpan@binn.cas.cn; tel:+8618518768163)

Supplementary Text

Discussion about the influence of the gap on the thickness of perovskite.

The gap can be tuned by changing the pressure of the clamp. After placing the hydrophobic glass substrate on the target substrate, we use a clamp to hold the two pieces of substrate. By changing the pressure of the clamp, the gap could be tuned from 9 μm to 45 μm.

As shown in Fig. S2a, the thickness of the MPs decreases with reducing the gap between two substrates while the thickness of MPs remains smaller than the gap. However, the crystals fabricated with the gap of 9 μm demonstrate irregular shapes, which is because the perovskite tends to nucleate at the corner of the hydrophilic squares and grow along the edges (Fig. S2b). Under the large gap conditions, the edges of crystals become smooth due to the uncontrolled evaporation rate of the solvent of the precursor solution (Fig. S2c). Considering the control of the crystallization process and pixel positions, we adopted the gap of 20 μm in this work for the fabrication of perovskite crystal arrays.

Calculation of the trap density and carrier mobility.

For easy measurement, a large hydrophilic window is utilized for the crystal array growth. We firstly measured the I-V curve of the MAPbBr3 crystals in the dark condition (Fig. S9). It shows three different regimes: the ohmic regime at low bias, the trap-filled regime with a starting point of VTFL, and the child regime at high bias. The trap density (ntrap) and carrier mobility (μ) could be calculated by the following equations 1, 2:

(1)

(2)

where ε is the relative dielectric constant, ε0 is the vacuum permittivity, L is the distance between two electrodes, JD is the current density at the applied voltage of Vb. As a consequence, the trap density and carrier mobility were calculated to be 1.05 ×1012 cm-3 and 111.4 cm2 V-1 s-1, respectively.

Discussion of the perovskite MP cavity.

To confirm that the main contribution to the laser is the whispering gallery mode (WGM) cavity rather than Fabry-Pérot (F-P) cavity (Fig. S9), the quality factor (Q factor) of the F-P cavity is calculated by the equation:

(3)

where n1 is the refrae of the perovskite MP, L is the cavity length and λ is the emission wavelength and R is the reflectivity of the boundary. R can be calculated according to the equation:

(4)

where n2 is the refractive index of air, θ1 and θ2 are the angle of incidence and refraction which can be considered as 0° in the F-P cavity. In addition, the stimulated radiation wavelength and the thickness of the perovskite MP was measured in the experiment. According to the above formula, we can calculate Q factor of the F-P cavity as 92.6, which is much smaller than the test results (Q factor = 2915). Hence, the F-P cavity hardly contributes to the stimulated emissions 2-5.

The preparation process of the perovskite photodetector array.

- ITO electrodes were deposited on the glass by RF Magnetron sputtering (80 W, 30 min).

- The patterned substrate was obtained by the preparation process (Fig. S1).

- Perovskite MP array was fabricated according to the method as shown in Fig. 1a.

- PMMA as insulating and protective layers was spin-coated on the perovskite MP array (1000 rpm s-1, 1 min) and cured at 80 ℃ for 5 min.

- After finishing PMMA coverage, PMMA thin film was etched by RIE (~ 160 W, 1 min) for removal of redundant PMMA on the perovskite MP array.

- Patterned Ag as top electrodes was deposited with PET mask (prepared by laser cutting machine) by RF magnetron sputtering (60 W, 3 min).

Analysis of noise spectral density.

The noise in the dark current of the photodetector array was analyzed by a reported method 5 using a power source, a low noise current preamplifier (Stanford Research System SR 570) and an oscilloscope (Keysight, InfiniiVision MSOX4154A). The dark current was measured with a sampling rate of ~ 645 Hz, as shown in Fig. S17a. Through a Fourier transform (FFT) of the measured dark current 6, the noise spectral density was obtained, as shown in Fig. S17b. Then, the noise-equivalent-power (NEP) can be calculated by dividing the noise spectral density by the responsivity. The NEP of the MAPbBr3 photodetector is calculated to be 1.43×10-14 W Hz-1/2 at a modulation frequency of 1 Hz. Thus, the specific detectivity (D*) could be calculated by

(7)

where A is the device area. The D* of the MAPbBr3 photodetector is calculated to be 4.2×1011 Jones.

Fig. S1. a Schematic illustration of the substrate preparation process. b The image of contact angle in different areas. The optical image of the patterned substrate c before and d after smearing perovskite solutions

Fig. S2. a The dependence of thickness of MPs on the gap between target and confinement substrate. The optical images of the MPs synthesized under b small and c large gap conditions.

Fig. S3. a Schematic illustration of the growth process about a perovskite MP. b The top-view microscopical optical image of samples.

Fig. S4. SEM images of MAPbBr3 MP with different perspectives.

Fig. S5. Fluorescence image of the large-scale perovskite array excited by 365 nm illumination. The inset is an enlarged image.

Fig. S6. Distribution of a width and b thickness of 100 perovskite MPs.

Fig. S7. Optical images of the as-fabricated perovskite MPs array on a Cr, b ITO, c NiO, and d PET substrate. e-h The corresponding microscope photograph of perovskite MP arrays. i-l Fluorescence image of the perovskite MPs array fabricated on different substrates.

Fig. S8. Schematic illustration of lattice about CsPbBr3 on STO (100) substrate.

Fig. S9. a SEM image of MAPbBr3 MPs array synthesized on KTO (100) substrate. b Statistics of the in-plane rotation of 100 perovskite MPs array synthesized on KTO (100) substrate.

Fig. S10. I-V characterization of the MAPbBr3 MPs devices in the dark condition.

Fig. S11. Schematic illustration of the entire optical path and test system for laser measurement.

Fig. S12. PL decay trace of the MAPbBr3 MPs.

Fig. S13. a FDTD simulations of WGM mode. Schematic diagram of the lightwave path in b WGM cavity and c F-P cavity in the perovskite MP.

Fig. S14. a The absolute electric field distribution |E| pattern in a 2.0×2.0×0.6 μm3 square MP, presented by an optical mode nm with a cavity quality factor Q = 1003. b and c are electric and magnetic field distributions of this mode in the z-direction. d The absolute electric field distribution |E| pattern in a 3.75×3.75×0.9 μm3 square MP, presented by an optical mode with a cavity quality factor Q = 3695. e and f are electric and magnetic field distributions of this mode in the z-direction. As shown in c and f, the magnetic field distribution in the z-direction is negligible, thus this mode is assigned as a TM mode.

Fig. S15. Schematic illustration of the preparation process of the perovskite photodetector array.

Fig. S16. Response time and decay time of the MAPbBr3 crystal photodetector.

Fig. S17. The dependence of current on power density at a bias voltage of 1 V.

Fig. S18. a The dark current waveform of the MAPbBr3 photodetector arrays. b Analysis of noise spectral density of photodetector based on the dark current waveform measured in a.

Fig. S19. Schematic illustration of measurement circuit about a 5×5 pixels photodetector array.

Table S1. Comparison of trap density between the previous reports and our work.

| Materials | Method | Trap density (cm-3) | Ref. |
| --- | --- | --- | --- |
| MAPbX3 MWs | Capillary-assisted method | 1.9 × 1013 | 7 |
| CsPbBr3 MPs | Inkjet printing and vapor phase growth | 2.1 × 1012 | 8 |
| MAPbBr3 MWs | Capillary-assisted method | 3.2 × 1011 | 9 |
| MAPbBr3 MWs | PDMS template-assisted method | 1.61 × 1011 | 10 |
| (R-MBA)2PbI4/ (S-MBA)2PbI4 NWs | Template-assisted and capillary-assisted method | 9.1 × 1012 | 11 |
| CsPbBr3 NWs | Capillary-assisted method | 1.06 × 1012 | 12 |
| MAPbBr3 MPs | Space confinement and antisolvent-assisted crystallization | 1.05 × 1012 | This work |

MW: microwire, MP: microplate, NW: nanowire

Table S2. Comparison of threshold and Q factor between the previous reports and our work.

| Materials | Method | Threshold (μJ cm-2) | Q factor | Array configuration | Ref. |
| --- | --- | --- | --- | --- | --- |
| MAPbBr3 MPs | Liquid knife | 3.5 | 1090 | Y | 13 |
| MAPbBr3 MPs | One-step solution | 9.1 | 2605 | N | 14 |
| MAPbBr3 microrods | Liquid-phase self-assembly | 62 | 657 | N | 15 |
| MAPbBr3 NWs | PDMS rectangular groove-templates | 12.3 | 500 | Y | 16 |
| MAPbBr3 NWs | Solution-processed | 9.8 | 1260 | N | 17 |
| MAPbBr3 thin film | Spin-coating | 16.2 | 1570 | Y | 18 |
| MAPbBr3 thin film | Spin-coating | 2.75 | 1025 | Y | 19 |
| CsPbBrxI3-x NWs | Vapor phase epitaxial growth | 28 | 1390 | N | 20 |
| CsPbBr3 MPs | Vapor phase growth | 4.0 | 6806 | Y | 8 |
| CsPbBr3 MWs | Template-confined antisolvent crystallization | 2.2 | 1555 | Y | 2 |
| CsPbBr3 rings | Novel self-healing lithographic patterning | 3.8 | 2200 | Y | 21 |
| MAPbBr3 MPs | Space confinement and antisolvent-assisted crystallization | 4.14 | 2915 | Y | This work |

MP: microplate, NW: nanowire, MW: microwire

REFERENCES

- Chen, J. et al. Single-crystal thin films of cesium lead bromide perovskite epitaxially grown on metal oxide perovskite (SrTiO3). Journal of the American Chemical Society 139, 13525-13532 (2017).

- Yang, Z. et al. Controllable growth of aligned monocrystalline CsPbBr3 microwire arrays for piezoelectric-induced dynamic modulation of single-mode lasing. Advanced Materials 31, 1800596 (2019).

- Zhu, Y. et al. Inhomogeneous trap-state-mediated ultrafast photocarrier dynamics in CsPbBr3 microplates. ACS Applied Materials & Interfaces 13, 6820-6829 (2021).

- Zhu, Y. et al. Spatiotemporal sectioning of two-photon fluorescence ellipsoid with a CsPbBr3 nanosheet. Nano Research 14, 4288-4293 (2021).

- Shi, L. et al. Status and outlook of metal-inorganic semiconductor-metal photodetectors. Laser & Photonics Reviews 15, 2000401 (2021).

- Liu, C. H. et al. Graphene photodetectors with ultra-broadband and high responsivity at room temperature. Nature Nanotechnology 9, 273-278 (2014).

- Gao, H. et al. Bandgap engineering of single-crystalline perovskite arrays for high-performance photodetectors. Advanced Functional Materials 28, 1804349 (2018).

- Gu, Z. et al. Controllable growth of high-quality inorganic perovskite microplate arrays for functional optoelectronics. Advanced Materials 32, 1908006 (2020).

- Li, S. X. et al. Curved photodetectors based on perovskite microwire arrays via in situ conformal nanoimprinting. Advanced Functional Materials 32, 2202277 (2022).

- Li, S. X. et al. Perovskite single-crystal microwire-array photodetectors with performance stability beyond 1 year. Advanced Materials 32, 2001998 (2020).

- Liu, Z. et al. Chiral hybrid perovskite single-crystal nanowire arrays for high-performance circularly polarized light detection. Advanced Science 8, 2102065 (2021).

- Pan, S. et al. Rapid capillary-assisted solution printing of perovskite nanowire arrays enables scalable production of photodetectors. Angewandte Chemie International Edition 59, 14942-14949 (2020).

- Feng, J. et al. "Liquid Knife" to fabricate patterning single-crystalline perovskite microplates toward high-performance laser arrays. Advanced Materials 28, 3732-3741 (2016).

- Wang, K. et al. Single-crystalline perovskite microlasers for high-Contrast and sub-Diffraction imaging. Advanced Functional Materials 29, 1904868 (2019).

- Zhang, W. et al. Controlling the cavity structures of two-photon-pumped perovskite microlasers. Advanced Materials 28, 4040-4046 (2016).

- Liu, P. et al. Organic-inorganic hybrid perovskite nanowire laser arrays. ACS Nano 11, 5766-5773 (2017).

- He, X. et al. Multi-color perovskite nanowire lasers through kinetically controlled solution growth followed by gas-phase halide exchange. Journal of Materials Chemistry C 5, 12707-12713 (2017).

- Wang, K. et al. Wettability-guided screen printing of perovskite microlaser arrays for current-driven displays. Advanced Materials 32, 2001999 (2020).

- Duan, Z. et al. Chip-scale fabrication of uniform lead halide perovskites microlaser array and photodetector array. Laser & Photonics Reviews 12, 1700234 (2018).

- Huang, L. et al. Composition-graded cesium lead halide perovskite nanowires with tunable dual-color lasing performance. Advanced Materials 30, 1800596 (2018).

- Xing, D. et al. Self-healing lithographic patterning of perovskite nanocrystals for large-area single-mode laser array. Advanced Functional Materials 31, 2006283 (2021).