##### SUPPLEMENTARY INFORMATION: Sensitive capacitive pressure sensors based on graphene membrane arrays

Makars Šiškins1, Martin Lee1, Dominique Wehenkel2, Richard van Rijn2, Tijmen W. de Jong1, Johannes R. Renshof1, Berend C. Hopman1, Willemijn S. J. M. Peters1, Dejan Davidovikj1, Herre S. J. van der Zant1, Peter G. Steeneken1, 3

1) Kavli Institute of Nanoscience, Delft University of Technology, Lorentzweg 1, 2628 CJ, Delft, The Netherlands

2) Applied Nanolayers B.V., Feldmannweg 17, 2628 CT, Delft, The Netherlands

3) Department of Precision and Microsystems Engineering, Delft University of Technology, Mekelweg 2, 2628 CD, Delft, The Netherlands

Correspondence: Makars Šiškins (m.siskins-1@tudelft.nl), Peter G. Steeneken (p.g.steeneken@tudelft.nl)

(Dated: 30 September 2020)

Contents

Fig. S1:  Detailed characterization of annealed double-layer graphene in a region where PMMA residues were observed	2

Fig. S2:  Capacitance response of a DLG sample to pressure step-changes after thermal annealing.	3

Fig. S3:  Simulated capacitance-pressure curves of the graphene pressure sensor with a different number of layers and pre-tension.	3

Fig. S4:  Simulated capacitance-pressure curves of the graphene pressure sensor with a different diameter of drums and pre-tension.	4

FIG. S1. Detailed characterization of annealed double-layer graphene in a region where PMMA residues were observed. (a) Optical image of a thermally annealed graphene sample with a 285 nm thickness of SiO2, results of which are also presented in Fig. 3 of the main text. (b) Tapping mode AFM image of the area indicated with a dashed blue line in (a). Numbered white lines indicate corresponding height profiles in (c). The extracted thickness of DLG is indicated for each case.

FIG. S2. Capacitance response of a DLG sample to pressure step-changes after thermal annealing. Coloured lines - change in capacitance of a single chip as a function of measurement time in response to ΔP, annealed for a time indicated in the legend.

FIG. S3. Simulated capacitance-pressure curves of the graphene pressure sensor with a different number of layers and pre-tension of (a) 0.045 N/m and (b) 0.45 N/m.

FIG. S4. Simulated capacitance-pressure curves of the graphene pressure sensor with a different diameter of drums and pre-tension of (a) 0.045 N/m and (b) 0.45 N/m.