Supplementary Information

Effect of Donor–Acceptor Molecular Orientations on Charge Photogeneration in Organic Solar Cells

Hansol Lee,1 Dongki Lee,1 Dong Hun Sin,1 Sang Woo Kim,2 Mun Seok Jeong,2 and Kilwon Cho*1

1 Department of Chemical Engineering, Pohang University of Science and Technology, Pohang 37673, Korea.

2 Department of Energy Science, Sungkyunkwan University, Suwon 16419, Korea

* Corresponding author (E-mail: kwcho@postech.ac.kr)

Figure S1. J-V characteristics of orientation-controlled P3HT/PCBM bilayer devices with various P3HT thicknesses. (a) Devices with face-on-rich P3HT layers. (b) Devices with edge-on-rich P3HT layers.

Figure S2. Pole figures of orientation-controlled P3HT films of various thicknesses. (a) Fast-dried films. (b) Slow-dried films. Thicknesses were varied from 10 nm to 130 nm.

Figure S3. GIWAXS results of the P3HT film used as a common interfacial layer. (a) 2D image of the P3HT film. (b) Corresponding pole figure of the P3HT (100) peak.

Figure S4. J-V characteristics of SCLC measurements. Hole-only devices were fabricated with a single layer of P3HT film (either face-on-rich or edge-on-rich). Symbols: experimental data; dashed lines: line fitted using Mott-Gurney’s law. Carrier mobilities were calculated as described elsewhere.

Figure S5. TA spectra of P3HT single layer samples with controlled P3HT orientation. (a): sample with the face-on-rich P3HT film; (b): sample with the edge-on-rich P3HT film.

Table S1. Photovoltaic parameters of orientation-controlled P3HT/PCBM bilayer devices with various P3HT thicknesses.

|  | P3HT thickness [nm] | PCE [%] | Jsc [mA cm-2] | Voc [V] | FF |
| --- | --- | --- | --- | --- | --- |
| P3HT(face-on-rich)/PCBM | 25 | 0.385 | 2.35 | 0.34 | 0.482 |
|  | 62 | 0.245 | 1.58 | 0.31 | 0.501 |
|  | 100 | 0.172 | 1.12 | 0.32 | 0.477 |
|  | 135 | 0.156 | 1.11 | 0.32 | 0.439 |
| P3HT(edge-on-rich)/PCBM | 25 | 0.259 | 1.72 | 0.30 | 0.502 |
|  | 42 | 0.140 | 1.43 | 0.31 | 0.316 |
|  | 80 | 0.145 | 1.17 | 0.32 | 0.388 |
|  | 130 | 0.149 | 0.871 | 0.33 | 0.519 |

Table S2. SCLC hole mobilities [cm2 V-1 s-1] of orientation-controlled P3HT films.

|  | P3HT (face-on-rich) | P3HT (edge-on-rich) |
| --- | --- | --- |
| µh, SCLC | 4.42 x 10-6 | 5.58 x 10-6 |