Supporting Information

Design and testing of hydrophobic core/hydrophilic shell nano/micro particles for drug-eluting stent coating

Ruolin Du#1, Yazhou Wang#1, Yuhua Huang1, Yinping Zhao1, Dechuan Zhang2, Dingyuan Du2, Yuan Zhang3, Zhenggong Li3, Sean McGinty4, Giuseppe Pontrelli5, Tieying Yin*1, Guixue Wang*1

1Key Laboratory for Biorheological Science and Technology of Ministry of Education, State and Local Joint Engineering Laboratory for Vascular Implants, Bioengineering College of Chongqing University, Chongqing 400030, China; 2Department of Radiology, Chongqing Emergency Medical Center, Chongqing 400014, China; 3Center of Cardiology, Chongqing People’s Hospital, Chongqing 400013, China; 4Division of Biomedical Engineering, University of Glasgow, Glasgow, UK; 5 Istituto per le Applicazioni del Calcolo - CNR, Via deiTaurini 19, 00185 Roma, Italy

#These authors contributed equally to this work

Correspondence:

Professor Guixue Wang, Key Laboratory for Biorheological Science and Technology of Ministry of Education, State and Local Joint Engineering Laboratory for Vascular Implants, Bioengineering College of Chongqing University, Chongqing 400030, China

E-mail: wanggx@cqu.edu.cn

Professor Tieying Yin, Key Laboratory for Biorheological Science and Technology of Ministry of Education, State and Local Joint Engineering Laboratory for Vascular Implants, Bioengineering College of Chongqing University, Chongqing 400030, China

E-mail:ilyyty28@126.com

Table S1   electrospray parameters. Overview of all electrosprayed parameters: the distance (cm), the voltage (KV), polymer concentration (mg/ml), the inner/outer flow rate (ml/h) and reception distance (cm). the parameter (0.2 ml/h (inner) and 0.6 ml/h (outer), PLGA concentration at 10 mg/ml, CS concentration at 2.5 mg/ml, 5 cm as reception distance, voltage at 14 kV).

| voltage（KV） | PLGA concentration（mg/ml） | CS concentration（mg/ml） | Inner/outer flowrate（ml/h） | reception distance（cm） |
| --- | --- | --- | --- | --- |
| 13 | 10 | 1.8 | 0.2, 0.6 | 5 |
| 14 | 30 | 2 | 0.3, 0.6 | 8 |
| 15 | 50 | 2.5 | 0.4, 0.6 | 10 |

Figure S1. Cell compatibility of the DPS. The cell SEM morphology of coating stent (×100，×500) : BMS (AD), BPS (BE) and DPS (CF); The NO release (G) and T-AOC (H) of HUVECs was shown. ( *, significant difference p<0.05; ***, significant difference p <0.001)

Figure S2. In vivo stent implantation and vessel segmants with stents.

Figure S3. HE staining of organs as heart, liver, spleen, lung and kidney

Figure S4. SEM imaging of stents demonstrating the degree of endothelial coverage after 1,3 and 6 months: BMS, BPS, SES, DPS-L and DPS-H.

Figure S5. SEM imaging of stents demonstrating the degree of endothelial coverage after 12 months: BMS, BPS, and DPS.

Figure S6. histomorphometric analysis results after stent implantation at 6 months for BMS and DPS. HE staining was performed after the stent was removed, and therefore some of the endothelium could have been injured.

Table S2. The routine blood examination of pigs (n＞3)

| Project unit | 0 month | 1 month | 3 month | 12 month |
| --- | --- | --- | --- | --- |
| RBC10^12/L | 6.27 ± 0.74 116.48 ± 8.89 39.62 ± 4.19 63.56 ± 6.06 18.69 ± 1.4 295.62 ± 24.62 19.38 ± 2.32 41.65 ± 4.69 412.1 ± 102.36 13.31 ± 5.88 8.96 ± 4.08 29.9 ± 16.89 0.38 ± 0.19 11.97 ± 6.3 | 6.06 ± 0.72 110 ± 10 37.18 ± 2.89 61.9 ± 3.9 18.28 ± 0.98 295.5 ± 4.25 18.98 ± 1.46 39.28 ± 1.68 515.75 ± 72.63 9.48 ± 4.74 7.9 ± 3.95 22.35 ± 11.17 0.43 ± 0.21 8.26 ± 1.33 | 5.86 ± 0.54 117.17 ± 12.29 36.67 ± 2.57 62.73 ± 2.78 19.98 ± 1.52 318.67 ± 14.67 18.13 ± 2.54 40.13 ± 4.82 369.83 ± 93.91 12.6 ± 6.29 7.9 ± 4.16 23.19 ± 20.64 0.31 ± 0.21 11.03 ± 5.84 | 6.43 ± 1.42 127.02 ± 32.29 41.3 ± 10.77 64.09 ± 5.57 19.74 ± 1.36 308.07 ± 8.72 41.4 ± 5.78 19.77 ± 3.48 395.37 ± 185.29 12.09 ± 3.95 10.39 ± 1.89 28.16 ± 16.4 0.48 ± 0.18 14.55 ± 5.2 |
| HGB g/L |  |  |  |  |
| HCT % |  |  |  |  |
| MCV fL |  |  |  |  |
| MCH pg |  |  |  |  |
| MCHC g/L |  |  |  |  |
| RDW-CV % |  |  |  |  |
| RDW-SD fL |  |  |  |  |
| PLT 10^9/L |  |  |  |  |
| PDW fL |  |  |  |  |
| MPV fL |  |  |  |  |
| P-LCR % |  |  |  |  |
| PCT % |  |  |  |  |
| WBC 10^9/L |  |  |  |  |

Table S3. The examination of blood biochemical indexes of pigs (n＞3)

| Project unit | 0 month | 1 month | 3 month | 12 month |
| --- | --- | --- | --- | --- |
| ALT U/L | 55.72 ± 11.62 51.57 ± 23.15 61.44 ± 37.96 77.69 ± 4.37 37.84 ± 3.85 39.84 ± 5.63 0.68 ± 0.50 4.68 ± 1.43 95.4 ± 28.75 3.9 ± 3.70 1.69 ± 0.35 0.29 ± 0.16 7.34 ± 2.72 145.39 ± 4.29 97.86 ± 3.24 2.29 ± 0.67 | 54 ± 7.07 | 58.83 ± 7.88 50.49 ± 15.94 39.67 ± 14.72 80.75 ± 4.1 37.72 ± 4.11 43.03 ± 5.28 1 ± 1.18 5.3 ± 1.49 135 ± 21.73 2.55 ± 2.13 1.37 ± 0.17 0.27 ± 0.15 5.64 ± 0.39 139.33 ± 2.99 104.22 ± 8.9 | 41.5 ± 9.65 54 ± 20.51 60 ± 51.22 78.82 ± 5.34 37.83 ± 2.99 40.98 ± 5.9 0.2 ± 0.15 3.62 ± 0.47 101.67 ± 16.22 2.85 ± 2.12 1.53 ± 0.27 0.36 ± 0.15 8.85 ± 4.98 146.1 ± 7.91 |
| AST U/L |  | 36.51 ± 25.47 |  |  |
| ALP U/L |  | 55.33 ± 4.51 |  |  |
| TP g/L |  | 69.7 ± 5.78 |  |  |
| ALB g/L |  | 36.5 ± 4.12 |  |  |
| GLB g/L |  | 33.2 ± 4.81 |  |  |
| TBIL umol/L |  | 0.4 ± 0.17 |  |  |
| UREA mmol/L |  | 4.27 ± 0.4 |  |  |
| CREA umol/L |  | 65.33 ± 12.9 |  |  |
| GLU mmol/L |  | 3.27 ± 2.89 |  |  |
| CHOL mmol/L |  | 1.44 ± 0.51 |  |  |
| TG mmol/L |  | 0.5 ± 0.24 |  |  |
| K mmol/L |  | 5.59 ± 0.23 |  |  |
| Na mmol/L |  | 140.33 ± 1.15 |  |  |
| Cl mmol/L |  | 111.67 ± 3.06 |  | 102.7 ± 9.84 2.32 ± 0.18 |
| Ca mmol/L |  | 2.25 ± 0.2 | 2.46 ± 0.13 |  |