Supporting Information for

Solvent-Engineered MoS2–Perovskite Heterostructures Enabling Defect Passivation and Enhanced Charge Transport

Mohammed Misbah Uddin,1,2,6 Md Fahim Al Fattah,3,6 Alexander Schleusener,4 Wisnu Tantyo Hadmojo,1,2 Asif Abdullah Khan,3 Fadi Dawaymeh,1,2 Mirko Prato,5 Roman Krahne,4 Dayan Ban,3 Marwa Abd-Ellah,1,2* Ahmed L. Abdelhady1,2*

1Department of Chemistry, Khalifa University of Science and Technology, Abu Dhabi, 127788, UAE

2Center for Catalysis and Separation (CeCaS), Khalifa University of Science and Technology, Abu Dhabi, 127788, UAE

3Department of Electrical and Computer Engineering, Waterloo Institute for Nanotechnology, University of Waterloo, Waterloo, ON N2L 3G1, Canada

4Optoelectronics Group, Istituto Italiano di Tecnologia, Via Morego 30, Genova, 16163, Italy

5Materials Characterization Facility, Istituto Italiano di Tecnologia, Via Morego 30, Genova 16163, Italy

6These authors contributed equally.

*Corresponding authors: A.L.A.: ahmed.abdelhady@ku.ac.ae and M.A.: marwa.abdellah@ku.ac.ae

Figure S1: Schematic representation of the fabrication process of the MoS2-perovskite microcrystalline films.

Figure S2: Absorbance spectrum of the stock solution prepared for crystallization of MoS2-MAPbBr3 heterostructures (inset: picture of the stock solution).

Figure S3: Photoluminescence emission spectra (excited at 419 nm) of the stock solution prepared for crystallization of MoS2-MAPbBr3 heterostructures.

XPS figures

Figure S4: XPS survey scan of control MAPbBr3 powders. The sample was pressed onto a high-purity indium substrate, as evidenced by the presence of In XPS peaks in the spectrum.

Figure S5: XPS survey scan of MoS2-MAPbBr3 powders. Also in this case, indium was used as substrate.

Figure S6: High-resolution XPS spectra of control MAPbBr3 (top) and MoS2-MAPbBr3 (bottom) powders.

Table S1: Ratios of Br, N and Pb in control and MoS2-MAPbBr3 samples

| Sample | Br 3d r % | N 1s r % | Pb 4f r % | Br/Pb | N/Pb | N:Pb:Br |
| --- | --- | --- | --- | --- | --- | --- |
| Control MAPbBr3 | 59.9 | 24.0 | 16.2 | 3.7 | 1.5 | 1.5:1:3.7 |
| MoS2-MAPbBr3 | 63.7 | 19.0 | 17.3 | 3.7 | 1.1 | 1.1:1:3.7 |

Table S2: Results of the PL decay fitting with the sum of two exponential functions, as well as the intensity-averaged lifetime.

| Sample | τ1 / ns | A1 | τ2 / ns | A2 | Intensity averaged lifetime / ns |
| --- | --- | --- | --- | --- | --- |
| control_PSK_glass_1 | 49.9 | 0.06 | 822.3 | 0.94 | 819.3 |
| control_PSK_glass_2 | 16.9 | 0.04 | 1047.1 | 0.96 | 1046.4 |
| MoS2_PSK_glass_1 | 29.5 | 0.1 | 569 | 0.9 | 566.0 |
| MoS2_PSK_glass_2 | 23.3 | 0.16 | 509.1 | 0.84 | 505.0 |

The time-resolved PL decay curves were fitted using a biexponential function of the form:

It=A1e-t/τ1+A2e-t/τ2

where τ1and τ2 are the fast and slow decay components, and A1 and A2 are their respective amplitudes. The intensity-averaged lifetime was calculated according to:

τavg=A1τ12+A2τ22A1τ1+A2τ2.

The first (fast) component shows a relatively low contribution to the overall PL decay, while the second (slow) component dominates the emission dynamics. Both lifetime components become shorter in the MAPbBr3/MoS2 heterostructure, while the relative amplitudes remain nearly unchanged. According to previous reports on metal halide perovskites, the fast component τ1 is typically attributed to radiative recombination of free excitons or free carriers, whereas the slower component τ2 originates from delayed recombination involving shallow trap states.1,2 In the case of single crystals, these two components are often further distinguished as surface-related (fast) and bulk-related (slow) recombination processes.3,4 Although a detailed discussion of the individual recombination pathways is beyond the scope of this work, the simultaneous shortening of both components and consequently of the intensity-averaged lifetime in the heterostructure indicates the presence of an additional non-radiative decay channel. This is further corroborated by the decrease in PL intensity reported in Figure 2d. We therefore attribute this new channel to the interfacial electron transfer from MAPbBr3 to MoS2.

Table S3: Summarized Hall effect measurement comparison of MAPbBr3 and MoS2-MAPbBr3 microcrystalline films.

| Sample | Hall voltage | Current | Magnetic Field | Type | Mobility | Carrier concentration |
| --- | --- | --- | --- | --- | --- | --- |
|  | V (V) | I (A) | B (T) |  | µ (cm2V-1s-1) | n (cm-3) |
| MAPbBr3 | 0.036 | 4×10-8 | 1 | P | 150 | 0.8×109 |
| MoS2-MAPbBr3 | -0.001 | 4×10-8 | 1 | N | 346 | 1.9×1012 |

Figure S7: Contact potential difference (CPD) of a) Au, b) ITO, c) MAPbBr3 (control), and d) MoS2-MAPbBr3.

Figure S8: Band alignment of device based on ITO/MAPbBr3 (control)/EGaIn (a) before and (b) after contact. The presence of hole barrier on both interfaces of MAPbBr3 suggest it exhibit unipolar electron only transport.

Figure S9: Band alignment of device based on ITO/MoS2-MAPbBr3/EGaIn (a) before and (b) after contact. Upshifted WF of MoS2-MAPbBr3 facilitates electron transport to EGaIn and hole transport to ITO.

Table S4: A comparison table of device performance, including the control, the hybrid, and previously reported state-of-the-art photodetectors.

| Perovskite material | Device structure | Trap density (cm-3) | Detectivity (Jones) | R (A/W) | Rise/fall time (ms/ms) | Ref. |
| --- | --- | --- | --- | --- | --- | --- |
| MAPbBr3 | lateral | 2×1011 | 1013 | 4,000 | 0.025/0.025 | 5 |
| MAPbBr3 | lateral | -- | -- | 2.2 | -- | 6 |
| FAPbI3 | lateral | 7.5×1011 | -- | 300 | -- | 7 |
| FAPbBr3 | lateral | 6.9×1011 | 1014 | 4000 | 0.67/0.75 | 8 |
| MAPbCl3 | lateral | -- | 1012 | 18 | 1/1 | 9 |
| CsPbBr3 | lateral | 4.5×1012 | 1013 | 6×104 | 0.5/1.6 | 10 |
| CsPbBr3 | Vertical | 2.8×1012 | 4.8×1012 | 0.172 | 0.14/0.12 | 11 |
| CsPbBr3 | Vertical | -- | 1014 | 150–300 | 100/20 | 12 |
| Cs2AgBiBr6 | Vertical | -- | 1.72×1011 | 1.58 | -- | 13 |
| CsPbBr3 NCs/monolayer MoS2 | lateral | -- | 3.38×1011 | 640 | 92 | 14 |
| MAPbI3BP/MoS2 | lateral | -- | 1.3×1012 | 11 | 0.15/0.24 | 15 |
| (PEA)2SnI4/few-layer MoS2 | lateral | -- | 8.09×109 | 1100 | 34/38 | 16 |
| MoS2/MAPbI3 | vertical | -- | -- | 68.11 | 205/206 | 17 |
| MoS2/MAPbI3 | lateral | -- | -- | 28 | 356/204 | 17 |
| MoS2 few-layer/Cs2CuBr4 | lateral | -- | 1.6×1011 | 0.137 | ∼32/∼79 | 18 |
| MoS2/MAPbI3 | lateral | -- | 4.28×1013 | 1.08× 104 | <45 | 19 |
| MAPbI3/MoS2 heterostructure | lateral | -- | 1018 | 1.2 | 0.178/0.212 | 20 |
| MoS2-MAPbBr3 | Vertical | 5.72×1010 | 2×1011 | 2.2 | 48/20 | This work |

Table S5: Mean and Standard deviation for performance-determining parameters of multiple MoS2-MAPbBr3 devices at constant optical power and fixed bias.

| Device No. | Average thickness (µm) | Rise (ms) | Decay (ms) | R (A/W) | EQE(%) | D*(Jones) |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 170 ± 30 | 42.6 ± 2.1 | 21.7 ± 3.9 | 2.1 ± 0.10 | 541.5 ± 10.6 | 3.1×1011 ± 6.10×109 |
| 2 |  | 44.7 ± 1.2 | 19.7 ± 2.1 | 2.0 ± 0.20 | 508.6 ± 36.9 | 2.9×1011 ± 2.10×1010 |
| 3 |  | 41.0 ± 2.7 | 22.3 ± 4.1 | 2.1 ± 0.10 | 525.5 ± 11.9 | 3.0×1011 ± 6.89×109 |
| 4 |  | 41.0 ± 1.0 | 22.7 ± 3.2 | 2.2 ± 0.01 | 562.2 ± 1.10 | 3.3×1011 ± 6.93×109 |

Figure S10: Operational stability of the MAPbBr3 (control) photodetector.

References

(1)	de Quilettes, D. W.; Vorpahl, S. M.; Stranks, S. D.; Nagaoka, H.; Eperon, G. E.; Ziffer, M. E.; Snaith, H. J.; Ginger, D. S. Impact of Microstructure on Local Carrier Lifetime in Perovskite Solar Cells. Science 2015, 348 (6235), 683–686. https://doi.org/10.1126/science.aaa5333.

(2)	Droseros, N.; Longo, G.; Brauer, J. C.; Sessolo, M.; Bolink, H. J.; Banerji, N. Origin of the Enhanced Photoluminescence Quantum Yield in MAPbBr3 Perovskite with Reduced Crystal Size. ACS Energy Lett. 2018, 3 (6), 1458–1466. https://doi.org/10.1021/acsenergylett.8b00475.

(3)	Shi, D.; Adinolfi, V.; Comin, R.; Yuan, M.; Alarousu, E.; Buin, A.; Chen, Y.; Hoogland, S.; Rothenberger, A.; Katsiev, K.; Losovyj, Y.; Zhang, X.; Dowben, P. A.; Mohammed, O. F.; Sargent, E. H.; Bakr, O. M. Low Trap-State Density and Long Carrier Diffusion in Organolead Trihalide Perovskite Single Crystals. Science 2015, 347 (6221), 519–522. https://doi.org/10.1126/science.aaa2725.

(4)	Zhumekenov, A. A.; Saidaminov, M. I.; Haque, M. A.; Alarousu, E.; Sarmah, S. P.; Murali, B.; Dursun, I.; Miao, X.-H.; Abdelhady, A. L.; Wu, T.; Mohammed, O. F.; Bakr, O. M. Formamidinium Lead Halide Perovskite Crystals with Unprecedented Long Carrier Dynamics and Diffusion Length. ACS Energy Lett. 2016, 1 (1), 32–37. https://doi.org/10.1021/acsenergylett.6b00002.

(5)	Saidaminov, M. I.; Adinolfi, V.; Comin, R.; Abdelhady, A. L.; Peng, W.; Dursun, I.; Yuan, M.; Hoogland, S.; Sargent, E. H.; Bakr, O. M. Planar-Integrated Single-Crystalline Perovskite Photodetectors. Nat Commun 2015, 6 (1), 8724. https://doi.org/10.1038/ncomms9724.

(6)	Yang, B.; Chen, J.; Shi, Q.; Wang, Z.; Gerhard, M.; Dobrovolsky, A.; Scheblykin, I. G.; Karki, K. J.; Han, K.; Pullerits, T. High Resolution Mapping of Two-Photon Excited Photocurrent in Perovskite Microplate Photodetector. J. Phys. Chem. Lett. 2018, 9 (17), 5017–5022. https://doi.org/10.1021/acs.jpclett.8b02250.

(7)	Wu, G.; Zhou, J.; Meng, R.; Xue, B.; Zhou, H.; Tang, Z.; Zhang, Y. Air-Stable Formamidinium/Methylammonium Mixed Lead Iodide Perovskite Integral Microcrystals with Low Trap Density and High Photo-Responsivity. Phys. Chem. Chem. Phys. 2019, 21 (6), 3106–3113. https://doi.org/10.1039/C8CP07271J.

(8)	Zhang, F.; Yang, B.; Zheng, K.; Yang, S.; Li, Y.; Deng, W.; He, R. Formamidinium Lead Bromide (FAPbBr3) Perovskite Microcrystals for Sensitive and Fast Photodetectors. Nano-Micro Lett. 2018, 10 (3), 43. https://doi.org/10.1007/s40820-018-0196-2.

(9)	Adinolfi, V.; Ouellette, O.; Saidaminov, M. I.; Walters, G.; Abdelhady, A. L.; Bakr, O. M.; Sargent, E. H. Fast and Sensitive Solution-Processed Visible-Blind Perovskite UV Photodetectors. Advanced Materials 2016, 28 (33), 7264–7268. https://doi.org/10.1002/adma.201601196.

(10)	Yang, B.; Zhang, F.; Chen, J.; Yang, S.; Xia, X.; Pullerits, T.; Deng, W.; Han, K. Ultrasensitive and Fast All-Inorganic Perovskite-Based Photodetector via Fast Carrier Diffusion. Advanced Materials 2017, 29 (40), 1703758. https://doi.org/10.1002/adma.201703758.

(11)	Zhou, H.; Zeng, J.; Song, Z.; Grice, C. R.; Chen, C.; Song, Z.; Zhao, D.; Wang, H.; Yan, Y. Self-Powered All-Inorganic Perovskite Microcrystal Photodetectors with High Detectivity. J. Phys. Chem. Lett. 2018, 9 (8), 2043–2048. https://doi.org/10.1021/acs.jpclett.8b00700.

(12)	Abiedh, K.; Dhanabalan, B.; Kutkan, S.; Lauciello, S.; Pasquale, L.; Toma, A.; Salerno, M.; Arciniegas, M. P.; Hassen, F.; Krahne, R. Surface-Dependent Properties and Tunable Photodetection of CsPbBr3 Microcrystals Grown on Functional Substrates. Advanced Optical Materials 2022, 10 (3), 2101807. https://doi.org/10.1002/adom.202101807.

(13)	Hossain, M.; Sheikh, M. S.; Rao, K. D. M. Hot-Spin Casting Synthesis of Freestanding Cs2AgBiBr6 Double Perovskite Facet-Oriented Microcrystals for Efficient Photodetectors. Advanced Materials Interfaces 2021, 8 (18), 2100570. https://doi.org/10.1002/admi.202100570.

(14)	Zhang, L.; Shen, S.; Li, M.; Li, L.; Zhang, J.; Fan, L.; Cheng, F.; Li, C.; Zhu, M.; Kang, Z.; Su, J.; Zhai, T.; Gao, Y. Strategies for Air-Stable and Tunable Monolayer MoS2-Based Hybrid Photodetectors with High Performance by Regulating the Fully Inorganic Trihalide Perovskite Nanocrystals. Advanced Optical Materials 2019, 7 (11), 1801744. https://doi.org/10.1002/adom.201801744.

(15)	Wang, L.; Zou, X.; Lin, J.; Jiang, J.; Liu, Y.; Liu, X.; Zhao, X.; Liu, Y. F.; Ho, J. C.; Liao, L. Perovskite/Black Phosphorus/MoS2 Photogate Reversed Photodiodes with Ultrahigh Light On/Off Ratio and Fast Response. ACS Nano 2019, 13 (4), 4804–4813. https://doi.org/10.1021/acsnano.9b01713.

(16)	Fang, C.; Wang, H.; Shen, Z.; Shen, H.; Wang, S.; Ma, J.; Wang, J.; Luo, H.; Li, D. High-Performance Photodetectors Based on Lead-Free 2D Ruddlesden–Popper Perovskite/MoS2 Heterostructures. ACS Appl. Mater. Interfaces 2019, 11 (8), 8419–8427. https://doi.org/10.1021/acsami.8b20538.

(17)	Bai, F.; Qi, J.; Li, F.; Fang, Y.; Han, W.; Wu, H.; Zhang, Y. A High-Performance Self-Powered Photodetector Based on Monolayer MoS2/Perovskite Heterostructures. Advanced Materials Interfaces 2018, 5 (6), 1701275. https://doi.org/10.1002/admi.201701275.

(18)	Pramanik, M.; Bera, A.; Karmakar, S.; Sinha, P.; Singha, A.; Das, K. High-Performance Broadband Self-Driven Photodetector Based on MoS2/Cs2CuBr4 Heterojunction. ACS Appl. Mater. Interfaces 2024, 16 (29), 38260–38268. https://doi.org/10.1021/acsami.4c06966.

(19)	Peng, Z.-Y.; Xu, J.-L.; Zhang, J.-Y.; Gao, X.; Wang, S.-D. Solution-Processed High-Performance Hybrid Photodetectors Enhanced by Perovskite/MoS2 Bulk Heterojunction. Advanced Materials Interfaces 2018, 5 (18), 1800505. https://doi.org/10.1002/admi.201800505.

(20)	Song, J.; Li, T.; Li, W.; Xiao, Z.; Chen, B.; Li, D.; Ducharme, S.; Lu, Y.; Huang, J.; Zia, R.; Hong, X. Enabling Fast Photoresponse in Hybrid Perovskite/MoS2 Photodetectors by Separating Local Photocharge Generation and Recombination. Nano Lett. 2024, 24 (45), 14307–14314. https://doi.org/10.1021/acs.nanolett.4c03950.