Nucleation effects of high molecular weight polymer additives on low molecular weight gels

Symone L. M. Alexandera,b and LaShanda T. J. Korleyb,c*

aDepartment of Macromolecular Science and Engineering, Case Western Reserve University

Cleveland, Ohio 44106-7202, United States

bDepartment of Materials Science and Engineering, University of Delaware

Newark, DE 19716, United States

cDepartment of Chemical and Biomolecular Engineering, University of Delaware

Newark, DE 19716, United States

SUPPLEMENTAL INFORMATION

Figure S1: 1H-NMR spectrum and peak identification of cholesterol-pyridine gelator

Figure S2: Scanning electron microscopy of neat CP, E-CP, and P-CP gels and the fiber structural evolution as a function of CP concentration.

Figure S3: Scanning electron microscopy of solution cast EO-EPI and PVAc.

Figure S4: Wide field SEM of E-CP gels exemplifying the persistence of network structures throughout the gels.

Figure S5: Wide field SEM of P-CP gels exemplifying the persistence of network structures throughout the gels.

Figure S6: 1-D SAXS and WAXS of polymer solutions. The solutions do not display scattering peaks, signifying that any structural order observed is due to the CP gel network.

Figure S7: Fitting of anisole-CP SAXS data with SasView lamellar model

Figure S8: Fitting of E-CP SAXS data with SasView lamellar and cylindrical models

Figure S9: Fitting of P-CP SAXS data with SasView cylindrical models