Supporting Information

Fabrication of thermally cross-linked poly(methacrylic acid)-based sponges with nano-layered structures and their degradation

Daiki Kobayashi, Haruki Uchida, Misaki Ishibane, Erika Kurita, Masayuki Kirihara, and Yohei Kotsuchibashi*

Department of Materials and Life Science, Shizuoka Institute of Science and Technology, 2200-2 Toyosawa, Fukuroi, Shizuoka 437-8555, Japan

* Corresponding author

# Department of Materials and Life Science, Shizuoka Institute of Science and Technology, 2200-2 Toyosawa, Fukuroi, Shizuoka 437-8555, Japan

# Telephone: +81-538-45-0170, Fax: +81-538-45-0110

E-mail: kotsuchibashi.yohei@sist.ac.jp

Fig. S1 Photo images of poly(MAAc)/PVA-M sponges (A) before and (B) after thermal cross-linking at 135 ℃ for 24 h.

Fig. S2 Calculated ratios of COOH/OH in the poly(MAAc)/PVA sponges.

Fig. S3 (A) Transmittance change of 30 mg/mL of mixed poly(MAAc) and PVA-S in water as a function of temperature. The poly(MAAc) and PVA-S aqueous solutions with 10, 25, and 50 wt% of poly(MAAc) showed no cloud point until 80 ℃. (B) Transmittance change of 30 mg/mL of mixed poly(MAAc) and PVA-M in water as a function of temperature. The poly(MAAc) and PVA-M aqueous solutions with 10 and 25 wt% of poly(MAAc) showed no cloud point until 80 ℃. (C) Transmittance change of 30 mg/mL of mixed poly(MAAc) and PVA-L in water as a function of temperature. The poly(MAAc) and PVA-L aqueous solutions with 10, 25, and 50 wt% of poly(MAAc) showed no cloud point until 80 ℃.

Fig. S4 GPC curves of (A) poly(MAAc) and (B) PVA-L after immersion in aqueous solution at different NaClO·5H2O at 25 ℃ for 24 h. The GPC solvent was 0.2 M PBS at pH 8.