Supporting information for

Rapid and highly efficient recombination of crosslinking points in hydrogels generated via the template polymerization of dynamic covalent three-dimensional nanoparticle crosslinkers

Mahmoud H. Othman1,2, Yoshihiro Ito1,3, Jun Akimoto1

1Emergent Bioengineering Materials Research Team, RIKEN Center for Emergent Matter Science, 2-1 Hirosawa, Wako, Saitama 351-0198, Japan

2Department of Pharmaceutics and Pharmaceutical Technology, Faculty of Pharmacy, Al-Azhar University, Assiut 71524, Egypt

3Nano Medical Engineering Laboratory, RIKEN Cluster for Pioneering Research, 2-1 Hirosawa, Wako, Saitama 351-0198, Japan

Supplementary Figures

Fig. S1 Results of gel permeation chromatography (GPC) of PTHMAAm (GPC system (JASCO, Tokyo) with -M column (Tosoh, Tokyo, Japan)) at 25 °C using water as an eluent with a flow rate of 1.0 mL/min.

Fig. S2 1H NMR spectra (JNM-ECZ400R, 400 MHz, JEOL, Tokyo, Japan) of PTHMAAm (solvent: D2O).

Fig. S3 Changes in G′ and G″ compared to those of original (A) MixGel(NP) and (B) TempGel(NP) under temperature cycles of 25 and 50 °C.

Fig. S4 1H NMR spectra of P(APBA-co-DMAAm) (LN) (solvent: D2O).

Fig. S5 Schematic illustration of the preparation of PBA-NPs by mixing PBA-b-PDMAPAAm-PBA and PBA-b-PDMAPAAm-DMAPAAm.

Supplementary Table

Table S1 Hydrodynamic diameters of the heterogeneous surface of PBA-NPsa

| Surface PBA functionality (wt%) | Diameter (nm) |
| --- | --- |
| 100 | 51.9 ± 41.6 |
| 75 | 53.9 ± 25.3 |
| 50 | 57.9 ± 37.1 |
| 25 | 59.2 ± 33.1 |
| 12.5 | 54.9 ± 28.2 |

a Measured using a dynamic light scattering instrument (ELSZ-2PL, Otsuka Electronics, Osaka, Japan).