Synthesis of a Molecularly Defined Single Active Site Heterogeneous Catalyst for Selective Oxidation of N-Heterocycles

Zhang et.al

I. Characterization results of the catalysts

Supplementary Figure 1 13C NMR spectra of PMMI (a), PPMI (b) and PPMI (c).

Supplementary Figure 2 XPS spectra of PMMI and PPMI. (a) C1s of PMMI, (b) N1s of PMMI, (c) O1s of PMMI, (d) C1s of PPMI, (e) N1s of PPMI and (f) O1s of PPMI.

Supplementary Figure 3 XPS spectra of PMI before use (black) and after use (red). (a) C1s, (b) N1s and (c) O1s.

Supplementary Figure 4 XPS survey scans of PMI (a), PMI used three times (b), PMMI (c) and PPMI (d).

Supplementary Figure 5 Ion selective MS of the addition products of tetrahydroquinoline and maleimide (m/z = 230 and 232)

Supplementary Figure 6 FT-IR spectra of maleimide (a), N-methylmaleimide (b), N-phenylmaleimide (c), PPMI (d) and PPMI (e).

Supplementary Figure 7 FT-IR spectra of fresh PMI (a) and PMI after being used for 5 times (b).

Supplementary Figure 8 Uv-Vis absorption spectra of the standard solutions (a) and the control reaction (b).

Supplementary Figure 9 B3PW91 thermodynamics between tetrahydroquinoline and 1H-pyrrole-2,5-dione.

II. DFT Computational details

Supplementary Table 1 B3PW91 optimized Cartesian Coordinates.

| H,0,-1.5414882137,0.142086892,-2.3838236648 C,0,-1.5373951148,0.1252319116,-1.2975050354 C,0,-1.5155529953,0.0713367771,1.4601107588 C,0,-0.3136432162,0.0390003281,-0.6417350468 C,0,-2.7398789001,0.1926153073,-0.6074305415 C,0,-2.7184619613,0.1671578831,0.7827730901 C,0,-0.3010809256,0.0060966043,0.7643672681 H,0,-3.6783145314,0.2623832671,-1.1446489206 H,0,-3.6446536317,0.2181004701,1.3449592637 H,0,-1.5049431182,0.0396451563,2.5457920892 N,0,0.8898404982,-0.1406781846,1.4596413833 H,0,0.8504888245,0.1251185499,2.4302146763 C,0,0.9838830923,-0.0035127381,-1.4131206219 H,0,1.2433814931,1.0099048358,-1.7441366187 H,0,0.8528580171,-0.5956853235,-2.3234906463 C,0,2.1291975859,-0.5661834058,-0.5764324338 H,0,3.0860358596,-0.4107184928,-1.0811970178 H,0,2.0008633898,-1.6441304254,-0.439910684 C,0,2.1514241991,0.1004909023,0.7906536111 H,0,2.3547800572,1.1767347048,0.6677852826 H,0,2.9526595404,-0.3149950205,1.4071337544 | H,0,-1.4181628763,0.033271906,-2.2371842193 C,0,-1.381110692,0.0824584015,-1.1529380045 C,0,-1.2937985829,0.2140963149,1.6164145788 C,0,-0.1484757175,0.1233527068,-0.5152510477 C,0,-2.5633147834,0.0953157904,-0.4203770803 C,0,-2.5184289256,0.1587672879,0.9671665333 C,0,-0.1075949789,0.1917992065,0.8861757276 H,0,-3.5175888703,0.0565302618,-0.9338141534 H,0,-3.437501219,0.1706996459,1.5422384025 H,0,-1.2286590002,0.2744181758,2.6966437357 C,0,1.1604422644,0.1421781086,-1.2555491729 H,0,1.4541692161,1.1851491698,-1.4343342237 H,0,1.0576142466,-0.3276217265,-2.2361510253 C,0,2.2390206373,-0.5475815,-0.4275010088 H,0,3.2355800904,-0.3736682369,-0.8394197696 H,0,2.0844766647,-1.636028346,-0.4302432087 N,0,1.1065592293,0.2626732357,1.6018374196 C,0,2.1754652174,-0.0742073523,0.99841665 H,0,3.101308028,-0.03160305,1.5738698666 |
| --- | --- |
| H,0,1.8194266137,-2.2196592073,-0.9069768218 C,0,0.8601051426,-1.7184499892,-0.9924897264 C,0,-1.5798779827,-0.4147082336,-1.1908110396 C,0,0.3602880048,-1.0415819737,0.1165998376 C,0,0.1592924012,-1.7587588981,-2.1905940492 C,0,-1.0609014814,-1.0987551148,-2.2813569703 C,0,-0.8823274544,-0.3787568024,0.0179779402 H,0,0.5605733237,-2.2931849815,-3.0432644901 H,0,-1.6205831137,-1.1176025,-3.2102214854 H,0,-2.5326148231,0.0994591806,-1.2749192337 C,0,1.0782464033,-0.9439886171,1.3774176536 H,0,2.1043568934,-1.2972319853,1.4102035139 C,0,0.5031406545,-0.4335496454,2.4680079558 H,0,1.0373272891,-0.3740471848,3.409745518 N,0,-1.3330273585,0.3541056391,1.0977501782 H,0,-2.2699832978,0.713212754,1.0090356538 C,0,-0.928705554,0.0129998123,2.4516694104 H,0,-1.5652960092,-0.7792246815,2.8907345531 H,0,-1.0567696445,0.8976894337,3.0829404901 | H,0,2.3579309285,0.,-1.1772589665 C,0,1.2726554863,0.,-1.1647413209 C,0,-1.5274076198,0.,-1.1224980564 C,0,0.6020567449,0.,0.0798515712 C,0,0.5616034682,0.,-2.3358821966 C,0,-0.8491893203,0.,-2.3130994143 C,0,-0.8228910793,0.,0.1029635752 H,0,1.0814940694,0.,-3.2872743807 H,0,-1.3974900427,0.,-3.2485822652 H,0,-2.6101245648,0.,-1.0808353666 N,0,-1.5341945314,0.,1.2619181602 C,0,-0.8672797233,0.,2.3892250774 H,0,-1.4614228457,0.,3.300409868 C,0,1.273350493,0.,1.3226554278 H,0,2.3586218793,0.,1.3440248681 C,0,0.5421627507,0.,2.4783302426 H,0,1.0201323752,0.,3.4508202689 |
| C,0,-0.2243212043,-0.0718304834,1.0528258025 H,0,-0.4161973756,0.8174340998,1.6425410552 C,0,0.3879876905,-1.2150962334,1.692676974 H,0,0.6431119176,-1.1440875453,2.7447134223 C,0,-0.5384599131,-0.1022416584,-0.2569094571 H,0,-0.9748258624,0.7624880443,-0.7470679286 C,0,0.6328463276,-2.3545066776,1.0167753768 H,0,1.0678172858,-3.2257343188,1.4920388245 C,0,-0.2594363638,-1.2733508644,-1.0589604908 C,0,0.2573923799,-2.4917071531,-0.3806356706 C,0,-0.3479834388,-1.287758862,-2.4047414497 H,0,-0.6465051363,-0.3921567255,-2.9431195398 N,0,0.3554207193,-3.6441878453,-0.9458136627 C,0,0.0743299675,-2.5038033218,-3.1599198895 H,0,1.1373666065,-2.4010876905,-3.4305732981 H,0,-0.4705776606,-2.5955304496,-4.1033139358 C,0,-0.1480909026,-3.7437548729,-2.3053652971 H,0,0.3004067673,-4.6213996227,-2.7757782493 H,0,-1.2291633044,-3.9478684194,-2.2373026862 | O2-Triplet O,0,0.,0.,0.834371757 O,0,0.,0.,-0.366371757 H2O H,0,0.,0.0004967663,-0.0000732467 O,0,0.,-0.0007050158,0.9605449511 H,0,0.,0.9274962495,1.207994294 H2O2 O,0,-0.1456779207,0.1056603005,0.9633472096 H,0,0.381594754,0.8552482316,1.2683044737 O,0,-0.0250422265,0.2669220776,-0.4653702631 H,0,-0.9537432531,0.3758907549,-0.7073159253 |
| H,0,0.0600533118,-0.0059137149,-0.0776568862 N,0,0.0168285638,-0.0023054076,0.9289611921 C,0,0.0198285196,1.151379403,1.7056390062 C,0,-0.0530931987,-1.1504037324,1.7107586419 C,0,-0.0564272114,0.6704189513,3.1239744201 H,0,-0.0706066498,1.3576552268,3.9574816874 C,0,-0.0985528709,-0.6592827456,3.1269319482 H,0,-0.1560866789,-1.3405325564,3.963483008 O,0,-0.0718075578,-2.2861628074,1.3122260867 O,0,0.0729859789,2.2842632434,1.3020605258 | H,0,0.5811406402,-0.3838932193,-2.0052964948 N,0,0.2441175745,-0.313638795,-1.059272378 C,0,0.0189236745,-1.4369489274,-0.2931254183 C,0,0.0113341103,0.3888634224,1.1103049708 H,0,-0.0644177725,1.0696634743,1.947697829 C,0,-0.1803362854,-0.9254116694,1.0978904944 H,0,-0.4352126856,-1.5802340144,1.9186526556 O,0,-0.0053808673,-2.5826946474,-0.6808359328 C,0,0.3449365823,0.8933860407,-0.276328982 H,0,1.3575403293,1.3098305411,-0.3096196084 O,0,-0.4813657137,1.9408879116,-0.7252832165 H,0,-1.3912796924,1.6201898829,-0.7247839718 |
| C,0,0.0122772827,-1.2584898236,1.9639661315 O,0,0.0633357941,-1.3425085456,3.1413571182 N,0,-0.0105467461,-2.4007646352,1.0604644553 H,0,0.0152458867,-3.3699233286,1.3589659701 O,0,-0.0996730817,-2.7858616935,-1.1647577638 H,0,-0.1423677295,-2.3536744744,-2.0335729909 C,0,-0.0423971197,-0.0678210428,1.0550833502 H,0,-0.0402039537,0.9458284768,1.4308704149 C,0,-0.0901671544,-0.4946904598,-0.2080754503 H,0,-0.1366576119,0.0873951012,-1.1184956583 C,0,-0.0689111525,-1.9657458865,-0.1770279811 | H,0,3.4661189904,1.4919179897,-1.9962678456 C,0,2.7963916296,1.5018594539,-1.1413578023 C,0,1.0569148747,1.5304648248,0.9968773876 C,0,1.7534964781,0.5873160697,-1.1140854551 C,0,3.0060148568,2.4122666979,-0.1130313472 C,0,2.1219405837,2.4187194963,0.9545644501 C,0,0.8620147068,0.5829215781,-0.0195467602 H,0,3.8342429025,3.1094077611,-0.1533599538 H,0,2.2445357341,3.1318811604,1.7624389906 H,0,0.3660049579,1.5997570936,1.827786116 N,0,-0.1788404143,-0.3396644126,0.0246431924 C,0,1.52753752,-0.380006309,-2.2406993927 H,0,2.0052500085,-1.3430285165,-2.0206149642 H,0,1.988157064,-0.0005675479,-3.1559392132 C,0,-0.5631412197,-1.1325152015,-1.1393213593 H,0,-1.6583728361,-1.1368624619,-1.2148050226 H,0,-0.2479766913,-2.1724379696,-0.9971928624 C,0,0.0310920458,-0.5927933975,-2.4263883545 H,0,-0.176026595,-1.3018102207,-3.2315731465 H,0,-0.442041564,0.3569706005,-2.6942527146 C,0,-0.9568085666,-0.521807903,1.2120941916 H,0,-0.3505707017,-0.2202172873,2.0708767532 C,0,-2.3255842665,0.1854370204,1.2773169564 H,0,-2.3247574156,1.1148869884,1.8464347018 H,0,-2.6939806901,0.4186937651,0.2749895142 C,0,-1.2870256026,-1.9971858581,1.513907687 O,0,-0.5586631973,-2.9496105713,1.4251328378 N,0,-2.5953061543,-2.0269108444,1.9636256386 H,0,-3.0296260707,-2.8719903421,2.3084112004 C,0,-3.271596509,-0.8147435709,1.9092237432 O,0,-4.3993937512,-0.6403480866,2.2901129934 |
| H,0,-1.3929967779,0.1209776001,-3.9076754289 C,0,-1.0748702677,0.7198852437,-3.0611272248 C,0,-0.2450229255,2.2629354672,-0.9200473099 C,0,-0.3600729311,0.0973551962,-2.0333473596 C,0,-1.3723649326,2.0705154421,-3.025958075 C,0,-0.9476084187,2.8517844192,-1.9557071052 C,0,0.0243266998,0.898617023,-0.9652980664 H,0,-1.9273278313,2.5217140645,-3.8397580381 H,0,-1.1568537203,3.9140122766,-1.9304039023 H,0,0.1037114544,2.86950208,-0.0896618683 C,0,0.0230495131,-1.3534127077,-2.1448546338 H,0,0.8278521171,-1.436645463,-2.8844234483 H,0,-0.8158546442,-1.9256237678,-2.5463588131 C,0,0.4798011241,-1.9423570191,-0.8199867048 H,0,1.0054582118,-2.8860924251,-0.9797685551 H,0,-0.3725190272,-2.1643175374,-0.1764831953 N,0,0.7751501729,0.3314635147,0.1818259699 H,0,1.549724931,0.9818131782,0.383834711 C,0,1.4249646713,-0.9997154037,-0.1091992766 H,0,2.2979772001,-0.7775009655,-0.7260811985 H,0,1.7701380013,-1.3982755532,0.8444826483 C,0,0.004727312,0.3715358359,1.5052756821 H,0,-0.576938029,1.2958821069,1.4562142062 C,0,-0.7998923064,-0.7865949113,1.9656485817 H,0,-1.7290642448,-1.1200042762,1.5312458384 C,0,-0.3654025962,-1.0853022318,3.2074817781 C,0,1.096017274,0.522885845,2.58806994 O,0,2.0826428676,1.2062711763,2.4681188032 N,0,0.7375999579,-0.3180074038,3.5955419802 H,0,1.2846824077,-0.4896645845,4.427640517 O,0,-0.7936073948,-1.9250739974,4.1342506586 H,0,-1.5574279766,-2.428562011,3.8265087323 | H,0,3.4898426509,1.126548941,-1.9835838472 C,0,2.869763264,1.207687495,-1.0966551301 C,0,1.2855437847,1.4073625456,1.1460434031 C,0,1.654900737,0.5305476611,-1.0798334675 C,0,3.3017494413,1.9792125848,-0.0293697686 C,0,2.5002203185,2.0730549223,1.0972471053 C,0,0.83410369,0.6473674375,0.0595117963 H,0,4.2535554411,2.4938935224,-0.0746899175 H,0,2.8199599541,2.6556071048,1.9530706631 H,0,0.7178477753,1.4802572542,2.0647386253 N,0,-0.4410057528,0.0289317776,0.0507596447 C,0,1.2576889931,-0.3012976214,-2.2736031424 H,0,1.8353698839,-1.2332142536,-2.2646352997 H,0,1.5398347836,0.2193088899,-3.1913377595 C,0,-0.6586574091,-1.0617701383,-0.8982427966 H,0,-1.719092952,-1.3211458205,-0.9051829381 H,0,-0.0984940147,-1.9625816825,-0.6039156935 C,0,-0.226602998,-0.6262317211,-2.2871212117 H,0,-0.4445796211,-1.4209623778,-3.0035331027 H,0,-0.8112058973,0.249965351,-2.5806759805 C,0,-1.3040077185,0.1268566726,1.1903394389 H,0,-1.0521297995,1.027143422,1.7492565257 C,0,-2.8131449521,0.0802260039,0.8915340468 H,0,-3.3550920506,0.8332288098,1.4700100566 H,0,-3.0536729554,0.2480707173,-0.1569274659 N,0,-2.1709662112,-1.8731740776,2.0675815468 H,0,-2.2592448943,-2.7936569776,2.4885390481 C,0,-3.294559569,-1.2754484723,1.3401446746 O,0,-4.326295201,-1.8385371991,1.2149365687 C,0,-1.1129061763,-1.0931342579,2.0701720751 O,0,0.0248291215,-1.3408326869,2.6267604712 H,0,0.097583334,-2.2096428262,3.0544358311 |
| Singlet State | Triplet state |
| H,0,3.1068851734,1.7575670478,-2.0509008765 C,0,2.6232416145,1.4701594215,-1.1238678126 C,0,1.4352695375,0.6892002758,1.2526690543 C,0,1.5297598755,0.6039487634,-1.1855798109 C,0,3.112667802,1.9394945925,0.0812574258 C,0,2.5286133428,1.5321492708,1.2771927114 C,0,0.9216900461,0.2688864234,0.0256098685 H,0,3.967283636,2.6054971109,0.0935483847 H,0,2.9310775545,1.8610869917,2.2271385155 H,0,1.0091166698,0.3380645261,2.1844415016 N,0,-0.2531548501,-0.6314454972,0.047489974 C,0,1.0822603325,0.0507047739,-2.5086905327 H,0,1.9581165479,-0.1368631761,-3.1320663591 H,0,0.4826498376,0.8012914864,-3.0379082403 C,0,-0.8183841175,-0.9449897246,-1.3094508016 H,0,-1.3948157731,-0.0675206609,-1.6073800781 H,0,-1.4903476754,-1.7894639565,-1.1602256485 C,0,0.2723217001,-1.2175706443,-2.31406718 H,0,0.9003665913,-2.0457807773,-1.9782331491 H,0,-0.2034602908,-1.5310585146,-3.2452801535 C,0,-1.3282643092,-0.2530810129,1.0860277989 H,0,-0.9419204082,0.5998070735,1.6301095439 C,0,-2.766941277,-0.0283759535,0.6396827751 H,0,-3.0801123563,1.0068949259,0.7689544563 H,0,-2.9904211993,-0.307798124,-0.3873078043 N,0,-2.7365309121,-1.7438235684,2.2456046893 H,0,-3.0733928511,-2.4037772339,2.9321164588 C,0,-3.6106889341,-0.9391108326,1.5370433403 O,0,-4.8027514588,-0.9628290704,1.6070632086 C,0,-1.3743416901,-1.4977374853,2.0099731816 O,0,-0.8567049903,-2.5369491493,1.1418184856 O,0,-0.5757083694,-1.3063929655,3.1079221188 H,0,-0.4566983264,-2.1320885689,3.5957500055 O,0,0.2842113276,-1.9181681671,0.5971220489 | H,0,3.3838276795,1.5021739442,-1.9048022548 C,0,2.7622598886,1.3439171209,-1.030802431 C,0,1.210611965,0.930355533,1.2525329284 C,0,1.5811068983,0.6436633446,-1.1739542127 C,0,3.1736064589,1.8383753218,0.2036598827 C,0,2.3928397433,1.6123352224,1.3473534761 C,0,0.7542003323,0.4474272326,-0.0111732951 H,0,4.1064129311,2.3839959498,0.2840441775 H,0,2.7301921253,1.9678080334,2.3131995372 H,0,0.6544563346,0.7196470945,2.1541118615 N,0,-0.4451072431,-0.1798426876,-0.1321818614 C,0,1.1566003508,0.1042577507,-2.5019159365 H,0,2.037227134,-0.1115760172,-3.1090601091 H,0,0.5896304552,0.8745913038,-3.0417961888 C,0,-0.8700037035,-0.7868008532,-1.4073652034 H,0,-1.5395502319,-0.0732388674,-1.902751281 H,0,-1.4488880297,-1.6764821635,-1.1635340842 C,0,0.2957892881,-1.1298079396,-2.3051417009 H,0,0.8817745457,-1.9413813556,-1.8648198371 H,0,-0.0978879528,-1.4935918722,-3.255401035 C,0,-1.4060351863,-0.2061725517,0.9682338408 H,0,-1.1836283532,0.6346784866,1.6219312828 C,0,-2.8886822405,-0.1247836215,0.6034823264 H,0,-3.2572653465,0.8956410233,0.5097836586 H,0,-3.1540874935,-0.6682680886,-0.3037014783 N,0,-2.5924754556,-1.5543856553,2.4319313971 H,0,-2.7994975548,-2.1307067197,3.2365716349 C,0,-3.5734523085,-0.835683988,1.7679858599 O,0,-4.7328228284,-0.797374093,2.0574813696 C,0,-1.3071009466,-1.4583378049,1.9019895839 O,0,-1.0824554828,-2.6938591796,0.9752445938 O,0,-0.3012446621,-1.4474352198,2.7958630405 H,0,0.3077039264,-2.1811316902,2.5341444494 O,0,0.0528363624,-3.2780794931,1.1964332083 |
| Singlet state | Triplet state |
| H,0,3.7260576546,0.9167190118,-1.6541475037 C,0,2.9479857236,1.0961231868,-0.9206990615 C,0,0.9494650133,1.5793255064,0.9479066655 C,0,1.7415798023,0.4206481162,-1.0391105908 C,0,3.1626420406,2.0009837543,0.1106684848 C,0,2.1578350731,2.2531262938,1.0342726005 C,0,0.7565421662,0.6529943261,-0.0720076164 H,0,4.1101301094,2.5211943427,0.1835503814 H,0,2.307896917,2.9789725234,1.8237792184 H,0,0.1712116036,1.8155075559,1.6617664809 N,0,-0.4890192659,-0.0718804146,-0.1931235768 C,0,1.4525967411,-0.5368072099,-2.1581701902 H,0,1.673981591,-1.563666194,-1.8456399723 H,0,2.0838061515,-0.3216641336,-3.02017381 C,0,-0.8622401556,-0.5404673377,-1.3381035016 C,0,-0.0189685257,-0.4174408881,-2.543311096 H,0,-0.3270809494,-1.1660134137,-3.2742592874 H,0,-0.2223850173,0.5656591401,-2.9961057169 C,0,-1.2832617501,-0.3587602691,1.0235091492 H,0,-0.8243798987,0.2051570931,1.8274355376 C,0,-2.7751247017,-0.066358977,0.9856066113 H,0,-3.0315261894,0.9587461459,1.2501834518 H,0,-3.2408194767,-0.2905793917,0.0231856017 N,0,-2.3354545112,-1.9396143475,2.3312597081 H,0,-2.5468509308,-2.7937231696,2.8302327747 C,0,-3.3449719229,-1.0483348222,2.0117801721 O,0,-4.4567700681,-1.0539918647,2.4569444009 C,0,-1.1811658602,-1.8502554673,1.4957625339 O,0,-1.2600678385,-2.6301315823,0.3227700081 O,0,0.0001489002,-2.158800351,2.1328981361 H,0,-0.1036272917,-2.0647337384,3.0862981864 O,0,-1.3468540672,-4.0103009332,0.7169743825 H,0,-2.1715396369,-4.2672330485,0.2778100313 H,0,-1.8122651294,-1.0577693424,-1.370442994 | H,0,3.41209713,1.4875235017,-1.9626278922 C,0,2.8090934073,1.2934402341,-1.0828481289 C,0,1.286975615,0.8349234433,1.2200517392 C,0,1.635551959,0.5776560406,-1.2238389598 C,0,3.2315295148,1.7673060272,0.1550190144 C,0,2.4639206624,1.5226875863,1.3085375447 C,0,0.8290281916,0.3599542162,-0.0448336453 H,0,4.1597641507,2.3211145292,0.2322517471 H,0,2.8127562039,1.8700317934,2.2733156462 H,0,0.7349570882,0.5977862451,2.1182606754 N,0,-0.3647413149,-0.2711961914,-0.1697149922 C,0,1.2133957777,0.0668535658,-2.5659259542 H,0,1.728300947,-0.882783697,-2.7545049915 H,0,1.5357066334,0.7605392903,-3.34537249 C,0,-0.6929806578,-0.9072522199,-1.4110305885 C,0,-0.3057182466,-0.1800360435,-2.6316390215 H,0,-0.5660124003,-0.7568324969,-3.5183593667 H,0,-0.8263497587,0.7827006197,-2.6941119511 C,0,-1.3638472016,-0.3018185932,0.8963422388 H,0,-1.1740538818,0.5385014654,1.5614473937 C,0,-2.8135675555,-0.2420291186,0.4226609819 H,0,-3.1814139194,0.7705397505,0.2664949808 H,0,-2.9747380021,-0.81391346,-0.4946980105 N,0,-2.655830832,-1.6528304845,2.2771499101 H,0,-2.900242282,-2.0825870083,3.1574281126 C,0,-3.5763656189,-0.9201920193,1.5578795042 O,0,-4.7498557286,-0.8349832688,1.788120415 C,0,-1.3101366679,-1.5617612435,1.8144162246 O,0,-0.942868992,-2.6456110442,0.9695028441 O,0,-0.3879473843,-1.3901281433,2.8253790909 H,0,-0.1344408199,-2.2611885403,3.163277021 O,0,-0.8521415158,-3.8111945383,1.801243256 H,0,-1.6528371447,-4.2972796079,1.5511720531 H,0,-0.8194810563,-1.9813104903,-1.3511449011 |
| C,0,-0.149202422,-1.148905925,1.8984161248 O,0,-0.3581492179,-1.2349042702,3.0549261731 N,0,-0.4822287086,-2.2224338278,0.9541421195 H,0,-0.8229567097,-3.1318535133,1.2583462607 C,0,-0.2143194125,-1.8914592863,-0.2774591691 O,0,-0.2909532747,-2.7044978924,-1.2593491871 H,0,0.0446633644,-2.262975026,-2.0773464556 O,0,1.371637214,-0.3213989886,-1.1638797638 O,0,0.913666712,-0.6668025459,-2.5005070152 H,0,1.6834581814,-0.4136550995,-3.034836752 C,0,0.2157414202,-0.4380455633,-0.3780501443 C,0,0.4922833457,-0.0535484909,1.0709655433 H,0,0.1034850615,0.9231492066,1.3533769075 H,0,1.568778601,-0.0640476512,1.2711827095 H,0,-0.607842255,0.1408087738,-0.8167696513 | C,0,0.1387463807,-1.235559242,1.8458083078 O,0,0.1900365411,-1.4439585324,3.0273359716 N,0,0.2533109063,-2.0875933113,0.7814395911 H,0,0.387299518,-3.0856433947,0.8958608024 C,0,0.1650370128,-1.4955338118,-0.5179288265 O,0,-0.9428551514,-1.9360428779,-1.1865017132 H,0,-0.821143844,-1.7683544982,-2.1345181655 O,0,1.3741452849,-1.8091279071,-1.1585362287 O,0,1.2630632093,-1.181003167,-2.4585156097 H,0,1.859313958,-1.7440168727,-2.9767807754 C,0,0.0746376166,0.039349543,-0.1798649947 H,0,1.0866452263,0.486711069,-0.3576719752 H,0,-0.5938205804,0.6730842121,-0.7768999172 C,0,-0.0973746138,0.1053935575,1.2178489748 H,0,-0.3730553485,0.9766565864,1.8111034964 |
| H,0,-1.5414882137,0.142086892,-2.3838236648 C,0,-1.5373951148,0.1252319116,-1.2975050354 C,0,-1.5155529953,0.0713367771,1.4601107588 C,0,-0.3136432162,0.0390003281,-0.6417350468 C,0,-2.7398789001,0.1926153073,-0.6074305415 C,0,-2.7184619613,0.1671578831,0.7827730901 C,0,-0.3010809256,0.0060966043,0.7643672681 H,0,-3.6783145314,0.2623832671,-1.1446489206 H,0,-3.6446536317,0.2181004701,1.3449592637 H,0,-1.5049431182,0.0396451563,2.5457920892 N,0,0.8898404982,-0.1406781846,1.4596413833 H,0,0.8504888245,0.1251185499,2.4302146763 C,0,0.9838830923,-0.0035127381,-1.4131206219 H,0,1.2433814931,1.0099048358,-1.7441366187 H,0,0.8528580171,-0.5956853235,-2.3234906463 C,0,2.1291975859,-0.5661834058,-0.5764324338 H,0,3.0860358596,-0.4107184928,-1.0811970178 H,0,2.0008633898,-1.6441304254,-0.439910684 C,0,2.1514241991,0.1004909023,0.7906536111 H,0,2.3547800572,1.1767347048,0.6677852826 H,0,2.9526595404,-0.3149950205,1.4071337544 | H,0,-1.4181628763,0.033271906,-2.2371842193 C,0,-1.381110692,0.0824584015,-1.1529380045 C,0,-1.2937985829,0.2140963149,1.6164145788 C,0,-0.1484757175,0.1233527068,-0.5152510477 C,0,-2.5633147834,0.0953157904,-0.4203770803 C,0,-2.5184289256,0.1587672879,0.9671665333 C,0,-0.1075949789,0.1917992065,0.8861757276 H,0,-3.5175888703,0.0565302618,-0.9338141534 H,0,-3.437501219,0.1706996459,1.5422384025 H,0,-1.2286590002,0.2744181758,2.6966437357 C,0,1.1604422644,0.1421781086,-1.2555491729 H,0,1.4541692161,1.1851491698,-1.4343342237 H,0,1.0576142466,-0.3276217265,-2.2361510253 C,0,2.2390206373,-0.5475815,-0.4275010088 H,0,3.2355800904,-0.3736682369,-0.8394197696 H,0,2.0844766647,-1.636028346,-0.4302432087 N,0,1.1065592293,0.2626732357,1.6018374196 C,0,2.1754652174,-0.0742073523,0.99841665 H,0,3.101308028,-0.03160305,1.5738698666 |
| H,0,1.8194266137,-2.2196592073,-0.9069768218 C,0,0.8601051426,-1.7184499892,-0.9924897264 C,0,-1.5798779827,-0.4147082336,-1.1908110396 C,0,0.3602880048,-1.0415819737,0.1165998376 C,0,0.1592924012,-1.7587588981,-2.1905940492 C,0,-1.0609014814,-1.0987551148,-2.2813569703 C,0,-0.8823274544,-0.3787568024,0.0179779402 H,0,0.5605733237,-2.2931849815,-3.0432644901 H,0,-1.6205831137,-1.1176025,-3.2102214854 H,0,-2.5326148231,0.0994591806,-1.2749192337 C,0,1.0782464033,-0.9439886171,1.3774176536 H,0,2.1043568934,-1.2972319853,1.4102035139 C,0,0.5031406545,-0.4335496454,2.4680079558 H,0,1.0373272891,-0.3740471848,3.409745518 N,0,-1.3330273585,0.3541056391,1.0977501782 H,0,-2.2699832978,0.713212754,1.0090356538 C,0,-0.928705554,0.0129998123,2.4516694104 H,0,-1.5652960092,-0.7792246815,2.8907345531 H,0,-1.0567696445,0.8976894337,3.0829404901 | H,0,2.3579309285,0.,-1.1772589665 C,0,1.2726554863,0.,-1.1647413209 C,0,-1.5274076198,0.,-1.1224980564 C,0,0.6020567449,0.,0.0798515712 C,0,0.5616034682,0.,-2.3358821966 C,0,-0.8491893203,0.,-2.3130994143 C,0,-0.8228910793,0.,0.1029635752 H,0,1.0814940694,0.,-3.2872743807 H,0,-1.3974900427,0.,-3.2485822652 H,0,-2.6101245648,0.,-1.0808353666 N,0,-1.5341945314,0.,1.2619181602 C,0,-0.8672797233,0.,2.3892250774 H,0,-1.4614228457,0.,3.300409868 C,0,1.273350493,0.,1.3226554278 H,0,2.3586218793,0.,1.3440248681 C,0,0.5421627507,0.,2.4783302426 H,0,1.0201323752,0.,3.4508202689 |
| C,0,-0.2243212043,-0.0718304834,1.0528258025 H,0,-0.4161973756,0.8174340998,1.6425410552 C,0,0.3879876905,-1.2150962334,1.692676974 H,0,0.6431119176,-1.1440875453,2.7447134223 C,0,-0.5384599131,-0.1022416584,-0.2569094571 H,0,-0.9748258624,0.7624880443,-0.7470679286 C,0,0.6328463276,-2.3545066776,1.0167753768 H,0,1.0678172858,-3.2257343188,1.4920388245 C,0,-0.2594363638,-1.2733508644,-1.0589604908 C,0,0.2573923799,-2.4917071531,-0.3806356706 C,0,-0.3479834388,-1.287758862,-2.4047414497 H,0,-0.6465051363,-0.3921567255,-2.9431195398 N,0,0.3554207193,-3.6441878453,-0.9458136627 C,0,0.0743299675,-2.5038033218,-3.1599198895 H,0,1.1373666065,-2.4010876905,-3.4305732981 H,0,-0.4705776606,-2.5955304496,-4.1033139358 C,0,-0.1480909026,-3.7437548729,-2.3053652971 H,0,0.3004067673,-4.6213996227,-2.7757782493 H,0,-1.2291633044,-3.9478684194,-2.2373026862 | O2-Triplet O,0,0.,0.,0.834371757 O,0,0.,0.,-0.366371757 H2O H,0,0.,0.0004967663,-0.0000732467 O,0,0.,-0.0007050158,0.9605449511 H,0,0.,0.9274962495,1.207994294 H2O2 O,0,-0.1456779207,0.1056603005,0.9633472096 H,0,0.381594754,0.8552482316,1.2683044737 O,0,-0.0250422265,0.2669220776,-0.4653702631 H,0,-0.9537432531,0.3758907549,-0.7073159253 |
| H,0,0.0600533118,-0.0059137149,-0.0776568862 N,0,0.0168285638,-0.0023054076,0.9289611921 C,0,0.0198285196,1.151379403,1.7056390062 C,0,-0.0530931987,-1.1504037324,1.7107586419 C,0,-0.0564272114,0.6704189513,3.1239744201 H,0,-0.0706066498,1.3576552268,3.9574816874 C,0,-0.0985528709,-0.6592827456,3.1269319482 H,0,-0.1560866789,-1.3405325564,3.963483008 O,0,-0.0718075578,-2.2861628074,1.3122260867 O,0,0.0729859789,2.2842632434,1.3020605258 | H,0,0.5811406402,-0.3838932193,-2.0052964948 N,0,0.2441175745,-0.313638795,-1.059272378 C,0,0.0189236745,-1.4369489274,-0.2931254183 C,0,0.0113341103,0.3888634224,1.1103049708 H,0,-0.0644177725,1.0696634743,1.947697829 C,0,-0.1803362854,-0.9254116694,1.0978904944 H,0,-0.4352126856,-1.5802340144,1.9186526556 O,0,-0.0053808673,-2.5826946474,-0.6808359328 C,0,0.3449365823,0.8933860407,-0.276328982 H,0,1.3575403293,1.3098305411,-0.3096196084 O,0,-0.4813657137,1.9408879116,-0.7252832165 H,0,-1.3912796924,1.6201898829,-0.7247839718 |
| C,0,0.0122772827,-1.2584898236,1.9639661315 O,0,0.0633357941,-1.3425085456,3.1413571182 N,0,-0.0105467461,-2.4007646352,1.0604644553 H,0,0.0152458867,-3.3699233286,1.3589659701 O,0,-0.0996730817,-2.7858616935,-1.1647577638 H,0,-0.1423677295,-2.3536744744,-2.0335729909 C,0,-0.0423971197,-0.0678210428,1.0550833502 H,0,-0.0402039537,0.9458284768,1.4308704149 C,0,-0.0901671544,-0.4946904598,-0.2080754503 H,0,-0.1366576119,0.0873951012,-1.1184956583 C,0,-0.0689111525,-1.9657458865,-0.1770279811 | H,0,3.4661189904,1.4919179897,-1.9962678456 C,0,2.7963916296,1.5018594539,-1.1413578023 C,0,1.0569148747,1.5304648248,0.9968773876 C,0,1.7534964781,0.5873160697,-1.1140854551 C,0,3.0060148568,2.4122666979,-0.1130313472 C,0,2.1219405837,2.4187194963,0.9545644501 C,0,0.8620147068,0.5829215781,-0.0195467602 H,0,3.8342429025,3.1094077611,-0.1533599538 H,0,2.2445357341,3.1318811604,1.7624389906 H,0,0.3660049579,1.5997570936,1.827786116 N,0,-0.1788404143,-0.3396644126,0.0246431924 C,0,1.52753752,-0.380006309,-2.2406993927 H,0,2.0052500085,-1.3430285165,-2.0206149642 H,0,1.988157064,-0.0005675479,-3.1559392132 C,0,-0.5631412197,-1.1325152015,-1.1393213593 H,0,-1.6583728361,-1.1368624619,-1.2148050226 H,0,-0.2479766913,-2.1724379696,-0.9971928624 C,0,0.0310920458,-0.5927933975,-2.4263883545 H,0,-0.176026595,-1.3018102207,-3.2315731465 H,0,-0.442041564,0.3569706005,-2.6942527146 C,0,-0.9568085666,-0.521807903,1.2120941916 H,0,-0.3505707017,-0.2202172873,2.0708767532 C,0,-2.3255842665,0.1854370204,1.2773169564 H,0,-2.3247574156,1.1148869884,1.8464347018 H,0,-2.6939806901,0.4186937651,0.2749895142 C,0,-1.2870256026,-1.9971858581,1.513907687 O,0,-0.5586631973,-2.9496105713,1.4251328378 N,0,-2.5953061543,-2.0269108444,1.9636256386 H,0,-3.0296260707,-2.8719903421,2.3084112004 C,0,-3.271596509,-0.8147435709,1.9092237432 O,0,-4.3993937512,-0.6403480866,2.2901129934 |
| H,0,-1.3929967779,0.1209776001,-3.9076754289 C,0,-1.0748702677,0.7198852437,-3.0611272248 C,0,-0.2450229255,2.2629354672,-0.9200473099 C,0,-0.3600729311,0.0973551962,-2.0333473596 C,0,-1.3723649326,2.0705154421,-3.025958075 C,0,-0.9476084187,2.8517844192,-1.9557071052 C,0,0.0243266998,0.898617023,-0.9652980664 H,0,-1.9273278313,2.5217140645,-3.8397580381 H,0,-1.1568537203,3.9140122766,-1.9304039023 H,0,0.1037114544,2.86950208,-0.0896618683 C,0,0.0230495131,-1.3534127077,-2.1448546338 H,0,0.8278521171,-1.436645463,-2.8844234483 H,0,-0.8158546442,-1.9256237678,-2.5463588131 C,0,0.4798011241,-1.9423570191,-0.8199867048 H,0,1.0054582118,-2.8860924251,-0.9797685551 H,0,-0.3725190272,-2.1643175374,-0.1764831953 N,0,0.7751501729,0.3314635147,0.1818259699 H,0,1.549724931,0.9818131782,0.383834711 C,0,1.4249646713,-0.9997154037,-0.1091992766 H,0,2.2979772001,-0.7775009655,-0.7260811985 H,0,1.7701380013,-1.3982755532,0.8444826483 C,0,0.004727312,0.3715358359,1.5052756821 H,0,-0.576938029,1.2958821069,1.4562142062 C,0,-0.7998923064,-0.7865949113,1.9656485817 H,0,-1.7290642448,-1.1200042762,1.5312458384 C,0,-0.3654025962,-1.0853022318,3.2074817781 C,0,1.096017274,0.522885845,2.58806994 O,0,2.0826428676,1.2062711763,2.4681188032 N,0,0.7375999579,-0.3180074038,3.5955419802 H,0,1.2846824077,-0.4896645845,4.427640517 O,0,-0.7936073948,-1.9250739974,4.1342506586 H,0,-1.5574279766,-2.428562011,3.8265087323 | H,0,3.4898426509,1.126548941,-1.9835838472 C,0,2.869763264,1.207687495,-1.0966551301 C,0,1.2855437847,1.4073625456,1.1460434031 C,0,1.654900737,0.5305476611,-1.0798334675 C,0,3.3017494413,1.9792125848,-0.0293697686 C,0,2.5002203185,2.0730549223,1.0972471053 C,0,0.83410369,0.6473674375,0.0595117963 H,0,4.2535554411,2.4938935224,-0.0746899175 H,0,2.8199599541,2.6556071048,1.9530706631 H,0,0.7178477753,1.4802572542,2.0647386253 N,0,-0.4410057528,0.0289317776,0.0507596447 C,0,1.2576889931,-0.3012976214,-2.2736031424 H,0,1.8353698839,-1.2332142536,-2.2646352997 H,0,1.5398347836,0.2193088899,-3.1913377595 C,0,-0.6586574091,-1.0617701383,-0.8982427966 H,0,-1.719092952,-1.3211458205,-0.9051829381 H,0,-0.0984940147,-1.9625816825,-0.6039156935 C,0,-0.226602998,-0.6262317211,-2.2871212117 H,0,-0.4445796211,-1.4209623778,-3.0035331027 H,0,-0.8112058973,0.249965351,-2.5806759805 C,0,-1.3040077185,0.1268566726,1.1903394389 H,0,-1.0521297995,1.027143422,1.7492565257 C,0,-2.8131449521,0.0802260039,0.8915340468 H,0,-3.3550920506,0.8332288098,1.4700100566 H,0,-3.0536729554,0.2480707173,-0.1569274659 N,0,-2.1709662112,-1.8731740776,2.0675815468 H,0,-2.2592448943,-2.7936569776,2.4885390481 C,0,-3.294559569,-1.2754484723,1.3401446746 O,0,-4.326295201,-1.8385371991,1.2149365687 C,0,-1.1129061763,-1.0931342579,2.0701720751 O,0,0.0248291215,-1.3408326869,2.6267604712 H,0,0.097583334,-2.2096428262,3.0544358311 |
| Singlet State | Triplet state |
| H,0,3.1068851734,1.7575670478,-2.0509008765 C,0,2.6232416145,1.4701594215,-1.1238678126 C,0,1.4352695375,0.6892002758,1.2526690543 C,0,1.5297598755,0.6039487634,-1.1855798109 C,0,3.112667802,1.9394945925,0.0812574258 C,0,2.5286133428,1.5321492708,1.2771927114 C,0,0.9216900461,0.2688864234,0.0256098685 H,0,3.967283636,2.6054971109,0.0935483847 H,0,2.9310775545,1.8610869917,2.2271385155 H,0,1.0091166698,0.3380645261,2.1844415016 N,0,-0.2531548501,-0.6314454972,0.047489974 C,0,1.0822603325,0.0507047739,-2.5086905327 H,0,1.9581165479,-0.1368631761,-3.1320663591 H,0,0.4826498376,0.8012914864,-3.0379082403 C,0,-0.8183841175,-0.9449897246,-1.3094508016 H,0,-1.3948157731,-0.0675206609,-1.6073800781 H,0,-1.4903476754,-1.7894639565,-1.1602256485 C,0,0.2723217001,-1.2175706443,-2.31406718 H,0,0.9003665913,-2.0457807773,-1.9782331491 H,0,-0.2034602908,-1.5310585146,-3.2452801535 C,0,-1.3282643092,-0.2530810129,1.0860277989 H,0,-0.9419204082,0.5998070735,1.6301095439 C,0,-2.766941277,-0.0283759535,0.6396827751 H,0,-3.0801123563,1.0068949259,0.7689544563 H,0,-2.9904211993,-0.307798124,-0.3873078043 N,0,-2.7365309121,-1.7438235684,2.2456046893 H,0,-3.0733928511,-2.4037772339,2.9321164588 C,0,-3.6106889341,-0.9391108326,1.5370433403 O,0,-4.8027514588,-0.9628290704,1.6070632086 C,0,-1.3743416901,-1.4977374853,2.0099731816 O,0,-0.8567049903,-2.5369491493,1.1418184856 O,0,-0.5757083694,-1.3063929655,3.1079221188 H,0,-0.4566983264,-2.1320885689,3.5957500055 O,0,0.2842113276,-1.9181681671,0.5971220489 | H,0,3.3838276795,1.5021739442,-1.9048022548 C,0,2.7622598886,1.3439171209,-1.030802431 C,0,1.210611965,0.930355533,1.2525329284 C,0,1.5811068983,0.6436633446,-1.1739542127 C,0,3.1736064589,1.8383753218,0.2036598827 C,0,2.3928397433,1.6123352224,1.3473534761 C,0,0.7542003323,0.4474272326,-0.0111732951 H,0,4.1064129311,2.3839959498,0.2840441775 H,0,2.7301921253,1.9678080334,2.3131995372 H,0,0.6544563346,0.7196470945,2.1541118615 N,0,-0.4451072431,-0.1798426876,-0.1321818614 C,0,1.1566003508,0.1042577507,-2.5019159365 H,0,2.037227134,-0.1115760172,-3.1090601091 H,0,0.5896304552,0.8745913038,-3.0417961888 C,0,-0.8700037035,-0.7868008532,-1.4073652034 H,0,-1.5395502319,-0.0732388674,-1.902751281 H,0,-1.4488880297,-1.6764821635,-1.1635340842 C,0,0.2957892881,-1.1298079396,-2.3051417009 H,0,0.8817745457,-1.9413813556,-1.8648198371 H,0,-0.0978879528,-1.4935918722,-3.255401035 C,0,-1.4060351863,-0.2061725517,0.9682338408 H,0,-1.1836283532,0.6346784866,1.6219312828 C,0,-2.8886822405,-0.1247836215,0.6034823264 H,0,-3.2572653465,0.8956410233,0.5097836586 H,0,-3.1540874935,-0.6682680886,-0.3037014783 N,0,-2.5924754556,-1.5543856553,2.4319313971 H,0,-2.7994975548,-2.1307067197,3.2365716349 C,0,-3.5734523085,-0.835683988,1.7679858599 O,0,-4.7328228284,-0.797374093,2.0574813696 C,0,-1.3071009466,-1.4583378049,1.9019895839 O,0,-1.0824554828,-2.6938591796,0.9752445938 O,0,-0.3012446621,-1.4474352198,2.7958630405 H,0,0.3077039264,-2.1811316902,2.5341444494 O,0,0.0528363624,-3.2780794931,1.1964332083 |
| Singlet state | Triplet state |
| H,0,3.7260576546,0.9167190118,-1.6541475037 C,0,2.9479857236,1.0961231868,-0.9206990615 C,0,0.9494650133,1.5793255064,0.9479066655 C,0,1.7415798023,0.4206481162,-1.0391105908 C,0,3.1626420406,2.0009837543,0.1106684848 C,0,2.1578350731,2.2531262938,1.0342726005 C,0,0.7565421662,0.6529943261,-0.0720076164 H,0,4.1101301094,2.5211943427,0.1835503814 H,0,2.307896917,2.9789725234,1.8237792184 H,0,0.1712116036,1.8155075559,1.6617664809 N,0,-0.4890192659,-0.0718804146,-0.1931235768 C,0,1.4525967411,-0.5368072099,-2.1581701902 H,0,1.673981591,-1.563666194,-1.8456399723 H,0,2.0838061515,-0.3216641336,-3.02017381 C,0,-0.8622401556,-0.5404673377,-1.3381035016 C,0,-0.0189685257,-0.4174408881,-2.543311096 H,0,-0.3270809494,-1.1660134137,-3.2742592874 H,0,-0.2223850173,0.5656591401,-2.9961057169 C,0,-1.2832617501,-0.3587602691,1.0235091492 H,0,-0.8243798987,0.2051570931,1.8274355376 C,0,-2.7751247017,-0.066358977,0.9856066113 H,0,-3.0315261894,0.9587461459,1.2501834518 H,0,-3.2408194767,-0.2905793917,0.0231856017 N,0,-2.3354545112,-1.9396143475,2.3312597081 H,0,-2.5468509308,-2.7937231696,2.8302327747 C,0,-3.3449719229,-1.0483348222,2.0117801721 O,0,-4.4567700681,-1.0539918647,2.4569444009 C,0,-1.1811658602,-1.8502554673,1.4957625339 O,0,-1.2600678385,-2.6301315823,0.3227700081 O,0,0.0001489002,-2.158800351,2.1328981361 H,0,-0.1036272917,-2.0647337384,3.0862981864 O,0,-1.3468540672,-4.0103009332,0.7169743825 H,0,-2.1715396369,-4.2672330485,0.2778100313 H,0,-1.8122651294,-1.0577693424,-1.370442994 | H,0,3.41209713,1.4875235017,-1.9626278922 C,0,2.8090934073,1.2934402341,-1.0828481289 C,0,1.286975615,0.8349234433,1.2200517392 C,0,1.635551959,0.5776560406,-1.2238389598 C,0,3.2315295148,1.7673060272,0.1550190144 C,0,2.4639206624,1.5226875863,1.3085375447 C,0,0.8290281916,0.3599542162,-0.0448336453 H,0,4.1597641507,2.3211145292,0.2322517471 H,0,2.8127562039,1.8700317934,2.2733156462 H,0,0.7349570882,0.5977862451,2.1182606754 N,0,-0.3647413149,-0.2711961914,-0.1697149922 C,0,1.2133957777,0.0668535658,-2.5659259542 H,0,1.728300947,-0.882783697,-2.7545049915 H,0,1.5357066334,0.7605392903,-3.34537249 C,0,-0.6929806578,-0.9072522199,-1.4110305885 C,0,-0.3057182466,-0.1800360435,-2.6316390215 H,0,-0.5660124003,-0.7568324969,-3.5183593667 H,0,-0.8263497587,0.7827006197,-2.6941119511 C,0,-1.3638472016,-0.3018185932,0.8963422388 H,0,-1.1740538818,0.5385014654,1.5614473937 C,0,-2.8135675555,-0.2420291186,0.4226609819 H,0,-3.1814139194,0.7705397505,0.2664949808 H,0,-2.9747380021,-0.81391346,-0.4946980105 N,0,-2.655830832,-1.6528304845,2.2771499101 H,0,-2.900242282,-2.0825870083,3.1574281126 C,0,-3.5763656189,-0.9201920193,1.5578795042 O,0,-4.7498557286,-0.8349832688,1.788120415 C,0,-1.3101366679,-1.5617612435,1.8144162246 O,0,-0.942868992,-2.6456110442,0.9695028441 O,0,-0.3879473843,-1.3901281433,2.8253790909 H,0,-0.1344408199,-2.2611885403,3.163277021 O,0,-0.8521415158,-3.8111945383,1.801243256 H,0,-1.6528371447,-4.2972796079,1.5511720531 H,0,-0.8194810563,-1.9813104903,-1.3511449011 |
| C,0,-0.149202422,-1.148905925,1.8984161248 O,0,-0.3581492179,-1.2349042702,3.0549261731 N,0,-0.4822287086,-2.2224338278,0.9541421195 H,0,-0.8229567097,-3.1318535133,1.2583462607 C,0,-0.2143194125,-1.8914592863,-0.2774591691 O,0,-0.2909532747,-2.7044978924,-1.2593491871 H,0,0.0446633644,-2.262975026,-2.0773464556 O,0,1.371637214,-0.3213989886,-1.1638797638 O,0,0.913666712,-0.6668025459,-2.5005070152 H,0,1.6834581814,-0.4136550995,-3.034836752 C,0,0.2157414202,-0.4380455633,-0.3780501443 C,0,0.4922833457,-0.0535484909,1.0709655433 H,0,0.1034850615,0.9231492066,1.3533769075 H,0,1.568778601,-0.0640476512,1.2711827095 H,0,-0.607842255,0.1408087738,-0.8167696513 | C,0,0.1387463807,-1.235559242,1.8458083078 O,0,0.1900365411,-1.4439585324,3.0273359716 N,0,0.2533109063,-2.0875933113,0.7814395911 H,0,0.387299518,-3.0856433947,0.8958608024 C,0,0.1650370128,-1.4955338118,-0.5179288265 O,0,-0.9428551514,-1.9360428779,-1.1865017132 H,0,-0.821143844,-1.7683544982,-2.1345181655 O,0,1.3741452849,-1.8091279071,-1.1585362287 O,0,1.2630632093,-1.181003167,-2.4585156097 H,0,1.859313958,-1.7440168727,-2.9767807754 C,0,0.0746376166,0.039349543,-0.1798649947 H,0,1.0866452263,0.486711069,-0.3576719752 H,0,-0.5938205804,0.6730842121,-0.7768999172 C,0,-0.0973746138,0.1053935575,1.2178489748 H,0,-0.3730553485,0.9766565864,1.8111034964 |

Supplementary Table 2 B3PW91 computed energetic data [total electronic energy, Etot, in Hartree; Zero-point energy, ZPE, in kcal/mol; number of imaginary frequencies, NImag; as well as sum of electronic and thermal enthalpy, Htot, in Hartree, and sum of electronic and thermal free energy, Gtot, in Hartree).

|  | Etot=-404,3178873 ZPE=114,09830 NImag=0 | Htot=-404,127140 Gtot= -404,168524 |
| --- | --- | --- |
|  | Etot=-403,0919357 ZPE=99,11662 NImag=0 | Htot=-402,925675 Gtot= -402,965857 |
|  | Etot=-401,8952482 ZPE=84,82509 NImag=0 | Htot=-401,752362 Gtot= -401,791267 |
|  | Etot=-403,0881373 ZPE=99,18848 NImag=0 | Htot=-402,921520 Gtot= -402,962158 |
|  | Etot=-403.0522151 ZPE=98.67151 NImag=0 | Htot=-402.886501 Gtot=-402,926919 |
| O2-Triplet | Etot=-150,3222601 ZPE=2,37844 NImag=0 | Htot=-150,315163 Gtot= -150,338427 |
| H2O | Etot=-76,4309618 ZPE=13,40154 NImag=0 | Htot=-76,405825 Gtot= -76,427244 |
| H2O2 | Etot=-151.5512043 ZPE=16.69142 NImag=0 | Htot=-151.520418 Gtot= -151,546254 |
|  | Etot=-359,4167242 ZPE=42,75284 NImag=0 | Htot=-359,342160 Gtot= -359,377277 |
|  | Etot =-763.7567474 ZPE= 159.58174 NImag=0 | Htot=-763.487511 Gtot= -763,544773 |
|  | Etot=-360,6140646 ZPE=57,55050 NImag=0 | Htot=-360,515381 Gtot= -360,552187 |
|  | Etot=-359.7311796 ZPE=50.54978 NImag=0 | Htot=-359.644022 Gtot= -359,679991 |
|  | Etot=-764.095968 ZPE=168.58324 NImag=0 | Htot=-763.812478 Gtot= -763,868321 |
|  | Etot=-764.0821811 ZPE=167.16690 NImag=0 | Htot=-763.800661 Gtot= -763,857862 |
|  | Singlet state Etot=-914.3997607 ZPE=173.10556 NImag=0 | Htot=-914.107889 Gtot= -914,165620 |
|  | Triplet state Etot=-914.4033131 ZPE=171.23303 NImag=0 | Htot=-914.113319 Gtot= -914,175410 |
|  | Singlet state Etot=-914.450505 ZPE=171.92192 NImag=0 | Htot= -914.158922 Gtot= -914,221179 |
|  | Triplet state Etot=-914.3785903 ZPE=169.68402 NImag=0 | Htot=-914.090235 Gtot= -914,153696 |
|  | Etot=-511.3242959 ZPE= 70.59269 NImag=0 | Htot= -511.202657 Gtot= -511,244788 |
|  | Etot=-511.2233489 ZPE= 66.73019 NImag=0 | Htot= -511.106915 Gtot= -511.151498 |

III. NMR data of products

(1, 95% ) Substrate: 63.6 mg, Product: 60.4 mg.1H NMR (400.1 MHz, CDCl3) δ 8.96 – 8.89 (m, 1H), 8.13 (m, J = 11.0, 9.1 Hz, 2H), 7.81 (d, J = 8.1 Hz, 1H), 7.75 – 7.68 (m, 1H), 7.54 (t, J = 7.5 Hz, 1H), 7.39 (m, J = 8.2, 4.2 Hz, 1H). 13C NMR (101 MHz, CDCl3) δ 150.43, 148.33, 136.05, 129.50, 129.46, 128.30, 127.80, 126.55, 121.08.1

(2, 92% ), Substrate: 72.4 mg, Product: 66.6 mg. 1H NMR (400.1 MHz, CDCl3) δ 8.79 (d, J = 4.0 Hz, 1H), 8.06 (d, J = 8.2 Hz, 1H), 8.01 (d, J = 8.5 Hz, 1H), 7.51 (d, J = 10.7 Hz, 2H), 7.34 (m, J = 8.2, 4.2 Hz, 1H), 2.47 (s, 3H). 13C NMR (101 MHz, CDCl3) δ 148.67, 145.76, 136.86, 136.36, 132.27, 128.35, 128.23, 126.63, 121.06, 21.58.2

(3, 91%) Substrate: 70.8 mg, Product: 64.4 mg. 1H NMR (400.1 MHz, CDCl3) δ 8.29 (d, J = 8.5 Hz, 1H), 8.22 (d, J = 8.4 Hz, 1H), 7.82 (d, J = 8.1 Hz, 1H), 7.73 (t, J = 7.2 Hz, 1H), 7.54 (t, J = 7.4 Hz, 1H), 7.36 (d, J = 8.4 Hz, 1H), 2.85 (s, 3H). 13C NMR (101 MHz, CDCl3) δ 158.25, 144.43, 139.24, 131.15, 127.72, 127.00, 126.61, 126.06, 122.35, 23.64.3

(4, 76%) Substrate: 81.3 mg, Product: 61.8 mg. 1H NMR (400.1 MHz, CDCl3) δ 8.74 (d, J = 3.1 Hz, 1H), 8.07 (m, J = 20.3, 8.7 Hz, 2H), 7.46 – 7.30 (m, 2H), 7.07 (d, J = 2.7 Hz, 1H), 3.91 (s, 3H). 13C NMR (101 MHz, CDCl3) δ 157.97, 147.08, 143.37, 135.70, 130.05, 129.45, 122.87, 121.38, 105.12, 55.60.2,4

(5, 96%) Substrate: 72.3 mg, Product: 69.4 mg. 1H NMR (400.1 MHz, CDCl3) δ 8.87 (m, J = 4.2, 1.3 Hz, 1H), 8.13 (m, J = 8.9, 5.3 Hz, 2H), 7.56 – 7.37 (m, 3H). 13C NMR (101 MHz, CDCl3) δ 161.70, 159.23, 149.28 (J = 3.03 MHz), 136.02 (J = 6.06 MHz), 131.54 (J = 9.09 MHz), 128.96 (J = 10.1 MHz), 121.83, 120.09 (J = 26.26 MHz), 110.79 (J = 21.21MHz).

(6, 83%) Substrate: 96.3 mg, Product: 79.9 mg. 1H NMR (400.1 MHz, CDCl3) δ 8.94 (d, J = 3.3 Hz, 1H), 8.13 (d, J = 8.2 Hz, 1H), 8.05 (d, J = 9.0 Hz, 1H), 7.98 (d, J = 2.0 Hz, 1H), 7.79 (m, J = 9.0, 2.1 Hz, 1H), 7.47 (m, J = 8.3, 4.2 Hz, 1H). 13C NMR (101 MHz, CDCl3) δ 149.86, 145.57, 136.17, 133.52, 130.25, 129.86, 129.36, 121.96, 120.95.1

(7, 93%) Substrate: 70.0 mg, Product: 65.1 mg. 1H NMR (400.1 MHz, CD3OD) δ 8.61 (m, J = 4.4, 1.2 Hz, 1H), 8.19 (d, J = 8.3 Hz, 1H), 7.87 (d, J = 9.1 Hz, 1H), 7.44 (m, J = 8.4, 4.4 Hz, 1H), 7.37 (m, J = 9.1, 2.6 Hz, 1H), 7.15 (d, J = 2.6 Hz, 1H). 13C NMR (101 MHz, CD3OD) δ 157.74, 147.06, 142.59, 137.92, 131.55, 129.35, 124.29, 122.59, 109.74.1

(8, 89%) Substrate: 74.6 mg, Product: 66.4 mg. 1H NMR (400.1 MHz, CD3OD) δ 8.58 (m, J = 4.8, 1.6 Hz, 1H), 8.27 (d, J = 8.2 Hz, 1H), 7.73 (d, J = 8.9 Hz, 1H), 7.27 (m, J = 8.2, 4.8 Hz, 1H), 7.19 – 7.04 (m, 2H). 13C NMR (101 MHz, CD3OD) δ 162.19, 149.06, 148.03, 140.92, 131.17, 124.88, 121.83, 119.47, 107.71.

(9, 85%) Substrate: 75.0 mg, Product: 63.8 mg. 1H NMR (400.1 MHz, CDCl3) δ 8.79 – 8.70 (m, 1H), 8.14 (d, J = 8.3 Hz, 1H), 7.45 – 7.38 (m, 2H), 7.31 (d, J = 8.1 Hz, 1H), 7.19 (d, J = 7.6 Hz, 1H). 13C NMR (101 MHz, CDCl3) δ 152.16, 147.80, 138.09, 136.37, 128.57, 127.82, 121.81, 117.92, 110.29.1

(10, 90%) Substrate: 77.0 mg, Product: 69.3 mg. 1H NMR (400.1 MHz, CDCl3) δ 8.11 (m, J = 9.2, 5.2 Hz, 1H), 8.04 (d, J = 8.5 Hz, 1H), 7.48 – 7.41 (m, 1H), 7.38 (m, J = 8.7, 2.8 Hz, 1H), 7.31 (d, J = 8.5 Hz, 1H), 2.75 (s, 3H). 13C NMR (101 MHz, CDCl3) δ 161.39, 158.92, 158.03 (J = 2.02 MHz), 136.77 (J = 5.05 MHz), 129.98 (J = 9.09 MHz), 127.57 (J = 10.1 MHz), 122.95, 120.18 (J = 25.25 MHz), 110.70 (J = 22.22 MHz), 24.45.

(11, 79%) Substrate: 58.0 mg, Product: 45.8 mg. 1H NMR (400.1 MHz, CDCl3) δ 8.35 (s, 1H), 7.36 (m, J = 7.0, 2.2 Hz, 1H), 7.31 – 7.27 (m, 2H), 7.17 (d, J = 7.2 Hz, 1H), 3.78 (t, J = 7.0 Hz, 2H), 2.85 – 2.67 (m, 2H). 13C NMR (101 MHz, CDCl3) δ 160.49, 136.36, 131.20, 127.46, 127.34, 127.13, 47.25, 25.03.

(12, 87%) Substrate: 72.7 mg, Product: 63.2 mg. 1H NMR (400.1 MHz, CD3OD) δ 8.06 (s, 1H), 7.19 (d, J = 8.5 Hz, 1H), 6.43 (m, J = 8.5, 2.2 Hz, 1H), 6.35 (s, 1H), 3.50 (t, J = 7.7 Hz, 2H), 2.70 (t, J = 7.8 Hz, 2H). 13C NMR (101 MHz, CD3OD) δ 161.44, 141.58, 135.71, 118.09, 117.96, 44.25, 26.73.

(13, 81%) Substrate: 84.0 mg, Product: 68.0 mg. 1H NMR (400.1 MHz, CDCl3) δ 8.29 (s, 1H), 7.48 (m, J = 8.0, 2.0 Hz, 1H), 7.41 (d, J = 1.9 Hz, 1H), 7.05 (d, J = 8.0 Hz, 1H), 3.78 (m, J = 11.1, 4.2 Hz, 2H), 2.74 – 2.66 (m, 2H). 13C NMR (101 MHz, CDCl3) δ 158.97, 143.47, 135.07, 133.90, 130.09, 129.15, 120.45, 47.20, 24.46.

(14, 62%) Substrate: 84.9 mg, Product: 52.6 mg. 1H NMR (400.1 MHz, CDCl3) δ 7.48 (d, J = 7.5 Hz, 1H), 7.37 – 7.26 (m, 2H), 7.18 (d, J = 7.7 Hz, 1H), 3.64 (t, J = 7.4 Hz, 2H), 2.70 (t, J = 7.3 Hz, 2H), 2.39 (s, 3H). 13C NMR (101 MHz, CDCl3) δ 164.74, 137.33, 130.79, 129.40, 127.44, 126.93, 125.44, 46.60, 25.96, 23.09.

(15, 76%) Substrate: 93.8 mg, Product: 71.3 mg. 1H NMR (400.1 MHz, CDCl3) δ 7.62 – 7.56 (m, 2H), 7.45 – 7.34 (m, 4H), 7.27 – 7.21 (m, 3H), 3.87 – 3.77 (t, 2H), 2.83 – 2.72 (t, 2H). 13C NMR (101 MHz, CDCl3) δ 167.39, 138.85, 130.77, 129.38, 128.84, 128.18, 128.01, 127.44, 126.61, 47.56, 26.33.

(16, 92%) Substrate: 51.8 mg, Product: 47.7 mg. 1H NMR (400.1 MHz, CDCl3) δ 8.06 (s, 1H), 7.65 (d, J = 7.8 Hz, 1H), 7.37 (m, J = 8.1, 0.8 Hz, 1H), 7.22 – 7.16 (m, 2H), 7.13 (m, J = 10.5, 4.0 Hz, 1H), 6.63 – 6.46 (m, 1H).13C NMR (101 MHz, CDCl3) δ 135.79, 127.87, 124.18, 122.02, 120.77, 119.85, 111.06, 102.64. 5

(17, 89%) Substrate: 56.0 mg, Product: 49.8 mg. 1H NMR (400.1 MHz, CD3OD) δ 7.41 (d, J = 7.7 Hz, 1H), 7.26 (d, J = 8.0 Hz, 1H), 7.05 – 6.91 (m, 3H), 2.38 (s, 3H). 13C NMR (101 MHz, CD3OD) δ 137.96, 128.93, 121.24, 121.06, 120.15, 119.86, 111.40, 111.21, 13.57.3

(18, 83%) Substrate: 53.2 mg, Product: 44.2 mg. 1H NMR (400.1 MHz, CD3OD) δ 7.53 – 7.44 (m, 1H), 7.36 – 7.23 (m, 1H), 7.11 – 7.06 (m, 1H), 7.03 – 6.94 (m, 2H), 2.31 (d, J = 1.1 Hz, 3H). 13C NMR (101 MHz, CD3OD) δ 138.12, 129.58, 123.07, 122.10, 119.30, 119.19, 111.98, 111.24, 9.76.

(19, 94%) Substrate: 57.6 mg, Product: 54.1 mg. 1H NMR (400.1 MHz, CDCl3) δ 8.22 (s, 1H), 7.24 (d, J = 8.2 Hz, 1H), 7.21 – 7.17 (m, 1H), 7.14 – 7.09 (m, 1H), 6.93 (d, J = 7.1 Hz, 1H), 6.58 (s, 1H), 2.58 (s, 3H). 13C NMR (101 MHz, CDCl3) δ 135.47, 130.23, 127.78, 123.55, 122.08, 119.90, 108.66, 101.06, 18.86.

(20, 63%) Substrate: 70.0 mg, Product: 44.1 mg. 1H NMR (400.1 MHz, CD3OD) δ 7.54 – 7.42 (m, 1H), 7.32 (dt, J = 8.1, 0.8 Hz, 1H), 7.11 – 7.06 (m, 1H), 7.03 – 6.95 (m, 2H), 2.31 (d, J = 1.1 Hz, 3H). 13C NMR (101 MHz, CD3OD) δ 155.14, 132.95, 129.82, 126.16, 112.73, 112.56, 103.08, 102.19, 56.26.

(21, 88%) Substrate: 99.7 mg, Product: 87.7 mg. 1H NMR (400.1 MHz, CDCl3) δ 8.36 (s, 1H), 7.32 (m, J = 10.5, 7.9 Hz, 2H), 7.25 – 7.21 (m, 1H), 7.09 – 7.02 (m, 1H), 6.61 (t, J = 2.3 Hz, 1H). 13C NMR (101 MHz, CDCl3) δ 136.03, 128.68, 124.78, 122.92, 122.76, 114.74, 110.31, 103.00.6

(22, 68%) Substrate: 76.3 mg, Product: 51.9 mg. 1H NMR (400.1 MHz, CDCl3) δ 8.99 (s, 1H), 8.61 (d, J = 2.1 Hz, 1H), 8.10 (m, J = 9.0, 2.2 Hz, 1H), 7.46 (d, J = 9.0 Hz, 1H), 7.42 – 7.35 (m, 1H), 6.73 (d, J = 2.2 Hz, 1H). 13C NMR (101 MHz, CDCl3) δ 141.82, 138.93, 129.16, 127.26, 117.98, 117.58, 111.19, 104.92.6

(23, 73%) Substrate: 66.4 mg, Product: 48.5 mg. 1H NMR (400.1 MHz, CDCl3) δ 8.86 (s, 2H), 8.12 (m, J = 6.4, 3.5 Hz, 2H), 7.79 (m, J = 6.4, 3.4 Hz, 2H). 13C NMR (101 MHz, CDCl3) δ 144.99, 143.04, 130.13, 129.52.1

IV. NMR spectra of the products

Supplementary Figure 10 1H NMR spectra of the quinoline

Supplementary Figure 11 13C NMR spectra of the quinoline

Supplementary Figure 12 1H NMR spectra of the 6-methylquinoline

Supplementary Figure 13 13C NMR spectra of the 6-methylquinoline

Supplementary Figure 14 1H NMR spectra of the 2-methylquinoline

Supplementary Figure 15 13C NMR spectra of the 2-methylquinoline

Supplementary Figure 16 1H NMR spectra of the 6-methoxyquinoline

Supplementary Figure 17 13C NMR spectra of the 6-methoxyquinoline

Supplementary Figure 18 1H NMR spectra of the 6-fluoroquinoline

Supplementary Figure 19 13C NMR spectra of the 6-fluoroquinoline

Supplementary Figure 20 1H NMR spectra of the 6-bromoquinoline

Supplementary Figure 2113C NMR spectra of the 6-bromoquinoline

Supplementary Figure 22 1H NMR spectra of the quinolin-7-ol

Supplementary Figure 23 13C NMR spectra of the quinolin-7-ol

Supplementary Figure 24 1H NMR spectra of the quinolin-7-ol

Supplementary Figure 25 13C NMR spectra of the quinolin-8-ol

Supplementary Figure 26 1H NMR spectra of the quinolin-8-ol

Supplementary Figure 27 13C NMR spectra of the 6-fluoro-2-methylquinoline

Supplementary Figure 28 1H NMR spectra of the 6-fluoro-2-methylquinoline

Supplementary Figure 29 13C NMR spectra of the 6-fluoro-2-methylquinoline

Supplementary Figure 30 1H NMR spectra of the 3,4-dihydroisoquinoline

Supplementary Figure 31 13C NMR spectra of the 3,4-dihydroisoquinoline

Supplementary Figure 32 1H NMR spectra of the 3,4-dihydroisoquinolin-6-ol

Supplementary Figure 33 13C NMR spectra of the 3,4-dihydroisoquinolin-6-ol

Supplementary Figure 34 1H NMR spectra of the 6-bromo-3,4-dihydroisoquinoline

Supplementary Figure 35 13C NMR spectra of the 6-bromo-3,4-dihydroisoquinoline

Supplementary Figure 36 1H NMR spectra of the 1-methyl-3,4-dihydroisoquinoline

Supplementary Figure 37 13C NMR spectra of the 1-methyl-3,4-dihydroisoquinoline

Supplementary Figure 38 1H NMR spectra of the 1-phenyl-3,4-dihydroisoquinoline

Supplementary Figure 39 13C NMR spectra of the 1-phenyl-3,4-dihydroisoquinoline

Supplementary Figure 40 1H NMR spectra of the indole

Supplementary Figure 41 13C NMR spectra of the indole

Supplementary Figure 42 1H NMR spectra of the 2-methyl-1H-indole

Supplementary Figure 43 13C NMR spectra of the 2-methyl-1H-indole

Supplementary Figure 44 1H NMR spectra of the 3-methyl-1H-indole

Supplementary Figure 45 13C NMR spectra of the 3-methyl-1H-indole

Supplementary Figure 46 1H NMR spectra of the 5-bromo-1H-indole

Supplementary Figure 47 13C NMR spectra of the 5-bromo-1H-indole

Supplementary Figure 48 1H NMR spectra of the 5-nitro-1H-indole

Supplementary Figure 49 13C NMR spectra of the 5-nitro-1H-indole

Supplementary Figure 50 1H NMR spectra of the quinoxaline

Supplementary Figure 51 13C NMR spectra of the quinoxaline

Supplementary References

[1]	Cui, X. et al. Synthesis and characterization of iron–nitrogen-doped graphene/core–shell catalysts: Efficient oxidative dehydrogenation of N-heterocycles. J. Am. Chem. Soc. 137, 10652–10658 (2015).

[2]	Tanaka, T.; Okunaga, K.-i.; Hayashi, M. Dehydrogenation of 1,2,3,4-tetrahydroquinoline and its related compounds: comparison of Pd/C–ethylene system and activated carbon–O2 system. Tetrahedron Lett. 2010, 51, 4633-4635 (2010).

[3]	Chakraborty, S.; Brennessel, W. W.; Jones, W. D. A Molecular iron ctalyst for the acceptorless dehydrogenation and hydrogenation of N-heterocycles. J. Am. Chem. Soc. 136, 8564-8567 (2014).

[4]	Mullick, K.; Biswas, S.; Angeles-Boza, A. M.; Suib, S. L. Heterogeneous mesoporous manganese oxide catalyst for aerobic and additive-free oxidative aromatization of N-heterocycles. Chem. Commun. 53, 2256-2259 (2017).

[5]	Muthaiah, S.; Hong, S. H. Acceptorless and base-free dehydrogenation of alcohols and amines using tuthenium-hydride complexes. Adv. Synth. Catal. 354, 3045–3053 (2012).

[6]	Sahoo, M. K.; Jaiswal, G.; Rana, J.; Balaraman, E. Organo-photoredox catalyzed oxidative dehydrogenation of N-heterocycles. Chem. Eur. J. 23, 14167–14172 (2017).