SUPPLEMENTAL INFORMATION

Defect Engineered Bioactive Transition Metals Dichalcogenides Quantum Dots

Defect Engineered Bioactive Transition Metals Dichalcogenides Quantum Dots

Xianguang Ding1,2, Fei Peng1, Zhou Jun3, Wenbin Gong5, Garaj Slaven2,3, Kian Ping Loh2,6, Chwee Teck Lim2,4,7,8* and David Tai Leong1*

1Department of Chemical and Biomolecular Engineering, National University of Singapore, Singapore 117585, Singapore

2Centre for Advanced 2D Materials, Graphene Research Centre, National University of Singapore, Singapore 117546, Singapore

3Department of Physics, National University of Singapore, Singapore 117542, Singapore

4Department of Biomedical Engineering, National University of Singapore, Singapore 117575, Singapore

5Division of Advanced Nanomaterials, Suzhou Institute of Nano-Tech and Nano-Bionics, Chinese Academy of Sciences, Suzhou 215123, China

6Department of Chemistry, National University of Singapore, Singapore 117543, Singapore

7Mechanobiology Institute, Mechanobiology Institute, Singapore 117411, Singapore

8Biomedical Institute for Global Health Research and Technology, Singapore 117599, Singapore

*Correspondence: cheltwd@nus.edu.sg (D.T.L.)

*Correspondence: ctlim@nus.edu.sg (C.T.L.)

Supplementary Figure 1. MoCl5 and MoO3 dissolve to a colorless stable MoO42- solution at high pH. Red circle demarcates insoluble MoO3 at pH 6.8.

# Supplementary Figure 2. XPS spectra of as-prepared MoS2 QDs: (a) Mo and (b) S.

Supplementary Figure 3. High storage stability of aqueous dispersion of MoS2 QDs.

Supplementary Figure 4. TEM image of MoS2 sheet exfoliated by using BSA. Scale bar: 100 nm.

Supplementary Figure 5. TGA of BSA-coated MoS2 QDs performed under inert nitrogen atmosphere.

Analyzing the result from TGA curves, three stages was observed: weight loss below 100 oC can be assigned to water; the weight loss from 200 oC to 450 oC is mainly due to the thermal decomposition of decomposed of BSA. The weight loss from 450 oC is correspond to the thermal decomposition of MoS2 (Composites Part A: Applied Science and Manufacturing 94 (2017): 1-9.). The incompletely decomposed carbonaceous product under N2 atmosphere at 450 oC was about 20 % of the total BSA amount according to the previous BSA report (Journal of colloid and interface science 389.1 (2013): 31-41). Then the total amount of BSA and MoS2 was calculated to be around 7.1 mg and 2.4 mg, separately.

The mass of per 3.9 nm MoS2 QDs (based on TEM results) and BSA molecule were further calculated:

mMoS2= 43πr3 x ρMoS2 = 43π(1.95 nm)3 x 5.06 g/cm3  = 1.5 x 10-19 g MoS2/QD

mBSA = MWBSA6.022 x 1023  = 1.1 x 10-19 g BSA/Molecule

Then the ratio of  NBSA to NMoS2 was calculated as:

NBSANMoS2 = 7.1mBSA7.4mMoS2 = 4.03

The ratio estimated from TGA result (4.03) was slightly greater than the DLS measurements but still at the same order of magnitude. Considering that the simple calculation above is based on a single size QDs average diameter, the actual QDs size distribution may also affect the number of BSA ligand binding on the surface.

| Group | -OH | -NH2 | -COOH | -C6H5 | -S-S- | -SH |
| --- | --- | --- | --- | --- | --- | --- |
| EMoS2+group (Ha) | -21730.435 | -21730.572 | -21843.732 | -21886.118 | -22490.650 | -22053.312 |
| EGroup (Ha) | -115.614 | -95.746 | -228.903 | -271.260 | -875.809 | -438.485 |
| EMoS2 (Ha) | -21614.81 | -21614.810 | -21614.810 | -21614.810 | -21614.810 | -21614.810 |
| Ead (Ha) | -0.011 | -0.017 | -0.019 | -0.047 | -0.031 | -0.017 |
| Ead (eV) | -0.304 | -0.453 | -0.510 | -1.29 | -0.835 | -0.455 |

Supplementary Table 1. Calculated binding affinities of the major functional groups in BSA to MoS2 QDs.

Ead= EMoS2+group- Egroup- EMoS2

where Egroup, EMoS2 and EMoS2 +group are the energies of the bound functional group, the MoS2 surface and the complex of MoS2 and functional group respectively.

The oxygen adsorption energies on the pristine and oxygen-atom doped MoS2 were also calculated. The oxygen-doped MoS2 was modeled by substituting oxygen atom for sulfur. The nearest three sulfur atoms around the oxygen adsorption site were replaced one by one to describe the doping level. All the structures were optimized by using the conjugate gradient method, in which the convergence for total energy and interaction force was set to be 10-5 eV and 2×10-3 eV/Å, respectively.

# Supplementary Figure 6. TEM images and size distribution of MoS2 QDs synthesized with dBSA. Scale bar: 100 nm.

# Supplementary Figure 7. TEM images and size distribution of MoS2 QDs synthesized with DBA. Scale bar: 100 nm.

Supplementary Figure 8. TEM images of MoS2 QDs sampled at the reaction of 10 s and 1 h showing in-discernible differences even with extended reaction time. Scale bar: 100 nm.

Supplementary Figure 9. TEM images of MoS2 QDs synthesized at the 24 oC, 60 oC and 90 oC showing in-discernible differences even with elevated reaction temperature. Scale bar: 50 nm.

Supplementary Figure 10. Schematic illustration of the purification process of MoS2 QDs by adding Cu2+.

Supplementary Figure 11. UV-vis spectra of MoTe2, MoSe2, WSe2, WS2, RuS2 and RuSe2 in aqueous condition.

# Supplementary Figure 12. The excitation-dependent PL behaviors of the MoS2-DH, MoS2-DM and MoS2-DL QDs.

|  | Atomic ratio of Mo/S by XPS |
| --- | --- |
| MoS2-DH | 1: 1.8 |
| MoS2-DM | 1: 2.29 |
| MoS2-DL | 1: 2.34 |

# Supplementary Figure 13. Elemental analyses of the MoS2-DH, MoS2-DM and MoS2-DL QDs.

# Supplementary Figure 14. Absorption spectra of three kinds of MoS2 QDs in the presence of ABDA without light irradiation: (a) MoS2-DH, (b) MoS2-DM and (c) MoS2-DL

# Supplementary Figure 15. 1H-NMR (a) and HPLC (b) spectrums of ABDA before and after irradiation for 8 mins.

Supplementary Figure 16. 1H-NMR spectrum of the product of ABDA with and without light irradiation: (a) Incubated with Rose Bengal (RB) without irradiation, (b) Incubated with RB with irradiation, (c) Incubated with MoS2 QDs without irradiation and (d) Incubated with MoS2 QDs with irradiation. For the MoS2 QDs incubation group, the MoS2 QDs were removed by using centrifugal filters (MWCO 10K) before 1H-NMR testing.

Supplementary Figure 17. Absorption spectrum of the mixture solution of MoS2-DL QDs and ABDA in dH2O (black curve) and D2O (blue curve) before and after 8 min of light exposure.

# Supplementary Figure 18. ESR spectrum of MoS2 QDs in the presence of TEMP.

Supplementary Figure 19. Decomposition rate of the photosensitizing process of MoS2-DH (a), MoS2-DM (b) and MoS2-DL (c) samples, where A0 is the absorbance of initial absorbance of ABDA and A is the absorbance of ABDA under light irradiation at different time points.

Supplementary Figure 20. (a) The quantification curve for BSA using the Bicinchoninic acid (BCA) reagent (37 oC/30 min incubation);（b）There is insignificant difference between the BSA amounts on three MoS2 QDs defect types.

# Supplementary Figure 21. Tauc plot h = A(h-Eg)1/2. Here  is the absorption coefficient, h is the Plank constant,  is the photon frequency.

Supplementary Figure 22. 3D tumor spheroids were used to check the in vitro toxicity of defective MoS2 QDs without light irradiation. Mean ± SD, n=10, Scale bar: 100 m.