Supplementary Information

Deactivation of redox mediators in lithium-oxygen batteries by singlet oxygen

Kwak et al

Supplementary Figures

Supplementary Figure 1. Stability characterizations. Stability of DMPZ (a) and TTF (b) in contact with Li2O2. 60 µM DMPZ or 60 µM TTF solutions, respectively, in 0.1 M LiTFSI/TEGDME were stirred for 24 h with ~1 mg Li2O2. Spectra were taken before and after contact with Li2O2 and are offset for better visibility.

Supplementary Figure 2. Stability of DMPZ and TTF in contact with O2, KO2 and Li2O2. 1H-NMR spectra (in DMSO-d6) were recorded before and after 24 h of contact with the compounds. 1 mg DMPZ or TTF in DME were stirred under O2 headspace, or stirred with ~1 mg KO2 or Li2O2. The DMSO peak is taken as internal reference for quantitative comparison of spectra. The * denotes a residue from DME evaporation, which amounts to a content of ~1 ppm in the DME.

Supplementary Figure 3. Stability of DMPZ and TTF in contact with 1O2. 1H-NMR spectra (in DMSO-d6) were recorded before and after photooxygenation. 1 mg DMPZ or TTF in DME was stirred under an O2 headspace. For photochemical 1O2 generation, 1 µM of the photosensitizer palladium(II) meso-tetra(4-fluorophenyl)-tetrabenzoporphyrin (Pd4F) was dissolved in the solution and illuminated with 643 nm radiation. The DMSO peak is taken as internal reference for quantitative comparison of spectra. The * denotes a residue from DME evaporation, which amounts to a content of ~1 ppm in the DME.

Supplementary Figure 4. Decomposition of TTF to 1,3-dithiol-2-one according to the mechanism proposed in the literature1.

Supplementary Figure 5. Integrals of the 1H-NMR spectra in Supplementary Fig 3a.

Supplementary Figure 6. Charge curves for the oxidation of the RMs to RM+. 50 μL electrolyte (0.02 M RM (DMPZ or TTF) and 0.1 M LiTFSI in TEGDME) were charged at 100 µA in a Swagelok-type cell using a Li1−xFePO4 counter electrode and a carbon paper working electrode with a diameter of 10 mm.

Supplementary Figure 7. The cell design used for electrochemically oxidizing the RM to RM+. The central piece is a union tee tube fitting from the company Swagelok (https://www.swagelok.com/en/catalog/Product/Detail?part=PFA-820-3) made from perfluoroalkoxy polymer (PFA). The plungers for counter, working and reference electrodes are made from stainless steel (grade SAE 316L).

Supplementary Reference

1. Zhang, X., Lin, F. & Foote, C. S. J. Org. Chem. 60, 1333 (1995)