Supplementary Information

Designing light-element materials with large effective spin-orbit coupling

Jiayu Li1, Qiushi Yao1, Lin Wu2, Zongxiang Hu1, Boya Gao1, Xiangang Wan2,* and Qihang Liu1,3,4,*

1Shenzhen Institute for Quantum Science and Engineering (SIQSE) and Department of Physics, Southern University of Science and Technology, Shenzhen 518055, China

2National Laboratory of Solid State Microstructures and School of Physics, Nanjing University, Nanjing 210093, China and Collaborative Innovation Center of Advanced Microstructures, Nanjing University, Nanjing 210093, China

3Shenzhen Key Laboratory of Advanced Quantum Functional Materials and Devices, Southern University of Science and Technology, Shenzhen 518055, China

4Guangdong Provincial Key Laboratory for Computational Science and Material Design, Southern University of Science and Technology, Shenzhen 518055, China

J. L., Q. Y., and L. W. contributed equally to this work.

*Emails: xgwan@nju.edu.cn; liuqh@sustech.edu.cn

Contents

Supplementary Note 1. Mean-field approach on the interplay between correlation and spin-orbit coupling	3

Supplementary Note 2. Space groups and layer groups that permit enhanced spin-orbit coupling effect and the corresponding Wyckoff Positions	5

Supplementary Note 3. Collection of light-element transition-metal materials with potentially large SOC effect in C2DB database	13

Supplementary Note 4. Results of monolayer hexagonal Fe2X2 (X = S, Se)	17

Supplementary Note 5. Spin-orbit gap enhanced by general correlation	21

Supplementary Note 6. Exchange coupling and magnetocrystalline anisotropy energy	25

# Supplementary Note 1. Mean-field approach on the interplay between correlation and spin-orbit coupling

## I. Orbital doublet case

In a lattice system, d orbital doublets permitted by the crystal field are E1=dxz,dyz, E2=dxy,dx2-y2, and E3=dz2,dx2-y2. The spin-orbit coupling (SOC) Hamiltonian reads

HSOC=mm'=1,⋯,M,σσ'λm,σL⋅Sm',σ'Cmσ†Cm'σ',                     (1)

where L and S are the angular momentum and spin operators; Cmσ† and Cmσ are the creation and annihilation operators on electron state at with orbital m, and spin σ, and λ denotes the strength of the SOC effect. As we concentrate on the 3d systems with strong exchange interaction, we can only consider the spin-preserved term L⋅S≈LzSz. Taking the doublet E1 as an example, we expand the SOC Hamiltonian matrix under the basis of |2,1,↑,|2,-1,↑,|2,1,↓,|2,-1,↓ as

HSOC=λℏ221-1-11,                                       (2)

with |2,±1,↑/↓=-|dxz,↑/↓±i|dyz,↑/↓/2. Hence, the SOC Hamiltonian Eq. (S1) can now be expressed via new creation and annihilation operators as HSOC=λℏ22n1,↑-n-1,↑-n1,↓+n-1,↓ with nmσ=Cmσ†Cmσ the occupation operator. Since in the strong spin splitting condition, electron states near the Fermi level are dominated by single spin channel, where the effective Hamiltonian near the Fermi level is fully spin-polarized. In the following, we neglect the spin-down states and omitted the spin index in both the electron states and the creation/annihilation operators, i.e., HSOC=λℏ22n1-n-1.

Notice that the matrix representation of the projected orbital momentum is also diagonal in the basis of |2,±1, we express the SOC Hamiltonian in terms of orbital momentum operator as

HSOC=λℏ2Lz,                                                           (3)

where Lz=m=±lzmLzmnm is the operator of the angular momentum. We should remind that the connection between angular momentum and SOC term is invalid for the doublet E3=dz2,dx2-y2 as |dz2=|2,0 and dz2,σL⋅Sdx2-y2,σ'=0. The energy splitting of the degenerated orbitals E1 due to the SOC effect is

ΔE0=λℏ2.                                                              (4)

The magnitude of the splitting energy reveals the strength of the SOC effect.

Now we introduce the electron-electron correlation effect. As the case in 3d systems with significant exchange interaction but weak SOC, the effective on-site correlation effect is captured by the Coulomb repulsion between states with parallel spin as Hc=Ueffn1n-1, where Ueff=U-3J with U and J are the Hubbard and Hund parameters, respectively. In addition to the angular momentum operator Lz=ℏn1-n-1 as defined before, we also define the total occupation operator of the doublet as n=n1+n-1. Hence, the correlation Hamiltonian is rewritten into

Hc=Ueff4n2-Lz2ℏ2.                                                  (5)

Under the Hartree-Fock approximation, we address A2=A+δA2≈2AA-A2 with the term δA2 neglected, where A denotes the expected value of A. The correlation Hamiltonian becomes

Hc≈UeffLz2ℏ2Lz+ξn,Lz,                                            (6)

where we defined the energy shift

ξn,Lz=12nn-n2+Lz22ℏ2.                                        (7)

Recalling that the SOC Hamiltonian takes the form of HSOC=λℏLz/2 in Eq. (3), we find that the joint effect of SOC and correlation leads to an effective Hamiltonian of

Hc+HSOC≈λeffℏ2Lz+Ueffξn,Lz,                                 (8)

which produces a modified SOC effect with an effective SOC parameter

λeff=λ+UeffLzℏ3.                                                   (9)

Hence, the energy splitting induced by the SOC effect is now enhanced as

ΔEeff=ΔE0+UeffLzℏ,                                             (10)

where ΔE0 is the unmodified splitting energy Eq. (4). As the splitting energy reveals the strength of the SOC effect, we find that the correlation effect considered in Eq. (5) can dramatically enlarge the SOC effect. Lz is also a function of λeff or Ueff, and depends on the inter-site hopping term. As the intrinsic SOC is relatively small, Lz can be expressed as a linear function of λ: Lz=χλ, where χ is the susceptibility depending on lattice and hopping term. Given a small intrinsic λ and Lz=χλ, Eq. (9) outputs a modified λ' through Eq. (9) and a corresponding Lz'=χλ'. The self-consistent condition is reached once the input and output are identical, i.e., λeff=λ+Ueffχλeffℏ3. Hence the self-consistent solution of the effective SOC gap ΔEeff=λeffℏ2 solves

ΔEeffΔE0≈1-U-3Jχℏ3-1.                                      (11)

For the orbital doublet E2, the derivation and results are similar.

## II. Orbital triplet case

In a periodic crystal, there is only one d orbital triplet allowed by the local crystal field as T=dxy,dyz,dxz. The SOC matrix in the basis |1,|-1,|0 reads

HSOC=λℏ221-10,                                        (12)

where |±1≡|dxz,↑±i|dyz,↑/2 and |0≡|dxy,↑. Under the same manner, we find that the SOC Hamiltonian recovers the form as in Eq (3) as the state |0 has no projected angular momentum. The difference is revealed in the correlation term as Hc=Ueffn1n0+n-1n0+n1n-1. With the definitions of the total occupation operator n, we rewrite Hc as

Hc=Ueff4n2-Lz2ℏ2+Ueff2 n-32n0.                           (13)

Notice that the first term above is same as Eq. (5), which leads to the same mean-field result of Eq. (6). For the second term containing n and n0, it can be absorbed into the energy shifting term ξn,Lz,n0 due to its independence on Lz.

Comparing orbital doublet in Eq. (5) and triplet in Eq. (13), we note the term -Lz2 is essential for the correlation-enhanced SOC effect as it provides an energy cost on state of electrons with opposite angular momenta. Then the splitting between single-particle energies of different orbital angular momenta is enlarged. Therefore, the effective SOC is also enhanced in orbital triplet case.

# Supplementary Note 2. Space groups and layer groups that permit enhanced spin-orbit coupling effect and the corresponding Wyckoff Positions

For a single ion, the quantum states of the spin-polarized d-shell electrons are five-fold degenerated due to the spherical symmetry. Exposed to a lattice environment, however, this high degeneracy is no longer preserved as the symmetry broken down from continuous to discrete. According to the group theory, the high-dimensional irreducible representation (irrep) corresponds to the degenerated states. The five-dimensional irrep Ad of the 3D rotation group SO(3) needs to be decomposed into direct sum of the irreps of the site-symmetry groups of Wyckoff positions in space groups. Considering the orbital multiplets permitted in 32 point groups, we simply find that there are four decompositions corresponding to four classes: I. tetragonal Ad=A1⊕B1⊕B2⊕E; II. triagonal Ad=A1⊕2E; III. hexagonal Ad=A1⊕E1⊕E2, and IV. cubic Ad=E⊕T, with Ai,Bi the 1D irreps, Ei the 2D irreps, and T the 3D irreps. Point groups with one of the four decompositions are listed in Supplementary Table 1.

After analyzing all the space groups, we observe 125 space groups out of 230, inside which the site-symmetry groups of the Wyckoff positions are those listed in Table S1. We present those 125 space groups along with the Wyckoff positions and the corresponding site-symmetry groups in Supplementary Table 2. One can directly predict that a material with 3d elements may have a greatly enhanced SOC effect only if the Wyckoff positions of the 3d atoms are given in Supplementary Table 2.

As the study of 2D materials are of great interest recently, we reproduce the above analysis on 80 layer groups analogously, where we extract 32 layer groups out of 80. In Supplementary Table 3, we deliver those 32 layer groups with the Wyckoff positions and the corresponding site-symmetry groups. In a same manner, one can predict that a 2D materials with 3d elements could possess an enhanced SOC effect once the Wyckoff positions of the 3d elements are listed in Supplementary Table 3.

Supplementary Table 1. 24 Single point groups with orbital multiplet for d orbits.

| Class | Decomposition (Basis) | Point groups |
| --- | --- | --- |
| Tetragonal | Ad=A1⊕B1⊕B2⊕E A1:d3z2-r2,B1:dx2-y2 B2:dxy,E:dxz,dyz | C4(4), S4(-4), C4h(4/m), D4(422), C4v(4mm), D2d(-42m), D4h(4/mmm) |
| Triagonal | Ad=A1⊕2E A1:d3z2-r2 E:dx2-y2,dxy;dxz,dyz | C3(3), S6(-3), D3(32), C3v(3m), D3d(-3m) |
| Hexagonal | Ad=A1⊕E1⊕E2 A1:d3z2-r2 E1:dx2-y2,dxy,E2:dxz,dyz | C6(6), C3h(-6), C6h(6/m), D6(622), C6v(6mm), D3h(-62m), D6h(6/mmm) |
| Cubic | Ad=E⊕T E:dx2-y2,d3z2-r2 T:dxz,dyz,dxy | T(23), Th(m-3), O(432), Td(-43m), Oh(m-3m) |

Supplementary Table 2. All the 125 space groups in which the site-symmetry groups of Wyckoff positions permit orbital multiplets. (SG: Space Group)

| Space group | Wyckoff position | Site-symmetry group | Space group | Wyckoff position | Site-symmetry group |
| --- | --- | --- | --- | --- | --- |
| P4 (SG75) | 1a,1b | 4 | P-62m (SG189) | 4h | 3 |
| I4 (SG79) | 2a | 4 |  | 2e | 3m |
| P-4 (SG81) | 1a,1b,1c,1d | -4 |  | 2c,2d | -6 |
| I-4 (SG82) | 2a,2b,2c,2d | -4 |  | 1a,1b | -62m |
| P4/m (SG83) | 2g,2h | 4 | P-62c (SG190) | 4e,4f | 3 |
|  | 1a,1b,1c,1d | 4/m |  | 2b,2c,2d | -6 |
| P42/m (SG84) | 2e,2f | -4 |  | 2a | 32 |
| P4/n (SG85) | 2c | 4 | P6/mmm (SG191) | 4h | 3m |
|  | 2a,2b | -4 |  | 2e | 6mm |
| P42/n (SG86) | 2a,2b | -4 |  | 2c,2d | -62m |
| I4/m (SG87) | 4e | 4 |  | 1a,1b | 6/mmm |
|  | 4d | -4 | P6/mcc (SG192) | 8h | 3 |
|  | 2a,2b | 4/m |  | 4e | 6 |
| I41/a (SG88) | 4a,4b | -4 |  | 4d | -6 |
| P422 (SG89) | 2g2h | 4 |  | 4c | 32 |
|  | 1a,1b,1c,1d | 422 |  | 2b | 6/m |
| P4212 (SG90) | 2c | 4 |  | 2a | 622 |
| I422 (SG97) | 4e | 4 | P63/mcm (SG193) | 8h | 3 |
|  | 2a,2b | 422 |  | 4e | 3m |
| P4mm (SG99) | 1a,1b | 4mm |  | 4d | 32 |
| P4bm (SG100) | 2a | 4 |  | 4c | -6 |
| P4cc (SG103) | 2a,2b | 4 |  | 2b | -3m |
| P4nc (SG104) | 2a | 4 |  | 2a | -62m |
| I4mm (SG107) | 2a | 4mm | P63/mmc (SG194) | 4e,4f | 3m |
| I4cm (SG108) | 4a | 4 |  | 2b,2c,2d | -62m |
| P-42m (SG111) | 1a,1b,1c,1d | -42m |  | 2a | -3m |
| P-42c (SG112) | 2e,2f | -4 | P23 (SG195) | 4e | 3 |
| P-421m (SG113) | 2a,2b | -4 |  | 1a,1b | 23 |
| P-421c (SG114) | 2a,2b | -4 | F23 (SG196) | 16e | 3 |
| P-4m2 (SG115) | 1a,1b,1c,1d | -42m |  | 4a,4b,4c,4d | 23 |
| P-4c2 (SG116) | 2c,2d | -4 | I23 (SG197) | 8c | 3 |
| P-4b2 (SG117) | 2a,2b | -4 |  | 2a | 23 |
| P-4n2 (SG118) | 2a,2b | -4 | P213 (SG198) | 4a | 3 |
| I-4m2 (SG119) | 2a,2b,2c,2d | -42m | I213 (SG199) | 8a | 3 |
| I-4c2 (SG120) | 2b,2c | -4 | Pm-3 (SG200) | 8i | 3 |
| I-42m (SG121) | 4d | -4 |  | 1a,1b | m-3 |
|  | 2a,2b | -42m | Pn-3 (SG201) | 8e | 3 |
| I-42d (SG122) | 4a,4b | -4 |  | 4b,4c | -3 |
| P4/mmm (SG123) | 2g,2h | 4mm |  | 2a | 23 |
|  | 1a,1b,1c,1d | 4/mmm | Fm-3 (SG202) | 32f | 3 |
| P4/mcc (SG124) | 4g,4h | 4 |  | 8c | 23 |
|  | 2b,2d | 4/m |  | 4a,4b | m-3 |
|  | 2a,2c | 422 | Fd-3 (SG203) | 32e | 3 |
| P4/nbm (SG125) | 4g | 4 |  | 16c,16d | -3 |
|  | 2c,2d | -42m |  | 8a,8b | 23 |
|  | 2a,2b | 422 | Im-3 (SG204) | 16f | 3 |
| P4/nnc (SG126) | 4e | 4 |  | 8c | -3 |
|  | 4d | -4 |  | 2a | m-3 |
|  | 2a,2b | 422 | Pa-3 (SG205) | 8c | 3 |
| P4/mbm (SG127) | 4e | 4 |  | 4a,4b | -3 |
|  | 2a,2b | 4/m | Ia-3 (SG206) | 16c | 3 |
| P4/mnc (SG128) | 4e | 4 |  | 8a,8b | -3 |
|  | 2a,2b | 4/m | P432 (SG207) | 8g | 3 |
| P4/nmm (SG129) | 2c | 4mm |  | 6e,6f | 4 |
|  | 2a,2b | -42m |  | 3c,3d | 422 |
| P4/ncc (SG130) | 4c | 4 |  | 1a,1b | 432 |
|  | 4b | -4 | P4232 (SG208) | 8g | 3 |
| P42/mmc (SG131) | 2e,2f | -42m |  | 4b,4c | 32 |
| P42/mcm (SG132) | 2b,2d | -42m |  | 2a | 23 |
| P42/nbc (SG133) | 4d | -4 | F432 (SG209) | 32f | 3 |
| P42/nnm (SG134) | 2a,2b | -42m |  | 24e | 4 |
| P42/mbc (SG135) | 4b | -4 |  | 8c | 23 |
| P42/mnm (SG136) | 4d | -4 |  | 4a,4b | 432 |
| P42/nmc (SG137) | 2a,2b | -42m | F4132 (SG210) | e | 3 |
| P42/ncm (SG138) | 4b | -4 |  | 16c,16e | 32 |
| I4/mmm (SG139) | 4e | 4mm |  | 8a,8b | 23 |
|  | 4d | -42m | I432 (SG211) | 16f | 3 |
|  | 2a,2b | 4/mmm |  | 12e | 4 |
| I4/mcm (SG140) | 8f | 4 |  | 8c | 32 |
|  | 4c | 4/m |  | 6b | 422 |
|  | 4b | -42m |  | 2a | 432 |
|  | 4a | 422 | P4332 (SG212) | 8c | 3 |
| I41/amd (SG141) | 4a,4b | -42m |  | 4a,4b | 32 |
| I41/acd (SG142) | 8a | -4 | P4132 (SG213) | 8c | 3 |
| P3 (SG143) | 1a,1b,1c | 3 |  | 4a,4b | 32 |
| R3 (SG146) | 3a | 3 | I4132 (SG214) | 16e | 3 |
| P-3 (SG147) | 2c,2d | 3 |  | 8a,8b | 32 |
|  | 1a,1b | -3 | P-43m (SG215) | 4e | 3m |
| R-3 (SG148) | 6c | 3 |  | 3c,3d | -42m |
|  | 3a,3b | -3 |  | 1a,1b | -43m |
| P312 (SG149) | 2g,2h,2i | 3 | F-43m (SG216) | 16e | 3m |
|  | 1a,1b,1c,1d, 1e,1f | 32 |  | 4a,4b,4c,4d | -43m |
| P321 (SG150) | 2c,2d | 3 | I-43m (SG217) | 12d | -4 |
|  | 1a,1b | 32 |  | 8c | 3m |
| R32 (SG155) | 6c | 3 |  | 6b | -42m |
|  | 3a,3b | 32 |  | 2a | -43m |
| P3m1 (SG156) | 1a,1b,1c | 3m | P-43n (SG218) | 8e | 3 |
| P31m (SG157) | 2b | 3 |  | 6c,6d | -4 |
|  | 1a | 3m |  | 2a | 23 |
| P3c1 (SG158) | 2a,2b,2c | 3 | F-43c (SG219) | 32e | 3 |
| P31c (SG159) | 2a,2b | 3 |  | 24c,24d | -4 |
| R3m (SG160) | 3a | 3m |  | 8a,8b | 23 |
| R3c (SG161) | 6a | 3 | I-43d (SG220) | 16c | 3 |
| P-31m (SG162) | 4h | 3 |  | 12a,12b | -4 |
|  | 2e | 3m | Pm-3m (SG221) | 8g | 3m |
|  | 2c,2d | 32 |  | 6e,6f | 4mm |
|  | 1a,1b | -3m |  | 3c,3d | 4/mmm |
| P-31c (SG163) | 4e,4f | 3 |  | 1a,1b | m-3m |
|  | 2a,2c,2d | 32 | Pn-3n (SG222) | 16f | 3 |
|  | 2b | -3 |  | 12e | 4 |
| P-3m1 (SG164) | 2c,2d | 3m |  | 12d | -4 |
|  | 1a,1b | -3m |  | 8c | -3 |
| P-3c1 (SG165) | 4c,4d | 3 |  | 6b | 422 |
|  | 2b | -3 |  | 2a | 432 |
|  | 2a | 32 | Pm-3n (SG223) | 16i | 3 |
| R-3m (SG166) | 6c | 3m |  | 8e | 32 |
|  | 3a,3b | -3m |  | 6c,6d | -42m |
| R-3c (SG167) | 12c | 3 |  | 2a | m-3 |
|  | 6b | -3 | Pn-3m (SG224) | 8e | 3m |
|  | 6a | 32 |  | 6d | -42m |
| P6 (SG168) | 2b | 3 |  | 4b,4c | -3m |
|  | 1a | 6 |  | 2a | -43m |
| P63 (SG173) | 2a,2b | 3 | Fm-3m (SG225) | 32f | 3m |
| P-6 (SG174) | 2g,2h,2i | 3 |  | 24e | 4mm |
|  | 1a,1b,1c,1d, 1e,1f | -6 |  | 8c | -43m |
| P6/m (SG175) | 4h | 3 |  | 4a,4b | m-3m |
|  | 2e | 6 | Fm-3c (SG226) | 643 | 3 |
|  | 2c,2d | -6 |  | 48f | 4 |
|  | 1a,1b | 6/m |  | 24d | 4/m |
| P63/m (SG176) | 4e,4f | 3 |  | 24c | -42m |
|  | 2a,2c,2d | -6 |  | 8b | m-3 |
|  | 2b | -3 |  | 8a | 432 |
| P622 (SG177) | 4h | 3 | Fd-3m (SG227) | 32e | 3m |
|  | 2e | 6 |  | 16c,16d | -3m |
|  | 2c,2d | 32 |  | 8a,8b | -43m |
|  | 1a,1b | 622 | Fd-3c (SG228) | 64e | 3 |
| P6322 (SG182) | 4e,4f | 3 |  | 48d | -4 |
|  | 2a,2b,2c,2d | 32 |  | 32c | -3 |
| P6mm (SG183) | 2b | 3m |  | 32b | 32 |
|  | 1a | 6mm |  | 2a | 23 |
| P6cc (SG184) | 4b | 3 | Im-3m (SG229) | 16f | 3m |
|  | 2a | 6 |  | 12e | 4mm |
| P63cm (SG185) | 4b | 3 |  | 12d | -42m |
|  | 2a | 3m |  | 8c | -3m |
| P63mc (SG186) | 2a,2b | 3m |  | 6b | 4/mmm |
| P-6m2 (SG187) | 2g,2h,2i | 3m |  | 2a | m-3m |
|  | 1a,1b,1c,1d, 1e,1f | -62m | Ia-3d (SG230) | 32e | 3 |
| P-6c2 (SG188) | 4g,4h,4i | 3 |  | 24d | -4 |
|  | 2b,2d,2f | -6 |  | 16b | 32 |
|  | 2a,2c,2e | 32 |  | 16a | -3 |

Supplementary Table 3. All the 32 layer groups in which the site-symmetry groups of Wyckoff positions permit orbital multiplets. (LG: Layer Group)

| Layer group | Wyckoff position | Site-symmetry group | Layer group | Wyckoff position | Site-symmetry group |
| --- | --- | --- | --- | --- | --- |
| p4 (LG49) | 1a,1b | 4 | p31m (LG70) | 2b | 3 |
| p-4 (LG50) | 1a,1b | -4 |  | 1a | 3m |
| p4/m (LG51) | 1a,1b | 4/m | p-31m (LG71) | 4e | 3 |
| p4/n (LG52) | 2b | 4 |  | 2c | 3m |
|  | 2a | -4 |  | 2b | 32 |
| p422 (LG53) | 2d,2e | 4 |  | 1a | -3m |
|  | 1a,1b | 422 | p-3m1 (LG72) | 2b,2c | 3m |
| p4212 (LG54) | 2b | 4 |  | 1a | -3m |
| p4mm (LG55) | 1a,1b | 4mm | p6 (LG73) | 2b | 3 |
| p4bm (LG56) | 2a | 4 |  | 1a | 6 |
| p-42m (LG57) | 1a,1b | -42m | p-6 (LG74) | 2d,2e,2f | 3 |
| p-421m (LG58) | 2a | -4 |  | 1a,1b,1c | -6 |
| p-4m2 (LG59) | 1a,1b | -42m | p6/m (LG75) | 4e | 3 |
| p-4b2 (LG60) | 2a | -4 |  | 2c | 6 |
| p4/mmm (LG61) | 2d,2e | 4mm |  | 2b | -6 |
|  | 1a,1b | 4/mmm |  | 1a | 6/m |
| p4/nbm (LG62) | 4d | 4 | p622 (LG76) | 4e | 3 |
|  | 2b | -42m |  | 2c | 6 |
|  | 2a | 422 |  | 2b | 32 |
| p4/mbm (LG63) | 4c | 4 |  | 1a | 622 |
|  | 2a | 4/m | p6mm (LG77) | 2b | 3m |
| p4/nmm (LG64) | 2b | 4mm |  | 1a | 6mm |
|  | 2a | -42m | p-6m2 (LG78) | 2d,2e,2f | 3m |
| p3 (LG65) | 1a,1b,1c | 3 |  | 1a,1b,1c | -6m2 |
| p-3 (LG66) | 2b,2c | 3 | p-62m (LG79) | 4e | 3 |
|  | 1a | -3 |  | 2c | 3m |
| p312 (LG67) | 2d,2e,2f | 3 |  | 2b | -6 |
|  | 1a,1b,1c | 32 |  | 1a | -62m |
| p321 (LG68) | 2b,2c | 3 | p6mmm (LG80) | 4e | 3m |
|  | 1a | 32 |  | 2c | 6mm |
| p3m1 (LG69) | 1a,1b,1c | 3m |  | 2b | -6m2 |
|  |  |  |  | 1a | 6/mmm |

# Supplementary Note 3. Collection of light-element transition-metal materials with potentially large SOC effect in C2DB database

As the Computational 2D materials database (C2DB)1, 2 contains a wealth of computed properties for plenty of 2D materials with over 300 citations, we apply the C2DB as our material pool, in which organizes more than 1600 2D materials. First, we select 859 2D materials containing 3d/4d transition metal atoms inside the element set Sc~Ni for 3d and Y~Rh. Among them, we concentrate on 560 materials, of which the layer groups belong to the ones mentioned in Supplementary Table 3, and so do the Wyckoff positions of the transition metal elements. Then we further perform the routine SOC-free DFT calculation without considering the correlation effect (set U=0) on 542 materials to check out the energy band near the Fermi energy. In this step, a candidate is picked once the orbital-doublet bands of the transition metal elements are partially occupied, where the degenerated states at certain momentum are located within 1 eV around the Fermi energy. Finally, we pin down 71 candidates to most potentially generate the correlation-enhanced SOC effect while further considering the correlation effect with finite U, where the full list is presented in Supplementary Table 4 and their structures are provided at [https://github.com/jylicmp/Structures].

After obtaining the candidates, we perform elaborate DFT calculation on them with the consideration of the SOC and correlation effect. The results of the SOC gap among the candidates show good consistency with our theorical prediction, in which the SOC gap is typically valued at hundreds of meV, i.e., an order larger than the general strength of the on-site SOC effect in 3d series. We will present the detail results in Supplementary Note 4 via two representative compounds Fe2S2 and Fe2Se2. With the SOC gap opened, the band topology of the occupied states can be directly determined by checking the Chern number or the chiral edge modes. Within the construction of the tight-binding model in Wannier-representation, we obtain 9 quantum anomalous Hall (QAH) insulators among 71 candidates with finite Chern numbers, which are denoted as “QAH” in Supplementary Table 4. As the SOC gap is enhanced by the correlation effect, the nontrivial gaps of the QAH insulators are naturally enlarged to resist the thermal fluctuation. As a simple application of our theory, it is an efficient way to design large amounts of high-temperature QAH insulators instead of case-by-case study.

Supplementary Table 4. 71 2D candidate materials that can produce the correlation-enhanced SOC effect screened from the Computational 2D materials database1, 2. In the table, LG denotes layer group and TME@WPs denotes the Wyckoff positions that the transition metal elements locate at. Tags “QAH” in the “Notes” column label the materials as the candidates of high-temperature QAH insulators.

| Compounds | LG | TME@WPs | Notes |
| --- | --- | --- | --- |
| CrS2_id1451 | p-4m2 (LG59) | Cr@1a |  |
| CrSe2_id443 | p-4m2 (LG59) | Cr@1a |  |
| FeCl2_id1463 | p-4m2 (LG59) | Fe@1a |  |
| FeBr2_id453 | p-4m2 (LG59) | Fe@1a |  |
| AlNi5Cl2_id727 | p4/mmm (LG61) | Ni@1a |  |
| AlNi5Br2_id1736 | p4/mmm (LG61) | Ni@1a |  |
| GaNi5Cl2_id1739 | p4/mmm (LG61) | Ni@1a |  |
| GaNi5Br2_id2751 | p4/mmm (LG61) | Ni@1a |  |
| InNi5Cl2_id2754 | p4/mmm (LG61) | Ni@1a |  |
| InNi5Br2_id3770 | p4/mmm (LG61) | Ni@1a |  |
| Ni2O2_id3361 | p4/mmm (LG61) | Ni@1a |  |
| Cr2S4_id441 | p4/mbm (LG63) | Cr@2a |  |
| Li2Mn2P2_id2976 | p4/nmm (LG64) | Mn@2a |  |
| Mn2Se2_id3049 | p4/nmm (LG64) | Mn@2a |  |
| Fe2Br2_id2236 | p4/nmm (LG64) | Fe@2a |  |
| Fe2Te2_id2298 | p4/nmm (LG64) | Fe@2a |  |
| Co2Li2Sb2_id2940 | p4/nmm (LG64) | Co@2a |  |
| Co2Na2Sb2_id917 | p4/nmm (LG64) | Co@2a |  |
| Co2S2_id1260 | p4/nmm (LG64) | Co@2a |  |
| KTiS2_id3097 | p3m1 (LG69) | Ti@1c |  |
| Ti2P2S6_id4036 | p-31m (LG71) | Ti@2b |  |
| V2Cl6_id3830 | p-31m (LG71) | V@2b | QAH |
| V2Br6_id2813 | p-31m (LG71) | V@2b | QAH |
| V2I6_id1801 | p-31m (LG71) | V@2b | QAH |
| Mn2Cl6_id1769 | p-31m (LG71) | Mn@2b | QAH |
| Fe2Cl6_id750 | p-31m (LG71) | Fe@2b | QAH |
| Fe2I6_id1760 | p-31m (LG71) | Fe@2b | QAH |
| Ru2Br6_id1788 | p-31m (LG71) | Ru@2b |  |
| Ru2I6_id2802 | p-31m (LG71) | Ru@2b | QAH |
| Sc2Cl2_id244 | p-3m1 (LG72) | Sc@2c |  |
| Sc2Br2_id223 | p-3m1 (LG72) | Sc@2c |  |
| Sc4N3_id2211 | p-3m1 (LG72) | Sc@2b, Sc@2c |  |
| Ti2N_id2541 | p-3m1 (LG72) | Ti@2c |  |
| Ti2Te2_id2408 | p-3m1 (LG72) | Ti@2c |  |
| Ti4C3_id186 | p-3m1 (LG72) | Ti@2b, Ti@2c |  |
| Cr2CS2_id2696 | p-3m1 (LG72) | Cr@2c |  |
| Cr2F2N_id688 | p-3m1 (LG72) | Cr@2c |  |
| Cr2S2_id1265 | p-3m1 (LG72) | Cr@2c |  |
| Cr4C3O2_id1188 | p-3m1 (LG72) | Cr@2b, Cr@2c |  |
| Cr4F2N3_id2198 | p-3m1 (LG72) | Cr@2b, Cr@2c |  |
| Cr4N3_id1197 | p-3m1 (LG72) | Cr@2b, Cr@2c |  |
| Cr4N3O2_id1191 | p-3m1 (LG72) | Cr@2b, Cr@2c |  |
| CrGa2Se4_id1054 | p-3m1 (LG72) | Cr@1a |  |
| Mn2CF2_id674 | p-3m1 (LG72) | Mn@2c |  |
| Mn2F2N_id2711 | p-3m1 (LG72) | Mn@2c |  |
| Mn2NO2_id691 | p-3m1 (LG72) | Mn@2c |  |
| Mn4C3F2_id173 | p-3m1 (LG72) | Mn@2b, Mn@2c |  |
| Mn4C3O2_id3218 | p-3m1 (LG72) | Mn@2b, Mn@2c |  |
| Mn4N3_id3227 | p-3m1 (LG72) | Mn@2b, Mn@2c |  |
| Mn4N3O2_id3221 | p-3m1 (LG72) | Mn@2b, Mn@2c |  |
| Fe2S2_id3313 | p-3m1 (LG72) | Fe@2c | QAH |
| Fe2Se2_id3314 | p-3m1 (LG72) | Fe@2c | QAH |
| Fe2Te2_id3315 | p-3m1 (LG72) | Fe@2c |  |
| FeO2_id456 | p-3m1 (LG72) | Fe@1a |  |
| Rh2F2_id2289 | p-3m1 (LG72) | Rh@2c |  |
| RhI2_id575 | p-3m1 (LG72) | Rh@2c |  |
| Y2Cl2_id30 | p-3m1 (LG72) | Y@2c |  |
| Y2I2_id2051 | p-3m1 (LG72) | Y@2c |  |
| Zr4C3_id187 | p-3m1 (LG72) | Zr@2b, Zr@2c |  |
| Cr3C2F2_id2170 | p-6m2 (LG78) | Cr@1a, Cr@2f |  |
| Cr3C2O2_id2173 | p-6m2 (LG78) | Cr@1a, Cr@2f |  |
| Mn3C2F2_id148 | p-6m2 (LG78) | Mn@1a, Mn@2f |  |
| Mn3C2O2_id151 | p-6m2 (LG78) | Mn@1a, Mn@2f |  |
| FeCl2_id2476 | p-6m2 (LG78) | Fe@1a |  |
| FeBr2_id2475 | p-6m2 (LG78) | Fe@1a |  |
| FeI2_id3494 | p-6m2 (LG78) | Fe@1a |  |
| Zr3N2_id2194 | p-6m2 (LG78) | Zr@1a, Zr@2f |  |
| Ti2Cl6_id1797 | p-62m (LG79) | Ti@2d |  |
| Zr2Cl6_id2819 | p-62m (LG79) | Zr@2d |  |
| Zr2Br6_id1806 | p-62m (LG79) | Zr@2d |  |
| Zr2I6_id1807 | p-62m (LG79) | Zr@2d |  |

# Supplementary Note 4. Results of monolayer hexagonal Fe2X2 (X = S, Se)

## I. Results of monolayer Fe2S2

Supplementary figure 1. Band structure of Fe2S2. (a-d) Band structures of monolayer Fe2S2 without SOC calculated by the DFT+U method using different U values. (e-h) Band structures with SOC under different U values.

Supplementary figure 2. Magnetic configurations and magnetocrystalline anisotropy energy. (a-b) Monolayer Fe2S2 with (a) ferromagnetic (FM) and (b) antiferromagnetic (AFM) configurations. (c) Calculated magnetocrystalline anisotropy energy by the DFT+U method using different U values. FM state with magnetic moments parallel to c-axis is more stable than the AFM state by 227.5 meV/Fe2S2 (U = 3 eV).

Supplementary figure 3. Magnitude of the pure SOC gap. (a) Pure SOC gap calculated by DFT+U method with U = 3 eV by treating SOC as a perturbation. (b) Pure SOC gap calculated by DFT+U method with U = 0 eV.

Supplementary figure 4. Edge states and Berry curvature. (a-b) Topological edge states calculated along the (100) direction (a) with SOC and (b) with 1 V/Å external electric field. The external electric field is parallel to the c-axis. (b) only shows the spin down channel. (c-d) Distribution of Berry curvature calculated (c) with SOC and (d) with 1 V/Å external electric field contributed by occupied valence bands in the momentum space. The external electric field is parallel to the c-axis. The hexagon represents the first Brillouin zone.

Supplementary figure 5. SOC increment as a function of the effective parameter Ueff=U-3J. The red curve is obtained by the four-band tight-binding model of Fe2S2 with interaction between parallel spin states considered only, while the other three curves are obtained by GGA+U calculations with different U and J. Consistent tendency is shown from all results. As expected, the simplified correlation term is more accurate in a strong exchange case (large J), with a reasonable susceptibility χ/ℏ≈0.73 eV-1 fitted by Eq. (11) [Eq. (4) in main text] with J=1.0 eV.

## II. Results of monolayer Fe2Se2

Supplementary figure 6. Band structure of Fe2Se2. (a-d) Band structures of monolayer Fe2Se2 without SOC calculated by the DFT+U method using different U values. (e-h) Band structures with SOC under different U values.

Supplementary figure 7. Magnetocrystalline anisotropy energy, evolution of the nontrivial SOC gap, and topological edge states of Fe2Se2. (a) Calculated magnetocrystalline anisotropy energy (MAE) by the DFT+U method using different U values. The FM state is more stable than the AFM state by 195.0 meV/Fe2Se2 (U = 3 eV). (b) Evolution of the nontrivial SOC gap of monolayer Fe2Se2 with the variation of U in DFT+U calculation. The SOC gap reaches 798 meV with U = 3 eV, while the system is a semiconductor with indirect band gap of 18 meV as shown in Fig. S5 (h). (c) Topological edge states calculated along the (100) direction with SOC, indicating the nonzero Chern number C=1.

# Supplementary Note 5. Spin-orbit gap enhanced by general correlation

In previous derivation, we concentrate on the strong spin-splitting limit that only interaction between electrons with parallel spins is considered. Here we perform a more general derivation of the enhanced SOC effect by counting all on-site correlation terms in the spin-splitting case. The general correlation Hamiltonian of d orbitals is taken as the Kanamori Hamiltonian3:

HCK=12mσUnmσnmσ+12m≠m',σσ'U'-Jδσσ'nmσnm'σ'                (14)

-12m≠m'σJCmσ†CmσCm'σ†Cm'σ+12m≠m'σJCmσ†Cmσ†Cm'σCm'σ,

where U'=U-2J for d orbitals and σ=-σ denotes opposite spin. Four terms in Eq. (14) describe intra-orbital Coulomb repulsion, inter-orbital Coulomb repulsion and exchange attraction, spin flipping, and double hopping, sequentially. Here we take E1=dxz,dyz as example, the SOC Hamiltonian matrix written in bases |2,±1,↑/↓=-|dxz,↑/↓±i|dyz,↑/↓/2 was shown in Eq. (2):

HSOC=λℏ221-1-11.                                      (2)

In this base, the Kanamori Hamiltonian specifically reads

HCK=Un+1,↑n+1,↓+n-1,↑n-1,↓+U'n+1,↑n-1,↓+n+1,↓n-1,↑                (15)

+U'-Jn+1,↑n-1,↑+n+1,↓n-1,↓

-JC+1,↑†C+1,↓C-1,↓†C-1,↑+C+1,↓†C+1,↑C-1,↑†C-1,↓

+J2C+1,↑†C+1,↓†C-1,↓C-1,↑+C+1,↓†C+1,↑†C-1,↑C-1,↓

+J2C-1,↑†C-1,↓†C+1,↓C+1,↑+C-1,↓†C-1,↑†C+1,↑C+1,↓,

where the double hopping term is written explicitly in a Hermitian form. Following the mean-field approach, we define nmσ≡nmσ and Φmσ;m'σ'≡Cmσ†Cm'σ' as the expected values of the density and non-density term, respectively. Thus the mean-field level Kanamori Hamiltonian for doublet E1 is

HcK≈H↑TT†H↓,                                                     (16)

where the Hamiltonian is written in block matrix form under the base C=C+1,↑,C-1,↑,C+1,↓,C-1,↓T previously defined for SOC matrix Eq. (2), and the irrelevant constant term are omitted. Inside, H↑,↓ denote the block that interaction between parallel spin states:

Hσ=

Un+1,σ+U'n-1,σ+U'-Jn-1,σJReΦ+1,σ;-1,σJReΦ+1,σ;-1,σUn-1,σ+U'n+1,σ+U'-Jn+1,σ,(17)

and T contains spin flipping terms that connects each spin block:

T=-J2Φ-1,↓;-1,↑Φ+1,↓;-1,↑Φ-1,↓;+1,↑Φ+1,↓;+1,↑.                                    (18)

As the SOC matrix is diagonal, the combination HSOC+HcK only modifies the diagonal block Hσ into

Hσ=Hσ+-1σλℏ22τz,                                              (19)

with τz the Pauli matrix and -1↑,↓≡±1.

In a spin-splitting case, we concentrate on the spin-up channel. To obtain the effective Hamiltonian of the spin-up state, we introduce the Green’s function as Gε≡ε-HSOC-HcK-1. Using the Dyson’s equation, we obtain the effective Green’s function of the spin-up block as G↑-1ε=G↑,0-1ε-Σ↑ε where G↑,0ε=ε-H↑-1 is the bare Green’s function and Σ↑ε=Tε-H↓-1T† is the self-energy. The effective Hamiltonian of the spin-up channel, given by G↑ ε=ε-H↑eff-1, is then derived as

H↑eff=H↑+Tε-H↓-1T†.                                      (20)

## I. Without spin-flipping, T=0

First, we consider the limit that spin-flipping is absent, i.e., T=0. In this limit, the effective Hamiltonian of spin-up state is identical to H↑. Even so, the spin-down channel also matters the energy gap due to Coulomb repulsion (U,U'). To see it, we decompose H↑ of Eq. (17) into two parts since A00B=A+B2+A-B2τz. Therefore, we have

H↑=U+U'n↓+U'-Jn↑2                                                                      (21)

+2JLz,↓-U'-JLz,↑+λℏ32ℏJReΦ+1,↓;-1,↓JReΦ+1,↓;-1,↓-2JLz,↓-U'-JLz,↑+λℏ32ℏ,

where the conventions nσ=n+1,σ+n-1,σ and Lz,σ=n+1,σ+n-1,σ are used. Two energies are solved as E↑,±=2U-Jn↓+U-3Jn↑2±ΔE↑/2, with a gap ΔE↑=E↑,+-E↑,- as

ΔE↑=214ℏ22JLz,↓-U-3JLz,↑+λℏ32+J2ϕ02.                     (22)

where ϕo≡ReΦ+1,↓;-1,↓ denotes the orbital flipping effect. Expanding ΔE↑ up to the linear order of λ, we obtain the effective energy gap as

ΔE↑≈ΔE0+2JLz,↓+U-3JLz,↑ℏ,                               (23)

with Lz,↓ assumed as the linear function of λ, and ΔE0=λℏ2 used. Eq. (23) is the modified result of Eq. (10) [Eq. (3) in the main text] with further considering the first order effect of the opposite spin state. Namely, the orbital polarization of the opposite spin states increases the energy gap as Lz,↑ does. In the strong splitting limit that spin-down state is fully occupied or unoccupied, i.e., Lz,↓=0, Eq. (23) recovers the previous result Eq. (10).

II. With spin-flipping, T≠0

Before evaluating the effective Hamiltonian in Eq. (20), we assume that spin flipping terms between the same orbital are orbital-independent Φ±1,↓;±1,↑≡ϕs and dominates the spin-orbit flipping terms Φ±1,↓;∓1,↑≈0. The self-energy is then approximated as

Σ↑ε≈J2ϕs241ε-E↓,+ε-E↓,-                                                                               (24)

×ε-Un-1,↑-U'n+1,↑-U'-Jn+1,↓-λ-Jϕo-Jϕoε-Un+1,↑-U'n-1,↑-U'-Jn-1,↓,

where E↓,± is the energy level of the spin-down channel

E↓±=U+U'n↑+U'-Jn↓2                                                                (25)

±14ℏ22JLz,↑-U'-JLz,↓+λℏ32+J2ϕ02.

Therefore, the effective Hamiltonian of the spin-up state Eq. (20) is

H↑eff≈2JLz,↓-U'-JLz,↑+λℏ32ℏJϕoJϕo-2JLz,↓-U'-JLz,↑+λℏ32ℏ              (26)

+J2ϕs241ε-E↓,+ε-E↓,-2JLz,↑-U'-JLz,↓-λℏ32ℏ-Jϕo-Jϕo-2JLz,↑-U'-JLz,↓-λℏ32ℏ,

where the terms with identity matrix are omitted. Taking ε as the mean value of the spin-up channel, i.e., ε≈E↑++E↑-2=U+U'n↓+U'-Jn↑2, the energy-resolved factor becomes

ε-E↓,+ε-E↓,-=U+J2n↓-n↑4-ΔE↓2≈U+J2n↓-n↑4.   (27)

Hence, H↑eff now is

H↑eff=2JLz,↓+αLz,↑-U'-JLz,↑+αLz,↓+1-αλℏ32ℏτz           (28)

+1-αJϕoτx,

with α=J2U+J2ϕsn↓-n↑2. Therefore, we obtain a more general effective gap as

ΔE↑≈ΔEeff+2JℏLz,↓-ϕsn↓-n↑2ΓLz,↑,Lz,↓,                        (29)

where

ΓLz,↑,Lz,↓=J2U+J2λℏ2+2JLz,↑+U-3JLz,↓ℏ,              (30)

and ΔEeff is defined in Eq. (10) [Eq. (3) in main text]. Besides the previously obtained gap ΔEeff, the orbital polarization of the opposite spin channel Lz, σ and a spin-flipping-induced term ∝ϕs2=Cmσ†Cmσ2 appear, where nσ-nσ counts the exchange effect. With zero spin flipping, the energy gap is still enhanced even the opposite spin channel is considered. On the other hand, finite spin flipping ϕs≠0 will reduce the enhancement, as the flipping weakens the orbital polarization of each channel. Nevertheless, a relative strong exchange splitting nσ-nσ≫ϕs in 3d systems renders our theory and design principles approximately valid.

# Supplementary Note 6. Exchange coupling and magnetocrystalline anisotropy energy

For an arbitrarily oriented spin, the SOC Hamiltonian reads4, 5

HSOC=12L+e-iϕcosθSx'-iSy'+sinθSz'                                  (31)

+12L-eiϕcosθSx'+iSy'+sinθSz'

+Lz-sinθSx'+cosθSz',

where n=sinθcosϕ,sinθsinϕ,cosθ is the direction of the spin. In the strong exchange limit in 3d systems, electrons near the Fermi surface are spin polarized, and SOC effect is dominated by the spin-conserved part

HSOCsc=λSz'Lzcosθ+12L+e-iϕsinθ+12L-eiϕsinθSz'.         (32)

For distinct frontier orbital, the SOC splitting energy result in the magnetic anisotropy.

## I. Orbital doublet E1=dxz,dyz

Considering single spin channel of |dxz;n,↑,|dyz;n,↑ under half-filling, the spin-conserved SOC Hamiltonian reads

HSOCsc=λℏ220-icosθicosθ0diag.-λℏ22cosθ00λℏ22cosθ,         (33)

where diag. denotes diagonalization of the matrix. Then the orbital degeneracy is splitted, and the occupied state takes the energy of E=-λℏ22cosθ, which is minimized when θ=0 or π, making out-of-plane magnetization favored.

## II. Orbital doublet E2=dxy,dx2-y2

In the subspace of |dx2-y2;n,↑,|dxy;n,↑, the spin-conserved SOC Hamiltonian reads

HSOCsc=λℏ2202icosθ-2icosθ0diag.-λℏ2cosθ00λℏ2cosθ,      (34)

where the occupied energy E=-λℏ2cosθ is also minimized when θ=0 or π.

## III. Orbital triplet T=dxy,dyz,dxz

In the subspace of |dxy;n,↑,|dyz;n,↑,|dxz;n,↑, the spin-conserved SOC Hamiltonian becomes

HSOCsc=λℏ22-0isinθsinϕ-isinθcosϕisinθsinϕ0icosθisinθcosϕ-icosθ0          (35)

diag.-λℏ220000000λℏ22.

The perturbed energies are independent to the orientation of the magnetization, indicating that the first order SOC effect is not the origin of the magnetic anisotropy for the orbital triplet in 3D lattice.

Therefore, for orbital doublets E1=dxz,dyz and E2=dxy,dx2-y2, the out-of-plane magnetization is favored with the energy of the magnetic anisotropy proportional to the SOC parameter λ. With the correlation effect combined, the SOC effect is enhanced via the augment λ→λeff, resulting in a significant gain of the magnetic anisotropy energy. Such an enhancement is efficient especially in the 2D case to stabilize the long-range magnetic order normal to the 2D plane.

Supplementary references

1.	Haastrup S., et al. The Computational 2D Materials Database: high-throughput modeling and discovery of atomically thin crystals. 2D Materials 5, 042002 (2018).

2.	Gjerding M. N., et al. Recent progress of the computational 2D materials database (C2DB). 2D Materials 8, 044002 (2021).

3.	Kanamori J. Electron Correlation and Ferromagnetism of Transition Metals. Prog. Theor. Phys. 30, 275-289 (1963).

4.	Dai D., Xiang H., Whangbo M.-H. Effects of spin-orbit coupling on magnetic properties of discrete and extended magnetic systems. J. Comput. Chem. 29, 2187-2209 (2008).

5.	Wang D., Tang F., Du Y., Wan X. First-principles study of the giant magnetic anisotropy energy in bulk Na4IrO4. Phys. Rev. B 96, 205159 (2017).