Supplementary Information

Simultaneously activating molecular oxygen and surface lattice oxygen on Pt/TiO2 for low-temperature CO oxidation

Tengfei Zhang 1,9, Peng Zheng 2,9, Jiajian Gao 3, Xiaolong Liu 1,*, Yongjun Ji 4,*, Junbo Tian 1, Yang Zou 1, Zhiyi Sun 5, Qiao Hu 6, Guokang Chen 6, Wenxing Chen 5,*, Xi Liu 6,*, Ziyi Zhong 7, Guangwen Xu 2,8, Tingyu Zhu 1,*, and Fabing Su 1,8,*

1 Institute of Process Engineering, Chinese Academy of Sciences, Beijing 100190, China

2 Key Laboratory on Resources Chemicals and Materials of Ministry of Education, Shenyang University of Chemical Technology, Shenyang, 110142, China

3 Institute of Sustainability for Chemicals, Energy and Environment (ISCE2), Agency for Science, Technology, and Research (A*STAR), 1 Pesek Road, Jurong Island, Singapore 627833, Republic of Singapore

4 School of Light Industry, Beijing Technology and Business University, Beijing 100048, China

5 Energy & Catalysis Center, School of Materials Science and Engineering, Beijing Institute of Technology, Beijing 100081, China

6 School of Chemistry and Chemical Engineering, in situ Center for Physical Sciences, Shanghai Jiao Tong University, Shanghai 200240, People’s Republic of China

7 Department of Chemical Engineering, and Guangdong Provincial Key Laboratory of Materials and Technologies for Energy Conversion (MATEC), Guangdong Technion Israel Institute of Technology (GTIIT), 241 Daxue Road, Shantou, 515063, China

8 Institute of Industrial Chemistry and Energy Technology, Shenyang University of Chemical Technology, Shenyang, 110142, China

9 These authors contributed equally: Tengfei Zhang and Peng Zheng.

* liuxl@ipe.ac.cn, yjji@btbu.edu.cn, wxchen@bit.edu.cn, liuxi@sjtu.edu.cn, tyzhu@ipe.ac.cn, and fbsu@ipe.ac.cn.

Supplementary Fig. 1 | Photos of (a) TiO2-R and (b) TiO2.

Supplementary Fig. 2 | EPR spectra of TiO2 and TiO2-R.

Supplementary Fig. 3 | H2-TPR curve of TiO2.

Supplementary Fig. 4 | Raman spectra of TiO2 and TiO2-R.

Supplementary Fig. 5 | XRD patterns of all the catalysts.

Supplementary Fig. 6 | HRTEM image of PtNP/TiO2-R.

Supplementary Fig. 7 | HRTEM image of PtPt-TiISAA+NP/TiO2-R.

Supplementary Fig. 8 | HRTEM image of PtNP/TiO2.

Supplementary Fig. 9 | HAADF-STEM image and the corresponding EDS element mappings of PtNP/TiO2-R.

Supplementary Fig. 10 | HAADF-STEM image and the corresponding EDS element mappings of PtPt-TiISAA+NP/TiO2-R.

Supplementary Fig. 11 | HAADF-STEM image and the corresponding EDS element mappings of PtNP/TiO2.

Supplementary Fig. 12 | Scanning transmission electron microscope-secondary electron image of PtNP/TiO2-R.

Supplementary Fig. 13 | Scanning transmission electron microscope-secondary electron image of PtPt-TiISAA+NP/TiO2-R.

Supplementary Fig. 14 | Scanning transmission electron microscope-secondary electron image of PtNP/TiO2.

Supplementary Fig. 15 | AC-HAADF-STEM image of PtNP/TiO2.

Supplementary Fig. 16 | AC-HAADF-STEM image of PtNP/TiO2-R.

Supplementary Fig. 17 | AC-HAADF-STEM images of (a) PtNP/TiO2-R and (b) PtNP/TiO2.

Supplementary Fig. 18 | Schematic diagram of Pd–Ti crystal structure.

Supplementary Fig. 19 | Corresponding FFT patterns for the region d (a) and region e (b) in Fig. 1b.

Supplementary Fig. 20 | (a)–(c) Representative AC-HAADF-STEM images of PtPt-TiISAA+NP/TiO2-R.

Supplementary Fig. 21 | AC-HAADF-STEM image of PtNP/TiO2-H2.

Supplementary Fig. 22 | (a) and (b) AC-HAADF-STEM images of 0.5 wt%PtPt-TiISAA+NP/TiO2-R.

Supplementary Fig. 23 | k space EXAFS spectra of Pt foil.

Supplementary Fig. 24 | q space EXAFS spectra of Pt foil.

Supplementary Fig. 25 | R space EXAFS spectra of Pt foil.

Supplementary Fig. 26 | k space EXAFS spectra of PtNP/TiO2-R.

Supplementary Fig. 27 | q space EXAFS spectra of PtNP/TiO2-R.

Supplementary Fig. 28 | R space EXAFS spectra of PtNP/TiO2-R.

Supplementary Fig. 29 | k space EXAFS spectra of PtPt-TiISAA+NP/TiO2-R.

Supplementary Fig. 30 | q space EXAFS spectra of PtPt-TiISAA+NP/TiO2-R.

Supplementary Fig. 31 | R space EXAFS spectra of PtPt-TiISAA+NP/TiO2-R.

Supplementary Fig. 32 | Ti 2p XPS spectra of all the catalysts.

Supplementary Fig. 33 | In situ DRIFTS spectra of the CO adsorption for TiO2 and TiO2-R supports.

Supplementary Fig. 34 | In situ NAP-XPS of O 1s spectra from PtPt-TiISAA+NP/TiO2-R at 150 °C.

Supplementary Fig. 35 | In situ NAP-XPS of Pt 4f spectra obtained from PtPt-TiISAA+NP/TiO2-R at 150 °C.

Supplementary Fig. 36 | CO conversion of TiO2 and TiO2-R supports as a functional of reaction temperature. (Reaction conditions: 0.4 g of Cat., 1 vol% CO, 16 vol% O2 mix balanced with N2; v = 400 mL min−1, GHSV = 60000 mL g−1 h−1)

Supplementary Fig. 37 | CO conversion as a function of reaction temperature over PtNP/TiO2-H2 and PtNP/TiO2. (Reaction conditions: 0.4 g of Cat., a gas mix containing 1 vol% CO and 16 vol% O2 balanced with N2.)

Supplementary Fig. 38 | Intermediates and transition states for PtNP/TiO2.

Supplementary Table 1. Structural parameters extracted from the Pt L3-edge EXAFS fitting. (S02=0.85)

| sample | Scattering pair | CN | R(Å) | σ2(10-3Å2) | ΔE0(eV) | R factor |
| --- | --- | --- | --- | --- | --- | --- |
| PtNP/TiO2-R | Pt-O | 1.1 | 1.98 | 4.5 | 2.0 | 0.008 |
|  | Pt-Pt | 8.3 | 2.72 | 5.7 | 2.0 |  |
| PtPt-TiISAA+NP/TiO2-R | Pt-O | 1.3 | 1.97 | 5.8 | 1.5 | 0.006 |
|  | Pt-Ti | 5.6 | 2.57 | 6.7 | 1.5 |  |
|  | Pt-Pt | 3.8 | 2.75 | 5.6 | 1.5 |  |

S02 is the amplitude reduction factor; CN is the coordination number; R is interatomic distance (the bond length between central atoms and surrounding coordination atoms); σ2 is Debye-Waller factor (a measure of thermal and static disorder in absorber-scatterer distances); ΔE0 is edge-energy shift (the difference between the zero kinetic energy value of the sample and that of the theoretical model). R factor is used to value the goodness of the fitting.

Error bounds that characterize the structural parameters obtained by EXAFS spectroscopy were estimated as N ± 20%; R ± 1%; σ2 ± 20%; ΔE0 ± 20%.

Supplementary Table 2. T50, T100, and turnover frequencies (TOFs) of some typical catalysts reported in the literature.

| Catalyst | Metal loading (wt%) | Reaction condition | Temp. (°C) | TOFPt (s–1) | Space Velocity (mL/(gcat.h)) | T50 (°C) | T100 (°C) | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| PtPt-TiISAA+NP/TiO2-R | 0.15 | 1.0 vol% CO, 16.0 vol% O2 | 80 | 11.59 | 60,000 | ~88 | ~120 | This work. |
| PtPt-TiISAA+NP/TiO2-R | 0.15 | 1.0 vol% CO, 4.0 vol% O2 | 80 | 5.94 | 60,000 | ~106 | ~140 | This work. |
| Pt NP/TiO2 | 1.00 | 0.1 vol% CO, 5.0 vol% O2 | 115 | 0.01 | 60,000 | ~78 | ~120 | 1 |
| Pt/CNT-600 | 1.00 | 1.0 vol% CO, 20.0 vol% O2 | 100 | 0.05 | 60,000 | 120 | 140 | 2 |
| Ptn/CeCu | 1.77 | 1.0 vol% CO, 10.0 vol% O2 | 80 | 0.26 | 120,000 | ~34 | ~40 | 3 |
| Pt1/CeOx-TiO2 | 0.25 | 1.0 vol% CO, 4.0 vol% O2 | 200 | 0.09 | 60,000 | ~170 | 190 | 4 |
| Pt/Sn0.2Ti0.8O2 | 0.50 | 1.0 vol% CO, 1.0 vol% O2 | 100 | 0.30 | 60,000 | 75 | 120 | 5 |
| Pt1/CeO2 | 1.00 | 0.4 vol% CO, 10.0 vol% O2 | n.a | n.a | 200,000 | ~140 | ~148 | 6 |
| Pt/CeO2 | 17.00 | 10.0 vol% CO, 5.0 vol% O2 | 285 | 1.05 | ~ | ~270 | ~310 | 7 |
| Pt/CeO2 | 1.00 | 1.0 vol% CO, 1.0 vol% O2 | n.a | n.a | 400,000 | ~180 | ~250 | 8 |
| Pt-O-Pt/CeO2 | 0.27 | 0.1 vol% CO, 5.0 vol% O2 | 150 | 1.97 | 2,400,000 | ~120 | ~170 | 9 |
| Pt/m-Al2O3 | 0.20 | 2.5 vol% CO, 2.5 vol% O2 | 200 | 0.02 | 24,000 | ~260 | ~300 | 10 |
| Au-SA/Def-TiO2 | 0.30 | 1.0 vol% CO, 16.0 vol% O2 | n.a | n.a | 30,000 | ~100 | ~120 | 11 |

Supplementary References

1.	Hojo H, Gondo M, Yoshizaki S, Einaga H. Atomic and electronic structure of Pt/TiO2 catalysts and their relationship to catalytic activity. Nano Lett. 22, 145-150 (2022).

2.	Chen W, et al. Molecular-level insights into the electronic effects in platinum-catalyzed carbon monoxide oxidation. Nat. Commun. 12, 6888 (2021).

3.	Liu X, et al. Activation of subnanometric Pt on Cu-modified CeO2 via redox-coupled atomic layer deposition for CO oxidation. Nat. Commun. 11, 4240 (2020).

4.	Yoo M, et al. A tailored oxide interface creates dense Pt single-atom catalysts with high catalytic activity. Energy Environ. Sci. 13, 1231-1239 (2020).

5.	Chen J, et al. Reverse oxygen spillover triggered by CO adsorption on Sn-doped Pt/TiO2 for low-temperature CO oxidation. Nat. Commun.14, 3477 (2023).

6.	Nie L, et al. Activation of surface lattice oxygen in single-atom Pt/CeO2 for low-temperature CO oxidation. Science 358, 1419-1423 (2017).

7.	Vincent JL, Crozier PA. Atomic level fluxional behavior and activity of CeO2-supported Pt catalysts for CO oxidation. Nat. Commun. 12, 5789 (2021).

8.	Tan W, et al. Fine-tuned local coordination environment of Pt single atoms on ceria controls catalytic reactivity. Nat. Commun. 13, 7070 (2022).

9.	Wang H, et al. Surpassing the single-atom catalytic activity limit through paired Pt-O-Pt ensemble built from isolated Pt1 atoms. Nat. Commun. 10, 3808 (2019).

10.	Zhang Z, et al. Thermally stable single atom Pt/m-Al2O3 for selective hydrogenation and CO oxidation. Na.t Commun.8, 16100 (2017).

11.	Wan J, et al. Defect effects on TiO2 nanosheets: Stabilizing single atomic site Au and promoting catalytic properties. Adv. Mater. 30, 1705369 (2018).