Supplementary information for “Atomic and Electronic Basis for the Serrations of Refractory High Entropy Alloys”

William Yi Wang,1,2,* Shun Li Shang,2 Yi Wang,2 Fengbo Han,1 Kristopher A. Darling,3 Yidong Wu,4 Xie Xie,5 Oleg N. Senkov,6 Jinshan Li,1 Xi Dong Hui,4,* Karin A. Dahmen,7 Peter K. Liaw,5,* Laszlo J. Kecskes,3 and Zi-Kui Liu2,*

1 State Key Laboratory of Solidification Processing, Northwestern Polytechnical University, Xi´an, Shaan Xi Province 710072, China

2 Department of Materials Science and Engineering, The Pennsylvania State University, University Park, PA 16802, USA

3 U.S. Army Research Laboratory, Weapons and Materials Research Directorate, RDRL-WMM-B, Aberdeen Proving Ground, MD 21005, USA

4 State Key Laboratory for Advanced Metals and Materials, University of Science and Technology Beijing, Beijing 100083, China

5 Department of Materials Science and Engineering, The University of Tennessee, Knoxville, TN 37996, USA

6 Air Force Research Laboratory, Materials and Manufacturing Directorate, Wright-Patterson Air Force Base, OH 45433, USA

7 Department of Physics, University of Illinois at Urbana Champaign, Urbana IL 61801, USA

* Corresponding authors. Emails: ZKL (dr.liu@psu.edu) or PKL (pliaw@utk.edu) or XDH (xdhui@ustb.edu.cn) or WYW (wywang@nwpu.edu.cn)

Materials and Methods

Fig. S1.  The analysis and comparison of the power-law scaled yield strength of high-entropy alloys (HEAs) and metallic glasses (MGs) to an experimental data set.

Fig. S2.  Bonding-charge-density isosurface (Δρ = 0.009 e- Å-3) of the BCC MoTaVW high entropy alloy together with its response to elastic deformation..

Fig. S3.  Bonding-charge-density isosurface (Δρ = 0.009 e- Å-3) of the BCC MoNbVW high entropy alloy together with its response to elastic deformation.

Table S1. Properties of HEAs and HE MGs mentioned in the present work (Figure 2), including the crystal structure, bulk modulus (B), Shear modulus (G), Young’s modulus (E), hardness (Hv), yield strength (σ0.2), ultimate strength (σf), valence-electron-concentration (VEC), and electron work function (EWF).

Table S2. Predicted properties of pure elements (W, Mo, Ta, Nb, and V) and their corresponding HEAs.

Table S3. Predicted elastic properties of pure elements (W, Mo, Ta, Nb, and V) and their corresponding HEAs.

Table S4. Predicted properties of pure elements and HfNbTiZr HEA.

Table S5. Predicted elastic properties of pure elements and HfNbTiZr HEA.

Table S6. Predicted Young’s modulus and shear modulus of pure elements and their corresponding HEA

Table S7. CPFE parameters for HfNbTiZr and MoNbTaW, including the reference strain rate (), the inverse strain-rate-sensitivity exponent(n), the initial hardening modulus (h0), the initial value of the slip resistance (τ0), and the saturation value of the slip resistance (τs),

1. Equations of State (EOS) Fitting

The four-parameter Birch-Murnaghan (BM4) equation 1-3 is used to describe the relation between the volume and energy, shown as follows,

(1)

where the fitting parameter, a, is defined as .  The parameters of V0, E0, B0, and , represent the equilibrium volume, energy, bulk modulus, and its first derivative with respect to the pressure, respectively.

Table S1. Properties of HEAs and HE MGs mentioned in the present work (Figure 2), including the crystal structure, bulk modulus (B), Shear modulus (G), Young’s modulus (E), hardness (Hv), yield strength (σ0.2), ultimate strength (σf), valence-electron-concentration (VEC), and electron work function (EWF)

| Composition | Phase | B GPa | G GPa | E GPa | Hv MPa | σ0.2 MPa | σ0.2(Cal) MPa | VEC | EWF | Ref |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| HfNbTiZr | BCC | - | - | - | - | 879 | 1,084 # | 4.25 * | 4.14 * | 4 |
| HfNbTaTiZr | BCC | - | - | - | 3,826 | 929 | 1,118 # | 4.40 * | 4.17 * | 5 |
| MoNbTaW | BCC | - | - | - | 4,500 | 1,135 (RT) 405 (1,873K) | 1,605 # | 5.50 | 4.42 * | 6-8 |
| MoNbTaVW | BCC | - | - | - | 5,300 | 1,246 (RT) 1,536 (1,073K) 477 (1,873K) | 1,551 # | 5.40 | 4.40 * |  |
| NbTiVZr | BCC+ | 118.6 | 45.70 | 121.1 80 | 3,285 3,035 | 1,105 (RT) 834 (873K) | 1,251 # | 4.50 | 4.25 * | 9-11 |
| NbTiV2Zr | BCC+ | - | - | 98 | 2,987 2,958 | 918 (RT) 571 (873K) | 1,347 # | 4.60 * | 4.30 * | 11 |
| CrNbTiZr | BCC+ | - | - | 120 | 4,099 3,888 | 1,260 (RT) 1,035 (873K) | 1,347 # | 4.75 * | 4.30 * |  |
| CrNbTiVZr | BCC+ | - | - | 100 | 4,720 4,402 | 1,298 (RT) 1,230 (873K) | 1,348 # | 4.80 * | 4.30 * |  |
| CrMo0.5NbTa0.5TiZr | BCC | - | - | - | 5,288 | 1,595 (RT) | 1,392 # | 4.90 * | 4.32 * | 12, 13 |
| AlMo0.5NbTa0.5TiZr | BCC | - | - | 178.6 80 | 5,800 | 2,000 (RT) 1,597 (1,073K) | 1,309 # | 4.30 * | 4.28 * | 12, 13 |
| Al0.4Hf0.6NbTaTiZr | BCC | - | - | 78.1 | 4,900 | 1,841 (RT) 796 (1,073K) | 1,167 # | 3.96 * | 4.20 * | 13 |
| CuHfNiTiZr | AM | - | - | - | - | 1,920 | 1,585 # | 6.60 * | 4.42 * | 14, 15 |
| Ti40Zr25Cu12Ni3Be20 | AM | 109.6 | 35.5 | 96.2 | - | 1,680 | 1,667 # | 6.54 | 4.45 * | 7, 16, 17 |
| Zr41.2Ti13.8Cu12.5Ni10Be22.5 | AM | 114.7 114.1 | 37.4 34.1 | 101.3 95 | - - | - 1,860 | 1,735 # | 5.03 | 4.48 * | 7, 16, 18 |
| Ti32.8Zr30.2Cu5.3Ni9Be22.7 | AM |  | 36.1 | 97.8 | - | 1,831 | 1,737 # | 4.46 * | 4.48 * | 14, 19 |
| Ti55Zr10Cu9Ni8Be18 | AM | - | - | - | - | 2,050 2,097 | 1,807 # | 4.75 * | 4.51 * | 14, 20 |
| Ti45Zr16Cu10Ni9Be20 | AM | - | - | - | - | 2,105 | 1,826 # | 4.84 * | 4.52 * | 14, 20 |
| Ti20Zr20Cu20Ni20Be20 | AM | - | - | - | - | 2,315 | 2,111 # | 6.2 * | 4.63 * | 14 |

Note: * indicates that the EWFs of HEAs are estimated by the ideal mixing of those of pure elements while # presents the data predicted in the current work. The abbreviations of AM and BCC+ mean the amorphous state and the BCC matrix combined with a second phase, respectively. RT indicates room temperature.

Table S2. Predicted properties of pure elements  (W, Mo, Ta, Nb, and V) and their corresponding HEA

|  |  |  | Lattice Parameter Å | V0 Å3/atom | E0 eV atom-1 | ΔHmix KJ mole-1 | B GPa | Bʹ | Rs/a0 Å | EF eV | EWF |  | Hv MPa | σ0.2 MPa |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  |  |  |  | HD | Exp. |  |  |
| W (BCC) |  | FP | 3.187 | 16.185 | -12.78005 | - | - | - | 2.171 | 10.610 | 4.170 |  |  | - |
|  |  | BM4 | 3.190 3.190a | 16.231 16.229b | -12.78011 | - | 302.35 302.2b | 4.29 4.29b | 2.174 2.04c | 10.590 11.47c | 4.168 4.41c | 4.55e | 3,430d | - |
| Mo (BCC) |  | FP | 3.151 | 15.644 | -10.90748 | - | - | - | 2.147 | 10.854 | 4.193 |  |  | - |
|  |  | BM4 | 3.153 3.178a | 15.665 15.956b | -10.90793 | - | 264.89 260.4b | 4.53 4.41b | 2.148 2.03c | 10.840 11.36c | 4.192 4.46c | 4.6e | 1,530d | - |
| Ta (BCC) |  | FP | 3.318 | 18.260 | -11.73280 | - | - | - | 2.261 | 9.789 | 4.086 |  |  | - |
|  |  | BM4 | 3.321 3.320a | 18.306 18.313b | -11.73279 | - | 195.64 195.3b | 3.91 3.82b | 2.263 2.13c | 9.771 10.19c | 4.085 4.37c | 4.25e | 873d | - |
| Nb (BCC) |  | FP | 3.306 | 18.068 | -10.19391 | - | - | - | 2.253 | 9.860 | 4.094 |  |  | - |
|  |  | BM4 | 3.310 3.322a | 18.133 18.342b | -10.19400 | - | 171.25 172.3b | 3.76 3.89b | 2.255 2.13c | 9.836 10.82c | 4.091 4.25c | 4.3e | 1,320d | - |
| V (BCC) |  | FP | 2.990 | 13.363 | -8.95884 | - | - | - | 2.037 | 12.054 | 4.305 |  |  | - |
|  |  | BM4 | 2.999 2.992a | 13.480 13.453b | -8.95940 | - | 181.61 182.9b | 4.00 3.84b | 2.043 2.09c | 11.982 11.09c | 4.298 4.32c | 4.3e | 628d | - |
| MoNbTaW |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| O1 |  | FP | 3.233 | 16.894 | -11.48474 | -7.833 | - | - | 2.203 | 10.310 | 4.140 | - | 4,498.9 | 1,076.1 |
|  |  | BM4 | 3.234 | 16.916 | -11.48476 | -7.820 | 234.05 | 4.18 | 2.204 | 10.304 | 4.139 | - | 4,494.8 | 1,075.1 |
| O2 |  | FP | 3.235 | 16.931 | -11.52368 | -11.590 | - | - | 2.204 | 10.297 | 4.139 | - | 4,490.6 | 1,074.1 |
|  |  | BM4 | 3.237 | 16.952 | -11.52366 | -11.573 | 234.30 | 4.21 | 2.206 | 10.285 | 4.137 | - | 4,482.3 | 1,072.1 |
| R1 |  | FP | 3.236 | 16.944 | -11.48997 | -8.337 | - | - | 2.205 | 10.291 | 4.138 | - | 4,486.4 | 1,073.1 |
|  |  | BM4 | 3.237 | 16.964 | -11.48995 | -8.321 | 230.81 | 4.15 | 2.206 | 10.285 | 4.137 | - | 4,482.3 | 1,072.1 |
| R2 |  | FP | 3.234 | 16.918 | -11.48593 | -7.947 | - | - | 2.204 | 10.304 | 4.139 | - | 4,494.8 | 1,075.1 |
|  |  | BM4 | 3.235 | 16.931 | -11.48591 | -7.931 | 232.47 | 4.17 | 2.204 | 10.297 | 4.139 | - | 4,490.6 | 1,074.1 |
| R3 |  | FP | 3.234 | 16.913 | -11.49185 | -8.519 | - | - | 2.204 | 10.304 | 4.139 | - | 4,494.8 | 1,075.1 |
|  |  | BM4 | 3.235 | 16.930 | -11.49186 | -8.505 | 232.97 | 4.18 | 2.204 | 10.297 | 4.139 | - | 4,490.6 | 1,074.1 |
| MoNbTaW (Exp.) |  |  | 3.220c 3.213d |  |  | -6.50f |  |  |  |  |  | 4.373* | 4,500c 4,455d | 1,135c (RT) |
| MoNbVW |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| O1 | FP |  | 3.159 | 15.764 | -10.77261 | -6.034 | - | - | 2.152 | 10.799 | 4.188 | - | 4,822.6 | 1,153.5 |
|  | BM4 |  | 3.161 | 15.791 | -10.77262 | -6.007 | 229.92 | 4.23 | 2.154 | 10.785 | 4.187 | - | 4,813.4 | 1,151.4 |
| O2 | FP |  | 3.159 | 15.765 | -10.78981 | -7.694 | - | - | 2.152 | 10.799 | 4.188 | - | 4,822.6 | 1,153.5 |
|  | BM4 |  | 3.162 | 15.802 | -10.78985 | -7.669 | 232.06 | 4.17 | 2.154 | 10.778 | 4.186 | - | 4,808.9 | 1,150.3 |
| R1 | FP |  | 3.163 | 15.821 | -10.76278 | -5.086 | - | - | 2.155 | 10.772 | 4.185 | - | 4,804.3 | 1,149.2 |
|  | BM4 |  | 3.164 | 15.844 | -10.76278 | -5.058 | 225.97 | 4.21 | 2.156 | 10.765 | 4.185 | - | 4,799.7 | 1,148.1 |
| R2 | FP |  | 3.162 | 15.803 | -10.76716 | -5.508 | - | - | 2.154 | 10.778 | 4.186 | - | 4,808.9 | 1,150.3 |
|  | BM4 |  | 3.164 | 15.832 | -10.76720 | -5.484 | 228.88 | 4.19 | 2.156 | 10.765 | 4.185 | - | 4,799.7 | 1,148.1 |
| R3 | FP |  | 3.162 | 15.807 | -10.77075 | -5.855 | - | - | 2.154 | 10.778 | 4.186 | - | 4,808.9 | 1,150.3 |
|  | BM4 |  | 3.163 | 15.823 | -10.77077 | -5.829 | 228.83 | 4.22 | 2.155 | 10.772 | 4.185 | - | 4,804.3 | 1,149.2 |
| MoNbVW |  |  |  |  |  |  |  |  |  |  |  | 4.360* |  |  |
| MoTaVW |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| O1 | FP |  | 3.165 | 15.822 | -11.17814 | -8.042 | - | - | 2.155 | 10.772 | 4.185 | - | 4,804.3 | 1,149.2 |
|  | BM4 |  | 3.164 | 15.843 | -11.17818 | -8.020 | 235.33 | 4.22 | 2.156 | 10.765 | 4.185 | - | 4,799.7 | 1,148.1 |
| O2 | FP |  | 3.163 | 15.849 | -11.16675 | -6.943 | - | - | 2.157 | 10.758 | 4.184 | - | 4,795.2 | 1,147.0 |
|  | BM4 |  | 3.167 | 15.877 | -11.16683 | -6.925 | 235.51 | 4.18 | 2.158 | 10.744 | 4.183 | - | 4,786.1 | 1,144.8 |
| R1 | FP |  | 3.167 | 15.877 | -11.16075 | -6.364 | - | - | 2.158 | 10.744 | 4.183 | - | 4,786.1 | 1,144.8 |
|  | BM4 |  | 3.168 | 15.900 | -11.16075 | -6.338 | 232.19 | 4.19 | 2.159 | 10.738 | 4.182 | - | 4,781.6 | 1,143.7 |
| R2 | FP |  | 3.165 | 15.855 | -11.16473 | -6.748 | - | - | 2.157 | 10.758 | 4.184 | - | 4,795.2 | 1,147.0 |
|  | BM4 |  | 3.166 | 15.874 | -11.16473 | -6.722 | 234.45 | 4.18 | 2.157 | 10.751 | 4.183 | - | 4,790.6 | 1,145.9 |
| R3 | FP |  | 3.166 | 15.863 | -11.17499 | -7.738 | - | - | 2.157 | 10.751 | 4.183 | - | 4,790.6 | 1,145.9 |
|  | BM4 |  | 3.167 | 15.878 | -11.17489 | -7.703 | 235.39 | 4.22 | 2.158 | 10.744 | 4.183 | - | 4,786.1 | 1,144.8 |
| MoTaVW |  |  |  |  |  |  |  |  |  |  |  | 4.390* |  |  |

Note: * indicates that the EWFs of HEAs are estimated by the ideal mixing of these of pure elements.

a Wang et al., first-principles calculations with PAW-GGA 21

b Shang et al., first-principles calculations with PAW-GGA 3

c Halas et al., key parameters calculating EWF by the Halas-Durakiewicz (HD) model 22

d  Senkov et al., experimental measurements 23

e Michaelson, EWF from experimental measurements 24

f Guo et al., calculations7

Table S3. Predicted elastic properties of pure elements (W, Mo, Ta, Nb, and V) and their corresponding HEAs

|  |  | c11 |  | c12 | c44 | c12-c44 | cʹ | AZ | B | G | E | B/G | v | AVR |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| W | GGA | 526.451 |  | 198.220 | 141.194 | 385.257 | 164.116 | 0.86033 | 307.63 | 149.96 | 386.99 | 2.05 | 0.290 | 0.00271 |
|  | GGA | 517.8a |  | 201.7a | 139.4a | 378.4a | - | - | - | - | - | - | - | - |
| Mo | GGA | 472.813 |  | 169.751 | 56.782 | 416.031 | 151.531 | 0.37472 | 270.77 | 85.20 | 231.34 | 3.18 | 0.358 | 0.11127 |
|  | GGA | 466.0a |  | 165.2a | 99.5a | - | - | - | - | - | - | - | - | - |
| Ta | GGA | 262.180 |  | 164.916 | 62.081 | 200.099 | 48.632 | 1.27655 | 197.34 | 56.30 | 154.23 | 3.51 | 0.370 | 0.00714 |
|  | GGA | 260.9a |  | 165.2a | 70.4a | - | - | - | - | - | - | - | - | - |
| Nb | GGA | 248.209 |  | 137.339 | 2.512 | 245.697 | 55.435 | 0.04531 | 174.30 | 13.87 | 40.54 | 12.56 | 0.461 | 0.70705 |
|  | GGA | 247.2a |  | 140.0a | 14.2a | - | - | - | - | - | - | - | - | - |
| V | GGA | 286.938 |  | 138.105 | 18.367 | 268.571 | 74.4165 | 0.24681 | 187.72 | 33.54 | 94.96 | 5.60 | 0.416 | 0.21619 |
|  | GGA | 272.0a |  | 144.8a | 17.6a | - | - | - | - | - | - | - | - | - |
| MoNbTaW |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| MoNbTaW | O1 |  | 369.072 | 168.697 | 48.321 | 320.751 | 100.188 | 0.48231 | 235.49 | 65.00 | 178.58 | 3.62 | 0.374 | 0.06251 |
|  | O2 |  | 384.122 | 160.274 | 64.144 | 319.978 | 111.924 | 0.5731 | 234.89 | 80.30 | 216.27 | 2.92 | 0.347 | 0.03676 |
|  | R1 |  | -184.595 | -66.545 | -107.129 | * | * | * | * | * | * | * | * | * |
|  | R2 |  | 376.488 | 162.684 | 66.741 | 309.747 | 106.902 | 0.62432 | 233.95 | 80.67 | 217.07 | 2.90 | 0.345 | 0.02641 |
|  | R3 |  | 370.985 | 162.628 | 70.955 | 300.03 | 104.179 | 0.68109 | 232.08 | 82.79 | 221.97 | 2.80 | 0.341 | 0.0176 |
| MoNbVW |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| MoNbVW | O1 |  | 382.523 | 159.104 | 51.069 | 331.454 | 111.710 | 0.45716 | 233.58 | 70.28 | 191.62 | 3.32 | 0.363 | 0.0718 |
|  | O2 |  | 394.338 | 149.980 | 62.182 | 332.156 | 122.179 | 0.50894 | 231.43 | 81.78 | 219.49 | 2.83 | 0.342 | 0.0538 |
|  | R1 |  | 381.889 | 151.830 | 70.884 | 311.005 | 115.030 | 0.61622 | 228.52 | 86.14 | 229.57 | 2.65 | 0.333 | 0.02788 |
|  | R2 |  | 381.921 | 154.305 | 61.002 | 320.919 | 113.808 | 0.53601 | 230.18 | 78.51 | 211.50 | 2.93 | 0.347 | 0.04598 |
|  | R3 |  | 381.921 | 154.305 | 61.002 | 320.919 | 113.808 | 0.53601 | 230.18 | 78.51 | 211.50 | 2.93 | 0.347 | 0.04598 |
| MoTaVW |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| MoTaVW | O1 |  | 354.584 | 174.180 | 41.031 | 313.553 | 90.202 | 0.45488 | 234.31 | 56.59 | 157.11 | 4.14 | 0.388 | 0.07269 |
|  | O2 |  | 373.399 | 169.311 | 54.093 | 319.306 | 102.044 | 0.53009 | 237.34 | 69.94 | 191.06 | 3.39 | 0.366 | 0.04761 |
|  | R1 |  | 371.826 | 163.176 | 71.446 | 300.380 | 104.325 | 0.68484 | 232.73 | 83.17 | 222.96 | 2.80 | 0.340 | 0.01711 |
|  | R2 |  | 370.752 | 165.318 | 64.207 | 306.545 | 102.717 | 0.62509 | 233.80 | 77.57 | 209.54 | 3.01 | 0.351 | 0.02627 |
|  | R3 |  | 364.810 | 169.724 | 65.424 | 299.386 | 97.543 | 0.67072 | 234.75 | 76.81 | 207.77 | 3.06 | 0.352 | 0.01903 |

Note: * indicates that the improper arrangement of atoms causes the large lattice distortion/misfit, and, thus, to result in a mechanically-unstable state (i.e., negative values of elastic constants).

a Shang et al., first-principles calculations with PAW-GGA 3

Table S4. Predicted properties of the pure elements and HfNbTiZr HEA

|  |  | Lattice Parameter Å | V0 Å3/atom | E0 eV atom-1 | ΔHmix KJ mole-1 | B GPa | Bʹ | Rs/a0 Å | EF eV | EWF |  | Hv MPa | σ0.2 MPa |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  |  |  | FP | Exp. |  |  |
| Zr (BCC) | FP | 3.570 | 22.746 | -8.35526 | - | - | - | 2.432 | 8.456 | 3.940 | 4.05e | - | - |
|  | BM4 | 3.576 3.574a | 22.873 22.885b | -8.35539 | - | 89.20 89.7b | 3.24 3.13b | 2.437 2.33c | 8.427 8.50c | 3.936 4.19c | - | - | - |
| Ti (BCC) | FP | 3.240 | 17.003 | -7.69395 | - | - | - | 2.208 | 10.266 | 4.135 | 4.33e | - | - |
|  | BM4 | 3.251 3.241a | 17.182 17.123b | -7.69456 | - | 106.70 107.3b | 3.27 3.47b | 2.215 2.24c | 10.196 8.84c | 4.128 4.36c | - | - | - |
| Hf (BCC) | FP | 3.533 | 22.053 | -9.65480 | - | - | - | 2.407 | 8.634 | 3.960 | 3.9e | - | - |
|  | BM4 | 3.538 3.538a | 22.137 22.128b | -9.65489 | - | 102.00 101.8b | 3.17 3.32b | 2.411 2.43c | 8.609 8.69c | 3.957 3.89c | - | - | - |
| Nb (BCC) | FP | 3.306 | 18.068 | -10.19391 | - | - | - | 2.253 | 9.860 | 4.094 | 4.3e | 1,320d | - |
|  | BM4 | 3.310 3.322a | 18.133 18.342b | -10.19400 | - | 171.25 172.3b | 3.76 3.89b | 2.255 2.13c | 9.836 10.82c | 4.091 4.25c | - | - | - |
| HfNbTiZr |  |  |  |  |  |  |  |  |  |  |  |  |  |
| O1 | FP | 3.408 | 19.790 | -8.92984 | 4.307 | - | - | 2.322 | 9.278 | 4.032 | - | - | 918.7 |
|  | BM4 | 3.413 | 19.885 | -8.93029 | 4.286 | 112.11 | 3.47 | 2.325 | 9.251 | 4.029 | - | - | 914.7 |
| O2 | FP | 3.416 | 19.938 | -8.95379 | 1.996 | - | - | 2.328 | 9.235 | 4.027 | - | - | 912.3 |
|  | BM4 | 3.424 | 20.074 | -8.95484 | 1.917 | 108.28 | 3.78 | 2.333 | 9.192 | 4.023 | - | - | 905.9 |
| R1 | FP | 3.425 | 20.091 | -8.99100 | -1.594 | - | - | 2.334 | 9.187 | 4.022 | - | - | 905.1 |
|  | BM4 | 3.433 | 20.226 | -8.99320 | -1.784 | 107.75 | 3.01 | 2.339 | 9.144 | 4.017 | - | - | 898.8 |
| R2 | FP | 3.426 | 20.107 | -8.97026 | 0.407 | - | - | 2.334 | 9.181 | 4.022 | - | - | 904.3 |
|  | BM4 | 3.433 | 20.225 | -8.97102 | 0.356 | 106.98 | 3.55 | 2.339 | 9.144 | 4.017 | - | - | 898.8 |
| R3 | FP | 3.426 | 20.115 | -8.97289 | 0.153 | - | - | 2.334 | 9.181 | 4.022 | - | - | 904.3 |
|  | BM4 | 3.431 | 20.195 | -8.97296 | 0.169 | 107.87 | 3.56 | 2.338 | 9.155 | 4.019 | - | - | 900.4 |
| HfNbTiZr (Exp) |  |  |  |  |  |  |  |  |  |  | 4.145* | - | 879f |

Note: * indicates that the EWFs of HEAs are estimated by the ideal mixing of these of pure elements.

a Wang et al., first-principles calculations with PAW-GGA 21

b Shang et al., first-principles calculations with PAW-GGA 3

c Halas et al., key parameters calculating EWF by the Halas-Durakiewicz (HD) model 22

d  Senkov et al., experimental data 23

e Michaelson, experimental data 24

f Wu et al., experimental data 4

Table S5. Predicted elastic properties of pure elements and HfNbTiZr HEA

|  |  | c11 | c12 | c44 | c12 -c44 | cʹ |  | AZ | B | G | E | B/G | v |  | AVR |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Ti (BCC) | GGA | 100.935 | 112.484 | 38.383 | 62.552 | -5.775 |  | -6.647 | 108.63 | * | * | * | * |  | * |
|  | GGA | 95.9a | 115.9a | 40.3a | 55.6 | -10 |  | -4.03 | 109.23 | * | * | * | * |  | * |
| Zr (BCC) | GGA | 64.236 | 102.601 | 29.953 | 385.257 | 164.116 |  | 0.860 | 307.63 | 149.96 | 386.99 | 2.05 | 0.290 |  | 0.00271 |
|  | GGA | 81.8a | 94.3a | 30.2a | 378.4 | 158.05 |  | 0.882 | 307.07 | 146.58 | 379.38 | 2.09 | 0.294 |  | 0.00189 |
| Hf (BCC) | GGA | 94.018 | 107.906 | 54.263 | 39.755 | -6.944 |  | -7.814 | 103.28 | * | * | * | * |  | * |
|  | GGA | 73.7a | 117.0a | 51.7a | 22 | -21.65 |  | -2.388 | 102.57 | * | * | * | * |  | * |
| Nb (BCC) | GGA | 248.209 | 137.339 | 2.512 | 245.697 | 55.435 |  | 0.045 | 174.30 | 13.87 | 40.54 | 12.56 | 0.461 |  | 0.70705 |
|  | GGA | 247.2a | 140.0a | 14.2a | 233.0 | 53.6 |  | 0.265 | 175.73 | 25.04 | 71.71 | 7.02 | 0.432 |  | 0.19663 |
| HfNbTiZr | O1 | 98.659 | 122.264 | -41.911 | * |  | * | * | * | * | * | * |  | * | * |
|  | O2 | 115.418 | 92.291 | 25.471 | 89.947 |  | 11.564 | 2.203 | 100.00 | 18.55 | 52.42 | 5.39 |  | 0.413 | 0.07305 |
|  | R1 | 154.022 | 93.079 | 8.588 | 145.434 |  | 30.472 | 0.282 | 113.39 | 14.70 | 42.26 | 7.72 |  | 0.438 | 0.18006 |
|  | R2 | * | * | * | * |  | * | * | * | * | * | * |  | * | * |
|  | R3 | 148.707 | 91.204 | 34.680 | 114.027 |  | 28.752 | 1.206 | 110.37 | 32.17 | 87.97 | 3.43 |  | 0.367 | 0.00421 |

Note: * indicates that the improper arrangement of atoms causes the large lattice distortion/misfit, and, thus, to result in a mechanically-unstable state (i.e., negative values of elastic constants).

a Shang et al., first-principles calculations with PAW-GGA 3

Table S6. Predicted Young’s modulus and shear modulus of pure elements and their corresponding HEA

|  |  | Young’s Modulus |  |  | Shear Modulus |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | [100] | [110] | [111] | [100] | [110] | [111] |
| W |  | 328.23 | 269.50 | 254.33 | 141.19 | 173.78 | 188.26 |
| Mo |  | 303.06 | 154.12 | 132.43 | 56.78 | 89.02 | 109.80 |
| Ta |  | 97.26 | 89.67 | 87.39 | 62.08 | 69.61 | 72.55 |
| Nb |  | 110.87 | 9.47 | 7.25 | 2.51 | 4.88 | 7.12 |
| V |  | 148.83 | 55.36 | 45.78 | 18.37 | 31.49 | 41.33 |
| High Entropy Alloys |  |  |  |  |  |  |  |
| WMoTaNb | O1 | 200.38 | 118.32 | 104.11 | 48.32 | 72.61 | 87.22 |
|  | O2 | 223.85 | 147.30 | 132.23 | 64.14 | 91.35 | 106.39 |
|  | R1 | * | * | * | * | * | * |
|  | R2 | 213.80 | 147.27 | 133.43 | 66.74 | 92.96 | 106.96 |
|  | R3 | 208.36 | 150.28 | 137.50 | 70.95 | 96.31 | 109.33 |
| WMoNbV | O1 | 223.42 | 128.36 | 112.41 | 51.07 | 77.21 | 93.09 |
|  | O2 | 244.36 | 150.82 | 133.75 | 62.18 | 90.86 | 107.37 |
|  | R1 | 230.06 | 158.27 | 143.35 | 70.88 | 98.39 | 113.00 |
|  | R2 | 227.62 | 144.36 | 128.67 | 61.00 | 88.30 | 103.77 |
|  | R3 | 227.62 | 144.36 | 128.67 | 61.00 | 88.30 | 103.77 |
| WMoTaV | O1 | 180.40 | 102.28 | 89.37 | 41.03 | 62.88 | 76.45 |
|  | O2 | 204.09 | 127.62 | 113.45 | 54.09 | 79.27 | 93.83 |
|  | R1 | 208.65 | 150.91 | 138.17 | 71.45 | 96.81 | 109.81 |
|  | R2 | 205.43 | 141.28 | 127.96 | 64.21 | 89.65 | 103.30 |
|  | R3 | 195.09 | 138.93 | 126.76 | 65.42 | 89.76 | 102.46 |
| HfNbTiZr | O1 | * | * | * | * | * | * |
|  | O2 | 23.13 | 24.37 | 24.81 | 25.47 | 22.91 | 22.16 |
|  | R1 | 60.94 | 24.75 | 20.66 | 8.59 | 14.61 | 19.07 |
|  | R2 | * | * | * | * | * | * |
|  | R3 | 57.50 | 52.06 | 50.46 | 34.68 | 39.69 | 41.69 |

Note: * indicates that the improper arrangement of atoms causes the large lattice distortion/misfit, and, thus, to result in a mechanically-unstable state.

Table S7.CPFE parameters for HfNbTiZr and MoNbTaW, including the reference strain rate (), the inverse strain rate sensitivity exponent(n), the initial hardening modulus (h0), the initial value of the slip resistance (τ0), and the saturation value of the slip resistance (τs),

| HEA |  | Slip system |  | n | h0 MPa | τ0 MPa | τs MPa |
| --- | --- | --- | --- | --- | --- | --- | --- |
| HfNbTiZr | O2 |  | 0.001 | 50 | 10000 | 304.1 | 349.7 |
|  | R1 |  |  |  |  | 301.7 | 347 |
|  | R3 |  |  |  |  | 301.4 | 346.6 |
| MoNbTaW | O1 |  |  |  |  | 358 | 411.7 |
|  | O2 |  |  |  |  | 358.7 | 412.5 |
|  | R2 |  |  |  |  | 358.4 | 412.2 |
|  | R3 |  |  |  |  | 358.4 | 412.2 |

Figure S1 The analysis and comparison of the power-law scaled yield strength of high-entropy alloys (HEAs) and metallic glasses (MGs) to an experimental data set.  a): The EWFs of these alloys are estimated from the summation of EWF of the pure elements.  b): currently predicted yield strength of the ordered configurations (O1, O2, O3), random arrangements (R1, R2, R3) and  amorphous configurations (AM1, AM2, AM3, AM4, AM5, AM6 ) for the MoTaNbW, MoVNbW, MoVTaW, and HfNbTiZr HEAs, and Vitreloy-1 MG (Zr41Ti14Cu12.5Ni10Be22.5) Vit1, comparing to the available experimental data.  The solid and open symbols denote the measured yield strength as a function of the EWF values predicted by the summation of EWF of the pure elements and by first-principles calculations, respectively.  The solid-open symbols are the predicted values in the present work.  The calculated yield strength using the EWF-scaled power law () compared with the experimental data listed in Table S1.  The EWF (φ) are estimated by ideal mixing of the pure elements.

Figure S2 Bonding-charge-density 25, 26 isosurface (Δρ = 0.009 e- Å-3) of the BCC MoTaVW high entropy alloy together with its response to elastic deformation.  (A), 3D view of configurational transformations of O1, O2, R1, R2, and R3 structures shown in Figure 1 of the main content.  The embedded table presents the details of the first four nearest neighbors of the center atom.  Atoms in the CN12 cluster are written in red letters.  (B to F), (100)supercell view of the variations of the bonding-charge-density response to the elastic shear under a normal and shear strain (±0.01).

Figure S3 Bonding-charge-density 25, 26 isosurface (Δρ = 0.009 e- Å-3) of the BCC MoNbVW high entropy alloy together with its response to elastic deformation.  (A) 3D view of configurational transformations of O1, O2, R1, R2, and R3 structures shown in Figure 1 of the main content.  The embedded table presents the details of the first four nearest neighbors of the center atom.  Atoms in the CN12 cluster are written in red letters.  (B to F) (100)supercell view of the variations of the bonding-charge-density response to the elastic shear under a normal and shear strain (±0.01). ).

References

1.	Birch F. Finite Elastic Strain of Cubic Crystals. Phys Rev, 71, 809 (1947).

2.	Birch F. Finite strain isotherm and velocities for single-crystal and polycrystalline NaCl at high-pressures and 300 degree K. J Geophys Res, 83, 1257-1268 (1978).

3.	Shang SL, Saengdeejing A, Mei ZG, Kim DE, Zhang H, Ganeshan S, Wang Y, Liu ZK. First-principles calculations of pure elements: Equations of state and elastic stiffness constants. Comp Mater Sci, 48, 813-826 (2010).

4.	Wu YD, Cai YH, Wang T, Si JJ, Zhu J, Wang YD, Hui XD. A refractory Hf25Nb25Ti25Zr25 high-entropy alloy with excellent structural stability and tensile properties. Mater Lett, 130, 277-280 (2014).

5.	Senkov ON, Scott JM, Senkova SV, Miracle DB, Woodward CF. Microstructure and room temperature properties of a high-entropy TaNbHfZrTi alloy. J Alloy Compd, 509, 6043-6048 (2011).

6.	Senkov ON, Wilks GB, Scott JM, Miracle DB. Mechanical properties of Nb25Mo25Ta25W25 and V20Nb20Mo20Ta20W20 refractory high entropy alloys. Intermetallics, 19, 698-706 (2011).

7.	Guo S, Liu CT. Phase stability in high entropy alloys: Formation of solid-solution phase or amorphous phase. Prog Nat Sci, 21, 433-446 (2011).

8.	Zou Y, Ma H, Spolenak R. Ultrastrong ductile and stable high-entropy alloys at small scales. Nat Commun, 6, 7748 (2015).

9.	Tian F, Varga LK, Chen N, Shen J, Vitos L. Ab initio design of elastically isotropic TiZrNbMoVx high-entropy alloys. J Alloy Compd, 599, 19-25 (2014).

10.	Tian F, Varga LK, Chen N, Shen J, Vitos L. Empirical design of single phase high-entropy alloys with high hardness. Intermetallics, 58, 1-6 (2015).

11.	Senkov ON, Senkova SV, Miracle DB, Woodward C. Mechanical properties of low-density, refractory multi-principal element alloys of the Cr-Nb-Ti-V-Zr system. Mater Sci Eng A, 565, 51-62 (2013).

12.	Senkov ON, Woodward CF. Microstructure and properties of a refractory NbCrMo0.5Ta0.5TiZr alloy. Mater Sci Eng A, 529, 311-320 (2011).

13.	Senkov ON, Senkova SV, Woodward C. Effect of aluminum on the microstructure and properties of two refractory high-entropy alloys. Acta Mater, 68, 214-228 (2014).

14.	Ding HY, Yao KF. High entropy Ti20Zr20Cu20Ni20Be20 bulk metallic glass. J Non-Cryst Solids, 364, 9-12 (2013).

15.	Ma LQ, Wang LM, Zhang T, Inoue A. Bulk glass formation of Ti-Zr-Hf-Cu-M (M=Fe, Co, Ni) alloys. Mater Trans, 43, 277-280 (2002).

16.	Wu Y, Wang H, Cheng Y, Liu X, Hui X, Nieh T, Wang Y, Lu Z. Inherent structure length in metallic glasses: simplicity behind complexity. Sci Rep, 5, 12137 (2015).

17.	Liu ZQ, Qu RT, Zhang ZF. Elasticity dominates strength and failure in metallic glasses. J Appl Phys, 117, 014901 (2015).

18.	Chen M. Mechanical Behavior of Metallic Glasses: Microscopic Understanding of Strength and Ductility. Annu Rev Mater Res, 38, 445-469 (2008).

19.	Tang MQ, Zhang HF, Zhu ZW, Fu HM, Wang AM, Li H, Hu ZQ. TiZr-base Bulk Metallic Glass with over 50 mm in Diameter. J Mater Sci Technol, 26, 481-486 (2010).

20.	Park JM, Chang HJ, Han KH, Kim WT, Kim DH. Enhancement of plasticity in Ti-rich Ti-Zr-Be-Cu-Ni bulk metallic glasses. Scripta Mater, 53, 1-6 (2005).

21.	Wang Y, Curtarolo S, Jiang C, Arroyave R, Wang T, Ceder G, Chen LQ, Liu ZK. Ab initio lattice stability in comparison with CALPHAD lattice stability. CALPHAD, 28, 79-90 (2004).

22.	Halas S, Durakiewicz T. Work functions of elements expressed in terms of the Fermi energy and the density of free electrons. J Phys: Condes Matter, 10, 10815 (1998).

23.	Senkov ON, Wilks GB, Miracle DB, Chuang CP, Liaw PK. Refractory high-entropy alloys. Intermetallics, 18, 1758-1765 (2010).

24.	Michaelson HB. The work function of the elements and its periodicity. J Appl Phys, 48, 4729-4733 (1977).

25.	Nakashima PNH, Smith AE, Etheridge J, Muddle BC. The bonding electron density in aluminum. Science, 331, 1583-1586 (2011).

26.	Wang Y, Wang WY, Chen L-Q, Liu Z-K. Bonding charge density from atomic perturbations. J Comput Chem, 36, 1008-1014 (2015).