Supplementary information

Realizing Giant Ferroelectricity in Stable wz-Al1-xBxN Alloys by Controlling the Microstructure and Elastic Constant

Jie Su abc*, Zhengmao Xiao ab, Xinhao Chen a, Yong Huang b*, Zhenhua Lin a, Jingjing Changa*, Jincheng Zhanga, Yue Haoa

a State Key Laboratory of Wide Bandgap Semiconductor Devices and Integrated Technology, Faculty of Integrated Circuit, Xidian University, Xi’an, 710071, China.

b Xidian-Wuhu Research Institute, Wuhu, 241002, China

c Guangzhou Wide Band Gap Semiconductor Innovation Center, Guangzhou Institute

of Technology, Xidian University, Guangzhou, 51055, China

Email: sujie@xidian.edu.cn; huangyong@xdwh-inst.com; jjingchang@xidian.edu.cn;

Supplementary Table S1. The structure and symmetry features of wz-Al1-xBxN alloy models in this study.

| Models | Supercell | Lattice parameter | crystallographic point group | Space group |
| --- | --- | --- | --- | --- |
| wz-AlN | 1×1×1 | a=b=3.13Å, c=5.02Å α=β=90°,γ =120° | 6mm | P63mc |
| wz-AlN | 2×2×2 | a=b=6.26Å, c=10.03Å α=β=90°,γ =120° | 6mm | P63mc |
| wz-Al0.0625B0.9375N | 2×2×2 | a=b=6.20Å, c=9.93Å α=β=90°,γ =120° | 3m | P3m1 |
| wz-Al0.125B0.875N | 2×2×2 | a=b=6.14Å, c=9.80Å α=β=90°,γ =120° | 3m | P3m1 |
| wz-Al0.1875B0.8125N | 2×2×2 | a=b=6.07Å, c=9.72Å α=β=90°,γ =120° | 3m | P3m1 |
| wz-Al0.25B0.75N | 2×2×2 | a=b=6.00Å, c=9.62Å α=β=90°,γ =120° | 3m | P3m1 |
| wz-Al0.3125B0.6875N | 2×2×2 | a=b=5.95Å, c=9.51Å α=β=90°,γ =120° | 3m | P3m1 |

Notes: For the wz-AlN model, its lattice constants and symmetry characteristics are consistent with previous reports1,2. Moreover, the space group and crystallographic point group are irrespective of the supercell size. For the wz-Al1-xBxN alloy models, the lattice parameter characteristics are similar to those of wz-AlN, but the space group and crystallographic point group are changed into the P3m1 and 3m, respectively. Because the B atom induces perturbation of surrounding atoms, and then reduces the atomic symmetry.

Supplementary Table S2. Elastic constants (unit in GPa) and spontaneous polarization (unit in C/m2) of zb-Al1-xBxN alloys

| x | C11 | C12 | C13 | C22 | C23 | C33 | C44 | C55 | C66 | Psp |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 62.5% | 501.96 | 196.76 | 167.94 | 427.92 | 195.39 | 507.47 | 273.63 | 252.09 | 275.02 | 0.17 |
| 75% | 573.28 | 185.92 | 185.79 | 534.03 | 198.81 | 533.82 | 312.94 | 301.68 | 301.78 | 0.08 |
| 93.8% | 712.56 | 177.27 | 178.32 | 715.79 | 177.43 | 712.95 | 396.98 | 393.74 | 397.01 | 0.01 |
| 1 | 768.76 | 173.75 | 173.75 | 768.76 | 173.75 | 768.76 | 425.33 | 425.33 | 425.33 | 0 |

Notes: Although the zinc blende structure belongs to the cubic system, the zb-Al1-xBxN alloy is modeled by the 2 × 1 × 1 supercell. Meanwhile, the B atom can disorder the atomic arrangement with high symmetry. As a result, zinc blende supercell structure can be described by the system with the orthorhombic symmetry3. Thus, C11, C22, C33, C44, C55, C66, C12, C13, C23 of zb-Al1-xBxN alloys are obtained. These elastic constants of zb-Al1-xBxN alloys meet the Born stability criteria, suggesting the mechanical stability for zb-Al1-xBxN alloys with the high B concentration4. However, the spontaneous polarization of these stable zb-Al1-xBxN alloys are small and even close to zero, which are far lower than those of wz-Al1-xBxN alloys and the application requirement. Thus, just the microstructure and electronic properties of wz-Al1-xBxN alloys are studied in this study.

Supplementary Figure 1. Formation enthalpies ∆H of (a) wz-Al1-xBxN alloys and (b) zb-Al1-xBxN alloys with and without 5% strain.

Supplementary Figure 2. The slopes of the elastic constant curves for wz-Al1-xBxN alloys before the phase transformation occurs.

Supplementary Figure 3. (a) Schematic diagram of wz-Al1-xBxN alloy with strain along the horizontal (//) and vertical axis (⊥) direction. The elastic constants (b) C12, (c) C13, and (d) C44 of wz-Al1-xBxN alloy with and without strain.

Supplementary Figure 4. DOS of wz-Al1-xBxN alloy: (a) x = 0, (b) x = 0.625, (c) x = 0.1875, (d) x = 0.3125, (e) x = 1. The orbital contribution ratio of Al atoms for wz-Al1-xBxN alloy.

Supplementary Figure 5. The bond length of (a) Al-N and (b) B-N bond of wz-Al1-xBxN alloys with and without strain.

Supplementary Figure 6. The anlges of N-B-N and B-N-Al of the wz-Al1-xBxN alloy along the c-aixs direction.

Supplementary Figure 7. (a-b) Orbitals of Al and N atoms projected band structures for wz-AlN alloy. (c) The unfold band structures of wz-Al1-xBxN alloy models. (d-f) Orbitals of Al, B, N atoms projected band structures for wz-Al0.75B0.25N alloy.

Supplementary Figure 8. The polarization switching field ESwitch and breakdown field EBreak of wz-Al1-xBxN alloys with strain along the (a) horozontial and (b) c-axis direction.

Supplementary note in Supplementary Figure 8

The polarization switching field ESwitch of wz-Al1-xBxN alloy is calculated by the following equation: ESwitch = EBarrier/∆P, where the ∆P is the displacement of cation. The breakdown field EBreak of wz-Al1-xBxN alloys is calculated by the following equation: EBreak = 24.442exp[0.315√(Egωmax)], where Eg is the band gap and ωmax is the phonon cutoff frequency5. Here, the ωmax of wz-Al1-xBxN alloy is assumed equal to that of wz-AlN. The the ωmax of wz-AlN is about 105 meV6. The calculated EBreak of wz-AlN is about 12.63 MV/cm, which is close to the previous reports7.

Supplementary References

1.	Wagner, J.-M. & Bechstedt, F. Properties of strained wurtzite GaN and AlN: Ab initio studies. Physical Review B 66, 115202 (2002).

2.	Liu, Z., Wang, X., Ma, X., Yang, Y. & Wu, D. Doping effects on the ferroelectric properties of wurtzite nitrides. Applied Physics Letters 122, 122901 (2023).

3.	Golesorkhtabar, R., Pavone, P., Spitaler, J., Puschnig, P. & Draxl, C. ElaStic: A tool for calculating second-order elastic constants from first principles. Computer Physics Communications 184, 1861–1873 (2013).

4.	Mouhat, F. & Coudert, F.-X. Necessary and sufficient elastic stability conditions in various crystal systems. Physical Review B 90, 224104 (2014).

5.	Kim, C., Pilania, G. & Ramprasad, R. From Organized High-Throughput Data to Phenomenological Theory using Machine Learning: The Example of Dielectric Breakdown. Chemistry of Materials 28, 1304–1311 (2016).

6.	Nipko, J. C. & Loong, C.-K. Phonon excitations and related thermal properties of aluminum nitride. Physical Review B 57, 10550–10554 (1998).

7.	Higashiwaki, M., Sasaki, K., Kuramata, A., Masui, T. & Yamakoshi, S. Gallium oxide (Ga2O3) metal-semiconductor field-effect transistors on single-crystal β-Ga2O3 (010) substrates. Applied Physics Letters 100, (2012).