Supplementary Materials: Generative Deep Learning for Predicting Ultrahigh Lattice Thermal Conductivity Materials

Liben Guo,1,† Yuanbin Liu,2,† Zekun Chen,3 Hongao Yang,1 Davide Donadio,3,* Bingyang Cao1,*

1Key Laboratory for Thermal Science and Power Engineering of Ministry of Education, Department of Engineering Mechanics, Tsinghua University, Beijing 100084, China

2Inorganic Chemistry Laboratory, Department of Chemistry, University of Oxford, Oxford OX1 3QR, UK

3Department of Chemistry, University of California, Davis, Davis, California 95616, USA

†These authors contributed equally

*e-mail: ddonadio@ucdavis.edu and caoby@tsinghua.edu.cn

- Details of pre-trained Allegro potential

Fig. S1 Comparison of DFT reference result and pre-trained Allegro potential prediction on: a energy per atom b force components.

Table S1. Accuracy of the pre-trained Allegro potential on various configuration types.

| Configuration types | Size of testing set | MAE of energy (meV atom−1) | RMSE of force (meV Å−1) |
| --- | --- | --- | --- |
| Crystalline (SACADA) | 523 | 25.5 | 205.9 |
| Crystalline (RSS) | 365 | 26.2 | 162.7 |
| Crystalline (Bulk) | 60 | 9.3 | 19.3 |
| Amorphous | 60 | 19.2 | 582.3 |
| Diamond | 30 | 11.8 | 23.8 |
| Graphite | 30 | 11.3 | 31.2 |
| Nanotube | 10 | 19.7 | 224.4 |
| Fullerene | 10 | 12.3 | 384.3 |
| Total | 1088 | 24.3 | 273.0 |

- High 𝜅L materials screening with structural similarity metrics

Table S2. 𝜅L of 10-nearest neighbors of diamond and BCO-C16.

| Benchmark | 𝜅L of 10-nearest neighbors of benchmark (W m−1 K−1) |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | #1 | #2 | #3 | #4 | #5 | #6 | #7 | #8 | #9 | #10 |
| Diamond | 2572 | 1953 | 1785 | 1784 | 1729 | 1677 | 1677 | 1130 | 1010 | 770 |
| BCO-C16 | 553 | 462 | 372 | 304 | 300 | 249 | 198 | 145 | 68 | 17 |

- Energy convex hull

Fig. S2 Energy convex hull of carbon allotropes by the active-learned Allegro potential. The baselines of data are derived from Material Project (MP).1 The positions of materials with ultrahigh 𝜅L predicted in this work are close to diamond within a hull energy of 0.5 eV.

- Detailed structural information carbon allotropes with ultrahigh 𝜅L

The link https://github.com/Dio2k/Ultrahigh_kappa_Carbon_Supplementary provides the POSCAR files of all 34 high 𝜅L structures. Detailed information of six representative carbon allotropes is presented in Table S3.

Table S3. Detailed structural information of six representative carbon allotropes

| Structure (space group) | a (Å) | b (Å) | c (Å) | Atomic positions |
| --- | --- | --- | --- | --- |
| C18-cfe-15 (R3m) | 2.512 | 2.512 | 18.750 | 6c (0.0000, 0.0000, 0.2645) 6c (0.0000, 0.0000, 0.1806) 6c (0.0000, 0.0000, 0.0411) |
| C10-hccch-C13 (P3m1) | 2.516 | 2.516 | 10.376 | 2c (0.0000, 0.0000, 0.4255) 2d (0.3333, 0.6667, 0.2268) 2d (0.3333, 0.6667, 0.3757) 2d (0.3333, 0.6667, 0.9747) 2d (0.3333, 0.6667, 0.8233) |
| C8-cfc-659 (P63/mmc) | 2.514 | 2.514 | 8.311 | 4e (0.0000, 0.0000, 0.0928) 4f (0.3333, 0.6667, 0.1554) |
| C16-cag-172 (Cmca) | 4.333 | 5.023 | 4.352 | 16g (0.1809, 0.1349, 0.5898) |
| C16-pcl-9191 (Cmcm) | 4.779 | 4.905 | 4.371 | 16h (0.1653, 0.3573, 0.5728) |
| C8-sra-208 (Imma) | 2.543 | 4.829 | 4.180 | 8h (0.0000, 0.0854, 0.6463) |

- Phonon properties of six representative predicted carbon allotropes with ultrahigh 𝜅L

Fig. S3 Group velocity, phonon scattering rate and cumulative 𝜅L results of six representative structures from DFT.

- Bandgaps distribution of predicted carbon allotropes with ultrahigh 𝜅L

Fig. S4 Bandgaps distribution of predicted carbon allotropes with ultrahigh 𝜅L. Only one structure out of 34 materials displays metallic properties, which is beyond the scope of our study on lattice thermal conductivity.

- Comparison between RTA and full converged solution

Fig. S5 Comparing of the 𝜅L predictions on KNN structures between RTA method and full converged solution method (LBTE). RTA tends to underestimate 𝜅L of carbon-based materials. Most of these discrepancies fall within the 300 W m−1 K−1 range, and the excepted 8 structures with differences beyond this value are all confirmed to be diamond polytypes. By correcting 𝜅L with full converged solution, the number of ultrahigh 𝜅L materials increases from 34 to 37, which has a minimal impact on our overall outcomes.

- Converging test for 𝜅L calculation

Fig. S6 Cutoff radius converging verification of 𝜅L prediction. The 𝜅L results using a cutoff radius distance of 3 Å in this work for calculation force constants are very close to results with a larger radius (5 Å). This indicates that using the setting of cutoff radius of 3 Å has already shown good convergence.

Fig. S7 Mesh converging verification of 𝜅L prediction. Here convergence is reached if 𝜅L reaches 90% of the converged value of fitted curve κL=κ∞[1-exp(-Nmesh/A)].2 The setting that mesh numbers multiply the respective lattice lengths exceeding 25 promises convergence for most cases.

References

- Jain, A. et al. Commentary: The Materials Project: A materials genome approach to accelerating materials innovation. APL Mater. 1, 011002 (2013).

- Li, W., Carrete, J., A. Katcho, N. & Mingo, N. ShengBTE: A solver of the Boltzmann transport equation for phonons. Comput. Phys. Comm. 185, 1747–1758 (2014).