Supporting Information

Passivation Behaviour of Aluminium Current Collector in Ionic Liquid Alkyl Carbonate (hybrid) Electrolytes

Sowmiya Theivaprakasam1,3,4, Gaetan Girard2, Patrick Howlett2, Maria Forsyth2, Sagar Mitra3, Douglas MacFarlane4.

1IITB-Monash Research Academy, Powai, Mumbai, India 400076.

2Institute for Frontier Materials, Deakin University, Burwood, VIC 3125, Australia.

3Department of Energy Science and Engineering, Indian Institute of Technology Bombay (IITB), Mumbai 400076, India.

4Australian Centre for Electromaterials Science, School of Chemistry, Monash University, VIC 3800, Australia.

C3mpyr+

TFSI-

FSI-

DEC, EC

Figure S1 Chronoamperometry of the aluminium foils treated in [C3mpyr][TFSI], [C3mpyr] [FSI], HE 1 and HE 2.

Figure S2 SEM and EDXS spectra of LP 40

10m

100m

Figure S3 SEM and EDXS spectra of Neat [C3mpyr][TFSI]

100m

Figure S4 SEM and EDXS spectra of HE 1

100m

Figure S5 SEM and EDXS spectra of Neat [C3mpyr][FSI]

100m

Figure S6 SEM and EDXS spectra of HE 2

100m

100m

Figure S7 Average roughness of aluminium surface after anodising treatment in [C3mpyr][TFSI], [C3mpyr][FSI], HE 1 and HE 2 obtained by optical profilometry

| Sample | Sa / µm (roughness average) |
| --- | --- |
| Neat [C3mpyr][TFSI] | 0.52 ± 0.2 |
| HE 1 | 0.48 ± 0.1 |
| Neat [C3mpyr][FSI] | 0.79 ± 0.7 |
| HE 2 | 0.53 ± 0.01 |

Figure S8 High resolution C 1s region spectra for the Al surfaces treated in Neat [C3mpyr][TFSI], HE 1, Neat [C3mpyr][FSI] and HE 2 solutions before and after etching.

Figure S9 High resolution N 1s region spectra for the Al surfaces treated in Neat [C3mpyr][TFSI], HE 1, Neat [C3mpyr][FSI] and HE 2 solutions before and after etching.

Figure S10 High resolution O 1s region spectra for the Al surfaces treated in Neat [C3mpyr][TFSI], HE 1, Neat [C3mpyr][FSI] and HE 2 solutions before and after etching.

Figure S11 High resolution S 2p region spectra for the Al surfaces treated in Neat [C3mpyr][TFSI], HE 1, Neat [C3mpyr][FSI] and HE 2 solutions before and after etching.

Figure S12 Schematic representation of the moieties present in the passivation layer of aluminum current collector treated with different electrolytes.
(The position or the number of moieties in the picture were chosen based on our interpretation of microscopic and spectroscopic analysis).

Table S1. Assignment for the FTIR spectrum data of aluminium surfaces – neat samples

(ν: stretching, δ: bending, s: strong, m: medium, w: weak, b: broad)

| Assignment |  | Samples |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Neat [C3mpyr][ TFSI] | Neat [C3mpy] [TFSI]-Al | Neat [C3mpyr] [FSI] | Neat [C3mpyr] [FSI]-Al | Neat LP40 | LP40 Al | HE 1 | HE 2 | References |
| 1. | δa(SO2) | 569 (s) | 570 (w) | 567 (s) | 570 |  |  | 570 | 570 | 1 |
| 2. | νs (SNS) | 740 | 740 | 729 (b) | 745 |  |  | 740 (w) | 740 | 1, 2, 3, 4 |
| 3. | νa (SNS) & ν(SF) | 789 | 789 |  | 828 |  |  | 843 | 832 | 2, 4, 5 |
| 4. | νs (R-C-R) |  |  |  |  | 835(s) | 835 (s) |  |  | 6 |
| 5. | ν (CO) |  |  |  |  | 1079 (s) | 1079 (s) |  |  | 6 |
| 6. | νa (SO2-N-SO2) | 1051 (s) | 1051 (s) | 1101 | 1103 |  |  | 1052 (s) | 1054 | 1, 5, 7 |
| 7. | νa (R-C-R) |  |  |  |  | 1152 (s) 1189 | 1153 (s) 1189 |  |  | 6 |
| 8. | νs (SO2-N-SO2) | 1133 (s) 1175 (s) | 1133 (w) 1176 (s) | 1172 1216 | 1175 1216 |  |  | 1133 1177 (s) | 1104 1136 1174 (s) | 1, 5, 7 |
| 9. | νa (SO2) | 1330 (s) | 1329 (s) | 1360 (s) | 1360 |  |  | 1329 | 1332 (w) 1350 | 1, 4, 5 |
| 10. | νa (SO2) | 1348 (s) | 1347 (s) | 1377 (s) | 1378 |  |  | 1348 | 1381 | 1, 5 |
| 11. | ν (CH2) ν(CH3) | 1473 | 1472 (m) | 1471 | 1472 |  |  | 1473 | 1472 | 1, 8, 9 |
| 12. | ν (C=O) from R-O-COOR |  |  |  |  | 1763 (s) | 1764 (s) |  |  | 6 |

| Assignment |  | Samples |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Neat [C3mpyr][ TFSI] | Neat [C3mpy] [TFSI]-Al | Neat [C3mpyr] [FSI] | Neat [C3mpyr] [FSI]-Al | Neat LP 40 | LP 40 Al | HE 1 | HE 2 | References |
| 13. | ν (CH2) | 2889 | 2889 (w) | 2887 | 2887 |  |  | 2889 | 2888 | 1, 4, 7, 9 |
| 14. | ν (CH2) | 2950 | 2948 (w) | 2945 | 2946 | 2940 | 2940 | 2949 | 2947 | 1, 4, 7, 9 |
| 15. | ν (CH2) | 2982 | 2981 | 2980 | 2979 |  |  | 2981 | 2980 | 1, 4, 7, 9 |
| 16. | ν (CH2) |  |  |  |  | 3004 | 3008 |  |  | 1, 4, 9 |
| 17. | ν (CH2) |  | 3042 (w) |  | 3042 (w) |  |  |  |  | 9 |
| 18. | ν (OH) |  |  |  |  | 3630 (s,b) | 3630 (s,b) |  |  | 6 |

Table S2 Atomic percent (± 0.1 - 1 %) summary determined from the survey spectra for the aluminium surfaces before (initial) and after etching (etched) for five minutes

| Element | Atomic concentration (%) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Neat [C3mpyr][TFSI] |  | HE 1 |  | Neat [C3mpyr][FSI] |  | HE 2 |  |
|  | Inital | Etched | Inital | Etched | Inital | Etched | Inital | Etched |
| F (1s) | 16.4 | 30.9 | 18.6 | 20.7 | 9.2 | 18.8 | 10.0 | 14.2 |
| O (1s) | 41.7 | 28.3 | 31.2 | 22.4 | 31.7 | 31.0 | 24.3 | 20.0 |
| N (1s) | 3.6 | 1.8 | 4.3 | 3.3 | 6.0 | 3.9 | 5.4 | 6.3 |
| C (1s) | 17.9 | 8.0 | 19.9 | 19.6 | 34.3 | 17.8 | 45.1 | 36.3 |
| S (2p3/2) | 6.2 | 2.7 | 5.1 | 3.9 | 8.8 | 5.2 | 7.6 | 8.8 |
| P (2p3/2) | - | - | 8.3 | 12.0 | - | - | - | 2.2 |
| Al (2p) | 14.2 | 28.3 | 12.7 | 18.2 | 9.9 | 23.3 | 7.6 | 12.2 |

Table S3 Summary of XPS data and assignments for the aluminium surfaces of neat [C3mpyr][TFSI] and HE 1 samples (before and after etching)

| Element | Assignment | Peak position (eV) |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  | Neat [C3mpyr][TFSI] |  | HE 1 |  |
|  |  | Inital | Etched | Inital | Etched |
| F (1s) | -CF3 | 689.4 (37.7) | 688.7 (45.5) 688.2 (7.3) | 690.6 (0.4) 688.7 (35.2) | 689.9 (5.6) |
|  | -SO2F | 688.9 (31.4) | 687.6 (4) 687.0 (8.4) | 688.2 (30.4) | 688.2 (41.9) |
|  | AlF3 (686.3) metal fluoride (684-685.5) | 686.8 (8) 685.7 (23) | 686.6 (34.7) | 685.6 (14.1) 685.1 (19) 684.2 (0.8) | 686.2 (50) 684.4 (2.5) |
| O (1s) | O-F (ca. 535) | 534.3 (6) | 534.1 (42.5) | - | 534.6 (1.8) |
|  | Organic C=O (ca. 533) | 533.3 (41.1) 533.0 (3.2) | 533.6 (9.6) 533.1 (1.2) | 533.8 (2.3) | 533.4 (5.7) 532.7 (46.8) |
|  | CO32- (531.5-532) organic C-O or SO2- | 532.6 (47.5) | 532.6 (5.4) 531.9,532 (41.4) | 532.2 (59.2) 531.7 (5.5) 531.5 (32) | 532.0 (26.3) 530.8 (19.5) |
|  | Al oxide (529-530) | 531.1 (2.3) | - | 529.9 (1) | - |
| N (1s) | N+ | 403.6 (2.9) 402.7 (22.4) 402.1 (0.5) 401.5 (5.0) | 404.5 (8.5) 402.2 (47.8) | 403.9 (1) 402.6 (10.4) 402.1 (34.7) 401.1 (0.2) | 403.3 (10.7) 401.9 (36.2) |
|  | N- | 400.7 (13.4) 399.7 (43.1) 399.6 (12.7) | 400.6 (21.2) 399.9 (2.1) 399.1 (20.5) | 399.5-20.8 399.1-28.1 398.1-4.9 | 400.4 (7.4) 398.8 (45.7) |
| C (1s) | -CF3 | 293.5 (9.2) 292.9 (10.3) | 292.9 (6) | 292.6 (14.1) | 292.6 (3.5) 292.3 (5.6) |
|  | Chetero CO32- O-C=O | 289.4 (6.5) | 290.8 (6.1) 288.9 (6.2) | 288.3 (3.1) | 289.7 (4.4) |
|  | C-O-C (ca. 286 eV) C-N | 287.1 (17.4) 286.4 (19.4) | 286.9 (47.3) | 286.3 (41.8) | 287.1 (12.5) 286.1 (21.7) |
|  | Caliphatic C-C / C-H | 285.6 (1.9) 285.4 (22.1) 284.8 (13.1) | 285.9 (16.2) 284.8 (18.2) | 285.1 (31.8) 284.8 (9.2) | 284.8 (52.3) |

| S (2p3/2) | -SO2CF3 | 169.7 (31.4) 170.9 (15.7) 169.0 (31.9) 170.2 (16) | 173.7 (1.4) 172.5 (2.8) 170.2 (30.6) 171.4 (15.3) | 168.6 (45.8) 169.7 (22.9) | 169.9,170 (2.9) 171.1 (1.4) 168.3 (24.8) 169.5 (12.4) |
| --- | --- | --- | --- | --- | --- |
|  | Oxidized S (sulfone, sulfite) | 167.3 (3.4) 168.4 (1.7) | 168.5 (16.4) 169.6 (8.2) | 167.9 (19.2) 169.0 (9.6) | 168.1 (19.8) 169.2 (9.9) |
|  | Sulfide species (160-165) and S0 (164.1, 164) | - | 165.4 (11.3) 166.5 (5.7) 163.8 (5.6) 164.9 (2.8) | 163.8 (1.7) 164.9 (0.9) | 163.5 (13.8) 164.7 (6.9) 164.2 (2.7) 163.0 (5.4) |
| Al (2p3/2) | AlF3 (76.6) | - | 77.2 (23.1) 78.4 (11.5) | 74.8 (23) 76.6 (2.3) | 76.8 (18.8) 75.7 (37.7) |
|  | Al oxide on Al foil (75.6) | 76.0 (31) 75.4 (8) 74.9 (61.3) | 75.4 (42.5) 76.6 (21.3) | - | - |
|  | Al oxide (74.4-74.6) | - | - | 74.4 (47.5) 74.1 (26.4) | 75.5 (14.5) 74.4 (28.9) |
|  | Al0 (72.6-72.9) | - | 70.8 (1.6) | - | - |

Table S4 Summary of XPS data and assignments for the aluminium surfaces of neat [C3mpyr][FSI] and HE 2 samples (before and after etching)

| Element | Assignment | Peak position (eV) |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  | Neat [C3mpyr][FSI] |  | HE 2 |  |
|  |  | Inital | Etched | Inital | Etched |
| F (1s) | -CF3 | - | - | - | - |
|  | -SO2F | 688.2 (18.5) 687.6 (20.3) | 688.0 (58.4) | 688.5 (16.1) 687.9 (30.8) 687.1 (41.3) | 688.7 (0.2) 688.3 (37.3) 687.4 (34.6) |
|  | AlF3 (686.3) Metal fluoride (684-685.5) | 686.7 (61.2) | 686.6 (29.4) 685.2 (12.1) | 686.2 (3.3) 685.8 (8.6) | 686.4 (22.9) 685.1 (5.1) |
| O (1s) | O-F (ca. 535) | 535.0 (3.9) 534.2 (6.9) | 534.2 (30.3) | 534.5 (8.9) | - |
|  | Organic C=O (ca. 533) | 533.5 (47.4) |  | 533.4 (43.7) | 533.6 (25.1) 533.3 (31.8) |
|  | CO32- (531.5-532) organic C-O or SO2- | 532.5 (41.8) | 532.7 (67.1) 531.1 (2.4) | 532.7 (36.5) 532.0 (10.8) | 532.7 (26.1) 531.5 (17) |
|  | Al oxide (529-530) | - | 529.6 (0.3) | - | - |
| N (1s) | N+ | 403.2 (28.9) 401.9,402 (3.8) | 404.3 (9.8) 403.0 (14.2) 401.7 (36.9) | 403.9,404 (5.3) 402.4 (41.5) | 402.7 (34.2) 402.4 (7.9) |
|  | N- | 400.5 (59.9) 399.1 (7.5) | 400.4 (6.9) 399.3 (32.2) | 400.6 (10) 399.5 (38.2) 398.3 (5) | 400.3 (28.3) 399.5 (18) 398.7 (11.7) |
| C (1s) | -CF3 | - | - | - | - |
|  | Chetero CO32- O-C=O | 289.8 (2.5) 287.1(37.1) | 287.2 (59.3) | 287.6 (7.4) 287.1 (6) | - |
|  | C-O-C (ca. 286 eV) C-N | 285.9,286 (38.3) | 286.2 (9) 285.9 (9.5) | 286.4 (35.1) 285.3 (19.4) | 286.5 (50.8) 286.4 (16.1) 285.4 (13.4) |
|  | Caliphatic C-C / C-H | 284.8 (22.2) | 284.8 (22.1) | 284.8 (32.1) | 284.8 (19.8) |

| S (2p3/2) | -SO2F | 170.5 (8.4) 171.7-4.2 169.7 (55.5) 170.9 (27.8) 169.3 (2.8) 170.4 (1.4) | 170.9,171 (23.7) 172.1 (11.9) 170.3 (0.9) 171.4 (0.5) 169.5 (11) 170.6 (5.5) | 171.4 (5.3) 172.6 (2.6) 170.8 (3) 171.98 (1.5) | 170.8 (10) 171.9,172.0 (5) 169.7 (19.3) 170.9 (9.6) |
| --- | --- | --- | --- | --- | --- |
|  | Oxidized S (sulfone, sulfite) | - | 168.9 (11.2) 170.0 (5.6) 167.5 (6) 168.6 (3) | 169.6 (51.9) 170.8 (25.9) 168.3 (6.5) 169.4 (3.3) | 168.7 (14.7) 169.9 (7.3) |
|  | Sulfide species (160-165) and S0 (164.1, 164) | - | 164.9,165 (10.2) 166.1 (5.1) 163.1 (3.7) 164.3 (1.9) | - | 164.2 (18.2) 165.3 (9.1) 163.5 (4.5) 164.7 (2.3) |
| Al (2p3/2) | AlF3 (76.6) | 76.1 (24.9) 77.2 (12.5) | 76.8 (37.3) 77.2 (18.7) | 77.6 (7.1) 78.8 (3.6) 75.8 (59.6) 76.9,77.0 (29.8) | 76.1 (43.8) 77.3 (21.9) 76.0 (3.6) 77.2 (1.8) |
|  | Al oxide on Al foil (75.6) | 75.2 (40.9) 76.3 (20.5) | 75.1 (28.9) 76.3 (14.4) | - | 75.2 (19.2) 76.4 (9.6) |
|  | Al oxide (74.4-74.6) | - | - | - | - |
|  | Al0 (72.6-72.9) | 71.2 (1.2) | 70.2 (0.8) | - | - |

References

1.	Howlett PC, Brack N, Hollenkamp AF, Forsyth M, MacFarlane DR. Characterization of the lithium surface in N-methyl-N-alkylpyrrolidinium bis(trifluoromethanesulfonyl) amide room-temperature ionic liquid electrolytes. Journal of the Electrochemical Society 2006, 153(3): A595-A606.

2.	Yoon H, Best AS, Forsyth M, MacFarlane DR, Howlett PC. Physical properties of high Li-ion content N-propyl-N-methylpyrrolidinium bis(fluorosulfonyl)imide based ionic liquid electrolytes. Phys Chem Chem Phys 2015, 17(6): 4656-4663.

3.	Rey I, Lassègues JC, Grondin J, Servant L. Infrared and Raman study of the PEO-LiTFSI polymer electrolyte. Electrochimica Acta 1998, 43(10–11): 1505-1510.

4.	Colthup NB, Daly LH, Wiberley SE. Chapter 12 - Compounds Containing Boron, Silicon, Phosphorus, Sulfur, Or Halogen. In: Colthup NB, Daly LH, Wiberley SE (eds). Introduction to Infrared and Raman Spectroscopy (Third Edition). Academic Press: San Diego, 1990, pp 355-385.

5.	Li LF, Zhou SS, Han HB, Li H, Nie J, Armand M, et al. Transport and Electrochemical Properties and Spectral Features of Non-Aqueous Electrolytes Containing LiFSI in Linear Carbonate Solvents. Journal of the Electrochemical Society 2011, 158(2): A74-A82.

6.	Nyquist RA, Potts WJ. Infrared absorptions characteristic of organic carbonate derivatives and related compounds. Spectrochimica Acta 1961, 17(7): 679-697.

7.	Bednarska-Bolek B, Jakubas R, Bator G, Baran J. Vibrational study of the structural phase transition in bis(pyrrolidinium)-chloride-hexachloroantimonate(V) by infrared spectroscopy. Journal of Molecular Structure 2002, 614(1–3): 151-157.

8.	Adebahr J, Johansson P, Jacobsson P, MacFarlane DR, Forsyth M. Ab initio calculations, Raman and NMR investigation of the plastic crystal di-methyl pyrrolidinium iodide. Electrochimica Acta 2003, 48(14–16): 2283-2289.

9.	R. A. Nyquist CLP, M. A. Leugers. Handbook of Infrared and Raman Spectra of Inorganic Compounds and Organic Salts. Academic Press, 1997.