Supplementary Information to

Phase-dependent growth of Pt on MoS2 for highly efficient H2 evolution

Zhenyu Shi1,2†, Xiao Zhang3†, Xiaoqian Lin4†, Guigao Liu1†, Chongyi Ling5†, Shibo Xi6†, Bo Chen1, Yiyao Ge1, Chaoliang Tan1, Zhuangchai Lai1, Zhiqi Huang1, Xinyang Ruan1, Li Zhai1,7, Lujiang Li1, Zijian Li1, Xixi Wang1, Gwang-Hyeon Nam2, Jiawei Liu2, Qiyuan He8, Zhiqiang Guan1,9, Jinlan Wang5, Chun-Sing Lee1,9, Anthony R. J. Kucernak4* and Hua Zhang1,7,10*

1Department of Chemistry, City University of Hong Kong, Hong Kong, China.

2Center for Programmable Materials, School of Materials Science and Engineering, Nanyang Technological University, Singapore, Singapore.

3Department of Mechanical Engineering, Research Institute for Advanced Manufacturing, The Hong Kong Polytechnic University, Hong Kong, China.

4Department of Chemistry, Molecular Science Research Hub, Imperial College London, London, UK.

5School of Physics, Southeast University, Nanjing, China.

6Institute of Sustainability for Chemicals, Energy and Environment (ISCE2), A*STAR (Agency for Science, Technology and Research), Singapore, Singapore.

7Hong Kong Branch of National Precious Metals Material Engineering Research Center (NPMM), City University of Hong Kong, Hong Kong, China.

8Department of Materials Science and Engineering, City University of Hong Kong, Hong Kong, China.

9Center of Super-Diamond and Advanced Films (COSDAF), City University of Hong Kong, Hong Kong, China.

10Shenzhen Research Institute, City University of Hong Kong, Shenzhen, China.

*Correspondence author. Email: hua.zhang@cityu.edu.hk, anthony@imperial.ac.uk

†These authors contributed equally to this work.

# Supplementary Fig. 1 | Characterizations of KxMoS2 crystals. a, Scanning electron microscope (SEM) image, and b, Energy-dispersive X-ray spectroscopy (EDS) spectrum of the prepared KxMoS2 crystals. Inset in (b): the corresponding element percentages of the prepared KxMoS2 crystals.

# Supplementary Fig. 2 | Characterizations of obtained 1T′-MoS2 nanosheets (NSs). a, Optical microscopy, and b, SEM images of the obtained 1T′-MoS2 NSs.

# Supplementary Fig. 3 | High-angle annular dark-field scanning transmission electron microscopy (HAADF-STEM) image analysis of 1T′-MoS2 NS. a, HAADF-STEM image of 1T′-MoS2 NS. b, The corresponding line scan intensity profile obtained from the white dotted line in (a).

# Supplementary Fig. 4 | Atomic structures of 1T′-MoS2 and 2H-MoS2. a,b Schematic illustrations of the atomic structures of 1T′-MoS2 (ref. 1) (a) and 2H-MoS2 (b). The red dashed lines in (a) show the zig-zag chain of Mo atoms in 1T′-MoS2 with a shortest Mo-Mo distance of 2.78 Å. The black dashed lines in (b) show the (100) planes of 2H-MoS2 with a theoretical interlayer spacing of 2.74 Å.

# Supplementary Fig. 5 | Transmission electron microscopy (TEM) analysis of 1T′-MoS2 NS. a, TEM image of a representative 1T′-MoS2 NS. b, The corresponding selected area electron diffraction (SAED) pattern obtained from the 1T′-MoS2 NS in (a).

# Supplementary Fig. 6 | STEM-EDS analysis of 1T′-MoS2 NS. a, STEM image, and b,c, the corresponding EDS mappings of a representative 1T′-MoS2 NS. d, EDS spectrum of the 1T′-MoS2 NSs, indicating no detectable potassium (Kα 3.31 eV), bromide (Lα 1.48 eV), and other residues in 1T′-MoS2 NSs. Inset in (d): the corresponding element percentages.

# Supplementary Fig. 7 | K 2p X-ray photoelectron spectroscopy (XPS) spectra of the KxMoS2 crystals and the obtained 1T′-MoS2 NSs.

# Supplementary Fig. 8 | Ultraviolet-visible (UV-Vis) absorption spectra of the exfoliated 1T′-MoS2 NSs and 2H-MoS2 NSs dispersed in N,N-dimethylformamide. Four featured peaks are clearly observed in the UV-Vis absorption spectrum of 2H-MoS2 NSs as indicated by the black dashed lines.

# Supplementary Fig. 9 | EDS mapping results of Pt nanoparticles (PtNPs)/2H-MoS2. a-d, STEM image (a) and the corresponding EDS mappings (b-d) of PtNPs/2H-MoS2.

# Supplementary Fig. 10 | HAADF-STEM analysis of single-atomically dispersed Pt (s-Pt)/1T′-MoS2. a, HAADF-STEM image of s-Pt/1T′-MoS2. b, The corresponding line scan intensity profile obtained from the white dotted rectangle in (a).

# Supplementary Fig. 11 | Atomic structural models of Pt substituting Mo site (Ptsub), Pt adsorbed on the top site of S (Ptads-S), and Pt adsorbed on the top site of Mo (Ptads-Mo) showing the bonding environment of Pt. a, Top view, and b, side view of Ptsub. The Ptsub is located in the 1T′-MoS2 lattice, substituting the Mo site, and coordinated with six surrounding S atoms. c, Top view, and d, side view of Ptads-S. The Ptads-S is located on the top site of S in 1T′-MoS2 and coordinated with two adjacent S atoms. e, Top view and f, side view of Ptads-Mo. The Ptads-Mo is located on the top site of Mo in 1T′-MoS2 and coordinated with three adjacent S atoms. The yellow, blue, and red balls represent the S, Mo, and Pt atom, respectively.

# Supplementary Fig. 12 | Fitting curves for the extended X-ray absorption fine structure (EXAFS) profiles of the Fourier transform at Pt L3-edge. a-d, Pt L3-edge EXAFS spectra and the corresponding fitting curves of s-Pt/1T′-MoS2 (a), PtNPs/2H-MoS2 (b), commercial PtS2 powder (c), and Pt foil (d). The fitting results are summarized in Supplementary Table 2.

# Supplementary Fig. 13 | Pt L3-edge X-ray absorption near-edge spectroscopy (XANES) spectra and structural model of s-Pt/1T′-MoS2. a, Pt L3-edge XANES spectrum of s-Pt/1T′-MoS2 and the simulated spectrum using b, the simulated density functional theory (DFT) model with the coexistence of Ptsub, Ptads-S, and Ptads-Mo on 1T′-MoS2 (denoted as Ptsub+Ptads-S+Ptads-Mo). The yellow, blue, and red balls in (b) represent the S, Mo, and Pt atoms, respectively.

The Pt L3-edge XANES spectrum of s-Pt/1T′-MoS2 (Fig. 3a and Supplementary Fig. 13a) shows that the Pt is single-atomically dispersed on 1T′-MoS2 NSs. The HAADF-STEM analysis and the DFT calculation results (Fig. 2c-f and Supplementary Fig. 11) indicate that the s-Pt/1T′-MoS2 contains three kinds of Pt atomic structures, i.e., Ptsub, Ptads-S, and Ptads-Mo. After a systematic screening, a DFT model containing Ptsub, Ptads-S, and Ptads-Mo was established, which is denoted as Ptsub+Ptads-S+Ptads-Mo (Supplementary Fig. 13b). The simulated Pt L3-edge XANES spectrum based on this model matches well with the experimental curve of s-Pt/1T′-MoS2 (Supplementary Fig. 13a). This result reveals the coexistence of Ptsub, Ptads-S, and Ptads-Mo in the prepared s-Pt/1T′-MoS2, which is consistent with the HAADF-STEM analysis (Fig. 2c-f).

# Supplementary Fig. 14 | Raman characterization of as-prepared samples. a, Raman spectra of 2H-MoS2 NSs and PtNPs/2H-MoS2. b, Raman spectra of 1T′-MoS2 NSs and s-Pt/1T′-MoS2.

As shown in Supplementary Fig. 14a, the phase of 2H-MoS2 maintained after the growth of Pt on 2H-MoS2 to form the PtNPs/2H-MoS2, although the Raman peaks of PtNPs/2H-MoS2 slightly shifted to higher wavenumbers compared to the 2H-MoS2 NSs, which could be ascribed to the interaction between the 2H-MoS2 and PtNPs (ref.2,3). Similarly, all the Raman peaks of s-Pt/1T′-MoS2 also shift to higher wavenumbers compared to the 1T′-MoS2 NSs (Supplementary Fig. 14b). Importantly, the characteristic E2g1 peak of 2H-MoS2 located at 382.8 cm-1 cannot be observed, indicating that no 1T′-to-2H phase transition occurred after the growth of Pt on 1T′-MoS2.

# Supplementary Fig. 15 | Photograph of the floating electrode setup. Abbreviations: WE, working electrode; RE, reference electrode; CE, counter electrode.

# Supplementary Fig. 16 | Measurements of electrocatalytic hydrogen evolution reaction (HER) on the second batch of floating electrodes. a, HER polarization curves for s-Pt/1T′-MoS2 (Electrode 3, denoted as E3) and HiSPEC 9100 Pt/C (Electrode 4, denoted as E4), showing the geometric current densities (jgeometric). b, HER polarization curves for s-Pt/1T′-MoS2 and HiSPEC 9100 Pt/C, showing the mass-normalized current densities (jmass,Pt).

# Supplementary Fig. 17 | Measurements of electrocatalytic HER on the third batch of floating electrodes. a, HER polarization curves for s-Pt/1T′-MoS2 (Electrode 5, denoted as E5) and HiSPEC 9100 Pt/C (Electrode 6, denoted as E6), showing the jgeometric. b, HER polarization curves for s-Pt/1T′-MoS2 and HiSPEC 9100 Pt/C, showing the jmass,Pt.

# Supplementary Fig. 18 | Durability test of s-Pt/1T′-MoS2. The polarization curves were recorded before and after 10,000 cyclic voltammetry cycles.

# Supplementary Fig. 19 | Pt 4f spectra of s-Pt/1T′-MoS2 before and after the durability test. The empty dots and curves show the experimental XPS data and the corresponding deconvoluted spectra, respectively.

The Pt 4f XPS data in Supplementary Fig. 19 shows a negligible difference after the durability test. No Pt0 peak can be assigned which indicates that the Pt species are not in the metallic state.

# Supplementary Fig. 20 | XPS spectra of s-Pt/1T′-MoS2 before and after the durability test. a, Mo 3d spectra, b, S 2p spectra, and c, O 1s spectra of s-Pt/1T′-MoS2 before and after the durability test. The empty dots and curves show the experimental XPS data and the corresponding deconvoluted spectra, respectively.

The Mo 3d, S 2p XPS spectra in Supplementary Fig. 20a,b show no shift after the durability test, indicating the structure of the 1T′-MoS2 still maintained. A small peak in Mo 3d, located at ~233 cm-1, (pointed out by the black arrow in Supplementary Fig. 20a), can be attributed to the remained electrolyte (0.5 M H2SO4)4. In addition, the broad S 2p peak located at ~169 cm-1 in Supplementary Fig. 20b and the O 1s peak in Supplementary Fig. 20c can also be assigned to the remained electrolyte (0.5 M H2SO4)5.

# Supplementary Fig. 21 | Raman spectrum of s-Pt/1T′-MoS2 before (solid curve) and after (dashed curve) the durability test.

The Raman spectrum of the s-Pt/1T′-MoS2 after the durability test (Supplementary Fig. 21) shows the same five characteristic peaks as compared with the original s-Pt/1T′-MoS2, and no 2H peak can be detected. It confirms that no phase transition of 1T′-MoS2 NSs occurred in the s-Pt/1T′-MoS2 after the durability test.

# Supplementary Fig. 22 | Structural characterization of s-Pt/1T′-MoS2 after the durability test. a, TEM and b, High-resolution TEM (HRTEM) images. Inset in (b): the corresponding fast Fourier transform (FFT) pattern of s-Pt/1T′-MoS2. c, STEM image and the corresponding EDS mappings of s-Pt/1T′-MoS2.

The s-Pt/1T′-MoS2 after the durability test was characterized by TEM and EDS mapping. Obviously, no PtNPs are observed in the TEM and HRTEM images (Supplementary Fig. 22a,b). The FFT pattern (inset in Supplementary Fig. 22b) shows the featured pattern of 1T′-MoS2, in which no diffraction spot can be assigned to the PtNP. In addition, the EDS mappings (Supplementary Fig. 22c) show the dispersion of Pt, Mo, and S elements.

# Supplementary Fig. 23 | Characterizations of the activity and stability of s-Pt/1T′-MoS2 during HER in an H-type cell. a, Polarization curves of s-Pt/1T′-MoS2 and commercial HiSPEC 9100 Pt/C loaded on carbon fiber paper and tested in an H-type cell. b, The polarization curves of s-Pt/1T′-MoS2 recorded initially and after the 240-h test at a current density of 1,500 mA cm-2. c, Chronopotentiometry curve of the s-Pt/1T′-MoS2 catalyst used as cathode, tested in H-type cell at a current density of 1,500 mA cm-2. All the HER measurements in H-type cell were conducted in 0.5 M H2SO4 aqueous solution. All the current densities were normalized by the geometric area of the electrode. The scan rate is 5 mV s-1. Note: The Pt loadings for s-Pt/1T′-MoS2 and HiSPEC 9100 Pt/C were kept at 0.0175 mg cm-2.

# Supplementary Fig. 24 | Photograph of the prototype PEM electrolyser.

# Supplementary Fig. 25 | Characterizations of the activity and stability of s-Pt/1T′-MoS2 during water splitting in a proton exchange membrane (PEM) electrolyser. a,b, Polarization curves with iR-correction (a) and without iR-correction (b) of the PEM electrolyser using s-Pt/1T′-MoS2 and commercial HiSPEC 9100 Pt/C catalyst as cathode material. c, Chronopotentiometry curve of the PEM electrolyser using s-Pt/1T′-MoS2 catalyst as cathode material at a current density of 100 mA cm-2. Note: The Pt loadings for s-Pt/1T′-MoS2 and HiSPEC 9100 Pt/C were kept at 0.04 mg cm-2.

# Supplementary Table 1 | Inductively coupled plasma-optical emission spectrometry (ICP-OES) results and the corresponding Pt mass loadings in the as-synthesized samples.

| Sample | Mo concentration (ppm) | Pt concentration (ppm) | Pt wt% |
| --- | --- | --- | --- |
| PtNPs/2H-MoS2 | 6.760 | 1.190 | ~9.6 |
| s-Pt/1T′-MoS2 | 7.757 | 1.434 | ~10.0 |
| s-Pt-4/1T′-MoS2 | 12.360 | 0.925 | ~4.3 |
| s-Pt-6/1T′-MoS2 | 9.647 | 1.106 | ~6.4 |
| PtNPs-12/1T′-MoS2 | 2.480 | 0.574 | ~12.2 |
| PtNPs-15/1T′-MoS2 | 2.327 | 0.714 | ~15.5 |

The obtained samples were first washed three times by Milli-Q water, and then re-dispersed in Milli-Q water. 10 μl of the obtained dispersion of samples were dissolved in 1 ml of aqua regia. The obtained solution was diluted to 10 ml with Milli-Q water, which was then used for the ICP-OES analysis to determine the Mo and Pt concentrations. The Pt mass loadings in the as-synthesized samples were calculated based on the ICP-OES results.

# Supplementary Table 2 | The fitting parameters of Pt L3-edge EXAFS curves showing the structure parameters around Pt in the s-Pt/1T′-MoS2, commercial PtS2 powder, PtNPs/2H-MoS2, and Pt foil.

| Material | Path | CN | σ2 (Å2) | R (Å) | R factor* |
| --- | --- | --- | --- | --- | --- |
| s-Pt/1T′-MoS2 | Pt-S | 4.2(±0.8) | 0.0079(±0.0025) | 2.30(±0.01) | 0.014 |
| PtS2 | Pt-S | 4.2(±0.3) | 0.0033(±0.0007) | 2.36(±0.01) | 0.006 |
| PtNPs/2H-MoS2 | Pt-Pt | 8.9(±1.2) | 0.0070(±0.0008) | 2.75(±0.01) | 0.006 |
| Pt foil | Pt-Pt | 12 | 0.0044(±0.0002) | 2.76(±0.01) | 0.005 |

Abbreviations: CN, coordination number; σ2, the Debye-Waller factor; R, average bond length. *R factor indicates the percentage misfit between the data and theory.

# Supplementary Table 3 | The mass loadings of Pt on different floating electrodes tested by inductively coupled plasma mass spectrometry (ICP-MS).

|  | Samples | Loading (ng cm-2) |
| --- | --- | --- |
| Batch 1 | s-Pt/1T′-MoS2 (Electrode 1, denoted as E1) | 398 |
|  | HiSPEC 9100 Pt/C (Electrode 2, denoted as E2) | 286 |
| Batch 2 | s-Pt/1T′-MoS2 (Electrode 3, denoted as E3) | 583 |
|  | HiSPEC 9100 Pt/C (Electrode 4, denoted as E4) | 570 |
| Batch 3 | s-Pt/1T′-MoS2 (Electrode 5, denoted as E5) | 618 |
|  | HiSPEC 9100 Pt/C (Electrode 6, denoted as E6) | 833 |
| Average | s-Pt/1T′-MoS2 | 533±118* |
|  | HiSPEC 9100 Pt/C | 563±273* |

*The errors of Pt loadings are the standard deviations obtained from the separate ICP-MS tests on three batches of floating electrodes, i.e., E1, E3, E5 for s-Pt/1T′-MoS2 and E2, E4, E6 for HiSPEC 9100 Pt/C.

# Supplementary Table 4 | Comparison of HER activities of s-Pt/1T′-MoS2 and HiSPEC 9100 Pt/C with some representative reported Pt-based catalysts tested in acidic media.

| Catalysts | Pt loading (μg cm-2) | Pt weight percentage (wt%) | Overpotential (mV)@10 mA cm-2 | Mass activity (A mg-1) | Tafel slope (mV dec-1) | References |
| --- | --- | --- | --- | --- | --- | --- |
| s-Pt/1T′-MoS2 | 0.533±0.118 | 10.0 | -19±5* | 11±5@-10 mV* 22±9@-20 mV* 39±12@-30mV* 57±17@-40 mV* 85±23@-50 mV* 150±29@-70 mV* | 118 | This work |
| HiSPEC 9100 Pt/C | 0.563±0.273 | 60.0 | -24±3* | 8±4@-10 mV* 19±8@-20 mV* 32±10@-30 mV* 50±12@-40 mV* 70±17@-50 mV* 121±26@-70 mV* | 118 | This work |
| Pt/C | 3.7 | 47.8 wt% | N/A | 142@-70 mV† | N/A | 6 |
| PtRu/C | 8.2 | 54 wt% Pt:Ru 1:1.5 | N/A | 75.2@-70 mV† | N/A | 6 |
| PtNi/C | 10.1 | 40 wt% Pt:Ni 3:1 | N/A | 43.1@-70 mV† | N/A | 6 |
| ALD50Pt/N-doped graphene | 76 | 2.1 | -50 mV to reach 16 mA cm-2 | 10.1@-50 mV | 31 | 7 |
| 1Pt/VS2/carbon paper | 3.25 | 0.65 | -77 | 22.88@-200 mV | 39.46 | 8 |
| Pt-single atoms/WS2 | 0.45 | 4.1 | -32 | 130.2@-100 mV | 28 | 9 |
| Pt-single atoms/MoS2 | 0.45 | 5.1 | -59 | 17.14@-50 mV | 31 | 10 |
| Pt-doped 1T-MoS2 | N/A | 3 | -140 | N/A | 57 | 11 |
| K2PtCl4/N-doped carbon | 5.5 | 1.92 | -11 | 5.5@-20 mV | 21 | 12 |
| Pt-single atoms/N-carbon framework | 6.25 | 2.5 | -19 | N/A | 14.2 | 13 |
| Pt-single atoms decorated Co0.85Se | 20.4 | 1.03 | -55 | 1.32@-100 mV | 37 | 14 |
| Pt-single atoms/curved carbon | 1.68 | 0.33 | -38 | 7.4@-30 mV | 35 | 15 |
| Pt-single atoms/MoS2 | 18 | 1.7 | -150 | N/A | 96 | 16 |
| Pt1O1/Ti1-xO2 | 3.81 | 1.27 | -20.6 | 23.92@-50 mV | 31 | 17 |
| Pt-single atoms/MoO2 | 6.16 | 1.1 | -9.3 | 69.5@-300 mV | 28.78 | 18 |
| Pt/TiO2-OVs | 0.12 | 0.77 | -60 | 62.34@-50 mV | 34 | 19 |
| Pt/TiO2-X | 0.072 | 1.69 | -95 | 39.1@-50 mV | 34.3 | 20 |
| 1.2%PtCo/N-doped graphite porous carbon | 1.3 | 1.2 | -14 | 13.83@-20 mV | 21.2 | 21 |
| Pt/tungsten oxide/ reduced graphene oxide aerogel | 0.81 | 0.8 | -40 | 28.70@-50 mV | 30 | 22 |
| Mo2TiC2Tx-PtSA | 12 | 1.2 | -30 | 8.3@-77 mV | 30 | 23 |
| 400-single-walled carbon nanotube/Pt | 0.57 | 0.75 at% | -27 | N/A | 38 | 24 |
| Pt-single atoms/graphene | 7.07 | 0.44 | -12 | 22.4@-50 mV | 29.3 | 25 |
| Pt-graphitic tubes-FeCo/Cu | 1.4 | 0.5 | -18 | N/A | 24 | 26 |
| PtNPs/MoS2 | 27 | 36 | -80 | N/A | 40 | 27 |
| Pt/TiS2 | N/A | N/A | -70 | N/A | 40.6 | 28 |
| Pt clusters/carbon spheres | 7.6 | 5.08 | -20 | N/A | 28.3 | 29 |

Abbreviation: N/A, not available in the listed reference.

*The errors of overpotentials and mass activities are the standard deviations obtained from separate HER measurements on three batches of floating electrodes, i.e., E1, E3, E5 for s-Pt/1T′-MoS2 and E2, E4, E6 for HiSPEC 9100 Pt/C.

†Mass activities of these samples are obtained by using floating electrode techniques.

# Supplementary Table 5 | Comparison of exchange current densities of s-Pt/1T′-MoS2 and HiSPEC 9100 Pt/C with some representative Pt-based catalysts in acidic HER.

| Catalysts | Condition | Pt loading (ugPt cm-2) | j0,spec (mA cmPt-2) | j0,mass (A mgPt-1) | References |
| --- | --- | --- | --- | --- | --- |
| s-Pt/MoS2 | Floating electrode, 1M HClO4, 25 oC | 0.533±0.118 | N/A | 127 | This work |
| HiSPEC 9100 Pt/C | Floating electrode, 1M HClO4, 25 oC | 0.563±0.273 | 147 | 131 |  |
| 3.8 nm Pt nanoparticles | RDE (1600 r.p.m.), H2-saturated 0.5 M H2SO4 | 0.013 | 140 | 77* | 30 |
| Pt/C | H2 pump, 313 K | 3 | 216±50 | 237.6±55* | 31 |
| Pt/C | Floating electrode, 1 M HClO4, 25 oC, Fit 1 | 0.84 | 86 | 76.54* | 32 |
| Pt/C | Floating electrode, 1 M HClO4, 25 oC, Fit 2 | 0.84 | 101 | 89.89* |  |
| Pt/C | H2 pump, 313 K, Butler-Volmer fit | 2 | 120±10 | 132±11* | 33 |
|  | H2 pump, 313 K, Micropolarization fit | 2 | 135±40 | 148±44* |  |
| Pt/C | H2 pump, 80 oC | N/A | 235-300 | 211.5-276* | 34 |
| Pt/C | H2 pump, 30 oC | N/A | 100 | 92* |  |
| Pt/C | Single particle microelectrode, 0.1 M H2SO4, 23 oC | N/A | 24 | N/A | 35 |
| 0.25 ML Pt/TiWC | Gas diffusion electrodes, 1.0 M HClO4, 30 oC | 0.63 | N/A | 30.2±0.8 | 36 |
| Pt/C |  | 51 | N/A | 2.3±0.1 |  |
| Pt-Ru/CNT | GCE, N2-saturated 0.5 m H2SO4, RT | N/A | 2.43 | 2.28* | 37 |
| Pt NP/N-graphene | GCE, N2-saturated 0.5 m H2SO4, RT | 5.65 | 0.989 | 0.90* | 38 |
| Pt-MoS2 | GCE, N2-saturated 0.5 m H2SO4, RT | 13 | 0.373 | 0.276* | 39 |
| Pt/C | RDE, N2-saturated 0.5 m H2SO4, RT | 88.7 | 0.27 | 0.19* | 40 |
| Pt/C | RDE, 0.5 M H2SO4, 25 oC | 1 | 1 | N/A | 41 |
| PtRu20 |  | 1 | 1.14 | N/A |  |
| Pt/C | RDE, 0.1 M HClO4, 25 oC | 0.032 | 27.2±3.5 | N/A | 42 |
| Pt1O1/Ti1-xO2 | GCE, 0.5 M H2SO4, RT | 3.81 | 1.74 | N/A | 17 |
| Pt/C |  | N/A | 0.63 | N/A |  |
| Pt-single atoms/MoO2 | GCE, 0.5 M H2SO4, RT | 6.16 | 4.75 | N/A | 18 |
| Pt/C |  | 112 | 2.95 | N/A |  |
| Pt/TiO2-OVs | 0.5M H2SO4 (H2 saturated electrode), 25 oC | 0.12 | 0.45 | N/A | 19 |
| Pt/C |  | 3.1 | 0.56 | N/A |  |
| Mo2TiC2Tx-PtSA | Carbon paper electrode, 0.5M Ar-saturated H2SO4, RT | 12 | 1.54 | N/A | 23 |
| Pt/C |  | 400 | 1.4 | N/A |  |
| 400-single-walled carbon nanotube/Pt | GCE, 0.5 M H2SO4 saturated with N2 | 0.114 | 1.94 | N/A | 24 |
| Pt/C |  | 38 | 1.22 | N/A |  |

Abbreviations: RT, room temperature. j0,spec, electrochemically active surface area (ECSA)-normalized exchange current density. j0,mass, mass-normalized exchange current density. RDE, rotating disk electrode. GCE, glassy carbon electrode; N/A, not available in the listed reference.

*The j0,mass value was calculated from j0,spec by using the ECSA value in the listed reference.

# Supplementary Table 6 | Comparison of high-current-density HER performance of s-Pt/1T′-MoS2 and HiSPEC 9100 Pt/C with the previously reported catalysts in acid media.

| Catalysts | Total mass loading (mg cm-2) | Overpotential (η, mV) at different current density |  |  | Stability test | References |
| --- | --- | --- | --- | --- | --- | --- |
|  |  | η@1,000 mA cm-2 | η@1,500 mA cm-2 | η@2,000 mA cm-2 |  |  |
| s-Pt/1T′-MoS2 | 0.175 | -91 | -112 | -131 | 240 h@1,500 mA cm-2 | This work |
| HiSPEC 9100 Pt/C | 0.175 | -227 | -325 | -419 | N/A | This work |
| CH4/H2 treated Mo2S/Mo2C | 10 | -412 | N/A | N/A | 24 h@500 mA cm-2 | 43 |
| 20 wt% Pt/C | 2 | -500 | N/A | N/A | N/A |  |
| α-MoB2 | N/A | -334 | N/A | N/A | 60 h@1,500 mA cm-2 | 44 |
| 20 wt% Pt/C | 0.2 | -898 | N/A | N/A | N/A |  |
| Rh/Si nanowire | 0.193 | -950 | N/A | N/A | ~138 h@-0.1 V (~25 mA cm-2) | 45 |
| 40 wt% Pt/C | 0.193 | -1,120 | N/A | N/A | N/A |  |
| MoS2/Mo2C | 0.3 | -227 | N/A | N/A | 24 h@200 mA cm-2 | 46 |
| Pt foil | N/A | N/A | N/A | N/A | N/A |  |
| 20 wt% Pt/C/Nafion | 0.2 | N/A | N/A | N/A | N/A |  |
| N and P codoped MoS2/carbon cloth | 1.2 | N/A | N/A | N/A | 20 h@1,000 mA cm-2 | 47 |
| Co(10.4)/Se-MoS2-nanofoam | 0.5 | -382 | N/A | N/A | 360 h@1,000 mA cm-2 | 48 |
| 40 wt% Pt/C | 0.5 | -671 | N/A | N/A | N/A |  |
| 2H Nb1+xS2 | N/A | -370 | N/A | N/A | 120 h (Current density not available) | 49 |
| Pt | N/A | N/A | N/A | N/A | N/A |  |

Abbreviation: N/A, not available in the listed reference.

# Supplementary Table 7 | Summary of two-dimensional (2D) electrocatalysts used as cathode materials in PEM electrolyser.

| 2D electrocatalyst | PEM setup |  | Performance | Test condition | References |
| --- | --- | --- | --- | --- | --- |
|  | Cathode | Anode |  |  |  |
| s-Pt/1T′-MoS2 | s-Pt/1T′-MoS2 dropped on carbon cloth (0.025 mgpt cm-2) | IrO2 (Dioxide Materials, USA) | 1.61 V@100 mA cm-2, 1.82 V@1,000 mA cm-2, 500 h stability@100 mA cm-2 | RT, 1 M H2SO4 on the anode, 8 ml min-1 | This work |
| 1T-2H MoS2 nanosheet | 1T-2H MoS2/CP (0.14 mg cm-2) | IrRuOx | 1.96 V@1,000 mA cm-2 | 80 oC | 50 |
| Transition metal-doped (Fe, Co, Ni, Cu) single-layer MoS2 | Fe, Co, Ni, Cu-MoS2 (single layer) on CP (4.5±0.25 mg cm-2), hot-pressed | IrO2 | 2.4 V@1,000 mA cm-2 | 80 oC, 20 ml min-1 | 51 |
| FeMoS(mw) | FeMoS(mw) on CP (2 mg cm-2), hot-pressed | A Pt-coated titanium mesh (FuelCellStore, USA) | 1.77 V@500 mA·cm-2 and 1.85 V@1,000 mA cm-2 | 80 °C | 52 |
| Greigite Fe3S4 | Greigite Fe3S4 on CP (~3.52 mg cm-2), hot-pressed | IrO2 | 2.13 V@1,000 mA cm-2 | 80 °C, 3.33 mL min-1 | 53 |

Abbreviations: RT, room temperature. CP, carbon paper.

References

1	Lai, Z. et al. Metastable 1T′-phase group VIB transition metal dichalcogenide crystals. Nat. Mater. 20, 1113-1120 (2021).

2	Zuo, P. et al. Metal (Ag, Pt)-MoS2 hybrids greenly prepared through photochemical reduction of femtosecond laser pulses for SERS and HER. ACS Sustain. Chem. Eng 6, 7704-7714 (2018).

3	Gong, C. et al. Metal contacts on physical vapor deposited monolayer MoS2. ACS Nano 7, 11350-11357 (2013).

4	Strohmeier, B. R. & Hercules, D. M. Surface spectroscopic characterization of manganese/aluminum oxide catalysts. J. Phys. Chem. 88, 4922-4929 (1984).

5	Chastain, J. & King Jr, R. C. Handbook of X-ray photoelectron spectroscopy. Perkin-Elmer Corporation 40, 221 (1992).

6	Jackson, C., Raymakers, L. F. J. M., Mulder, M. J. J. & Kucernak, A. R. J. Assessing electrocatalyst hydrogen activity and CO tolerance: Comparison of performance obtained using the high mass transport ‘floating electrode’ technique and in electrochemical hydrogen pumps. Appl. Catal. B 268 (2020).

7	Cheng, N. et al. Platinum single-atom and cluster catalysis of the hydrogen evolution reaction. Nat. Commun. 7, 13638 (2016).

8	Zhu, J. et al. Enhanced electrocatalytic hydrogen evolution activity in single-atom Pt-decorated VS2 nanosheets. ACS Nano 14, 5600-5608 (2020).

9	Shi, Y. et al. Electronic metal-support interaction modulates single-atom platinum catalysis for hydrogen evolution reaction. Nat. Commun. 12, 3021 (2021).

10	Shi, Y. et al. Site-specific electrodeposition enables self-terminating growth of atomically dispersed metal catalysts. Nat. Commun. 11, 4558 (2020).

11	Lau, T. H. M. et al. Engineering monolayer 1T-MoS2 into a bifunctional electrocatalyst via sonochemical doping of isolated transition metal atoms. ACS Catal. 9, 7527-7534 (2019).

12	Jin, H. et al. Simple and scalable mechanochemical synthesis of noble metal catalysts with single atoms toward highly efficient hydrogen evolution. Adv. Funct. Mater. 30, 2000531 (2020).

13	Fang, S. et al. Uncovering near-free platinum single-atom dynamics during electrochemical hydrogen evolution reaction. Nat. Commun. 11, 1029 (2020).

14	Jiang, K. et al. Single platinum atoms embedded in nanoporous cobalt selenide as electrocatalyst for accelerating hydrogen evolution reaction. Nat. Commun. 10, 1743 (2019).

15	Liu, D. et al. Atomically dispersed platinum supported on curved carbon supports for efficient electrocatalytic hydrogen evolution. Nat. Energy 4, 512-518 (2019).

16	Deng, J. et al. Triggering the electrocatalytic hydrogen evolution activity of the inert two-dimensional MoS2 surface via single-atom metal doping. Energy Environ. Sci. 8, 1594-1601 (2015).

17	Lu, F. et al. Engineering platinum-oxygen dual catalytic sites via charge transfer towards highly efficient hydrogen evolution. Angew. Chem. Int. Ed. 59, 17865-17871 (2020).

18	Qiu, Y. et al. Synergistic effect between platinum single atoms and oxygen vacancy in MoO2 boosting pH-Universal hydrogen evolution reaction at large current density. Chem. Eng. J. 427, 131309 (2022).

19	Cheng, X. et al. Engineering local coordination environment of atomically dispersed platinum catalyst via lattice distortion of support for efficient hydrogen evolution reaction. Mater. Today Energy 20, 100653 (2021).

20	Tian, Y., Yu, L., Zhuang, C., Zhang, G. & Sun, S. Fast synthesis of Pt single-atom catalyst with high intrinsic activity for hydrogen evolution reaction by plasma sputtering. Mater. Today Energy 22, 100877 (2021).

21	Guo, F. et al. Confined sub-nanometer PtCo clusters as a highly efficient and robust electrocatalyst for the hydrogen evolution reaction. J. Mater. Chem. A 9, 5468-5474 (2021).

22	Li, Y. et al. Tungsten oxide/reduced graphene oxide aerogel with low-content platinum as high-performance electrocatalyst for hydrogen evolution reaction. Small 17, e2102159 (2021).

23	Zhang, J. et al. Single platinum atoms immobilized on an MXene as an efficient catalyst for the hydrogen evolution reaction. Nat. Catal. 1, 985-992 (2018).

24	Tavakkoli, M. et al. Electrochemical activation of single-walled carbon nanotubes with pseudo-atomic-scale platinum for the hydrogen evolution reaction. ACS Catal. 7, 3121-3130 (2017).

25	Ye, S. et al. Highly stable single Pt atomic sites anchored on aniline-stacked graphene for hydrogen evolution reaction. Energy Environ. Sci. 12, 1000-1007 (2019).

26	Tiwari, J. N. et al. Multicomponent electrocatalyst with ultralow Pt loading and high hydrogen evolution activity. Nat. Energy 3, 773-782 (2018).

27	Huang, X. et al. Solution-phase epitaxial growth of noble metal nanostructures on dispersible single-layer molybdenum disulfide nanosheets. Nat. Commun. 4, 1444 (2013).

28	Zeng, Z., Tan, C., Huang, X., Bao, S. & Zhang, H. Growth of noble metal nanoparticles on single-layer TiS2 and TaS2 nanosheets for hydrogen evolution reaction. Energy Environ. Sci. 7, 797-803 (2014).

29	Wan, X. K., Wu, H. B., Guan, B. Y., Luan, D. & Lou, X. W. D. Confining sub-nanometer Pt clusters in hollow mesoporous carbon spheres for boosting hydrogen evolution activity. Adv. Mater. 32, e1901349 (2020).

30	Hansen, J. N. et al. Is there anything better than Pt for HER? ACS Energy Lett. 6, 1175-1180 (2021).

31	Durst, J. et al. New insights into the electrochemical hydrogen oxidation and evolution reaction mechanism. Energy Environ. Sci. 7, 2255-2260 (2014).

32	Zalitis, C. M., Sharman, J., Wright, E. & Kucernak, A. R. Properties of the hydrogen oxidation reaction on Pt/C catalysts at optimised high mass transport conditions and its relevance to the anode reaction in PEFCs and cathode reactions in electrolysers. Electrochim. Acta 176, 763-776 (2015).

33	Durst, J., Simon, C., Hasché, F. & Gasteiger, H. A. Hydrogen oxidation and evolution reaction kinetics on carbon supported Pt, Ir, Rh, and Pd electrocatalysts in acidic media. J. Electrochem. Soc. 162, F190-F203 (2015).

34	Neyerlin, K. C., Gu, W., Jorne, J. & Gasteiger, H. A. Study of the exchange current density for the hydrogen oxidation and evolution reactions. J. Electrochem. Soc. 154, B631-B635 (2007).

35	Song, C. et al. PEM fuel cell reaction kinetics in the temperature range of 23-120°C. Electrochim. Acta 52, 2552-2561 (2007).

36	Hunt, S. T., Milina, M., Wang, Z. & Román-Leshkov, Y. Activating earth-abundant electrocatalysts for efficient, low-cost hydrogen evolution/oxidation: sub-monolayer platinum coatings on titanium tungsten carbide nanoparticles. Energy Environ. Sci. 9, 3290-3301 (2016).

37	Zhang, D. et al. Noble metal (Pt, Rh, Pd, Ir) doped Ru/CNT ultra-small alloy for acidic hydrogen evolution at high current density. Small 18, e2104559 (2022).

38	Jiang, B., Liao, F., Sun, Y., Cheng, Y. & Shao, M. Pt nanocrystals on nitrogen-doped graphene for the hydrogen evolution reaction using Si nanowires as a sacrificial template. Nanoscale 9, 10138-10144 (2017).

39	Li, S., Lee, J. K., Zhou, S., Pasta, M. & Warner, J. H. Synthesis of surface grown Pt nanoparticles on edge-enriched MoS2 porous thin films for enhancing electrochemical performance. Chem. Mater. 31, 387-397 (2019).

40	Esparbé, I. et al. Structure and electrocatalytic performance of carbon-supported platinum nanoparticles. J. Power Sources 190, 201-209 (2009).

41	Wang, J. X., Brankovic, S. R., Zhu, Y., Hanson, J. C. & Adz̆ić, R. R. Kinetic characterization of PtRu fuel cell anode catalysts made by spontaneous Pt deposition on Ru nanoparticles. J. Electrochem. Soc. 150, A1108-A1117 (2003).

42	Sun, Y., Lu, J. & Zhuang, L. Rational determination of exchange current density for hydrogen electrode reactions at carbon-supported Pt catalysts. Electrochim. Acta 55, 844-850 (2010).

43	Zhang, C. et al. High-throughput production of cheap mineral-based two-dimensional electrocatalysts for high-current-density hydrogen evolution. Nat. Commun. 11, 3724 (2020).

44	Chen, Y. et al. Highly active, nonprecious electrocatalyst comprising borophene subunits for the hydrogen evolution reaction. J. Am. Chem. Soc. 139, 12370-12373 (2017).

45	Zhu, L. et al. A rhodium/silicon co-electrocatalyst design concept to surpass platinum hydrogen evolution activity at high overpotentials. Nat. Commun. 7, 12272 (2016).

46	Luo, Y. et al. Morphology and surface chemistry engineering toward pH-universal catalysts for hydrogen evolution at high current density. Nat. Commun. 10, 269 (2019).

47	Sun, K. et al. Design of basal plane active MoS2 through one-step nitrogen and phosphorus co-doping as an efficient pH-universal electrocatalyst for hydrogen evolution. Nano Energy 58, 862-869 (2019).

48	Zheng, Z. et al. Boosting hydrogen evolution on MoS2 via co-confining selenium in surface and cobalt in inner layer. Nat. Commun. 11, 3315 (2020).

49	Yang, J. et al. Ultrahigh-current-density niobium disulfide catalysts for hydrogen evolution. Nat. Mater. 18, 1309-1314 (2019).

50	Xie, Z. et al. MoS2 nanosheet integrated electrodes with engineered 1T-2H phases and defects for efficient hydrogen production in practical PEM electrolysis. Appl. Catal. B 313, 121458 (2022).

51	Mo, J. et al. Transition metal atom-doped monolayer MoS2 in a proton-exchange membrane electrolyzer. Mater. Today Adv. 6, 100020 (2020).

52	Morozan, A. et al. Nonprecious bimetallic iron-molybdenum sulfide electrocatalysts for the hydrogen evolution reaction in proton exchange membrane electrolyzers. ACS Catal. 10, 14336-14348 (2020).

53	Giovanni, C. D. et al. Low-cost nanostructured iron sulfide electrocatalysts for PEM water electrolysis. ACS Catal. 6, 2626-2631 (2016).