Supplementary Materials

Ferromagnetic domain walls as spin wave filters and the interplay between domain walls and spin waves

Liang-Juan Chang1, Yen-Fu Liu1, Ming-Yi Kao1, Li-Zai Tsai1, Jun-Zhi Liang2, *, and Shang-Fan Lee1, **

1 Institute of Physics, Academia Sinica, Taipei 11529, Taiwan

2 Department of Physics, Fu Jen Catholic University, Taipei 24205, Taiwan

The rotation of the domain wall (DW) plane plays a crucial role in the DW dynamics. When a spin wave (SW) with a relatively low frequency f = 20 GHz and large enough amplitude H0/MS = 0.19 is applied, we observed from the simulation a forward DW motion, shown in Fig. 3(b) in the main article, and a rotation of the DW plane. The temporal evolution of the rotation at the center of the DW plane, , is shown in Fig. S1(a). While the DW is moving away from the source, the wall plane rotates in a close analogue to the slope of the DW displacement. In the initial state, the local magnetization M inside a 180°-domain-wall is located at x = 0, with azimuth angle φ = 0°, oriented as defined in Fig. 1. The dynamics of the interaction between the SW and the DW is described by the modified Landau-Lifshitz-Gilbert (LLG) equation [S1],

∂M∂t=-γM×Heff+αMsM×∂M∂t-∂Jm∂x                                  (S1)

, where γ is the gyromagnetic ratio, α is the Gilbert damping parameter, Ms is the saturation magnetization, and Heff is the effective magnetic field consisting of anisotropy, demagnetization, and exchange fields, and where Jm Jm is the magnon spin current. Hinzke et al. [S2] and Yan et al. [S3] have proposed a magnonic STT mechanism to explain the SW-induced wall motion. The DW must propagate in the opposite direction to that of the magnon with a velocity Vm Vm to compensate the magnon spin current changes. This scenario is valid only when the wavelength is smaller than the DW size. As a SW passes through the DW, the total instantaneous magnetization can be expressed as the vector sum of a main equilibrium component and a small fluctuating time-varying component, M(x,t) = M0 + m(x,t) with m(x,t)=m0exp⁡[-i(kx-ωt)]exp⁡(-x/Λ)  in the Cartesian coordinates, where  is the characteristic attenuation length. In our case  ~ 370 nm. At the center of the DW, M0 is perpendicular to the easy axis ez. Therefore, only the fluctuation component contributes to the effective anisotropy field hK. In this case,  hK=2K⊥δmzezμ0Ms2 [S4], where δmz=mz0e-x/Λ, and mz0 is the z component of the fluctuation at x=0 (the initial position of the DW). As shown in Fig. S1, hK along ez exerts a torque τK that rotates the DW around the ez axis, and raises δφ,

dδφtdt=γhK-hWsin2δφ,	(S2)

with hW being the Walker field [S5].

When the hK exerts a torque to rotate the DW magnetization, an effective demagnetization field hd=-NyMyey, where Ny is the demagnetization factor related to the DW itself, is simultaneously generated. The demagnetization torque τd=-γM×hd  cants the magnetization of the DW, resulting in the DW motion with the same direction of the SW, as shown in Fig. S1. The instantaneous DW velocity Vd  Vd induced by this demagnetization field in the presence of damping can be obtained using the rigid DW model [S6],

Vd=-γΔ21+α2MSM×hd∙ezex           	(S3)

where  is the DW width. To estimate the total instantaneous velocity VDW=Vd+Vm, we follow Ref. [S3] and obtain

VDW=(γΔMSNy-Nx21+α2sin2δφ - e-x-x0/Λ22∂ω∂k)ex	(S4)

, where ∂ω∂k=2Ak is the SW group velocity, x0 is the location of the SW source. The rotation of the DW plane , the total instantaneous velocity VDW, and the DW acceleration are calculated and shown as red lines in Figs. S2(a) and (b), and (c), which show good agreements with the simulation results presented as circle, diamond, and triangle symbols, respectively. The magnitude of the VDWVDW first increases as the  increases, then the DW propagates away from the SW source, and the wall motion stops eventually because the magnitude of the effective anisotropy torque can no longer overcome the shape anisotropy effect. The maximum VDW = 27 m/sVDW=27m/s occurs around  = 40. At higher SW frequencies and for H0 > HWH0>HW, as in Fig. 3(c),  can reach 45 and the first term on the right of Eq. (S4) vanishes, thus the Walker breakdown occurs.

The total effective field for a Néel wall in Eq. (S1) is given by

Heff=Hd+hxeiωt=(Hdx+hxeiωt, Hdy+hyeiωt, hzeiωt),          (S5)

Hdx=-MSNxcosδφ                                              (S6)

Hdy=-MSNysinδφ                                              (S7)

where h(h≪Hd) is the r. f. exciting magnetic field with an angular frequency .

The magnetization at the center of the DW can be described by,

M=(Mx+mxeiωt, My+myeiωt, mzeiωt)                           (S8)

Mx=MScosδφ                                                (S9)

My=MSsinδφ .                                               (S10)

Inserting Eqs. (S5) – (S10) into the modified LLG equation (S1) and neglecting the higher order terms, we write the dynamic equations as

iω0-ωy0iωωxωy-ωxiωmxmymz=-γMs-sinδφhzcosδφhzsinδφhx-cosδφhy .               (S11)

Then,

mxmymz=-iγMsωx2+ωy2-ω2-ω2+ωx2ωωxωyωiωyωxωyω-ω2+ωy2ω-iωx-iωyiωx-ω-sinδφhzcosδφhzsinδφhx-cosδφhy        (S12)

with

ωx=γHdx+αMsiωMx                                          (S13)

ωy=γHdy+αMsiωMy.                                          (S14)

Inside the DW, we consider the dispersion relation of the magnetostatic surface spin wave (MSSW) [S7]

ω2=ωHωH+ωM+ωM221+coth⁡(kd)                               (S15)

with ωH=ωxωyω  and ωM=γMs. Using k=kr-iκ we get an identity

11+coth⁡(kd)=121-e-2krd+idΛe-2krd                             (S16)

with Λ=1/κ. After substituting H in terms of Eqs. (S13) and (S14), M, and Eq. (S16) into Eq. (S15), one obtains

1ΛD=1de-2kdαγMsωNx+NyNxNysin22δφ+αNx+Nysin2δφ,      (S17)

where D is the attenuation length inside the DW. We find the TDW, defined as the spin wave amplitude ratio with and without DW on the +x side of DW, to be

TDW=e-2Δ1ΛD - 1Λ0,                                              (S18)

where  is the width of the DW and 0 is the attenuation length outside the DW.

Results for CoFeB

The time evolution of the DW motion driven by SWs for the PMA materials of CoFeB is shown in Fig. S3. The strip width is 50 nm and thickness is 1 nm, following the experimental structure Ta(5 nm)/Co20Fe60B20(1 nm)/MgO(2 nm)/Ta(5 nm) [S8]. The values of material parameters for CoFeB were saturation moments MS = 8.75 A/m, exchange stiffness constants A = 1.0 J/m, the perpendicular anisotropy constants K = 5.1 J/m3, and the damping parameter α = 0.01. For CoFeB with f = 5 GHz, the initial transient backward motion for all cases is associated with the separation between the DW and the SW source. When compared with the data of NiFe, the DW motion in CoFeB shows similar behaviors. As we describe in the main article, forward displacement after the initial transient motion was obtained in the wide range with small excitation amplitude shown as black line for H0 = 120 mT, red line for H0 = 130 mT, and blue line for 135 mT in Fig. S3(a). These motions are associated with changes of azimuthal angle, , at the center of the DW structure. CoFeB shows region I behavior when H0  138 mT. The damped oscillatory motion of the DW is due to the relativity larger attenuation length of the propagation SWs in this material. CoFeB shows region II behavior when 139 mT  H0  139.9 mT. We did not find localized oscillatory motion with 0.01 mT resolution between regions II and III. In region III, oscillatory motions of the DW associated with propagations in the opposite direction to the SW as shown by the pink line for H0 =139.93 mT, green line for H0 =140 mT, and purple line for H0 =160 mT in Fig. S3.

References:

S1. 	Wang, X.-g., Guo, G.-h., Nie, Y.-z., Zhang, G.-f., and Li, Z.-x. Domain wall motion induced by the magnonic spin current. Phys. Rev. B 86, 054445 (2012).

S2. 	Hinzke D. and Nowak, U. Domain wall motion by the magnonic spin Seebeck effect. Phys. Rev. Lett. 107, 027205 (2011).

S3. 	Yan, P., Wang, X. S., and Wang, X. R. All-magnonic spin-transfer torque and domain wall propagation. Phys. Rev. Lett. 107, 177207 (2011).

S4. 	Stancil D. D. and Prabhakar, A. Spin Waves Theory and Applications (Springer, New York, 2009).

S5.  Mougin, A., Cormier, M., Adam, J. P., Metaxas P. J., and Ferré, J. Domain wall mobility, stability and Walker breakdown in magnetic nanowires. Europhys. Lett. 78, 57007 (2007).

S6. 	Hillebrands B. and Thiaville, A. Spin Dynamics in Confined Magnetic Structures III (Springer, New York, 2006).

S7.  Kaboš P. and Staĺmachov, V. S. Magnetostatic Waves and their Applications (Springer, Netherlands, 1994).

S8. Lo Conte, R. et al. Role of B diffusion in the interfacial Dzyaloshinskii-Moriya interaction in Ta/Co20Fe60B20/MgO nanowires. Phys. Rev. B 91, 014433 (2015).

Fig. S1. The cones indicate the precession of the magnetizations.  is the rotation of the magnetization at the center of the domain wall. τd, hd, τK, and hK are the torques and effective fields due to demagnetization and anisotropy, respectively. Drawing is not to scale.

Fig. S2. (a) The rotation angle of the magnetization, , (b) instantaneous velocity, and (c) acceleration of the domain wall versus time for the case of Fig. 2 (b), SW frequency 20 GHz, amplitude H0/MS = 0.19.

Fig. S3. Typical domain wall displacement as functions of simulation time and magnetic field amplitude of the spin wave with frequencies of 5 GHz for CoFeB.