Supporting Information

Electrochemical properties of novel FeV2O4 as an anode for Na-ion batteries

Irish Valerie B. Maggay,1† Lyn Marie Z. De Juan,2† Jeng-Shin Lu,1† Mai Thanh Nguyen,2 Tetsu Yonezawa,2 Ting-Shan Chan,3 and Wei-Ren Liu1*

1Department of Chemical Engineering, Chung Yuan Christian University, Taoyuan City, Chungli 32023, Taiwan, R.O.C.

*E-mail: WRLiu1203@gmail.com

Tel:+886 3-265-4140; fax: +886 3-265-4199

2Division of Materials Science and Engineering, Faculty of Engineering, Hokkaido University

Kita 13 Nishi 8, Kita-ku, Sapporo, Hokkaido 060-8628, Japan

3National Synchrotron Radiation Research Center (NSRRC), Hsinchu, 30076, Hsinchu, Taiwan

Fig. S1. (a) Lattice parameters and (b) cell volume of FeV2O4 with their corresponding error bars.

Fig. S2. Comparison of FeV2O4 calcined at 400°C with different XRD scan rate.

Fig. S2 (a) EDS spectra of FeV2O4 and (b) its error bar.

Fig. S3. Elemental mapping of FeV2O4.

Fig. S4. (a) X-ray absorption near edge (XANES) spectra of V K-edge and the (b) zoomed in graph of the edge energies.

Fig. S5. Ex-situ SEM images of FVO-PVdF electrodes (a) before, after the (b) 1st and (c) 200th charge/discharge cycle. Cross-section SEM images of (d) before, (e) after the 1st, and (f) low and (g) high magnification of the electrode after the 200th cycle.

Table 1. Measured thickness of FVO-PVdF electrode before and after charge/discharge cycle.

| FVO-PVdF | Before (µm) | After 1st C/D Cycle (µm) | After 200th C/D Cycle (µm) |
| --- | --- | --- | --- |
| D1 | 11.00 | 15.82 | 34.64 |
| D2 | 13.08 | 15.03 | 34.43 |
| D3 | 9.14 | 15.36 | 34.65 |
| D4 | 9.93 | 17.66 | 34.10 |
| D5 | 12.34 | 15.76 | 33.44 |
| D6 | 12.45 | 15.70 | 33.55 |
| Dave | 11.32 | 15.88 | 34.14 |
| Expansion: 201% |  |  |  |

Fig. S6. Ex-situ SEM images of FVO-CMC/SBR electrodes (a) before, after the (b) 1st and (c) 200th charge/discharge cycle. Cross-section SEM images of (d) before, after the (e) 1st and (f) 200th charge/discharge cycle.

Table 2. Measured thickness of FVO-CMC/SBR electrode before and after charge/discharge cycle.

| FVO-CMC/SBR | Before (µm) | After 1st C/D Cycle (µm) | After 200th C/D Cycle (µm) |
| --- | --- | --- | --- |
| D1 | 11.07 | 13.72 | 21.46 |
| D2 | 11.22 | 13.43 | 21.45 |
| D3 | 12.11 | 14.35 | 22.96 |
| D4 | 12.31 | 13.72 | 23.49 |
| D5 | 12.12 | 14.56 | 22.51 |
| D6 | 12.73 | 14.44 | 22.53 |
| Dave | 11.93 | 14.04 | 22.40 |
| Expansion: 88% |  |  |  |

(a)

(b)

(c)

Fig. S7. Molecular structures of (a) PVdF, (b) CMC1, and (c) SBR.

1	Biswal, D. & Singh, R. Characterisation of carboxymethyl cellulose and polyacrylamide graft copolymer. Carbohydr. Polym.  57, 379-387 (2004).

Fig. S8. CV profiles of FVO-CMC/SBR at a scan rate of 0.1 mV·s-1 from 0.01 – 3.0V.